Extended Data Figure 1 | TEM and XRD characterizations of aCNS. a, selected-area electron diffraction (SAED) pattern of aCNS. b, XRD spectrum of aCNS.

Extended Data Table 1 | pH, surface area, pore volume and volatile % of AB, KJ and aCNS. AB was commercially available acetylene black (Soltex, Acetylene Black 50%-01) and KJ was commercially available Ketjenblack carbon black(Ketjenblack EC-600JD).

Extended Data Figure 2 | Different components to make a Na/Cl coin cell battery.

Extended Data Figure 3 | Electrochemical impedance spectroscopy (EIS) of battery during its first discharge and the first discharge of a Na/Cl battery using neutral electrolyte. a, Impedance measurements along the curve of first discharge of the battery when 4M AlCl3 in SOCl2 + 2 wt% NaFSI/NaTFSI was used as the electrolyte. b, first discharge curve of Na/Cl battery when 4M AlCl3 + 4M NaCl in SOCl2 was used as the electrolyte.

Extended Data Figure 4 | Percentage change of the mass spectrum intensity of Cl2 and SCl2 in charged and discharged battery compared to their respective fragmented intensity. By taking the mass spectrum of pure electrolyte, pure SO2Cl2 and pure S2Cl2, the intensity ratio between Cl2 and SOCl2, Cl2 and SO2Cl2, Cl2 and S2Cl2 could be determined, respectively. Similarly, the ratio between SCl2 and SOCl2, SCl2  and SO2Cl2, SCl2 and S2Cl2 could also be calculated (Extended Data Table 2). From these ratios, we could calculate the fragmented intensity of either Cl2 or SCl2, the intensity of Cl2 or SCl2 contributed by fragmentations of SOCl2, S2Cl2 and SO2Cl2, in the actual opened battery spectrum. Afterward, the percent difference between the actual intensity of Cl2 or SCl2 and its fragmented intensity could be calculated and were reported in this figure. See Text S1 for detailed analysis.

Extended Data Figure 5 | Ar normalized mass spectroscopy data of the species in battery at different battery states (after first discharge, 0 hour retention, 24 hours retention, 72 hours retention, 120 hours retention and discharged). See Text S1 for detailed analysis.

Extended Data Figure 6 | Characterizations of sodium immersed in 4 M AlCl3 in SOCl2 with and without 2 wt% NaFSI/NaTFSI and charge – discharge curves of the normal battery versus decayed battery a, atomic percentage of different elements on the Na metal when immersed in 4 M AlCl3 in SOCl2 with and without 2 wt% NaFSI/NaTFSI as additives. b, F 1s spectrum of Na immersed in 4 M AlCl3 in SOCl2 with/without additives. c, S 2p spectrum of Na immersed in 4 M AlCl3 in SOCl2 with/without additives. d, Cl 2p spectrum of Na immersed in 4 M AlCl3 in SOCl2 with/without additives. e, charge – discharge curves of the battery at normal state and after the battery started to decay.

Extended Data Figure 7 | RGA300 setup with chamber connected. See Text S1 for detailed analysis.

Extended Data Figure 8 | Argon normalized mass spectrum of standard solutions and species inside battery at different states a, fresh electrolyte. b, fresh S2Cl2. c, fresh SO2Cl2. d, species in charged battery with no retention. e, species in charged battery retained for 24 hours at open-circuit. f, mass spectrum of species in charged battery retained for 72 hours at open-circuit. g, mass spectrum of species in charged battery retained for 120 hours at open-circuit. h, mass spectrum of species in discharged battery. See Text S1 for detailed analysis.

Extended Data Table 2 | Ratios between peak intensity of different species/fragments and peak intensity of molecular peak in pure S2Cl2, pure SO2Cl2 and fresh electrolyte. See Text S1 for detailed analysis.