SUPPLEMENTARY INFORMATION

Supplementary Discussion

Text S1. Mass Spectroscopy Analysis of Chemical Compositions in Na/Cl Battery Cells

S1.1. Instrument Setup and Measurement

The chemical compositions in a Na/Cl coin cell battery was analyzed using a residual gas analyzer (RGA300) from Stanford Research System. Ions were generated by impact ionization known to generate fragments in addition to molecular peaks. When the battery reached the desire cycle number and charged or discharged state, the battery was opened inside an argon filled glovebox and was immediately put into a Swagelok chamber with a closed Swagelok high vacuum valve attached. The chamber was then transferred outside of the glovebox and connected to our RGA300 setup (Extended Data Fig. 7). After opening the valve connecting between the chamber and the RGA300 instrument, the turbo pump would keep pumping to pull species in the opened battery in the chamber to the detector of the RGA300 instrument, and a mass spectrum of species from the battery was measured. After obtaining our opened battery mass spectrum at different battery states, we normalized each spectrum with respect to the argon peak at m/z = 40 (Ar came from glovebox and normalized Ar peak intensity = 100, Extended Data Fig. 8). We also took the mass spectrum of fresh electrolyte (mostly SOCl2, 4 M AlCl3 in SOCl2 + 2 wt% NaFSI + 2 wt% NaTFSI), pure S2Cl2 and pure SO2Cl2 as our standard spectra (Extended Data Fig. 8). In each standard spectrum, the ratio between the peak intensity of any fragmented species (SO2, Cl2, SCl2 etc.) and the molecular peak intensity (SOCl2, S2Cl2 and SO2Cl2) was calculated (Extended Data Table 2).

S1.2. Quantitative Analysis of S2Cl2 and SO2Cl2

A peak at m/z = 134 was detected inside our batteries after cycling, attributed to a combination of SO2Cl2 and S2Cl2 with the same molecular mass. SO2Cl2 and S2Cl2 also have a common fragment at m/z = 99, corresponding to SO2Cl and S2Cl respectively. The intensity ratios between m/z = 99 and the molecular peak at m/z = 134 in standard spectra of SO2Cl2 and S2Cl2 respectively were calculated (Extended Data Table 2) and compared with the measured ratio in a battery after cycling. The ratio of 4.03 between the m/z = 99 and m/z = 134 peaks detected in the cycled battery was in between 2.48 and 24.34 for pure SO2Cl2 and S2Cl2. Therefore, the peak at m/z = 134 must be due to a mixture of SO2Cl2 and S2Cl2. To determine how much of each species was present in the cycled battery, we used the following equations and solved for the intensity of S2Cl2 and SO2Cl2:

Imz=99=2.48×IS2Cl2+24.34×ISO2Cl2	                               (1)

Imz=134=IS2Cl2+ISO2Cl2	  	  	     	       (2)

In equation 1 and equation 2, Imz=99 and Imz=134 were the peak intensities at m/z = 99 and m/z = 134 detected in the cycled battery respectively. We then solved for IS2Cl2and ISO2Cl2 that were the peak intensity or relative abundance of S2Cl2 and SO2Cl2, respectively.

S1.3. Determination of Molecular Fragments Detected by Mass Spectroscopy in Batteries

After determining the mass-spec peak intensities of S2Cl2 and SO2Cl2, we then used the ratios in Extended Data Table 2 to determine the peak intensity of fragments due to different species in the battery, i.e.,  SOCl2, S2Cl2 and SO2Cl2. For example, the Cl2 fragment from these molecular species could be determined by:

Ifragmented, Cl2=1.62×ISOCl2+1.45×IS2Cl2+35.16×ISO2Cl2	       (3)

In equation 3, Ifragmented, Cl2 was the measured intensity of Cl2 fragments from SOCl2, S2Cl2 and SO2Cl2 in the cycled battery cell.  ISOCl2, IS2Cl2, ISO2Cl2 were the measured peak intensity of SOCl2, S2Cl2 and SO2Cl2 respectively in the same experiment. Similar calculation could be done for other fragments. For a given species, if its detected intensity was greater than that of fragments added up from larger molecules in the battery, then the extra intensity must be due to the generation of ‘free molecular species’ over battery operation. We also realized that the peak ratio between SOCl (m/z = 83) to SOCl2 (m/z = 118) would slightly change as the pumping time changed, resulting in slight change of the peak ratios between fragmented species to SOCl2. Therefore, when calculating the fragmented intensity of any species contributed by SOCl2, we would make sure that the actual spectrum had similar 83/118 ratio as in our standard SOCl2 spectra.

S1.4. Determination of Free Molecular Cl2 Species Generated over Battery Cycling

To determine whether Cl2 was generated over battery operation, we first calculated the fragmented peak intensity of that species by using equation 3. Then we calculated the difference between the actual peak intensity and the fragmented peak intensity. For example, the amount of free Cl2 could be calculated by:

Ifree Cl2=Iactual, Cl2-Ifragmented, Cl2		                   (4)

In equation 4, Iactual, Cl2 was the actual peak intensity of Cl2 and Ifragmented, Cl2 was the fragmented peak intensity of Cl2 obtained from equation 3. Such difference reflected the amount of Cl2 generated in the system.

S1.5. Data Analysis and Interpretation for Fig. 2e, Fig. 2f

For each of the species reported in Fig. 2e and Fig. 2f (Cl2, SO2 and SO2Cl2), we first calculated the amount of these species that are non-fragments in nature (‘free’ species, e.g., Ifree Cl2,   X hours retained) at different battery states (charged and then retained for 0 hour, 24 hours, 72 hours, or 120 hours and then discharged), and divided by the amount for the charged battery at 0 retention time (e.g., Ifree Cl2,   0 hour retained). This ratio was shown in percentage for the y-axis of Fig. 2e and Fig. 2f. It was compared with the percentage of discharging plateaus retained at 3.55 V and 3.18 V at the respective battery states in Fig. 2e and Fig. 2f. For example, when analyzing Cl2, we would compare the following two quantities and plotted them in Fig. 2e:

Ifree Cl2, 24 hours retainedIfree Cl2, 0 hour retained versus Capacity of 3.55 V plateau, 24 hours retainedCapacity of 3.55 V plateau, 0 hour retained

In the above two expressions,  Ifree Cl2, 24 hours retained and Ifree Cl2, 0 hour retained  were the amount of free Cl2 determined from equation 4 when the battery retained at open circuit for 24 hours and 0 hour, respectively.

S1.6. Data Analysis and Interpretation for Extended Data Fig. 4

Similarly, for any species of interest in our battery after stable cycling, we could calculate the percent difference between the actual detected peak intensity and its peak intensity due to fragmentation of larger molecules by:

percent difference = Iactual-IfragmentedIfragmented×100%			       (5)

If in any battery state, the percent difference of a given species obtained from equation 5 was larger than 0, then there must be free species generated at that state. On the other hand, if the percent difference was close to 0, then all the peak intensity of that species in the spectrum was contributed by the fragmentations of SOCl2, S2Cl2 and SO2Cl2 and no free species existed at that battery state. Such data was reported in Extended Data Fig. 4, in which we analyzed how the amount of free Cl2 and SCl2 changed as the battery was either fully charged or fully discharged.

Text S2. Proposed Reactions During Battery Charge – Discharge

Cl2 could be formed during charging by the oxidation of Cl- in NaCl and further reacted with S to form S2Cl2 and SCl2 by the following reactions:

2 NaCl → 2 Na++Cl2+2e- 				       (6)

S+Cl2→SCl2 					       (7)

2 SCl2⇄S2Cl2+Cl2				       (8)

SCl2 was known to undergo dissociation to form S2Cl2 and Cl2 (equation 8). In addition, S2Cl2 and Cl2 could also be formed by SOCl2 oxidation and SOCl2 reaction with S according to the following reactions:

4 SOCl2→2 SO2+S2Cl2+3 Cl2 		                   (9)

SOCl2→SOCl++12 Cl2+e- 		                 (10)

2 SOCl2+3 S→SO2+2 S2Cl2		                 (11)

The oxidized SOCl2 was regenerated during discharge when NaCl was produced and reacted with AlCl4-•SOCl+, which was formed by combining SOCl+ and AlCl4-, by the following reaction:

NaCl+AlCl4-·SOCl+→NaAlCl4+SOCl2 			     (12)

Also, the SO2 generated during the first discharge and subsequent charging was well known to react with Cl2 to form SO2Cl2 via:

SO2+Cl2⇌SO2Cl2			                 (13)

These reactions led to the coexistence of Cl2, SCl2, SOCl2, S2Cl2 and SO2Cl2 in the electrolyte.

It was reported that SCl2/S2Cl2 were generated and showed obvious reduction when oxidation scan passed 4.5 V vs. Li, with reduction voltage at 3.65 V – 3.8 V vs. Li. Also, different  studies on lithium/thionyl chloride cells reported that SO2Cl2 had a reduction potential ~ 0.35 V lower than Cl2, which was consistent with our observation.

The reduction reactions happened at each discharge voltage were as follows:

2 Na++SCl2+2 e-→S+2 NaCl 	                     ~ 3.69 V

2 Na++S2Cl2+2 e-→2 S+2 NaCl		         ~ 3.69 V

2 Na++Cl2+2 e-→2 NaCl		         ~ 3.55 V

2 Na++SO2Cl2+2 e-→SO2+2 NaCl	                     ~ 3.18 V