# Supplementary Information for

# Inelastic phonon transport across atomically sharp metal/semiconductor interfaces

Houfu Song1,*, Fang Liu2,3,*, Song Hu4,*, Qinshu Li1,*, Susu Yang2, Lu Zhao1, Hailing Jiang2, Jinlin Wang2, Tao Wang5, Yee Kan Koh6, Feiyu Kang1,7, Junqiao Wu8,9, Xiaokun Gu4,†, Bo Sun1,7,† and Xinqiang Wang2,3,†

1Tsinghua-Berkeley Shenzhen Institute, Tsinghua University, Shenzhen 518055, China.

2State Key Laboratory for Mesoscopic Physics and Frontiers Science Center for Nano-optoelectronics, School of Physics, Peking University, Beijing 100871, China.

3Collaborative Innovation Center of Quantum Matter, Beijing 100871, China.

4Institute of Engineering Thermophysics, School of Mechanical Engineering, Shanghai Jiao Tong University, Shanghai 200240, China.

5Electron Microscopy Laboratory, School of Physics, Peking University, Beijing 100871, China.

6Department of Mechanical Engineering and Center of Advanced 2D Materials, National University of Singapore, 117576 Singapore.

7Tsinghua Shenzhen International Graduate School and Guangdong Provincial Key Laboratory of Thermal Management Engineering & Materials, Shenzhen 518055, China.

8Department of Materials Science and Engineering, University of California, Berkeley, CA 94720, USA.

9Materials Sciences Division, Lawrence Berkeley National Laboratory, Berkeley, CA 94720, USA.

*These authors contributed equally.

†To whom correspondence should be addressed: sun.bo@sz.tsinghua.edu.cn, wangshi@pku.edu.cn, xiaokun.gu@sjtu.edu.cn

I. MBE growth of Al (111) film on Si (111) substrate

The high-energy electron diffraction (RHEED) is used to monitor the growth process of an 80-nm-thick Al film on Si substrate. As depicted in Fig. S1a, the Si surface has a typical (7×7) reconstructed diffraction patterns after thermal treatment at 900 ℃ for 30 minutes, indicating that there is no oxide layer on its surface. As the epitaxy starts at 100 °C, the stripe patterns of the Al film immediately appeared and remained unchanged. This phenomenon is mainly due to the formation of a sharp epitaxial interface between Al and Si. The X-ray diffraction (XRD) spectrum in Fig. S1b shows a sharp peak at 38.4° from Al(111) plane and another sharp peak from Si(111) plane at 28.4°, and the full width at half maximum (FWHM) value of the -rocking curves for the Al(111) plane is 0.13°, which further confirms the high crystallinity of the epitaxial Al film1,2. Then, the surface morphology of the Al film is characterized by atomic force microscopy (AFM). It is found that the Al film grown at 100 ℃ (Al/Si Sample 1) has a continuous flat surface with a small root mean square (RMS) roughness of 0.26 nm, as depicted in Fig. S1c. When the epitaxial temperature rises to 300 ℃, the surface morphology of the Al film was deteriorated significantly (Fig. S1d), and the RMS roughness of the Al film (Al/Si Sample 2) increases to 17.1 nm.

Figure S1 (a) In-situ RHEED patterns of the Si (111) substrate just before Al (111) growth (I), after 1-minute growth (Ⅱ) and after 20-minutes growth (III) at 100 ℃ with the incident electron beam parallel to the [01-1] direction of the Si substrate. (b) XRD 2- scan and -scan spectrum of the epitaxial Al film on Si. (c) AFM image with a 3×3 µm2 scanned area of Al/Si Sample 1. (d) AFM image with a 3×3 µm2 scanned area of Al/Si Sample 2.

II. Characterization of interface structure of Al/Si Sample 2

The high-angle annular dark-field scanning transmission electron microscopy (HAADF-STEM) was performed to demonstrate the interface structure of Al/Si Sample 2, as shown in Fig. S2a. We found that there is an around 2-nm-thick intermediate layer with nearly disordered lattice arrangement between the epilayer and the substrate. Energy-dispersive x-ray spectroscopy (EDX) further reveals this intermediate layer is composed of Si and Al atoms (in Fig. S2c and Fig. S2d), where Si atoms are enriched on the side close to the substrate and Al atoms are enriched on the side close to the epilayer shown as the result of EDX line scan analysis (in Fig. S2b). This indicates that the intermediate layer is most likely originated from the intermixing of Al and Si atoms at a higher growth temperature, resulting in a relatively rough interface3. Note that EDX measurements only give a quantitative analysis due to limited spatial resolution.

Figure S2 (a) STEM image of Al/Si Sample 2 interface. (b) EDX line scan analysis of Al/Si interface, showing the Al and Si atomic fraction at the interfacial region. (c-d) EDX mapping images taken at the Al/Si interface. (Dash lines cover the same region in (a-d)).

III. The calculated Gpp for Al/Si Sample 1, Sample 2 and Al/GaN interfaces

Here, to calculate the phonon-phonon transport induced interface thermal conductance alone, we follow Majumdar and Reddy’s treatment of electron-phonon coupling and use G=GepGppGep+Gpp, explained in detail in the main text.

Figure S3 Thermal conductance of Al/Si and Al/GaN interfaces. (a) The calculated Gpp of Al/Si Sample 1 (red diamonds) and Sample 2 (blue diamonds). (b) The calculated Gpp of Al/GaN (red diamonds).

Ⅳ. TDTR measurement and estimation of measurement uncertainty

# Before TDTR measurement, we do the sensitivity analysis to determine the optimized parameters. The sensitivity is defined as,

Sα= ∂(-VinVout)∂lnα# AUTONUM

where –Vin/Vout is TDTR signal, and α is the parameter that is used in our thermal model. In a typical measurement, there are usually two unknown parameters, interface thermal conductance between transducer and substrate (G) and thermal conductivity of the substrate (). Table S1 and S2 shows the calculated sensitivity to all parameters in our thermal model, where hAl, ΛAl, CAl, CSi, w0 and φ are the thickness, thermal conductivity and heat capacity of Al, heat capacity of Si, laser spot radius, and phase of the lock-in amplifier, respectively.

# Table S1 Sensitivity to the parameters in TDTR measurement of thermal conductance of Al/Si interface.

| T |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 704.8 K | 0.765 | 0.055 | 0.858 | 0.437 | 0.340 | 0.061 | 7.045 |
| 604.2 K | 0.770 | 0.052 | 0.860 | 0.435 | 0.355 | 0.065 | 7.339 |
| 503.7 K | 0.780 | 0.050 | 0.870 | 0.434 | 0.320 | 0.070 | 7.633 |
| 403.5 K | 0.790 | 0.048 | 0.880 | 0.433 | 0.325 | 0.075 | 8.499 |
| 352.5 K | 0.799 | 0.047 | 0.882 | 0.433 | 0.327 | 0.080 | 9.111 |
| 302.5 K | 0.813 | 0.038 | 0.893 | 0.426 | 0.366 | 0.085 | 10.229 |
| 242.0 K | 0.817 | 0.038 | 0.894 | 0.402 | 0.386 | 0.112 | 10.972 |
| 191.7 K | 0.825 | 0.037 | 0.894 | 0.398 | 0.429 | 0.114 | 12.709 |
| 151.3 K | 0.831 | 0.036 | 0.897 | 0.342 | 0.489 | 0.174 | 14.171 |
| 121.3 K | 0.840 | 0.033 | 0.905 | 0.304 | 0.556 | 0.214 | 17.557 |
| 101.3 K | 0.856 | 0.029 | 0.911 | 0.170 | 0.635 | 0.354 | 22.145 |
| 81.2 K | 0.860 | 0.025 | 0.915 | 0.188 | 0.710 | 0.339 | 26.238 |

# Table S2 Sensitivity to parameters in TDTR measurement of thermal conductance of Al/GaN interface.

| T |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 604.2 K | 0.480 | 0.014 | 0.510 | 0.260 | 0.360 | 0.120 |  | 9.585 |
| 503.7 K | 1.000 | 0.040 | 1.030 | 0.257 | 0.310 | 0.010 |  | 9.299 |
| 403.5 K | 0.980 | 0.020 | 1.000 | 0.430 | 0.310 | 0.020 |  | 10.744 |
| 352.5 K | 0.960 | 0.030 | 0.980 | 0.430 | 0.300 | 0.030 |  | 11.190 |
| 302.5 K | 0.930 | 0.020 | 0.960 | 0.434 | 0.312 | 0.020 |  | 11.458 |
| 242.0 K | 0.890 | 0.020 | 0.910 | 0.430 | 0.300 | 0.020 |  | 12.838 |
| 191.7 K | 0.834 | 0.030 | 0.862 | 0.440 | 0.310 | 0.030 |  | 14.151 |
| 151.3 K | 0.754 | 0.014 | 0.784 | 0.414 | 0.380 | 0.030 |  | 16.092 |
| 121.3 K | 0.655 | 0.015 | 0.686 | 0.440 | 0.427 | 0.036 |  | 17.308 |
| 101.3 K | 0.550 | 0.016 | 0.580 | 0.410 | 0.470 | 0.040 |  | 18.325 |
| 81.2 K | 0.366 | 0.020 | 0.400 | 0.370 | 0.550 | 0.069 |  | 19.352 |

After all the sensitivity parameters are calculated, the measurement uncertainty of interface thermal conductance of Al/Si and Al/GaN interfaces can be calculated using the following equation:

(2)

The uncertainties we used for the parameters are shown in the following table.

Table S3 Uncertainties for the parameters used in our thermal model.

|  | uncertainty |
| --- | --- |
|  | ±3.75% |
|  | ±10% |
|  | ±2% |
|  | ±2% |
|  | ±10% |
|  | 0.001 |

Put the uncertainties in Tab. S3 into Eq.2, we then calculated the measurement uncertainty of G, which shows in our Fig. 1 in the main text.

Ⅴ. Raw TDTR data for Sample 1 and Sample 2

TDTR raw data of Sample1 and Sample 2 are presented here from 80 K to 700 K. Here, G1 and G2 represent the measured thermal conductance of Sample 1 and Sample 2 respectively.

Figure S4 Measured TDTR signals from 80 K to 700 K for Al/Si Sample1 and Sample 2.

Here, we used modulation frequency of 10.1 MHz to measure Sample 1. The 1/e2 radius of both pump beam and probe beam is 10.6 μm form 80 K to 350 K and 5.3 μm form 400 K to 700 K. For Sample 2, we used the 1/e2 radius of 10.6 μm of the pump beam and probe beam with modulation frequency of 10.1 MHz from 80 K to 400 K and 1.01 MHz for 500 K and 600 K.

Ⅵ. MD simulation

# Table S4 Simulated result of thermal conductance as a function of temperature by MD. dT is temperature difference of heat bath, and ΔT is simulated temperature drop across interface obtained from linear fit.

| Interface | Length L (nm) | Heat bath dT (K) | Temperature T (K) | Temperature drop ΔT (K) | Heat flux J (ev ps-1) | Thermal conductance G (MW m-2 K-1) |
| --- | --- | --- | --- | --- | --- | --- |
| sharp | 44 | 60 | 300 | 63.64 | 0.9 | 623 |
|  |  |  | 500 | 48.00 | 0.73 | 738 |
|  |  |  | 700 | 35.23 | 0.57 | 826 |
| rough | 44 | 60 | 300 | 57.42 | 1.02 | 496 |
|  |  |  | 500 | 39.43 | 0.83 | 533 |
|  |  |  | 700 | 28.78 | 0.67 | 567 |

Figure S5 Computational geometry across a rectangle-shaped interface of with (a) sharp and (b) rough configuration of Al/Si interface. (c) An example of simulated temperature profile of sharp interface at 500 K with length of 33 nm and heat bath temperature difference of 60 K.

References

1.	Cheng, F. et al. Epitaxial Growth of Atomically Smooth Aluminum on Silicon and Its Intrinsic Optical Properties. ACS Nano 10, 9852–9860 (2016).

2.	Chou, Y. H. et al. High-Operation-Temperature Plasmonic Nanolasers on Single-Crystalline Aluminum. Nano Lett. 16, 3179–3186 (2016).

3.	Hopkins, P. E., Norris, P. M., Stevens, R. J., Beechem, T. E. & Graham, S. Influence of Interfacial Mixing on Thermal Boundary Conductance Across a Chromium/Silicon Interface. J. Heat Transf. 130, (2008).