# Enhanced photocatalytic removal of nitric oxide over Ag-decorated ZnSn(OH)6 microcubes

Minh-Thuan Pham1, 2, 3, Nguyen Thi Van2, Truc Mai Thi Nguyen2, 4, Hong-Huy Tran5, Hieu Trung Nguyen1, Jheng-Jie Jiang2, Sheng-Jie You2, 3*, Ya-Fen Wang2, 3*

1Department of Civil Engineering, Chung Yuan Christian University, Taoyuan 32023, Taiwan.

2Department of Environmental Engineering, Chung Yuan Christian University, Chung Li 32023, Taoyuan, Taiwan.

3Center for Environmental Risk Management, Chung Yuan Christian University, Chung Li 32023, Taoyuan, Taiwan.

4 Center for Environmental Toxin and Emerging-Contaminant Research, Cheng Shiu University, Kaohsiung, Taiwan, ROC.

5 Université Grenoble Alpes, CNRS, Grenoble INP (Institute of Engineering, Université Grenoble Alpes), LMGP, 38000 Grenoble, France.

* Corresponding authors: Ya-Fen Wang: yfwang@cycu.edu.tw; Sheng-Jie You: sjyou@cycu.edu.tw

The NO degradation, NO2 conversion, and apparent quantum efficiency (AQE) were caculated by Eq S1, Eq S2, and Eq S3, respectively.

|  | (S1) |
| --- | --- |
|  | (S2) |
|  | (S3) |

Herein,

- CNO (ppb) is the concentration of NO.

- CNO2is the concentration of NO2, i is the initial state, and f is the final state.

- NA (mol-1) is the Avogadro constant.

- Vt (L min-1) is the flow rate of NO.

- M (g mol-1) is the molar mass of NO.

- The photon flux is 2.72 1019 cm-2 min-1.

- The irradiation area is 113.1 cm2 for the 12 cm diameter dish.

Table S1. EDS mapping data of 20% Ag:cZHS.

| Element | Apparent Concentraton | Wt% | Wt% Sigma |
| --- | --- | --- | --- |
| C | 3.11 | 5.25 | 0.37 |
| O | 37.43 | 31.24 | 0.49 |
| Zn | 13.74 | 21.12 | 0.44 |
| Ag | 3.94 | 2.83 | 0.31 |
| Sn | 53.40 | 39.57 | 0.51 |
| Total |  | 100.00 |  |

Fig. S1 Full spectrum of Xenon lamp of photocatalytic system. (the picture is provided by Prosper Optolectronic co., Ltd. Taiwan).

Fig. S2 EDS spectra of 20% Ag:cZHS (a), the elemental mapping of O (b), Sn (c), Zn (d), and Ag (e).

Fig. S3 Time-dependent ESR of 20% Ag:cZHS in the dark condition (a), and UV condition (b).