Single Crystal X-ray Diffraction Study of [c2] Daisy Chains and Inclusion Complexes from A1/A2-Functionalized Pillar[5]arenes with Varying Chain Lengths

Anshel Saldanha, Mickey Vinodh  Fatemeh H Alipour, Rajani Krishnapillai, Nisha Manoj and Talal F. Al-Azemi

Chemistry Department, Kuwait University, P.O. Box 5969, Safat 13060, Kuwait.

Table of contents

| Table S1 Summary of the key crystallographic parameters of P8_D & P10_D | S2 |
| --- | --- |
| Table S2 Summary of the key crystallographic parameters of P8.ADN & P10.ADN | S3 |
| Fig. S1 Thermal ellipsoid representation the asymmetric unit of P8_D | S4 |
| Fig. S2 Thermal ellipsoid representation the asymmetric unit of P10_D | S5 |
| Fig. Thermal ellipsoid representation the asymmetric unit of P8.ADN | S6 |
| Fig. S4 Thermal ellipsoid representation the asymmetric unit of P10.ADN | S7 |
| Fig. S5 Possible intermolecular interactions between P10_D dimeric systems in crystal network with adjacent pillar[5]arene dimers | S8 |
| Fig. S6 Hirshfeld surfaces (mapped with dnorm) of the P8.ADN and P10.ADN crystals. | S9 |
| Fig. S7 Packing pattern of P8_D and P10_D crystals. | S10 |
| Fig. S8 Packing pattern of P8.ADN and P10.ADN crystals. | S11 |
| checkCif report of P8_D | S12 |
| checkCif report of P10_D | S15 |
| checkCif report of P8.ADN | S18 |
| checkCif report of P10.ADN | S21 |

Table S1. Summary of the key crystallographic parameters of P8_D & P10_D

| Crystal sample | P8_D | P10_D |
| --- | --- | --- |
| Chemical formula | C111H131Cl9O20 | C62H80O10 |
| Mr | 2104.20 | 985.26 |
| Crystal system, space group | Monoclinic, C2/c | Monoclinic, P21/c |
| Temperature (K) | 293 | 293 |
| a, b, c (Å) | 39.539 (4), 12.6249 (12), 22.946 (2) | 21.690 (2), 12.8951 (14), 22.960 (2) |
| α, β, γ (°) | 90, 108.114 (8), 90 | 90, 116.539 (8), 90 |
| V (Å3) | 10886.3 (19) | 5745.2 (11) |
| Z | 4 | 4 |
| Radiation type | Mo Kα | Mo Kα |
| µ (mm−1) | 0.30 | 0.08 |
| Crystal size (mm) | 0.22 × 0.06 × 0.03 | 0.21 × 0.09 × 0.03 |
| Diffractometer | Rigaku R-AXIS RAPID | Rigaku R-AXIS RAPID |
| Absorption correction | Multi-scan ABSCOR (Rigaku, 1995) | Absorption correction ABSCOR (Rigaku, 1995) |
| Tmin, Tmax | 0.267, 0.990 | 0.178, 0.998 |
| No. of measured, independent & observed [I > 2σ(I)] reflections | 34210, 9287, 3680 | 37991, 10045, 3132 |
| Rint | 0.119 | 0.150 |
| (sin θ/λ)max (Å−1) | 0.590 | 0.594 |
| R[F2 > 2σ(F2)], wR(F2), S | 0.113, 0.342, 1.23 | 0.110, 0.331, 1.08 |
| No. of reflections | 9287 | 10045 |
| No. of parameters | 652 | 656 |
| No. of restraints | 114 | 101 |
| H-atom treatment | Mixed | Constrained |
| Δρmax, Δρmin (e Å−3) | 0.88, −0.59 | 0.41, −0.31 |

Table S2 Summary of the key crystallographic parameters of P8.ADN & P10.ADN

| Crystal sample | P8_ADN | P10_ADN |
| --- | --- | --- |
| Chemical formula | C60H72N2O10 | C62H76N2O10 |
| Mr | 981.19 | 1009.24 |
| Crystal system, space group | Monoclinic, P21/n | Triclinic, P-1 |
| Temperature (K) | 293 | 293 |
| a, b, c (Å) | 12.1153(6), 12.4294(7), 37.2417 (19) | 11.2701(12), 12.0419(13), 24.328 (3) |
| α, β, γ (°) | 90, 90.735 (6), 90 | 76.594 (5), 89.067 (6), 63.961 (5) |
| V (Å3) | 5607.6 (5) | 2871.8 (6) |
| Z | 4 | 2 |
| Radiation type | Mo Kα | Mo Kα |
| µ (mm−1) | 0.08 | 0.08 |
| Crystal size (mm) | 0.20 × 0.20 × 0.04 | 0.20 × 0.06 × 0.04 |
| Diffractometer | Rigaku R-AXIS RAPID | Rigaku R-AXIS RAPID |
| Absorption correction | Multi-scan ABSCOR (Rigaku, 1995) | Absorption correction ABSCOR (Rigaku, 1995) |
| Tmin, Tmax | 0.698, 0.982 | 0.149, 0.997 |
| No. of measured, independent & observed [I > 2σ(I)] reflections | 54642, 9866, 4515 | 22097, 9772, 3255 |
| Rint | 0.058 | 0.092 |
| (sin θ/λ)max (Å−1) | 0.595 | 0.595 |
| R[F2 > 2σ(F2)], wR(F2), S | 0.108, 0.342, 0.95 | 0.107, 0.349, 1.04 |
| No. of reflections | 9866 | 9772 |
| No. of parameters | 658 | 676 |
| No. of restraints | 166 | 146 |
| H-atom treatment | Constrained | Constrained |
| Δρmax, Δρmin (e Å−3) | 0.48, −0.53 | 0.40, −0.31 |

Fig. S1 Thermal ellipsoid representation ( 30% probability) the asymmetric unit of P8_D

Fig. S2 Thermal ellipsoid representation ( 30% probability) the asymmetric unit of P10_D

Fig. S3 Thermal ellipsoid representation ( 30% probability) the asymmetric unit of P8.ADN

Fig. S4 Thermal ellipsoid representation ( 30% probability) the asymmetric unit of P10.ADN

Fig. S5: Possible intermolecular interactions between P10_D dimeric systems  in crystal network with adjacent pillar[5]arene dimers of different symmetries.  Symmetry code: (i) 2-x, 2-y, 2-z; (ii) x, -1+y,z; (iii) 2-x, 1-y, 2-z; (iv) x, 1+y, z & (v) 2-x, 3-y,2-z; 5 is the centroid of the phenyl ring constituting C29-C34.

Fig. S6. Hirshfeld surfaces (mapped with dnorm) of the P8.ADN and P10.ADN crystals.

Fig. S7. Packing pattern of P8_D and P10_D crystals.

Fig. S8. Packing pattern of P8.ADN and P10.ADN crystals.

checkCIF_ P8_D

heckCIF (basic structural check) running

Checking for embedded fcf data in CIF ...
Found embedded fcf data in CIF. Extracting fcf data from uploaded CIF, please wait . . . .

checkCIF/PLATON (basic structural check)

Structure factors have been supplied for datablock(s) P8_D

THIS REPORT IS FOR GUIDANCE ONLY. IF USED AS PART OF A REVIEW PROCEDURE FOR PUBLICATION, IT SHOULD NOT REPLACE THE EXPERTISE OF AN EXPERIENCED CRYSTALLOGRAPHIC REFEREE.

No syntax errors found.

CIF dictionary Please wait while processing ....  Interpreting this report Structure factor report

Datablock: P8_D

| Bond precision: | C-C = 0.0106 A | Wavelength=0.71075 |
| --- | --- | --- |

| Cell: | a=39.539(4) | b=12.6249(12) | c=22.946(2) |
| --- | --- | --- | --- |
|  | alpha=90 | beta=108.114(8) | gamma=90 |
| Temperature: | 293 K |  |  |

|  | Calculated | Reported |
| --- | --- | --- |
| Volume | 10886.4(19) | 10886.3(19) |
| Space group | C 2/c | C 2/c |
| Hall group | -C 2yc | -C 2yc |
| Moiety formula | 2(C54 H64 O10), 3(C H Cl3) | ? |
| Sum formula | C111 H131 Cl9 O20 | C111 H131 Cl9 O20 |
| Mr | 2104.21 | 2104.20 |
| Dx,g cm-3 | 1.284 | 1.284 |
| Z | 4 | 4 |
| Mu (mm-1) | 0.298 | 0.298 |
| F000 | 4440.0 | 4440.0 |
| F000' | 4447.25 |  |
| h,k,lmax | 46,14,27 | 46,14,26 |
| Nref | 9394 | 9287 |
| Tmin,Tmax | 0.979,0.991 | 0.267,0.990 |
| Tmin' | 0.937 |  |

| Correction method= # Reported T Limits: Tmin=0.267 Tmax=0.990 AbsCorr = MULTI-SCAN |  |
| --- | --- |

| Data completeness= 0.989 | Theta(max)= 24.807 |
| --- | --- |

| R(reflections)= 0.1129( 3680) | wR2(reflections)= 0.3424( 9287) |
| --- | --- |
| S = 1.228; Npar= 652. |  |

The following ALERTS were generated. Each ALERT has the format

test-name_ALERT_alert-type_alert-level.

Click on the hyperlinks for more details of the test.

Alert level B

PLAT260_ALERT_2_B Large Average Ueq of Residue Including       Cl1      0.324 Check

Response: Due to bad crystal quality, the solvents peaks are not well refined.

PLAT340_ALERT_3_B Low Bond Precision on  C-C Bonds ...............    0.01063 Ang.

Respnse: This is due to the bad crystal quality.

PLAT910_ALERT_3_B Missing FCF Reflection(s) Below Theta(Min)[Deg]=       3.13 Note

1  1  0,   2  0  0,   3  1  0,   4  0  0,  -5  1  1,  -3  1  1,

-1  1  1,   1  1  1,   3  1  1,  -4  0  2,  -3  1  2,  -2  0  2,

-1  1  2,   0  0  2,   1  1  2,   2  0  2,

Response: The unit cell is reasonable large and these low angle reflections are probably missing due to beamstop. This occurs rather frequently with Mo radiation and our gonoimeter geometry, especially for larger unit cells.

Alert level C

PLAT026_ALERT_3_C Ratio Observed / Unique Reflections (too) Low ..        40% Check

PLAT082_ALERT_2_C High R1 Value ..................................       0.11 Report

PLAT084_ALERT_3_C High wR2 Value (i.e. > 0.25) ...................       0.34 Report

PLAT220_ALERT_2_C NonSolvent   Resd 1  C   Ueq(max)/Ueq(min) Range        5.3 Ratio

PLAT222_ALERT_3_C NonSolvent Resd 1  H   Uiso(max)/Uiso(min) Range        5.0 Ratio

PLAT234_ALERT_4_C Large Hirshfeld Difference C22      --C27      .       0.16 Ang.

PLAT241_ALERT_2_C High   'MainMol' Ueq as Compared to Neighbors of        C41 Check

PLAT242_ALERT_2_C Low    'MainMol' Ueq as Compared to Neighbors of         O4 Check

And 5 other PLAT242 Alerts

More ...

PLAT244_ALERT_4_C Low    'Solvent' Ueq as Compared to Neighbors of        C55 Check

PLAT260_ALERT_2_C Large Average Ueq of Residue Including       Cl4      0.294 Check

PLAT906_ALERT_3_C Large K Value in the Analysis of Variance ......     36.567 Check

And 2 other PLAT906 Alerts

More ...

PLAT911_ALERT_3_C Missing FCF Refl Between Thmin & STh/L=    0.590         89 Report

-5  1  2,   2  0  4,   4  0  4,   2  0  6,   4  0  6,   2  0  8,

4  0  8,   4  0 10,  -2  0 14, -11  7 17, -10  0 20,  -8  0 20,

-6  0 20, -16  0 22, -14  0 22, -12  0 22, -10  0 22,  -8  0 22,

-6  0 22,  -4  0 22, -20  0 24, -18  0 24, -16  0 24, -14  0 24,

-12  0 24, -11  1 24, -10  0 24,  -9  1 24,  -8  0 24,  -6  0 24,

(   59 More Missing: see the .ckf listing file)

Alert level G

PLAT002_ALERT_2_G Number of Distance or Angle Restraints on AtSite         18 Note

PLAT003_ALERT_2_G Number of Uiso or U(i,j)  Restrained non-H-Atoms         15 Report

PLAT128_ALERT_4_G Alternate Setting for Input Space-group     C2/c       I2/a Note

PLAT172_ALERT_4_G The CIF-Embedded .res File Contains DFIX Records          4 Report

PLAT173_ALERT_4_G The CIF-Embedded .res File Contains DANG Records          2 Report

PLAT177_ALERT_4_G The CIF-Embedded .res File Contains DELU Records          3 Report

PLAT178_ALERT_4_G The CIF-Embedded .res File Contains SIMU Records          3 Report

PLAT192_ALERT_3_G A Non-default DELU Restraint Value for First Par     0.0200 Report

And 2 other PLAT192 Alerts

More ...

PLAT199_ALERT_1_G Reported _cell_measurement_temperature ..... (K)        293 Check

PLAT200_ALERT_1_G Reported   _diffrn_ambient_temperature ..... (K)        293 Check

PLAT299_ALERT_4_G Atom Site Occupancy Constrained at .............        0.5 Check

Cl5     C56     H56

PLAT302_ALERT_4_G Anion/Solvent/Minor-Residue Disorder (Resd    2)        50% Note

PLAT434_ALERT_2_G Short Inter HL..HL Contact Cl3      ..Cl5      .       3.23 Ang.

1-x,y,3/2-z  =      2_656 Check

PLAT779_ALERT_4_G Suspect or Irrelevant (Bond) Angle(s) in CIF ...      36.80 Deg.

C56  -CL5  -CL4     1_555   1_555   2_656 ......     #   11 Check

PLAT789_ALERT_4_G Atoms with Negative _atom_site_disorder_group  #          2 Check

PLAT822_ALERT_4_G CIF-embedded .res Contains Negative PART Numbers          1 Check

PLAT860_ALERT_3_G Number of Least-Squares Restraints .............        114 Note

PLAT883_ALERT_1_G Absent Datum for _atom_sites_solution_primary ..     Please Do !

PLAT933_ALERT_2_G Number of HKL-OMIT Records in Embedded .res File          3 Note

-5  1  2,  -2  0 14,  -5  1  1,

PLAT941_ALERT_3_G Average HKL Measurement Multiplicity ...........        3.7 Low

PLAT965_ALERT_2_G The SHELXL WEIGHT Optimisation has not Converged     Please Check

PLAT969_ALERT_5_G The 'Henn et al.' R-Factor-gap value ...........      5.402 Note

Predicted wR2: Based on SigI**2  6.34 or SHELX Weight 27.88

PLAT978_ALERT_2_G Number C-C Bonds with Positive Residual Density.          0 Info

0 ALERT level A = Most likely a serious problem - resolve or explain

3 ALERT level B = A potentially serious problem, consider carefully

19 ALERT level C = Check. Ensure it is not caused by an omission or oversight

25 ALERT level G = General information/check it is not something unexpected

3 ALERT type 1 CIF construction/syntax error, inconsistent or missing data

17 ALERT type 2 Indicator that the structure model may be wrong or deficient

14 ALERT type 3 Indicator that the structure quality may be low

12 ALERT type 4 Improvement, methodology, query or suggestion

1 ALERT type 5 Informative message, check

It is advisable to attempt to resolve as many as possible of the alerts in all categories. Often the minor alerts point to easily fixed oversights, errors and omissions in your CIF or refinement strategy, so attention to these fine details can be worthwhile. It is up to the individual to critically assess their own results and, if necessary, seek expert advice.

PLATON version of 26/09/2025; check.def file version of 20/09/2025

duplicate check

No duplication found

checkCIF_ P10_D checkCIF (basic structural check) running Checking for embedded fcf data in CIF ... Found embedded fcf data in CIF. Extracting fcf data from uploaded CIF, please wait . . . . checkCIF/PLATON (basic structural check) Structure factors have been supplied for datablock(s) P10_D THIS REPORT IS FOR GUIDANCE ONLY. IF USED AS PART OF A REVIEW PROCEDURE FOR PUBLICATION, IT SHOULD NOT REPLACE THE EXPERTISE OF AN EXPERIENCED CRYSTALLOGRAPHIC REFEREE. No syntax errors found. CIF dictionary Please wait while processing .... Interpreting this report Structure factor report Datablock: P10_D Bond precision:; C-C = 0.0129 A; Wavelength=0.71075. Cell:; a=21.690(2); b=12.8951(14); c=22.960(2). alpha=90; beta=116.539(8); gamma=90. Temperature:; 293 K. Calculated; Reported. Volume; 5745.1(10); 5745.2(11). Space group; P 21/c; P 21/c. Hall group; -P 2ybc; -P 2ybc. Moiety formula; C56 H68 O10, C6 H12; ?. Sum formula; C62 H80 O10; C62 H80 O10. Mr; 985.26; 985.26. Dx,g cm-3; 1.139; 1.139. Z; 4; 4. Mu (mm-1); 0.076; 0.076. F000; 2128.0; 2128.0. F000'; 2129.00. h,k,lmax; 25,15,27; 25,15,27. Nref; 10108; 10045. Tmin,Tmax; 0.992,0.998; 0.178,0.998. Tmin'; 0.984. Correction method= # Reported T Limits: Tmin=0.178 Tmax=0.998 AbsCorr = MULTI-SCAN. Data completeness= 0.994; Theta(max)= 24.995. R(reflections)= 0.1103( 3132); wR2(reflections)= 0.3309( 10045). S = 1.080; Npar= 656.. The following ALERTS were generated. Each ALERT has the format test-name_ALERT_alert-type_alert-level. Click on the hyperlinks for more details of the test. Alert level B PLAT026_ALERT_3_B Ratio Observed / Unique Reflections (too) Low .. 31% Check Respnse: Due to bad crystal quality, the high resolution reflections were poor. We are confident that the structural characterization is valid. PLAT340_ALERT_3_B Low Bond Precision on C-C Bonds ............... 0.01291 Ang. Respnse: This is due to the bad crystal quality. PLAT910_ALERT_3_B Missing FCF Reflection(s) Below Theta(Min)[Deg]= 3.06 Note 1 0 0, 1 1 0, 2 0 0, 2 1 0, -2 1 1, -1 1 1, 0 1 1, 1 1 1, -3 0 2, -2 0 2, -2 1 2, -1 0 2, -1 1 2, 0 0 2, 0 1 2, 1 0 2, Response: The unit cell is reasonable large and these low angle reflections are probably missing due to beamstop. This occurs rather frequently with Mo radiation and our gonoimeter geometry, especially for larger unit cells. Alert level C RINTA01_ALERT_3_C The value of Rint is greater than 0.12 Rint given 0.150 PLAT020_ALERT_3_C The Value of Rint is Greater Than 0.12 ......... 0.150 Report PLAT082_ALERT_2_C High R1 Value .................................. 0.11 Report PLAT084_ALERT_3_C High wR2 Value (i.e. > 0.25) ................... 0.33 Report PLAT220_ALERT_2_C NonSolvent Resd 1 C Ueq(max)/Ueq(min) Range 5.6 Ratio PLAT222_ALERT_3_C NonSolvent Resd 1 H Uiso(max)/Uiso(min) Range 6.7 Ratio PLAT234_ALERT_4_C Large Hirshfeld Difference O1 --C36 . 0.16 Ang. And 6 other PLAT234 Alerts More ... PLAT241_ALERT_2_C High 'MainMol' Ueq as Compared to Neighbors of C21 Check PLAT241_ALERT_2_C High 'MainMol' Ueq as Compared to Neighbors of C47 Check PLAT242_ALERT_2_C Low 'MainMol' Ueq as Compared to Neighbors of O4 Check And 2 other PLAT242 Alerts More ... PLAT243_ALERT_4_C High 'Solvent' Ueq as Compared to Neighbors of C58 Check PLAT244_ALERT_4_C Low 'Solvent' Ueq as Compared to Neighbors of C60 Check PLAT260_ALERT_2_C Large Average Ueq of Residue Including O1 0.119 Check PLAT260_ALERT_2_C Large Average Ueq of Residue Including C57 0.244 Check PLAT360_ALERT_2_C Short C(sp3)-C(sp3) Bond C57 - C62 . 1.42 Ang. And 2 other PLAT360 Alerts More ... PLAT372_ALERT_2_C Short C(sp)-C(sp) Bond C37 - C38 . 1.14 Ang. PLAT413_ALERT_2_C Short Inter XH3 .. XHn H50C ..H56C . 2.14 Ang. 2-x,2-y,2-z = 3_777 Check PLAT601_ALERT_2_C Unit-Cell Contains Solvent Accessible VOIDS .LE. 40 Ang**3 PLAT906_ALERT_3_C Large K Value in the Analysis of Variance ...... 104.605 Check And 6 other PLAT906 Alerts More ... PLAT911_ALERT_3_C Missing FCF Refl Between Thmin & STh/L= 0.594 47 Report -5 15 1, 6 2 1, 17 10 1, -22 6 2, 16 10 3, -5 15 4, 14 11 4, -4 15 5, 0 15 5, -25 0 6, -16 12 7, -16 12 8, 14 9 8, 16 7 8, 16 6 9, -13 13 10, -6 14 11, -4 14 11, -14 12 14, -9 13 14, -3 13 14, -13 12 15, -2 12 16, 0 11 17, -20 8 18, 1 10 18, 8 5 18, -8 11 19, -20 7 20, -4 10 20, ( 17 More Missing: see the .ckf listing file) Alert level G PLAT002_ALERT_2_G Number of Distance or Angle Restraints on AtSite 14 Note PLAT003_ALERT_2_G Number of Uiso or U(i,j) Restrained non-H-Atoms 11 Report PLAT172_ALERT_4_G The CIF-Embedded .res File Contains DFIX Records 2 Report PLAT173_ALERT_4_G The CIF-Embedded .res File Contains DANG Records 2 Report PLAT177_ALERT_4_G The CIF-Embedded .res File Contains DELU Records 2 Report PLAT178_ALERT_4_G The CIF-Embedded .res File Contains SIMU Records 2 Report PLAT188_ALERT_3_G A Non-default SIMU Restraint Value has been used 0.0100 Report PLAT188_ALERT_3_G A Non-default SIMU Restraint Value has been used 0.0100 Report PLAT199_ALERT_1_G Reported _cell_measurement_temperature ..... (K) 293 Check PLAT200_ALERT_1_G Reported _diffrn_ambient_temperature ..... (K) 293 Check PLAT790_ALERT_4_G Centre of Gravity not Within Unit-Cell: Resd. # 2 Note C6 H12 PLAT860_ALERT_3_G Number of Least-Squares Restraints ............. 101 Note PLAT883_ALERT_1_G Absent Datum for _atom_sites_solution_primary .. Please Do ! PLAT933_ALERT_2_G Number of HKL-OMIT Records in Embedded .res File 1 Note 6 2 1, PLAT941_ALERT_3_G Average HKL Measurement Multiplicity ........... 3.8 Low PLAT965_ALERT_2_G The SHELXL WEIGHT Optimisation has not Converged Please Check PLAT969_ALERT_5_G The 'Henn et al.' R-Factor-gap value ........... 3.771 Note Predicted wR2: Based on SigI**2 8.78 or SHELX Weight 30.64 PLAT978_ALERT_2_G Number C-C Bonds with Positive Residual Density. 0 Info 0 ALERT level A = Most likely a serious problem - resolve or explain 3 ALERT level B = A potentially serious problem, consider carefully 36 ALERT level C = Check. Ensure it is not caused by an omission or oversight 18 ALERT level G = General information/check it is not something unexpected 3 ALERT type 1 CIF construction/syntax error, inconsistent or missing data 20 ALERT type 2 Indicator that the structure model may be wrong or deficient 19 ALERT type 3 Indicator that the structure quality may be low 14 ALERT type 4 Improvement, methodology, query or suggestion 1 ALERT type 5 Informative message, check It is advisable to attempt to resolve as many as possible of the alerts in all categories. Often the minor alerts point to easily fixed oversights, errors and omissions in your CIF or refinement strategy, so attention to these fine details can be worthwhile. It is up to the individual to critically assess their own results and, if necessary, seek expert advice.. PLATON version of 26/09/2025; check.def file version of 20/09/2025 duplicate check No duplication found

checkCIF_ P8_ADN

checkCIF (basic structural check) running

Checking for embedded fcf data in CIF ...
Found embedded fcf data in CIF. Extracting fcf data from uploaded CIF, please wait . . . .

checkCIF/PLATON (basic structural check)

Structure factors have been supplied for datablock(s) P8_ADN

THIS REPORT IS FOR GUIDANCE ONLY. IF USED AS PART OF A REVIEW PROCEDURE FOR PUBLICATION, IT SHOULD NOT REPLACE THE EXPERTISE OF AN EXPERIENCED CRYSTALLOGRAPHIC REFEREE.

No syntax errors found.

CIF dictionary Please wait while processing ....  Interpreting this reportmStructure factor report

Datablock: P8_ADN

| Bond precision: | C-C = 0.0111 A | Wavelength=0.71075 |
| --- | --- | --- |

| Cell: | a=12.1153(6) | b=12.4294(7) | c=37.2417(19) |
| --- | --- | --- | --- |
|  | alpha=90 | beta=90.735(6) | gamma=90 |
| Temperature: | 293 K |  |  |

|  | Calculated | Reported |
| --- | --- | --- |
| Volume | 5607.6(5) | 5607.6(5) |
| Space group | P 21/n | P 21/n |
| Hall group | -P 2yn | -P 2yn |
| Moiety formula | C54 H64 O10, C6 H8 N2 | ? |
| Sum formula | C60 H72 N2 O10 | C60 H72 N2 O10 |
| Mr | 981.20 | 981.19 |
| Dx,g cm-3 | 1.162 | 1.162 |
| Z | 4 | 4 |
| Mu (mm-1) | 0.078 | 0.078 |
| F000 | 2104.0 | 2104.0 |
| F000' | 2104.99 |  |
| h,k,lmax | 14,14,44 | 14,14,44 |
| Nref | 9924 | 9866 |
| Tmin,Tmax | 0.985,0.997 | 0.698,0.982 |
| Tmin' | 0.985 |  |

| Correction method= # Reported T Limits: Tmin=0.698 Tmax=0.982 AbsCorr = MULTI-SCAN |  |
| --- | --- |

| Data completeness= 0.994 | Theta(max)= 25.024 |
| --- | --- |

| R(reflections)= 0.1084( 4515) | wR2(reflections)= 0.3417( 9866) |
| --- | --- |
| S = 0.954; Npar= 658. |  |

The following ALERTS were generated. Each ALERT has the format

test-name_ALERT_alert-type_alert-level.

Click on the hyperlinks for more details of the test.

Alert level B

PLAT260_ALERT_2_B Large Average Ueq of Residue Including        N1      0.339 Check

Response: Due to bad crystal quality, the encapsulated adiponitrile peaks are not well refined.

PLAT340_ALERT_3_B Low Bond Precision on  C-C Bonds ...............    0.01106 Ang.

Respnse: This is due to the bad crystal quality.

PLAT910_ALERT_3_B Missing FCF Reflection(s) Below Theta(Min)[Deg]=       3.19 Note

1  1  0,  -1  0  1,   1  0  1,  -1  1  1,   0  1  1,   1  1  1,

0  0  2,  -1  1  2,   0  1  2,   1  1  2,  -1  0  3,   1  0  3,

-1  1  3,   0  1  3,   1  1  3,   0  0  4,   0  1  4,

Response: The unit cell is reasonable large and these low angle reflections are probably missing due to beamstop. This occurs rather frequently with Mo radiation and our gonoimeter geometry, especially for larger unit cells.

Alert level C

PLAT026_ALERT_3_C Ratio Observed / Unique Reflections (too) Low ..        46% Check

PLAT082_ALERT_2_C High R1 Value ..................................       0.11 Report

PLAT084_ALERT_3_C High wR2 Value (i.e. > 0.25) ...................       0.34 Report

PLAT220_ALERT_2_C NonSolvent   Resd 1  C   Ueq(max)/Ueq(min) Range        5.6 Ratio

PLAT222_ALERT_3_C NonSolvent Resd 1  H   Uiso(max)/Uiso(min) Range        6.9 Ratio

PLAT230_ALERT_2_C Hirshfeld Test Diff for    O1       --C36      .        5.7 s.u.

PLAT230_ALERT_2_C Hirshfeld Test Diff for    C17      --C18      .        5.6 s.u.

PLAT234_ALERT_4_C Large Hirshfeld Difference O10      --C54      .       0.18 Ang.

And 2 other PLAT234 Alerts

More ...

PLAT241_ALERT_2_C High   'MainMol' Ueq as Compared to Neighbors of        C40 Check

PLAT241_ALERT_2_C High   'MainMol' Ueq as Compared to Neighbors of        C41 Check

PLAT242_ALERT_2_C Low    'MainMol' Ueq as Compared to Neighbors of         O2 Check

And 2 other PLAT242 Alerts

More ...

PLAT244_ALERT_4_C Low    'Solvent' Ueq as Compared to Neighbors of        C55 Check

PLAT244_ALERT_4_C Low    'Solvent' Ueq as Compared to Neighbors of        C60 Check

PLAT250_ALERT_2_C Large U3/U1 Ratio for <U(i,j)> Tensor(Resd    2)        2.7 Note

PLAT260_ALERT_2_C Large Average Ueq of Residue Including        O1      0.158 Check

PLAT410_ALERT_2_C Short Intra H...H Contact  H42B     ..H44B     .       1.98 Ang.

x,y,z  =      1_555 Check

PLAT410_ALERT_2_C Short Intra H...H Contact  H43B     ..H45A     .       1.98 Ang.

x,y,z  =      1_555 Check

PLAT906_ALERT_3_C Large K Value in the Analysis of Variance ......     33.455 Check

And 2 other PLAT906 Alerts

More ...

PLAT911_ALERT_3_C Missing FCF Refl Between Thmin & STh/L=    0.595         41 Report

2  0  0,   4  5  0,  -3  2  3,  -2  2  3,  14  3  5, -14  3  6,

13  6  6,   1  4  7,  14  0  8,  14  2  8,  14  1  9, -14  2  9,

11  9  9,  14  0 10,  -2 14 13,  -1 14 14,  13  3 16,   9 10 17,

12  5 19,  11  7 19,  12  0 24,  11  5 24,  10  6 26,  11  1 28,

8  7 30, -10  3 31,   9  4 32,   2 10 32,   9  3 33,  -8  5 34,

(   11 More Missing: see the .ckf listing file)

PLAT918_ALERT_3_C Reflection(s) with I(obs) much Smaller I(calc) .          6 Check

2  1  0,   3  0  1,  -2  0  4,  -1  0  5,  -1  1  7,   1  1  7,

PLAT977_ALERT_2_C Check Negative Difference Density on H41B      .      -0.33 eA-3

Alert level G

PLAT002_ALERT_2_G Number of Distance or Angle Restraints on AtSite         19 Note

PLAT003_ALERT_2_G Number of Uiso or U(i,j)  Restrained non-H-Atoms         21 Report

PLAT083_ALERT_2_G SHELXL Second Parameter in WGHT  Unusually Large       5.35 Why ?

PLAT172_ALERT_4_G The CIF-Embedded .res File Contains DFIX Records          4 Report

PLAT173_ALERT_4_G The CIF-Embedded .res File Contains DANG Records          4 Report

PLAT177_ALERT_4_G The CIF-Embedded .res File Contains DELU Records          3 Report

PLAT178_ALERT_4_G The CIF-Embedded .res File Contains SIMU Records          3 Report

PLAT188_ALERT_3_G A Non-default SIMU Restraint Value has been used     0.0100 Report

And 2 other PLAT188 Alerts

More ...

PLAT199_ALERT_1_G Reported _cell_measurement_temperature ..... (K)        293 Check

PLAT200_ALERT_1_G Reported   _diffrn_ambient_temperature ..... (K)        293 Check

PLAT343_ALERT_2_G Unusual sp?      Angle Range in Main Residue for        C37 Check

PLAT344_ALERT_2_G Unusual sp?       Angle Range in Solvent/Ion for        C60 Check

PLAT367_ALERT_2_G Long?  C(sp?)-C(sp?) Bond  C59      - C60      .       1.55 Ang.

PLAT432_ALERT_2_G Short Inter X...Y Contact  N1       ..C38      .       2.94 Ang.

x,y,z  =      1_555 Check

PLAT860_ALERT_3_G Number of Least-Squares Restraints .............        166 Note

PLAT883_ALERT_1_G Absent Datum for _atom_sites_solution_primary ..     Please Do !

PLAT933_ALERT_2_G Number of HKL-OMIT Records in Embedded .res File          5 Note

2  0  0,   4  5  0,  -3  2  3,  -2  2  3,   1  4  7,

PLAT965_ALERT_2_G The SHELXL WEIGHT Optimisation has not Converged     Please Check

PLAT969_ALERT_5_G The 'Henn et al.' R-Factor-gap value ...........      6.910 Note

Predicted wR2: Based on SigI**2  4.95 or SHELX Weight 35.81

PLAT978_ALERT_2_G Number C-C Bonds with Positive Residual Density.          1 Info

0 ALERT level A = Most likely a serious problem - resolve or explain

3 ALERT level B = A potentially serious problem, consider carefully

27 ALERT level C = Check. Ensure it is not caused by an omission or oversight

22 ALERT level G = General information/check it is not something unexpected

3 ALERT type 1 CIF construction/syntax error, inconsistent or missing data

25 ALERT type 2 Indicator that the structure model may be wrong or deficient

14 ALERT type 3 Indicator that the structure quality may be low

9 ALERT type 4 Improvement, methodology, query or suggestion

1 ALERT type 5 Informative message, check

It is advisable to attempt to resolve as many as possible of the alerts in all categories. Often the minor alerts point to easily fixed oversights, errors and omissions in your CIF or refinement strategy, so attention to these fine details can be worthwhile. It is up to the individual to critically assess their own results and, if necessary, seek expert advice.

PLATON version of 26/09/2025; check.def file version of 20/09/2025

duplicate check

No duplication found

checkCIF_ P10.ADN checkCIF (basic structural check) running Checking for embedded fcf data in CIF ... Found embedded fcf data in CIF. Extracting fcf data from uploaded CIF, please wait . . . checkCIF/PLATON (basic structural check) Structure factors have been supplied for datablock(s) P10_ADN THIS REPORT IS FOR GUIDANCE ONLY. IF USED AS PART OF A REVIEW PROCEDURE FOR PUBLICATION, IT SHOULD NOT REPLACE THE EXPERTISE OF AN EXPERIENCED CRYSTALLOGRAPHIC REFEREE. No syntax errors found. CIF dictionary Please wait while processing .... Interpreting this report Structure factor report Datablock: P10_ADN Bond precision:; C-C = 0.0124 A; Wavelength=0.71075. Cell:; a=11.2701(12); b=12.0419(13); c=24.328(3). alpha=76.594(5); beta=89.067(6); gamma=63.961(5). Temperature:; 293 K. Calculated; Reported. Volume; 2871.8(6); 2871.8(6). Space group; P -1; P -1. Hall group; -P 1; -P 1. Moiety formula; C56 H68 O10, C6 H8 N2; ?. Sum formula; C62 H76 N2 O10; C62 H76 N2 O10. Mr; 1009.25; 1009.24. Dx,g cm-3; 1.167; 1.167. Z; 2; 2. Mu (mm-1); 0.078; 0.078. F000; 1084.0; 1084.0. F000'; 1084.51. h,k,lmax; 13,14,28; 13,14,28. Nref; 10143; 9772. Tmin,Tmax; 0.994,0.997; 0.149,0.997. Tmin'; 0.985. Correction method= # Reported T Limits: Tmin=0.149 Tmax=0.997 AbsCorr = MULTI-SCAN. Data completeness= 0.963; Theta(max)= 25.014. R(reflections)= 0.1073( 3255); wR2(reflections)= 0.3491( 9772). S = 1.040; Npar= 676.. The following ALERTS were generated. Each ALERT has the format test-name_ALERT_alert-type_alert-level. Click on the hyperlinks for more details of the test. Alert level B PLAT026_ALERT_3_B Ratio Observed / Unique Reflections (too) Low .. 33% Check Respnse: Due to bad crystal quality, the high resolution reflections were poor. We are confident that the structural characterization is valid. PLAT340_ALERT_3_B Low Bond Precision on C-C Bonds ............... 0.01239 Ang. Respnse: This is due to the bad crystal quality. PLAT910_ALERT_3_B Missing FCF Reflection(s) Below Theta(Min)[Deg]= 3.10 Note 1 0 0, 0 1 0, 1 1 0, -1 -1 1, 0 -1 1, -1 0 1, 0 0 1, 1 0 1, 0 1 1, 1 1 1, -1 -1 2, 0 -1 2, -1 0 2, 0 0 2, 1 0 2, 0 1 2, 1 1 2, 0 0 3, 0 1 3, Response: The unit cell is reasonable large and these low angle reflections are probably missing due to beamstop. This occurs rather frequently with Mo radiation and our gonoimeter geometry, especially for larger unit cells. Alert level C PLAT029_ALERT_3_C _diffrn_measured_fraction_theta_full value Low . 0.963 Why? PLAT082_ALERT_2_C High R1 Value .................................. 0.11 Report PLAT084_ALERT_3_C High wR2 Value (i.e. > 0.25) ................... 0.35 Report PLAT220_ALERT_2_C NonSolvent Resd 1 C Ueq(max)/Ueq(min) Range 5.7 Ratio PLAT222_ALERT_3_C NonSolvent Resd 1 H Uiso(max)/Uiso(min) Range 6.1 Ratio PLAT234_ALERT_4_C Large Hirshfeld Difference O6 --C52 . 0.21 Ang. And 4 other PLAT234 Alerts More ... PLAT241_ALERT_2_C High 'MainMol' Ueq as Compared to Neighbors of O1 Check And 3 other PLAT241 Alerts More ... PLAT242_ALERT_2_C Low 'MainMol' Ueq as Compared to Neighbors of O6 Check And 5 other PLAT242 Alerts More ... PLAT243_ALERT_4_C High 'Solvent' Ueq as Compared to Neighbors of C58 Check PLAT244_ALERT_4_C Low 'Solvent' Ueq as Compared to Neighbors of C57 Check PLAT250_ALERT_2_C Large U3/U1 Ratio for <U(i,j)> Tensor(Resd 2) 2.3 Note PLAT260_ALERT_2_C Large Average Ueq of Residue Including O1 0.121 Check PLAT260_ALERT_2_C Large Average Ueq of Residue Including N1 0.257 Check PLAT372_ALERT_2_C Short C(sp)-C(sp) Bond C37 - C38 . 1.13 Ang. PLAT410_ALERT_2_C Short Intra H...H Contact H45A ..H47B . 1.91 Ang. x,y,z = 1_555 Check PLAT906_ALERT_3_C Large K Value in the Analysis of Variance ...... 72.082 Check And 4 other PLAT906 Alerts More ... PLAT911_ALERT_3_C Missing FCF Refl Between Thmin & STh/L= 0.595 353 Report -11 1 0, -10 1 0, 12 1 0, -11 2 0, -7 4 0, -7 5 0, -8 6 0, -7 6 0, -7 7 0, -6 8 0, -5 9 0, 5 -9 1, 6 -8 1, 7 -7 1, -5 -5 1, -12 -1 1, 11 -1 1, -12 0 1, -11 1 1, -2 1 1, 12 1 1, -11 2 1, -6 3 1, -7 4 1, -6 4 1, -7 5 1, -6 5 1, -8 6 1, -7 6 1, -7 7 1, ( 323 More Missing: see the .ckf listing file) PLAT918_ALERT_3_C Reflection(s) with I(obs) much Smaller I(calc) . 1 Check -3 3 4, Alert level G PLAT002_ALERT_2_G Number of Distance or Angle Restraints on AtSite 13 Note PLAT003_ALERT_2_G Number of Uiso or U(i,j) Restrained non-H-Atoms 18 Report PLAT172_ALERT_4_G The CIF-Embedded .res File Contains DFIX Records 2 Report PLAT173_ALERT_4_G The CIF-Embedded .res File Contains DANG Records 2 Report PLAT177_ALERT_4_G The CIF-Embedded .res File Contains DELU Records 2 Report PLAT178_ALERT_4_G The CIF-Embedded .res File Contains SIMU Records 2 Report PLAT188_ALERT_3_G A Non-default SIMU Restraint Value has been used 0.0200 Report PLAT188_ALERT_3_G A Non-default SIMU Restraint Value has been used 0.0200 Report PLAT199_ALERT_1_G Reported _cell_measurement_temperature ..... (K) 293 Check PLAT200_ALERT_1_G Reported _diffrn_ambient_temperature ..... (K) 293 Check PLAT344_ALERT_2_G Unusual sp? Angle Range in Solvent/Ion for C57 Check PLAT344_ALERT_2_G Unusual sp? Angle Range in Solvent/Ion for C62 Check PLAT367_ALERT_2_G Long? C(sp?)-C(sp?) Bond C57 - C58 . 1.52 Ang. PLAT367_ALERT_2_G Long? C(sp?)-C(sp?) Bond C61 - C62 . 1.52 Ang. PLAT860_ALERT_3_G Number of Least-Squares Restraints ............. 146 Note PLAT883_ALERT_1_G Absent Datum for _atom_sites_solution_primary .. Please Do ! PLAT941_ALERT_3_G Average HKL Measurement Multiplicity ........... 2.3 Low PLAT965_ALERT_2_G The SHELXL WEIGHT Optimisation has not Converged Please Check PLAT969_ALERT_5_G The 'Henn et al.' R-Factor-gap value ........... 5.606 Note Predicted wR2: Based on SigI**2 6.23 or SHELX Weight 33.55 PLAT978_ALERT_2_G Number C-C Bonds with Positive Residual Density. 1 Info 0 ALERT level A = Most likely a serious problem - resolve or explain 3 ALERT level B = A potentially serious problem, consider carefully 34 ALERT level C = Check. Ensure it is not caused by an omission or oversight 20 ALERT level G = General information/check it is not something unexpected 3 ALERT type 1 CIF construction/syntax error, inconsistent or missing data 25 ALERT type 2 Indicator that the structure model may be wrong or deficient 17 ALERT type 3 Indicator that the structure quality may be low 11 ALERT type 4 Improvement, methodology, query or suggestion 1 ALERT type 5 Informative message, check It is advisable to attempt to resolve as many as possible of the alerts in all categories. Often the minor alerts point to easily fixed oversights, errors and omissions in your CIF or refinement strategy, so attention to these fine details can be worthwhile. It is up to the individual to critically assess their own results and, if necessary, seek expert advice.. PLATON version of 26/09/2025; check.def file version of 20/09/2025 duplicate check No duplication found Datablock P10_ADN - ellipsoid plot.