Supporting Information

Facile preparation of hierarchically porous aromatic-cyclodextrin polymers and their application for the selective adsorption of cationic dyes

Hui-Ling Duan 1*, Yu Wang 1,Kai-Qi Cheng 1, Li-Juan Zhang 1, Ji-Chao Qi 1 and Xiang-Ai Ma 2,*

1	College of Food Science and Engineering, Shanxi Agricultural University, Taigu 030801, China;

2	College of Resources and Environment, Shanxi Agricultural University, Taigu 030801, China

*	Correspondence: duanhl@sxau.edu.cn (H.D.), Tel.: +13509734898; sxaumxa@163.com (X.M), Tel: +13835473916.

.

Contents

Characterization information

Simulated equations for kinetic sorption process

Adsorption isotherm models

Thermodynamic parameter equations

Table S1 The chemical structure and some properties of investigated dyes

Table S2 Elemental analysis results of P-aro-CDPs

Table S3 Adsorption kinetic parameters of MB on P-aro-CDPs

Table S4 Adsorption isotherm parameters of MB on P-aro-CDPs

Figure S1 Solid-state 13C-NMR spectrum of P-aro-CDPs

Figure S2 The XPS spectrum of N1s from P-aro-CDPs

Figure S3 Pseudo-first-order adsorption plots of MB on P-aro-CDPs

Figure S4 Elovich adsorption kinetic plots of MB on P-aro-CDPs

Figure S5 Weber-Morris adsorption plots of MB on P-aro-CDPs

Figure S6 Boyd adsorption plots of MB on P-aro-CDPs

Figure S7 Freundlich adsorption isotherm of MB on P-aro-CDPs

Figure S8 Temkin adsorption isotherm of MB on P-aro-CDPs

### Characterization information

Fourier transform infrared (FTIR) spectra were obtained using an Equinox 55 FTIR spectrometer (Bruker, Germany) using the KBr pellet method in the range of 400–4000 cm-1. Solid-state 13C-NMR spectra were acquired using a JNM-ECZ400R/S1 NMR spectrometer (JEOL, Japan). The presence of different functional groups was investigated using an Axis Ultra X-ray photoelectron spectrometer (XPS; Kratos Analytical Ltd.). Binding energies were calibrated using the contained carbon (C1s = 284.6 eV). Elemental analysis was performed using a Vario EL III elemental analyzer (Elementar, Germany) and energy-dispersive X-ray spectroscopy (EDS) analysis using an SU8220 field-emission scanning electron microscope (Hitachi, Japan), and the structure of P-aro-CDPs was determined by powder X-ray diffractometry (XRD) using a D8 Advance X-ray diffractometer (Bruker, Germany). Nitrogen (N2) adsorption–desorption isotherms were obtained at 77 K using an ASAP 2020M system (Micromeritics, Norcross, GA, USA). Approximately 0.1 g of the tested sample was outgassed at 120 °C for 12 h prior to testing in the analytical system. The specific surface area and pore size distribution data were calculated using the Brunauer–Emmett–Teller (BET) and density functional theory (DFT) methods, respectively. The surface charge of P-aro-CDPs was measured using a DelsaNano C particle size and a zeta potential analyzer (Beckman Coulter, USA). Thermogravimetric analysis (TGA) was performed using an SDT-Q600 thermogravimetric analyzer (TA Instruments, USA) between 273 and 1273 K at a heating rate of 10 K min−1 in a nitrogen-rich atmosphere. The microscopic structure of P-aro-CDPs was observed by scanning electron microscopy (SEM) using an SU8220 field-emission scanning electron microscope (Hitachi, Japan) and transmission electron microscopy (TEM) using a Tecnai G2 F20 field-emission transmission electron microscope (FEI, USA).

### Simulated equations for kinetic sorption process

The kinetic sorption process of MB on P-aro-CDPs was simulated by pseudo-first-order rate equation (1), pseudo-second-order rate equation (2), and Elovich kinetic equation (3) as follow:

(1)

(2)

(3)

where t is adsorption time; qt and qe is the adsorbed amount of MB per unit mass of adsorbent at t moment and equilibrium (mg g-1) respectively; k1 (min-1) and k2 (g mg-1 min-1) are the adsorption rate constants of pseudo-first-order equation and pseudo-second-order equation, respectively; A (mg g-1 min-1) is the initial adsorption rate and B (g mg-1) is related to the extent of surface coverage and activation energy for chemisorption; The value of (1/B) is indicative of the available number of sites for adsorption while (1/B)ln(AB) is the adsorption quantity when ln t =0.

In addition, the intraparticle diffusion kinetic model based on the theory proposed by Weber and Morris was tested by using the following equation (4):

(4)

where kp (mg g-1 min0.5) and C are the diffusion rate constant and the thickness of the boundary layer, respectively.

To distinguish between the pore and film diffusion step involved in the adsorption process, the kinetic data were further analyzed using the Boyd model (5):

(5)

### Adsorption isotherm models

Langmuir model equation

(6)

where Ce is the concentration of MB at equilibrium (mg L-1), qe is the adsorbed amount of MB per unit mass of adsorbent at equilibrium (mg g-1), KL represents the Langmuir equilibrium constant (L g-1), and qm is the saturated adsorption capacity (mg g-1).

Freundlich model equation

(7)

where qe is the adsorbed amount of MB per unit mass of adsorbent at equilibrium (mg g-1), KF represents the Freundlich equilibrium constant [(mg g-1) (L mg-1)1/n], 1/n is the adsorption intensity (mg g-1), and Ce is the concentration of MB at equilibrium (mg L-1).

Temkin model equation

(8)

where qe is the adsorbed amount of MB per unit mass of adsorbent at equilibrium (mg g-1), B is Temkin constant, A is the Temkin adsorption equilibrium constant (L g-1), and Ce is the concentration of MB at equilibrium (mg L-1).

### Thermodynamic parameter equations

The thermodynamic parameters of enthalpy change (ΔH), Gibbs free energy change (ΔG), and entropy change (ΔS) were computed following the equations:

(9)

(10)

(11)

where R (8.314 J mol-1 K-1) is the universal gas constant, T (K) is the absolute solution temperature, KL (L mg-1) is the Langmuir isotherm constant at various temperatures and A is the Arrhenius constant.

### Table S1 The chemical structure and some properties of investigated dyes

| Compound name | Chemical structure | Molar mass (g mol-1) | CAS# | λ max (nm) | Charge |
| --- | --- | --- | --- | --- | --- |
| Methylene blue (MB) |  | 373.9 | 7220-79-3 | 664 | Cationic |
| Rhodamine B (RB) |  | 479.01 | 81-88-9 | 526 | Cationic |
| Brilliant cresyl blue (BCB) |  | 801.95 | 81029-05-2 | 637 | Cationic |
| Astrazon orange R (AOR) |  | 426.98 | 4657-00-5 | 485 | Cationic |
| Basic red 9 (BR9) |  | 323.82 | 569-61-9 | 538 | Cationic |
| Auramine O (AO) |  | 303.84 | 2465-27-2 | 431 | Cationic |
| Basic orange 21 (BO22) |  | 350.88 | 3056-93-7 | 485 | Cationic |
| Tartrazine (T23) |  | 534.36 | 1934-21-0 | 428 | Anionic |
| Acid red 73 (AR73) |  | 556.48 | 5413-75-2 | 509 | Anionic |
| Eosin (ES) |  | 691.86 | 17372-87-1 | 515 | Anionic |
| Alizarin red S(ARS) |  | 342.26 | 130-22-3 | 422 | Anionic |
| Alizarin green (AG) |  | 725.25 | 4857-81-2 | 642 | Anionic |
| Methyl orange (MO) |  | 327.33 | 547-58-0 | 464 | Anionic |
| Congo red (CR) |  | 696.66 | 573-58-0 | 501 | Anionic |
| Sunset yellow FCF (SY) |  | 452.37 | 2783-94-0 | 481 | Anionic |

### Table S2 Elemental analysis results of P-aro-CDPs

| Material | Results of combustion method (%) |  |  | Results of EDX method (%) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | C | H | N | C | N | O |
| P-aro-CDPs | 68.8 | 4.988 | 6.4 | 78.38 | 5.52 | 16.11 |

### Table S3 Adsorption kinetic parameters of MB on P-aro-CDPs

| Kinetics models | Parameters | C0 (mg/L) |  |  |
| --- | --- | --- | --- | --- |
|  |  | 100 | 200 | 300 |
| Pseudo-first-order | k1 (min-1) | 0.0251 | 0.0094 | 0.0103 |
|  | q1,cal(mg/g) | 15.17 | 59.35 | 112.01 |
|  | R2 | 0.8708 | 0.8981 | 0.8105 |
| Pseudo-second-order | K2(g mg-1 min-1) | 0.0045 | 0.0008 | 0.0004 |
|  | q2,cal(mg/g) | 95.33 | 143.68 | 229.89 |
|  | R2 | 0.9999 | 0.9966 | 0.9975 |
| Elovich kinetic | A | 1348873.13 | 11181.7 | 744.23 |
|  | B | 0.1877 | 0.0936 | 0.0412 |
|  | R2 | 0.9539 | 0.9589 | 0.9919 |

### Table S4 Adsorption isotherm parameters of MB on P-aro-CDPs

| Langmuir |  |  | Freundlich |  |  | Temkin |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| qm (mg g-1) | KL (L mg-1) | R2 | KF (mg g-1)(L mg-1)1/n | 1/n | R2 | A(L/g) | B | R2 |
| 194.17 | 0.10 | 0.9994 | 71.19 | 0.19 | 0.8101 | 7.09 | 95.93 | 0.8837 |

Figure S1 Solid-state 13C-NMR spectrum of P-aro-CDPs

Figure S2 The XPS spectrum of N1s from P-aro-CDPs

### Figure S3 Pseudo-first-order adsorption plots of MB on P-aro-CDPs

### Figure S4 Elovich adsorption kinetic plots of MB on P-aro-CDPs

### Figure S5 Weber-Morris adsorption plots of MB on P-aro-CDPs

### Figure S6 Boyd adsorption plots of MB on P-aro-CDPs

### Figure S7 Freundlich adsorption isotherm of MB on P-aro-CDPs

### Figure S8 Temkin adsorption isotherm of MB on P-aro-CDPs