Support information for:

Optimising Viscoelastic Window in Reversible Liquid Crystal Elastomer-Based Pressure Sensitive Adhesives via Chain-Transfer

Lichang Lu a, Kailing Lin a, Mohand O Saed a*

a Cavendish Laboratory, University of Cambridge, J.J. Thomson Avenue, Cambridge CB3 0HE, U.K.

Table S1 Detailed rubbery modulus and crosslink density for various formulations

| Formulation | E’ at 100 °C (MPa) | d (mol cm−3) |
| --- | --- | --- |
| 1:1 | 1.69 | 1.81×10−4 |
| 1:1.5 | 0.95 | 1.02×10−4 |
| 1:2 | 0.023 | 2.47×10−6 |

Table S2 Characteristic temperatures of LCE adhesives with various formulations

| Formulation | Tg (measured by DSC) | Tg (measured by DMA) | Tni (°C) |
| --- | --- | --- | --- |
| 1:1 | 0.59 | 3.97 | 51.67 |
| 1:1.5 | -11.57 | -3.10 | 34.80 |
| 1:2 | -19.80 | -10.95 | 23.49 |

Figure S1 The working principle of the chain transfer reaction

Figure S2 Gel fraction of each LCE formulation

Figure S3 Comparison of the peel force – displacement curves of the LCE adhesive at slow (100 mm min-1) and fast (300 mm min-1) peeling rate

Figure S4 Representative failure modes of the LCE adhesives: (a) adhesive failure at room temperature, (b) adhesive failure at elevated temperature, and (c) cohesive failure.