Supplementary File

Facile synthesis of metal doped graphite carbon nitride for photocatalytic degradation of tetracycline under visible light irradiation

1. Results and discussion

Figure S1. Zeiss SmartEDX of 10 Cd/g-C3N4.

Table S1. The proportion of each element in the 10 Cd/g-C3N4 material.

| elements | Weight ratio% | Atomic percentage | Error% | intensity | K ratio |
| --- | --- | --- | --- | --- | --- |
| C K | 25.73 | 32.09 | 3.62 | 2391.51 | 0.2314 |
| N K | 61.98 | 66.28 | 7.98 | 2651.52 | 0.2666 |
| Cd L | 12.28 | 1.64 | 6.51 | 202.16 | 0.0802 |

Table S1. The analysis of energy-dispersive X-ray spectra (EDS) directly shows the atomic concentrations of Cd in the samples of Cd/g-C3N4 sample are 1.64%. Elemental mapping confirmed the uniform dispersion of Cd in the g-C3N4 layer structure, which illustrated that the cadmium was well doped in the g-C3N4 with a slight atomic ratio.

Figure S2. N2 adsorption−desorption isotherms of pure g-C3N4 and 10 Cd/g-C3N4 composite. The inset image is the pore size distributions of pure g-C3N4 and 10 Cd/g-C3N4 composite.

Table S2 Surface area, pore volume and pore size parameters for pure g-C3N4 and 10 Cd/g-C3N4.

| Samples | Surface area1 (m2 /g) | Pore volume2 (cm3 /g) | Pore size3 (nm) |
| --- | --- | --- | --- |
| g-C3N4 | 13.467 | 0.077 | 22.131 |
| Cd/g-C3N4 | 16.460 | 0.123 | 25.917 |

Figure S3. Band structure diagram of pristine g-C3N4 and 10 Cd/g-C3N4.

Figure S4. First-order plots of photocatalytic degradation with different amounts cadmium catalysts.

Figure S5. TOC removal curves of TC on 10 Cd/g-C3N4.

Scheme 1. The brief diagram of Cd/g-C3N4 prepared process.

Scheme 2. The transfer and separation of charges and degradation mechanisms in the 10 Cd/g-C3N4 composite under visible-light irradiation.