| Citation | Year | Material Composition | Morphology nanostructure | Synthesis method | Electrode configuration | Electrochemical techniques | Cycles | Efficiency |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| https://doi.org/10.1016/S0013-4686(01)00496-0 | 2001 | PEO–KOH–H2O | _ | casting technique | polymer electrolyte and activated carbon Powder | CV & GCD | _ | 93 F g−1 90 F g−1 |
| https://doi.org/10.1016/S0013-4686(02)00031-2 | 2002 | Mn3O4 | _ | electrochemically | PT foil and with an Ag/ AgNO3/ TBAClO4/ | CV & GCD | _ | 50 to 144 F g1 a |
| https://doi.org/10.1016/S0378-7753(02)00647-X | 2003 | MnOxnH2O | _ |  | Ag/AgCl , SHE, platinum gauze | CV & GCD | _ | 220 F g1 |
| 10.1016/j.elecom .2004.03.011 | 2004 | MnO2 _ nH2O | cross-linked and needle- | sol–gel | graphite electrode | CV & GCD | 1000 | 45 mF/cm2 |
| 10.1149/1. 2041147 | 2005 | ruthenium oxide , Pt plate and carbon paper substrate. | threedimensional nanoporous structure. | potential cycling method | ruthenium oxide, counter, reference, electrode | CV & GCD |  | 1170 F/g |
| https://doi.org/10.1016/j.jpowsour.2005.05.051 | 2006 | Polyaniline&Nickel | spongy and highly porous | deposited potentiodynamically | - Ag/AgCl - Nickel - platinum foil | CV,GCD,EIS | 50 | ∼4.05 × 102 F g− |
| https://doi.org/10.1016/j.jpowsour.2006.09.060 | 2007 | RuO2·xH2O/Ti substrate/RuCl3·xH2O | “mud-cracked” | anodic deposition of RuO2·xH2O onto Ti |  | EIS&CV&LSV |  | 460 - 552 F g− |
| https://doi.org/10.1016/j.electacta.2008.04.028 | 2008 | MnO2/PPy& graphite | highly porous | electrochemical co-deposition | s MnO2 and MnO2/PPy nanocomposite | CV & | 5000 1000 | 120 F g−1 180 F g−1 |
| https://doi.org/10.1016/j.jpowsour.2008.10.080 | 2009 | manganese oxide potassium & permanganate(VII) & manganese(II) sal | spherical grains | precipitation method | manganese oxide & carbon black/graphite fibres | CV and galvanostatic CD |  | 267 F g−1 |
| https://doi.org/10.1021/nn90131t | 2010 | (GOMnO2 | needle-like | a simple soft chemical route in a waterisopropyl alcohol system. | Platinum foil & (SCE) & Hg/HgO | CV & galvanostatic CD |  |  |
| 10.1149/1.3574021 | 2011 | (Ni-Co) | porous | sol-gel | - platinum plate - SCE | CV GCD | 2000 | 1539, 1447 and 1136 F g1 |
| https://doi.org/10.1039/C2JM30927K | 2012 | Co(NO3)2 + Ni(NO3)2+ NH4NO3 | Flower like | simple electrochemical method | F-doped SnO graphite rod SCE | CV GCD |  | f 89.2 F g1 |
| https://doi.org/10.1039/C3EE41143E | 2013 | 8 Ni(NO3)2·6H2O and Co(NO3)2·6H2O | nanodiscs | a co-precipitation | saturated calomel & platinum | CV GCD EIS | 5000 | 2360 F/g |
| https://doi.org/10.1016/j.jpowsour.2014.07.164 | 2014 | Ni–Co–Sn | revealed cracks | Pechini | ECs electrodes | cyclic voltammetry CV | 600 | 328 F g−1. |
| https://doi.org/10.1016/j.electacta.2015.02.095 | 2015 | NixCo(1−x)(OH)2 | flower-like | template-free | Pt foil and Hg/HgO | Cv gs | 4000 |  |
| https://pubs.acs.org/doi/abs/10.1021/acsami.6b05933 | 2016 | Co3O4–MnO2–NiO | nanostructure | facile | Ag/AgCl, and Pt electrodes | Cyclic voltammetry, Galvanostatic | 5700 | 2525 F/g |
| https://pubs.acs.org/doi/abs/10.1021/acssuschemeng.7b01860 | 2017 | ASCs (NCO-NS and NCO-NW | nanosheets ,nanowires |  | Ag/AgCl, and Pt electrodes | 3-electrode cell | 2000 | 91.12% |
| https://doi.org/10.1016/j.ceramint.2018.08.292 | 2018 | 3DG/NixCo1-xO |  | one-step | Pt foil as the counter electrode and Hg/HgO as the reference electrode. | CV),& galvanostatic discharge-charge (GCD) | 10,000 | 697.8 F g−1 |
| https://doi.org/10 1039/C8NR08077A | 2019 | Nickel Cobalt oxide | 3D flower-like | facile hydrothermal method | Ag/AgCl &pt | CV & GSD | 5000 | (~203.81 F.g-1 |
| https://doi.org/10.1016/j.cej.2019.123357 | 2020 | Zn-Ni-Co oxide | transparent foldable silk-like | hydrothermal process combined with post-annealing methods | Ag/AgCl and Pt foil | EIS, Cv& GCD | 10,000 |  |
| https://doi.org/10.1016/j.surfcoat.2021.126933 | 2021 | ## NiCo2O4 and NiCo2S4 | dandelion shape | facile hydrothermal method. |  | Cv& GCD | , 5000 | 3.65 F/cm2 |
| https://doi.org/10.1080/21 663831.2022.2077149 | 2022 | NiCo LDH, mesoporous and macroporous | sheet-like | Hydrothermal, low-temperature phosphating treatment | phosphorus and selenium facilitate | CV & GCD |  |  |
| https://doi.org/10.1007/s42452-023-05341-8 | 2023 | NiCo2O4 | 2D nanosheet structure | hydrothermal | (Pt) wire and Ag/AgCl | CV & GCD, EIS |  |  |
| https://doi.org/10.1007/s10854-024-13223-x | 2024 | NCP | microplatelike and nanoflakes | polyol-based reflux | Platinum wire (Pt) and Ag/AgCl | CV & GCD, EIS | 10,000 | 144.66 Fg− 1 |