Extended Data Tables

Waste Polystyrene Degradation in the World Oceans:

Newly identified sources of Contamination

Katsuhiko Saido,1a-3b*† Yoichi Kodera,2 Hideki Kimukai, 1b Hideto Sato,3a

Akifumi Okabe,3b Koshiro Koizumi,3b Kohei Takatama,4 Bum Gun Kwon,5

Seon Yong Chung,6 Masahiko Nishimura,7 Sibel Mentese8

Correspondence to: katsu.saido@gmail.com or

saido.katsuhiko@nihon-u.ac.jp

Extended Data sTable 1 Levels SOs remaining (mg kg–1) in commercial PS products sampled in some countries.

| Country | Number of samples | SM |  | SD |  | ST |  | SOs, |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | All | Av. | All | Av. | All | Av. | Av. |
| Japan | 30 | 77.1 | 2.57 | 44.1 | 1.47 | 651 | 21.7 | 25.7 |
| Korea | 20 | 23 | 1.15 | 45.8 | 2.29 | 738.4 | 36.9 | 40.3 |
| China | 20 | 20 | 1 | 21 | 1.05 | 360 | 18 | 20 |
| Italy | 10 | 11.2 | 1.12 | 8.2 | 0.82 | 1.7 | 0.17 | 2.1 |
| Spain | 5 | 6.75 | 1.35 | 4.35 | 0.87 | 7.35 | 1.47 | 3.7 |
| Greece | 5 | 3.7 | 0.74 | 6.6 | 1.32 | 0.8 | 0.16 | 2.2 |
| USA | 10 | 15.4 | 1.54 | 42 | 4.2 | 35 | 3.5 | 9.2 |
| Total | 100 |  |  |  |  |  |  |  |
| SO total |  | 157.2 |  | 172.1 |  | 1794.3 |  |  |
| Ratio of SM: SD: ST |  | 1 |  | 1.1 |  | 11.4 |  |  |

Av: average

Extended Data sTable 2 Mean SO values in sand (µg kg-1) and water (µg L-1) sampled in various countries 1 to 26

| Sites Number | Sampling Site and Survey Period, Day/Month (Year) | Number of Samples |  | Average level of Styrene Oligomer |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Sand (a) | Water (b) | Sand (c) | Water (d) |
| 1 | United Kingdom 28/9-5/10(2003), 4-8/12(2003), 1-7/12(2007) | 40 | 11 | 390 | 4 |
| 2 | France 27/8-5/9(2004) | 4 | 1 | 450 | 1.2 |
| 3 | Portugal 23-27/3(2009), São Miguel Is. 6-14/10(2012) | 60 | 15 | 270 | 1.3 |
| 4 | Spain 23-31/3(2009), 24-27/5(2010), Tenerife Is. 25-28/8(2015) | 60 | 15 | 1,140 | 1.2 |
| 5 | Italy 30/8-5/9(2005), 15-18/12(2005), Sardinia Is. 14-17/12(2010), 20-23/3(2013) | 68 | 17 | 380 | 0.5 |
| 6 | Tunisia 25-28/8(2010) | 32 | 8 | 92 | 3.3 |
| 7 | Croatia 28/3(2013) | 8 | 2 | 15 | 1.7 |
| 8 | Slovenia 8-10/12(2010) | 12 | 3 | 31 | 0.2 |
| 9 | Greece, Salamis, Aigina, Crete Is. 29/8-2/9(2010) | 40 | 10 | 31,400 | 1.4 |
| 10 | Turkey 6-9/9(2005), 26-27/3(2013), 25-30/6(2015) | 44 | 15 | 2,400 | 2.8 |
| 11 | Egypt 3-5/9(2010) | 8 | 2 | 320 | 1.4 |
| 12 | India 12-19/9(2005), 4-10/2(2014), Elephanta, Kanniyakumari 27/2-8/3(2015) | 60 | 25 | 940 | 4 |
| 13 | Sri Lanka 20-25/8(2005), 21/2-2/3(2009), 9-12/7(2014) | 40 | 15 | 238 | 11.5 |
| 14 | Malaysia, Penang Is. 15-23/12(2008) | 60 | 15 | 18,900 | 4 |
| 15 | Vietnam 10-2/15/2(2011), 10-16/2(2012), 10-14/2(2015) | 40 | 10 | 440 | 3.4 |
| 16 | Philippines, Luzon, 5-10/3(2006), Mindanao 16-21/3(2007) | 40 | 10 | 150 | 2 |
| 17 | Taiwan 4-7/10(2006), 17-22/10(2009) | 40 | 10 | 150 | 13 |
| 18 | China 7-15/8(2000), 17-22/10(2010), Hong Kong Is. 18-22/3(2007) | 32 | 10 | 1,410 | 10 |
| 19 | Korea 5-9/11(2003), 8-11/7(2006), 7-11/12(2006) | 120 | 40 | 580 | 6 |
| 20 | Japan every year in 2000 to 2015 |  |  |  |  |
| 20-01 | Honshu, Isolated island | 1601 | 307 | 700 | 2.4 |
| 20-02 | Openocean 18/5-4/6(2010), 31/10-7/11(2012), 6/7-19/8(2012) |  | 300 |  | 0.2 |
| 21 | United States of America |  |  |  |  |
| 21-01 | Alaska, Aleutian Is. 30/8-4/9(2011) | 41 | 12 | 20 | 0.1 |
| 21-02 | Washington 22/2-1/3(2010) | 40 | 10 | 510 | 30.4 |
| 21-03 | Oregon 22/2-1/3(2010) | 40 | 10 | 820 | 22 |
| 21-04 | California, Catarina Is. 29/3-4/4(2000), 2-6/4(2003), 21-30/3(2010), 25-29/3(2015) | 60 | 15 | 2,910 | 1.3 |
| 21-05 | Massachusetts 19-23/6(2005), 24-27/8(2008) | 40 | 10 | 7,370 | 6.9 |
| 21-06 | NewJersey 20-24/8(2000) | 40 | 10 | 159 | 3.5 |
| 21-07 | Virginia 7-17/9(2003) | 8 | 2 | 450 | 4.5 |
| 21-08 | Florida, Key-Lago, -west, ConchKey | 60 | 15 | 23,500 | 8.8 |
| 21-09 | Texas 25/6-1/7(2012), 9-14/6(2014) | 60 | 15 | 500 | 5.7 |
| 21-10 | Puerto Rico 20-26/8(2009), 31/7-6/8(2011) | 60 | 15 | 350 | 0.8 |
| 21-11 | Oahu, Kauai-, Maui-, Hawai’i-Is. 20-30/3(2011), 10-15/12(2012), 5-15/12(2013), 15-20/12(2015) and more | 120 | 60 | 16 | 0.02 |
| 22 | Guam 5-9/8(2009) | 32 | 8 | 1,499 | 4.3 |
| 23 | Micronesia, Pohnpei 3-5/8(2012) | 20 | 7 | 390 | 0.9 |
| 24 | Costa Rica 3-10/6(2009) | 28 | 7 | 2,630 | 8.4 |
| 25 | Bermuda 24-27/8(2010), 17-21/3(2014) | 32 | 8 | 1,200 | 3.7 |
| 26 | Mexico 21-27/8(2007), 17-20/4(2015) | 48 | 10 | 1,600 | 5.7 |
| subtotal |  | 3,138 | 1,055 |  |  |
| Total (sand: Σa × c, water: Σb × d ) |  | 3,143 | 1,055 | 5,070,844 | 2,837.1 |
| Average SO (all) values: Total sand/a or Total water/c |  |  |  | 1613.4 | 2.7 |
| Composition Ratio SM:SD:ST |  |  |  | 1:1:8 | 1:1:8 |

Extended Data sTable 3 SO contamination (ng L-1) on cruising HK12-3 from surface water during 6th July to 14th August 2012.

| Sampling station | Date | Latitude, N | Longitude, E | SO total | SM | SD | ST | Surface temp. °C | Water temp. °C | pH | Salinity permil | Flow knot |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | ng L–1 |  |  |  |  |  |  |  |  |
| Stn-1 | July 10 | 46°555.100´ | 159°59.8176´ | 157 | 5 | 25.6 | 131 | 8.1 | 8.9 | 8.04 | 32.8 | 0.4 |
| 2 | 12 | 43°30.169´ | 160°00.139´ | 15 | 0.6 | 14.1 | 132 | 14 | 13.3 | 7.96 | 32.9 | 0.5 |
| 3 | 13 | 39°59.995´ | 159°59.7917´ | 154 | 0.7 | 19.8 | 133.3 | 19.1 | 16.9 | 8.2 | 33.4 | 0.9 |
| 4 | 14 | 37°30.0835´ | 160°00.1599´ | 22 | 0.3 | 21.4 | 139 | 22.4 | 21.3 | 8.03 | 34.1 | 0.6 |
| 5 | 14 | 34°59.9444´ | 100°00.3908´ | 199 | 0.7 | 69.1 | 129 | 25.2 | 24.3 | 8.05 | 34.5 | 1.6 |
| 6 | 16 | 33°00.0618´ | 159°59.8779´ | 162 | 0.5 | 21.3 | 140.4 | 26 | 24.3 | 8.02 | 34.7 | 0.3 |
| 7 | 17 | 30°01.1139´ | 159°58.4579´ | 174 | 0.04 | 25.3 | 148.4 | 27.6 | 26.8 | 8.03 | 34.8 | 1.1 |
| 8 | 18 | 24°59.0949´ | 159°59.9460´ | 942 | 0.7 | 53.6 | 887.3 | 28.7 | 28.1 | 8.08 | 35 | 0.3 |
| 9 | 19 | 20°00.9884´ | 159°59.4324´ | 181 | 4 | 12.9 | 163.6 | 28.6 | 28.5 | 8.09 | 35 | 0.5 |
| 10 | 22 | 14°58.9970´ | 159°59.0250´ | 124 | 0.3 | 23.9 | 99.8 | 28.2 | 28.5 | 8.06 | 35.4 | 0.3 |
| 11 | 24 | 10°00.2840´ | 159°59.7093´ | 123 | 0.3 | 4.4 | 118 | 28.5 | 28.3 | 8.08 | 35.8 | 0.7 |
| 12 | Aug. 1 | 20°00.7549´ | 148°00.7702´ | 131 | 0.3 | 3 | 127.6 | 25.9 | 28.4 | 8.13 | 35.6 | 0.5 |
| 13 | 5 | 24°00.4415´ | 143°12.8222´ | 133 | 0.3 | 8.5 | 124.2 | 28.2 | 28.6 | 8.18 | 34.7 | 0.2 |
| 14 | 6 | 29°59.0387´ | 144°50.4752´ | 230 | 0.2 | 4.9 | 224.6 | 27.2 | 26.8 | 8.06 | 34.5 | 0.6 |
| 15 | 8 | 27°59.3591´ | 138°00.1555´ | 126 | 0.3 | 5.9 | 119.6 | 27.9 | 27.1 | 8.1 | 34.3 | 0.6 |
| 16 | 9 | 31°00.0244´ | 134°04.2201´ | 45 | 0.3 | 43.4 | 1.3 | 28 | 27 | 8.07 | 34.3 | 1 |
| 17 | 10 | 32°15.2999´ | 133°23.8904´ | 139 | 0.5 | 6.1 | 132.6 | 28.5 | 27.4 | 8.16 | 34.2 | 1.6 |
| 18 | 11 | 33°48.8382´ | 133°39.9826´ | 133 | 0.3 | 11.9 | 121.2 | 27.6 | 25.9 | 8.18 | 33.5 | 0.7 |
| Total |  |  |  | 3190 | 112 | 375.1 | 3,073 | 449.7 | 440.4 | 145.52 | 619.5 | 12.4 |
| Average |  |  |  | 177 | 6.2 | 21 | 171 | 24.5 | 8.08 | 34.4 | 0.7 |  |
| Ratio of SM : SD : ST |  |  |  | 1 : 3.4 : 25.7 |  |  |  |  |  |  |  |  |

Extended Data sTable 4   Low temperature decomposition of thermoplastics

| Application Plastic | Material | Range ºC | Product | Energy kJ mol-1 | Toxicity |
| --- | --- | --- | --- | --- | --- |
| Polystyrene (PS) | Styrene | 30 - 280 | Styrene | 42 | Carcinogenicity25 |
|  |  |  | 2,4-Diphenyl-1-butene |  |  |
|  |  |  | 2,4,6-Triphenyl-1hexene |  |  |
| Polycarbonate (PC) | 2,2-Bis(4-hydroxyphenyl) propane | 50 - 250 | Bisphenol-A | 57.2 | Endocrine disruptor23 reproductive |
|  | CO2, Ethylene oxide |  |  |  |  |
| Epoxy resin (EPX) | 2,2-Bis(4-hydroxyphenyl) propane | 50 - 250 | Bisphenol-A | 40.8 | Endocrine disruptor23 reproductive |
|  | 1-Chlor 2,3-epoxypropane |  |  |  |  |
| Polyethylene terephthalate (PET) | Terephthalic acid Ethylene glycol | 50 - 250 | Phthalic acid ester | 41.1 | Mutagen, reproductive / Teratogenicity24,25 |
| Poly urethane (PU) | Diisocyanate | 50 - 250 | Diisocyanate | 40.5 | Skin ailment26 |
|  | Polyol |  |  |  |  |

(  ) is an abbreviation

Supplementary Information

Waste Polystyrene Degradation in the World Oceans:

Newly identified sources of Contamination

Katsuhiko Saido,1a-3b*† Yoichi Kodera,2 Hideki Kimukai,1b Hideto Sato,3a

Akifumi Okabe,3b Koshiro Koizumi,3b Kohei Takatama,4 Bum Gun Kwon,5

Seon Yong Chung,6Masahiko Nishimura,7 Sibel Mentese8

Correspondence to: katsu.saido@gmail.com or

saido.katsuhiko@nihon-u.ac.jp

Section I. Characteristics of PS and PC, EPX

Artificial synthetic polymers such as PC and EPX [average molecular weight (Mn) = 10,000 or more] are formed by reaction of a monomer (BPA, Fw:228, dissoluble in water 120 mg L-1 at 25°C) as the polymerization initiator or in the presence of a catalyst.32 PS (Mn= 500,000) was used in this study produced by the polymerization number of 4,800 SM (Fw:104, dissoluble in water 300 mg L-1 at 25°C) or 1,600 ST (Fw:312).10 In 1935, Staudinger the term “polystyrene” as more appropriate than “metastyrene”. 33 Staudinger made numerous significant contributions to the study of polymer chemistry and showed PS to degrade only at >300 °C, with SM as the main product.33,34 Commercially-available PS pellets, however, usually contain unreacted SOs (90 mg kg-1 in this study), especially ST, along with various additives. To confirm the generation of SOs, purified PS (SO-free, under 0.1µ g kg-1) was prepared as the reactant and subjected to a novel thermal decomposition technique.10,17,22

Section II. Estimation of the total plastic production in the world

and the amount of SOs in the world ocean

- PS production10:

Based on the statistics for the annual global production of plastics, a continuous equation for the quantity of plastics produced, w [tons], in terms of years since 1950,

t [year], is depicted as Eq. (1). The sum of the total plastic produced is estimated at 6.98×109 MT in the world for the years 1950 to 2015 by integrating Eq. (1) with t ranging from 0 to 65.

dwdt=1.50×106+4.845×104t2.107　　　　　　　　　　　　　(1)

065w dt= [1.50×106 t+1.559×104 t3.107]065=6.98×109

- Decomposition10:

The simulation was conducted by using three differential equations (Eqs.2 through 4). The production share of PS at 7% 2 and inflow ratio at 3%15were assumed to be constant during 1950 to 2050. where w(t) (MT) is the annual plastic production at the eclipsed year t since 1950, P(t) (MT) is the cumulative amount of PS accumulated in the ocean at eclipsed year since 1950, t, S(t) (MT) is the total amount of SOs in the ocean at the year t. Eq.(2) is a fitting result to the statistical data of global plastic production2. In eq. (4), 3.232×10-7 (year-1) is the rate of ST formation at 30°C that equals to the rate of SOs formation. Eq. (3) was given by multiplying Eq. (2) by the share of PS 7% and inflow ratio 3%. Eq. (4) is based on the kinetic parameters of ST formation at 30°C.

dw(t)dt=1.50×106+4.845×104t2.107			      (2)

dP(t)dt=3.150×103+101.7t2.107-3.232×10-7P(t)	      (3)

dS(t)dt=3.232×10-7P(t)				      (4)

Each calculation using Mathematica™ under the initial values: P (0) = 3.150×103 MT,

S (0) = 0 MT at t = 0 as 1950. Details were shown another paper.10

3. Computations: of floating/drifting PS based on survey

a. Sea water volume: 1.4×1021 L

b.PS inflow since 1950 to 2015: 5.0 ×108 (MT) × 3/100 (from Ref.15) = 1.5 ×107 MT

c. Open water SO: 0.1 to 0.2 µg L-1 × a = 1.4 - 2.8 ×109 MT  See Table1

Convert to PS, c/ ST(Fw:1600) = 8.75×105 (deep) - 17.5×105 (surface) MT

Total(surface + deep): 2,625,000 MT

d. Degradation %: c/b ×100 = 17.5 %

Estimate floating/drifting PS: b - c = 1.2 ×107 MT

Section ⅡI. Dispersion: Design for determining SOs dispersion into the Northwest Pacific Ocean.

Dispersion of SOs from Japan to the near-surface Northwest Pacific Ocean was roughly estimated by using a series of equations below:

∂A∂t=-u∂A∂x-v∂A∂y+FA-k1A

∂B∂t=-u∂B∂x-v∂B∂y+k1A-k2B

Parameters and variables are defined as follow:

Prognostic variables: A and B are A- PS and SOs concentration, respectively. These values are assumed to be uniform in 0-200 m and set to 0 at the initial time (1950).

Chemical parameters: k1 = 7.28 ×10–5 a–1 and k2 = 0.1 k1 are rate of PS and SOs degradation at 20 °C, respectively.

FA = 84.59×10–5 kg a–1 m–2 is PS input on coastal grids surrounding main islands of Japan. This is equivalent to 10,000 MT per year, which is the typical amount of washed up PS onto Japanese coast, for 0.25 degree model resolution.

Physical parameters:

Pollutants are advected by annual mean climatological near-surface currents (u, v)

obtained from OSCAR.19

References

1.Geyer R., Jambeck J.R., Law K.L., Production, use, and fate of all plastics ever made, Sci.Adv.2017;3:e1700782

2.Plastics Europe, “The compelling facts about plastics: An analysis of plastic production, demand and recovery for 2006 in Europe” (Plastics Europe, 2008; https://www.plasticseurope.org/application/files/2815/1689/9283/2006compelling_fact_PubJan2008.pdf )

3.Carpenter E.D., Smith K.L. Jr., Plastics on the Sargasso Sea surface. Science 175, 1240-1241 (1972).

4.van Sebille E., Wilcox C., Lebreton L., Maximenko N., Hardesty B.D., Franeker J.A., Eriksen M., Siegel D.,Galgani F., Law K.L., A global inventory of small floating plastic debris. Environ. Res. Lett.10 doi: 10.1088/1748-9326/10/12/124006 2015 (2015).

5.Eriksen M.L., Lebereton C.M., Carson H.S., Thiel M., Moore C.J., Borerro C.J., Galgani F., Ryan P.G., Reisser J., Plastic pollution in the world’s oceans: more than 5 trillion plastic pieces weighing over 250,000 tons afloat at sea. PLOS ONE doi:10.1371/journal.pone.0111913 2014 (2014).

6.Cozar A., Echevarria F., Gonzalez-Gordillo J.I., Irigoien X., Ubeda B., Hernandez-Leon S., Palma A.T., Navarro S., Garcia-de-Lomas J., Ruiz A., Fernandez-de-Puelles M.L., Duarte C.M., Plastic debris in the open ocean. PNAS, 111(28) 10239-10244 doi:10.1073/pnas.1314705111 2014 (2014).

7.Lebreton L., Slat B., Ferrari F., Sainte-Rose B., Aitken J., Marthouse R., Hajbane S., Cunsolo S., Schwarz A., Levivier A., Noble K., Debeljak P., Maral H., Shoeneich-Argent R., Brambini R., Reisser J. Evidence that the great Pacific garbage patch is rapidly accumulating plastic. Nature Sci. Rep. 8, 4666 (2018).

8.Jennings S., Melin F., Blanchard J.L., Forster R.M., Dulvy N.K., Wilson R.W., Global-scale predictions of community and ecosystem properties from simple ecological theory (Proceedings of the Royal Society B, 2008)

https://doi.org/10.1098/rspb.2008.0192

9.Martin J., Lusher A., Thompson,R.C., Morley A., The deposition and accumulation of microplastics in marine sediments and bottom water from the Irish continental shelf 2017;7:10772|DOI:10.1038/s41598-017-11079-2.

10.Kimukai H., Kodera Y., Koizumi K., Okada M., Yamada K., Hiaki T., Saido K., Low temperature decomposition of polystyrene, Appl.Sci., 2020, 10,5100;

doi:10.3390/app10155100

11.Saido K., Koizumi K., Sato H., Ogawa N., Kwon B.G., Chung S.-Y., Kusui T., Nishimura M., Kodera Y., New analytical method for the determination of styrene oligomers formed from polystyrene decomposition and its application at the coastlines of North-West Pacific Ocean. Sci. Total Environ. 473-474, 490-495 (2014).

12.Kwon B.G., Amamiya K., Sato H., Chung S-Y., Kodera Y., Kim S-K., Lee E. J., Saido K., Monitoring of styrene oligomer as indicator of polystyrene plastic pollution in the North-West Pacific Ocean. Chemosphere, 180, 500-505 (2017).

13.Amamiya K., Saido K., Chung S-Y., Hiaki T., Lee D.S., Kwon B-G.. Evidence of transport of styrene oligomers originated from polystyrene plastic to oceans by runoff. Sci. Total Environ., 667, 57-63 (2019).

14.Amamiya K., Koizumi K., Yamada K., Hiaki T., Kusui T., Saido K.. Analysis of Drifting Polystyrene Degradation Surround Japan, Austin J. Environ.Txicol.,6, id1030 (2020).

15.Jambeck J.R., Geyer R., Wilcox C., Siegler T. R., Perryman M., Andrady A., Narayan R., Law K. L., Plastic waste inputs from land into the ocean. Science 347, 768-771 (2015). doi:10.1126/science.1260352

16.Lafeuille J-L., Buniak M-L., Vioujas M-C., Lefevre S., Natural formation of styrene by cinnamon mold flora. J. Food Sci. 74, 276–283 (2009).

17.Saido K., Taguchi H., Kodera Y., Ishihara Y., Ryu I-J., Chung S-Y., Novel method for polystyrene reactions at low temperature. Macromol. Res. 11, 87-91 (2003).

18.“2014 Research report on marine debris floating on the ocean surface and settled on the sea bed in offshore areas around Japan (summary),” Ministry of the Environment, 2015;<http://www.npec.or.jp/NWPacific_node/report/document/2014Research_report_on_marine_debris_floating_on_the_ocean_surface_around_Japan%20(revised_ver).pdf)>(September 2019).

19.Bonjean F., Lagerloef G.S.E., Diagnostic model and analysis of the surface current in the tropical Pacific Ocean. J.Phys. Oceanogr., 32, 2938- 2954 (2002).

20.Moore C.J., Moore S.L., Leecaster M.K., Weisberg S.B., A comparison of plastic and plankton in the north pacific central gyre. Marine Poll. Bull., 42, 1297-1300 (2001).

21.Isobe A., Iwasaki S., Uchida K., Tokai T., Abundance of non-conservative microplastics in the upper ocean from 1957 to 2066. Nature commun. (2019) 10:417 doi:10.1038/s41467-019-08316-9 2019

22.Saido K., Kodera Y.,Kuroki T., Park J-H., Chung S-Y., Low temperature decomposition of epoxy resin, Macromol. Res., 22, 490-492 (2004).

23.Preethi S., Sandhya K., Lebonah D. E., Prasad Ch. Venkata, Sreedevi B., Chandrasekhar K., Kumari J. P., Toxicity of bisphenol A on humans. Intern. Lettr. Natul Sci., Online: 2014-10-15 ISSN: 2300-9675, 27, 32-46 doi:10.18052/www.scipress.com /ILNS.27.32 2014

24.Dillingham E. 0., Autian J., Teratogenicity, Mutagenicity, and Cellular Toxicity of Phthalate Esters Environ. Health Persp., 3, 81-89 (1973).

25.Leibman K.C., Metabolism and Toxicity of Styrene. Environ. Health Persp., 11,115-119 (1975).

26.Pauluhn J., Inhalation Toxicity of 1,6-Hexamethylene Diisocyanate Homopolymer (HDI-IC) Aerosol: Results of Single Inhalation Exposure Studies, Toxicol. Sci., 58, 173–181 (2000., https://doi.org/10.1093/toxsci/58.1.173

# 27. M. Saunois et al., The global methane budget 2000-2017.Earth Syst.Sci. Data., 12,1561-1623 (2020). https:// doi.olg/10.5194/essd-12-1561-2020

# 28. Royer S-J., Ferron S., Wilson S.T., Karl D.M., Production of methane and ethylene from plastic in the environment 2018 https://doi.org/10.1371/journal.pone.0200574

# 29. Zheng J., Suh S., Strategies to reduce the global carbon footprint of plastics, Nat. Clim. Chang, 9, 374-379 (2019). http://doi.org/10.1038/s41558-019-0459-z

30.Kukulka T., Proskurowski G., Ferguson S. Morét, Meyer D.W., Law K.L.,

The effect of wind mixing on the vertical distribution of buoyant plastic debris. Geophys. Res. Lett., 39, L07601 (2012).

31.Bianco A., Sordello F., Ehn M., Vione D., Passanati M., Degradation of nanoplastics in the environment: Reactivity and impact on atmospheric and surface waters. Sci. Total Environ.,742 (2020) 140413, doi.org/10.1016/j.scitotenv.2020.140413.

32.Murphy J., Additives for Plastics Handbook (Elsevier, ed. 2, 2011).

33.Staudinger H., Steinhofer A., Über hochpolymere Verbindungen. 107. Beiträge zur Kenntnis der Polystyrole. Ann., 517, 35–53 (1935).

34.Madorsky S.L., Rate of thermal degradation of polystyrene and polyethylene in a vacuum. J. Polym. Sci., 9, 133–156 (1952).