Supplementary Information

Exploration of Nonlinear Optical Enhancement and Interesting Optical Behavior with Pyrene Moiety as the Conjugated Donor and Efficient Modification in Acceptor Moieties

Muhammad Khalid, *1 Muhammad Usman Khan,2 Nimra Azhar,1 Muhammad Nadeem Arshad3,4, Abdullah M. Asiri3,4, Ataualpa Albert Carmo Braga,5 Muhammad Nadeem Akhtar6

1Department of Chemistry, Khwaja Fareed University of Engineering & Information Technology, Rahim Yar Khan, 64200, Pakistan

2Department of Chemistry, University of Okara, Okara-56300, Pakistan

3Chemistry Department, Faculty of Science, King Abdulaziz University, Jeddah 21589, P.O. Box 80203, Saudi Arabia.

4Center of Excellence for Advanced Material Research (CEAMR), King Abdulaziz University, Jeddah 21589, P.O. Box 80203, Saudi Arabia

5Departamento de Química Fundamental, Instituto de Química, Universidade de São Paulo, Av. Prof. Lineu Prestes, 748, São Paulo, 05508-000, Brazil.

6Department of Chemistry, Baghdad-ul-Jadeed Campus, The Islamia University of Bahawalpur, Bahawalpur, 63100, Pakistan.

*Corresponding authors E-mail addresses:

Dr. Muhammad Khalid (muhammad.khalid@kfueit.edu.pk;  Khalid@iq.usp.br)

Table S1:Cartesian coordinates of HPPCR

| Atom | X-axis | Y-axis | Z-axis |
| --- | --- | --- | --- |
| C | 1.68542 | 0.05447 | -2.44988 |
| C | 0.34972 | 0.07538 | -2.80639 |
| C | -0.62572 | -0.41478 | -1.9342 |
| C | -0.23198 | -0.92066 | -0.66662 |
| C | 1.14633 | -0.92972 | -0.29745 |
| C | 2.10908 | -0.45482 | -1.21779 |
| C | -2.01319 | -0.40065 | -2.2735 |
| C | -1.22528 | -1.40717 | 0.23406 |
| C | -2.60037 | -1.42548 | -0.14611 |
| C | -2.95526 | -0.87937 | -1.42368 |
| C | -3.56026 | -1.93036 | 0.76085 |
| C | -3.14678 | -2.35709 | 2.027 |
| C | -1.81649 | -2.32932 | 2.40374 |
| C | -0.83709 | -1.86805 | 1.52017 |
| C | 0.54362 | -1.82427 | 1.88358 |
| C | 1.48949 | -1.37629 | 1.02127 |
| H | 2.5285 | -1.33284 | 1.33548 |
| H | 0.8219 | -2.15149 | 2.88394 |
| H | -2.30214 | 0.01861 | -3.23586 |
| H | 2.43703 | 0.411 | -3.15156 |
| H | 0.04565 | 0.46428 | -3.77654 |
| H | -4.00515 | -0.83426 | -1.69972 |
| H | -3.89408 | -2.74976 | 2.71395 |
| H | -1.51737 | -2.67962 | 3.38999 |
| C | 3.55939 | -0.46956 | -0.94025 |
| C | 4.32306 | 0.68447 | -1.15585 |
| C | 4.22445 | -1.63109 | -0.51969 |
| C | 5.68937 | 0.67675 | -0.94493 |
| H | 3.82636 | 1.59903 | -1.47323 |
| C | 5.59152 | -1.64402 | -0.30859 |
| H | 3.65611 | -2.54843 | -0.38234 |
| C | 6.35698 | -0.4824 | -0.5146 |
| H | 6.26442 | 1.58681 | -1.10873 |
| H | 6.06674 | -2.5676 | 0.00676 |
| C | 7.78955 | -0.37982 | -0.32726 |
| H | 8.20308 | 0.60154 | -0.55731 |
| C | 8.71328 | -1.28448 | 0.08306 |
| C | 8.40804 | -2.63178 | 0.4448 |
| N | 8.1359 | -3.72431 | 0.73695 |
| C | 10.15688 | -0.94237 | 0.19148 |
| O | 11.00314 | -1.72954 | 0.54238 |
| O | 10.40915 | 0.33127 | -0.14567 |
| C | 11.78841 | 0.72147 | -0.07459 |
| C | 11.86733 | 2.18094 | -0.45158 |
| H | 12.37507 | 0.09236 | -0.75911 |
| H | 12.15786 | 0.52371 | 0.93914 |
| C | 13.30215 | 2.67361 | -0.58551 |
| H | 11.33449 | 2.32127 | -1.4015 |
| H | 11.33049 | 2.77656 | 0.30107 |
| H | 13.28598 | 3.71805 | -0.92892 |
| H | 13.81178 | 2.10605 | -1.38076 |
| C | 14.12215 | 2.58857 | 0.69479 |
| C | 15.50123 | 3.21251 | 0.54789 |
| H | 14.23668 | 1.53832 | 1.00774 |
| H | 13.57785 | 3.08758 | 1.51409 |
| C | 16.32474 | 3.12593 | 1.821 |
| H | 16.03362 | 2.71739 | -0.2784 |
| H | 15.38942 | 4.26425 | 0.24339 |
| H | 17.31185 | 3.58476 | 1.7024 |
| H | 15.81933 | 3.63395 | 2.65186 |
| H | 16.47776 | 2.08207 | 2.12174 |
| C | -4.9958 | -2.03409 | 0.42818 |
| C | -5.95804 | -1.5448 | 1.32237 |
| C | -5.44135 | -2.68301 | -0.73 |
| C | -7.31038 | -1.6586 | 1.05489 |
| H | -5.6271 | -1.05994 | 2.23878 |
| C | -6.79561 | -2.81737 | -0.98843 |
| H | -4.71405 | -3.11498 | -1.41412 |
| C | -7.75503 | -2.27781 | -0.12146 |
| H | -8.02991 | -1.29104 | 1.78227 |
| H | -7.12566 | -3.34346 | -1.8828 |
| C | -9.16075 | -2.45804 | -0.45481 |
| H | -9.3814 | -3.37186 | -1.01065 |
| C | -10.2345 | -1.68749 | -0.16024 |
| C | -11.535 | -2.18012 | -0.49701 |
| N | -12.58 | -2.59675 | -0.79136 |
| C | -10.2332 | -0.34762 | 0.50094 |
| O | -11.1071 | 0.0258 | 1.24513 |
| O | -9.17166 | 0.37806 | 0.13561 |
| C | -9.02017 | 1.65214 | 0.78206 |
| C | -9.7867 | 2.73429 | 0.05763 |
| H | -7.94055 | 1.84422 | 0.76741 |
| H | -9.35291 | 1.56838 | 1.82454 |
| C | -9.56257 | 4.10024 | 0.68746 |
| H | -9.47763 | 2.74772 | -0.99754 |
| H | -10.856 | 2.48281 | 0.07578 |
| H | -9.86893 | 4.07299 | 1.74549 |
| H | -8.48559 | 4.33583 | 0.69163 |
| C | -10.3179 | 5.20904 | -0.02719 |
| C | -10.1079 | 6.57929 | 0.59779 |
| H | -11.3937 | 4.97095 | -0.03543 |
| H | -10.0112 | 5.23793 | -1.08547 |
| C | -10.867 | 7.67483 | -0.13045 |
| H | -10.417 | 6.54616 | 1.65342 |
| H | -9.032 | 6.8114 | 0.60824 |
| H | -10.7106 | 8.65739 | 0.32685 |
| H | -10.5515 | 7.74166 | -1.17917 |
| H | -11.9456 | 7.47438 | -0.12722 |

Table S2: Cartesian coordinates of HPPC1

| Atom | X-axis | Y-axis | Z-axis |
| --- | --- | --- | --- |
| C | -4.6856 | -2.47239 | -0.5195 |
| C | -3.38122 | -2.92751 | -0.5564 |
| C | -2.31411 | -2.03436 | -0.42782 |
| C | -2.58481 | -0.652 | -0.24084 |
| C | -3.93329 | -0.18767 | -0.18804 |
| C | -4.98792 | -1.11594 | -0.35437 |
| C | -0.95648 | -2.4773 | -0.45519 |
| C | -1.49844 | 0.26187 | -0.09826 |
| C | -0.15024 | -0.19753 | -0.18064 |
| C | 0.07494 | -1.60513 | -0.33509 |
| C | 0.90742 | 0.73371 | -0.06189 |
| C | 0.60605 | 2.07732 | 0.18447 |
| C | -0.69858 | 2.52436 | 0.28512 |
| C | -1.76736 | 1.63648 | 0.13624 |
| C | -3.12503 | 2.0683 | 0.23595 |
| C | -4.15781 | 1.2023 | 0.08453 |
| H | -5.1786 | 1.55882 | 0.19064 |
| H | -3.31579 | 3.11879 | 0.44968 |
| H | -0.76715 | -3.54411 | -0.56292 |
| H | -5.50481 | -3.17571 | -0.65587 |
| H | -3.17207 | -3.98618 | -0.69953 |
| H | 1.09752 | -1.97209 | -0.33354 |
| H | 1.42726 | 2.78653 | 0.26747 |
| H | -0.90648 | 3.57731 | 0.4676 |
| C | -6.41186 | -0.72691 | -0.36832 |
| C | -7.33989 | -1.45446 | 0.38827 |
| C | -6.89469 | 0.31555 | -1.17467 |
| C | -8.68629 | -1.14605 | 0.34387 |
| H | -6.98724 | -2.25979 | 1.02903 |
| C | -8.24075 | 0.63175 | -1.21855 |
| H | -6.1991 | 0.8679 | -1.80242 |
| C | -9.17055 | -0.09578 | -0.45434 |
| H | -9.39017 | -1.72097 | 0.94372 |
| H | -8.57223 | 1.43945 | -1.86416 |
| C | -10.5992 | 0.13646 | -0.43082 |
| H | -11.1591 | -0.5703 | 0.18087 |
| C | -11.3705 | 1.07701 | -1.03204 |
| C | -10.8593 | 2.11698 | -1.86663 |
| N | -10.4236 | 2.95661 | -2.54366 |
| C | -12.8471 | 1.1088 | -0.86159 |
| O | -13.5579 | 1.95081 | -1.35643 |
| O | -13.298 | 0.09753 | -0.10322 |
| C | -14.7189 | 0.06668 | 0.09246 |
| C | -15.0365 | -1.15631 | 0.91832 |
| H | -15.2155 | 0.03636 | -0.88748 |
| H | -15.027 | 1.00006 | 0.58021 |
| C | -16.5343 | -1.38316 | 1.07919 |
| H | -14.5743 | -2.02732 | 0.43493 |
| H | -14.5622 | -1.05679 | 1.90571 |
| H | -16.6916 | -2.32942 | 1.61672 |
| H | -16.9937 | -1.52314 | 0.0875 |
| C | -17.2628 | -0.26901 | 1.81815 |
| C | -18.7171 | -0.60731 | 2.10882 |
| H | -17.2245 | 0.66542 | 1.23606 |
| H | -16.7401 | -0.05376 | 2.7653 |
| C | -19.4455 | 0.51289 | 2.83051 |
| H | -19.2289 | -0.84067 | 1.16283 |
| H | -18.7591 | -1.53023 | 2.70702 |
| H | -20.4888 | 0.25571 | 3.04065 |
| H | -18.9609 | 0.74429 | 3.7873 |
| H | -19.4439 | 1.43313 | 2.23328 |
| C | 2.33037 | 0.35497 | -0.188 |
| C | 3.25805 | 0.78969 | 0.7654 |
| C | 2.81233 | -0.3803 | -1.27912 |
| C | 4.60492 | 0.48701 | 0.64896 |
| H | 2.90566 | 1.35182 | 1.62826 |
| C | 4.15965 | -0.6763 | -1.40324 |
| H | 2.12096 | -0.69002 | -2.06049 |
| C | 5.08395 | -0.25642 | -0.43674 |
| H | 5.29396 | 0.80933 | 1.42791 |
| H | 4.51396 | -1.21445 | -2.27998 |
| C | 6.49549 | -0.59895 | -0.57376 |
| C | 7.05018 | -1.6677 | -1.2329 |
| S | 7.74608 | 0.38397 | 0.14366 |
| C | 8.46127 | -1.7055 | -1.1639 |
| H | 6.45021 | -2.42082 | -1.73593 |
| C | 9.00456 | -0.66401 | -0.45465 |
| H | 9.07128 | -2.46711 | -1.64154 |
| C | 17.24227 | 0.77253 | 1.06153 |
| C | 16.36355 | 1.84548 | 0.97743 |
| C | 15.00269 | 1.63706 | 0.73276 |
| C | 14.52702 | 0.30788 | 0.56873 |
| C | 15.43146 | -0.7851 | 0.65559 |
| C | 16.78336 | -0.52945 | 0.90337 |
| C | 14.06507 | 2.71748 | 0.64143 |
| C | 13.14981 | 0.07225 | 0.31801 |
| C | 12.24072 | 1.16123 | 0.23814 |
| C | 12.74828 | 2.49184 | 0.40632 |
| C | 10.89148 | 0.90706 | -0.01137 |
| H | 10.20602 | 1.75004 | -0.09957 |
| C | 10.41452 | -0.39645 | -0.18165 |
| C | 11.31415 | -1.46446 | -0.09444 |
| C | 12.67133 | -1.25507 | 0.14796 |
| C | 13.60544 | -2.339 | 0.24477 |
| C | 14.92091 | -2.114 | 0.48647 |
| H | 15.62055 | -2.94543 | 0.55693 |
| H | 13.22995 | -3.35313 | 0.11806 |
| H | 14.43848 | 3.7326 | 0.76737 |
| H | 18.29726 | 0.95329 | 1.25304 |
| H | 16.72764 | 2.86402 | 1.10262 |
| H | 17.47529 | -1.3675 | 0.9704 |
| H | 12.04658 | 3.32167 | 0.33997 |
| H | 10.9444 | -2.48446 | -0.19134 |

Table S3: Cartesian coordinates of HPPC2

| Atom | X-axis | Y-axis | Z-axis |
| --- | --- | --- | --- |
| C | -4.69246 | -2.42153 | -0.60375 |
| C | -3.39087 | -2.87585 | -0.70391 |
| C | -2.31649 | -2.00727 | -0.49037 |
| C | -2.57658 | -0.65391 | -0.14437 |
| C | -3.92128 | -0.19097 | -0.03179 |
| C | -0.96121 | -2.44829 | -0.5887 |
| C | -1.48455 | 0.23164 | 0.09591 |
| C | -0.14028 | -0.22051 | -0.05366 |
| C | 0.07612 | -1.5992 | -0.38235 |
| C | 0.92331 | 0.68398 | 0.16794 |
| C | 0.6335 | 1.988 | 0.58243 |
| C | -0.66792 | 2.42676 | 0.74474 |
| C | -1.74321 | 1.57033 | 0.49385 |
| C | -3.09771 | 1.99571 | 0.64816 |
| C | -4.13614 | 1.15952 | 0.39957 |
| H | -3.28113 | 3.01466 | 0.98536 |
| H | -0.7777 | -3.49524 | -0.82487 |
| H | -5.51835 | -3.10078 | -0.80565 |
| H | -3.18932 | -3.91373 | -0.96296 |
| H | 1.09774 | -1.96454 | -0.44459 |
| H | 1.46079 | 2.67592 | 0.74562 |
| H | -0.86825 | 3.45103 | 1.05444 |
| C | -10.5178 | 0.43995 | -0.37449 |
| C | 2.34089 | 0.31899 | -0.0354 |
| C | 3.28986 | 0.59485 | 0.95515 |
| C | 2.7944 | -0.23674 | -1.23863 |
| C | 4.63281 | 0.31464 | 0.76047 |
| H | 2.95801 | 1.01394 | 1.90347 |
| C | 4.1381 | -0.50421 | -1.44135 |
| H | 2.08246 | -0.42178 | -2.04096 |
| C | 5.0859 | -0.24056 | -0.44264 |
| H | 5.3415 | 0.50845 | 1.56404 |
| H | 4.46905 | -0.89189 | -2.40248 |
| C | 6.49606 | -0.53868 | -0.66927 |
| C | 7.04705 | -1.45406 | -1.53113 |
| S | 7.75257 | 0.30923 | 0.19471 |
| C | 8.45942 | -1.47963 | -1.50344 |
| H | 6.44527 | -2.10768 | -2.15603 |
| C | 9.00917 | -0.58406 | -0.62049 |
| H | 9.06336 | -2.12462 | -2.13507 |
| C | 17.26595 | 0.78403 | 0.86277 |
| C | 16.34895 | 1.80084 | 1.09858 |
| C | 14.98411 | 1.59923 | 0.87031 |
| C | 14.54447 | 0.33576 | 0.39138 |
| C | 15.48767 | -0.70061 | 0.15308 |
| C | 16.84236 | -0.45397 | 0.39542 |
| C | 14.0077 | 2.62316 | 1.10123 |
| C | 13.16384 | 0.10893 | 0.15011 |
| C | 12.21677 | 1.14052 | 0.3895 |
| C | 12.68847 | 2.40567 | 0.87232 |
| C | 10.86595 | 0.89838 | 0.13697 |
| H | 10.1512 | 1.70624 | 0.29423 |
| C | 10.42178 | -0.33889 | -0.34037 |
| C | 11.35944 | -1.35412 | -0.56092 |
| C | 12.71996 | -1.15181 | -0.33151 |
| C | 13.69289 | -2.18141 | -0.55677 |
| C | 15.01185 | -1.96488 | -0.32685 |
| H | 15.74127 | -2.75387 | -0.50351 |
| H | 13.34438 | -3.14642 | -0.92137 |
| H | 14.35359 | 3.58841 | 1.468 |
| H | 18.32346 | 0.95847 | 1.04599 |
| H | 16.68552 | 2.76919 | 1.46567 |
| H | 17.56477 | -1.248 | 0.21298 |
| H | 11.95722 | 3.19236 | 1.05077 |
| H | 11.02326 | -2.33384 | -0.89775 |
| C | -14.0835 | -0.01476 | 0.48408 |
| C | -13.5218 | -1.10039 | 1.16516 |
| C | -14.276 | -2.00024 | 1.89646 |
| C | -15.6512 | -1.80606 | 1.94533 |
| C | -16.2303 | -0.73089 | 1.26817 |
| C | -15.4663 | 0.17286 | 0.53522 |
| C | -12.9999 | 0.74083 | -0.17552 |
| C | -11.733 | 0.04519 | 0.11149 |
| C | -12.0611 | -1.12034 | 0.97789 |
| H | -13.7813 | -2.8232 | 2.40661 |
| H | -16.2812 | -2.4886 | 2.50978 |
| H | -17.3074 | -0.59128 | 1.31196 |
| H | -15.9594 | 0.99244 | 0.02531 |
| H | -10.562 | 1.32361 | -1.00446 |
| H | -5.15446 | 1.50588 | 0.55167 |
| C | -13.1976 | 1.89283 | -0.90163 |
| C | -12.1657 | 2.65833 | -1.52396 |
| N | -11.3517 | 3.30932 | -2.04362 |
| C | -14.4876 | 2.46695 | -1.11108 |
| N | -15.5209 | 2.96605 | -1.30669 |
| O | -11.32 | -1.95739 | 1.46202 |
| C | -6.401 | -0.68289 | -0.26765 |
| C | -7.34018 | -1.46037 | 0.42685 |
| C | -6.86516 | 0.4357 | -0.97578 |
| C | -8.68567 | -1.14386 | 0.43575 |
| H | -6.99124 | -2.32299 | 0.99104 |
| C | -8.20815 | 0.75482 | -0.97852 |
| H | -6.1641 | 1.03634 | -1.55091 |
| C | -9.15479 | -0.02139 | -0.2735 |
| H | -9.39069 | -1.75145 | 0.99177 |
| H | -8.55187 | 1.6201 | -1.54498 |
| C | -4.98312 | -1.08824 | -0.29356 |

Table S4: Cartesian coordinates of HPPC3

| Atom | X-axis | Y-axis | Z-axis |
| --- | --- | --- | --- |
| C | -4.26595 | -2.69188 | 1.4677 |
| C | -2.93851 | -2.87935 | 1.81083 |
| C | -1.92359 | -2.2196 | 1.11142 |
| C | -2.26975 | -1.32876 | 0.05952 |
| C | -3.63871 | -1.12954 | -0.28415 |
| C | -4.63271 | -1.84948 | 0.41532 |
| C | -0.54389 | -2.39374 | 1.4405 |
| C | -1.24192 | -0.63081 | -0.64088 |
| C | 0.12978 | -0.85735 | -0.32477 |
| C | 0.43385 | -1.74739 | 0.75815 |
| C | 1.13003 | -0.16865 | -1.04855 |
| C | 0.74819 | 0.7614 | -2.02068 |
| C | -0.58212 | 0.99695 | -2.31896 |
| C | -1.59538 | 0.30219 | -1.65226 |
| C | -2.97783 | 0.52002 | -1.94194 |
| C | -3.95595 | -0.16079 | -1.29392 |
| H | -3.23403 | 1.26425 | -2.6941 |
| H | -0.29262 | -3.05419 | 2.26894 |
| H | -5.0473 | -3.23143 | 2.00055 |
| H | -2.67034 | -3.55164 | 2.62394 |
| H | 1.47325 | -1.88294 | 1.04444 |
| H | 1.52782 | 1.2843 | -2.57164 |
| H | -0.8529 | 1.71729 | -3.089 |
| C | -6.06075 | -1.73906 | 0.05619 |
| C | -7.00532 | -1.34352 | 1.01057 |
| C | -6.50482 | -2.05969 | -1.23382 |
| C | -8.33772 | -1.19432 | 0.66855 |
| H | -6.67246 | -1.11698 | 2.0215 |
| C | -7.84391 | -1.96406 | -1.56426 |
| C | -8.77319 | -1.47998 | -0.63318 |
| H | -9.05726 | -0.86451 | 1.41579 |
| H | -8.18078 | -2.22827 | -2.56495 |
| C | -10.1559 | -1.32541 | -1.03173 |
| C | 2.57238 | -0.39717 | -0.82193 |
| C | 3.43888 | 0.68078 | -0.61183 |
| C | 3.12869 | -1.68238 | -0.86155 |
| C | 4.79671 | 0.48258 | -0.41726 |
| H | 3.02947 | 1.68851 | -0.56829 |
| C | 4.48692 | -1.88174 | -0.6827 |
| H | 2.48409 | -2.53481 | -1.06797 |
| C | 5.35051 | -0.80346 | -0.4419 |
| H | 5.43523 | 1.34116 | -0.21544 |
| H | 4.89331 | -2.88809 | -0.75661 |
| C | 6.77349 | -1.03393 | -0.21772 |
| C | 7.40178 | -2.19862 | 0.14892 |
| S | 7.94258 | 0.25143 | -0.3855 |
| C | 8.80064 | -2.06847 | 0.29323 |
| H | 6.86638 | -3.12563 | 0.33236 |
| C | 9.26549 | -0.80154 | 0.043 |
| H | 9.45624 | -2.89269 | 0.55886 |
| C | 17.27625 | 1.98727 | 0.60031 |
| C | 16.36773 | 2.66964 | -0.19928 |
| C | 15.04504 | 2.22998 | -0.31285 |
| C | 14.63917 | 1.07186 | 0.40372 |
| C | 15.57363 | 0.37882 | 1.22048 |
| C | 16.88575 | 0.85406 | 1.30337 |
| C | 14.07825 | 2.9053 | -1.12797 |
| C | 13.30107 | 0.60788 | 0.30519 |
| C | 12.36141 | 1.29904 | -0.50585 |
| C | 12.79961 | 2.46189 | -1.22136 |
| C | 11.05115 | 0.82542 | -0.58725 |
| H | 10.34608 | 1.34816 | -1.23384 |
| C | 10.63809 | -0.30873 | 0.11978 |
| C | 11.5687 | -0.97957 | 0.92181 |
| C | 12.89043 | -0.54818 | 1.02191 |
| C | 13.85363 | -1.22583 | 1.84069 |
| C | 15.13234 | -0.7839 | 1.93343 |
| H | 15.85445 | -1.30778 | 2.55779 |
| H | 13.53151 | -2.1093 | 2.38959 |
| H | 14.39678 | 3.79084 | -1.67583 |
| H | 18.3008 | 2.34325 | 0.67678 |
| H | 16.67737 | 3.55738 | -0.74862 |
| H | 17.60086 | 0.32261 | 1.92929 |
| H | 12.07596 | 2.9851 | -1.84425 |
| H | 11.25423 | -1.84315 | 1.50611 |
| C | -13.2859 | 0.25195 | -0.11371 |
| C | -12.4083 | 1.15722 | 0.50135 |
| C | -12.9201 | 2.15104 | 1.33723 |
| C | -14.2903 | 2.1887 | 1.52474 |
| C | -15.1544 | 1.2818 | 0.89685 |
| C | -14.659 | 0.29824 | 0.06393 |
| C | -12.5206 | -0.71309 | -0.92626 |
| C | -11.0808 | -0.40581 | -0.66523 |
| C | -11.0317 | 0.86443 | 0.05742 |
| H | -12.3091 | 2.8861 | 1.85111 |
| H | -15.3202 | -0.40903 | -0.42908 |
| H | -10.5589 | -2.09696 | -1.6963 |
| C | -9.97838 | 1.74134 | 0.12428 |
| C | -8.75094 | 1.55499 | -0.58045 |
| N | -7.75461 | 1.47284 | -1.176 |
| C | -10.0695 | 2.98418 | 0.81992 |
| N | -10.1333 | 3.99157 | 1.3994 |
| O | -12.967 | -1.60478 | -1.61675 |
| H | -4.99956 | 0.05386 | -1.51395 |
| H | -5.78346 | -2.40342 | -1.97216 |
| F | -14.8225 | 3.1029 | 2.32117 |
| F | -16.4537 | 1.39082 | 1.12623 |

Table S5: Cartesian coordinates of HPPC4

| Atom | X-axis | Y-axis | Z-axis |
| --- | --- | --- | --- |
| C | -4.03437 | 2.46591 | -1.34374 |
| C | -2.72042 | 2.67848 | -1.7198 |
| C | -1.6767 | 2.0263 | -1.05669 |
| C | -1.98074 | 1.11612 | -0.00875 |
| C | -3.33734 | 0.88533 | 0.36419 |
| C | -4.36252 | 1.60045 | -0.29601 |
| C | -0.30968 | 2.22959 | -1.4184 |
| C | -0.92244 | 0.43236 | 0.66009 |
| C | 0.43691 | 0.69291 | 0.31691 |
| C | 0.69709 | 1.5969 | -0.76577 |
| C | 1.46785 | 0.0232 | 1.01552 |
| C | 1.12739 | -0.92337 | 1.98743 |
| C | -0.19035 | -1.19465 | 2.30864 |
| C | -1.2328 | -0.51882 | 1.66823 |
| C | -2.60306 | -0.77513 | 1.9808 |
| C | -3.60934 | -0.10865 | 1.36174 |
| H | -2.82604 | -1.53699 | 2.7259 |
| H | -0.0918 | 2.90248 | -2.24624 |
| H | -4.83567 | 3.00624 | -1.84487 |
| H | -2.48485 | 3.36819 | -2.52835 |
| H | 1.72613 | 1.75486 | -1.07686 |
| H | 1.93021 | -1.4309 | 2.51905 |
| H | -0.4283 | -1.92851 | 3.07673 |
| C | -5.77894 | 1.47212 | 0.09651 |
| C | -6.75686 | 1.1792 | -0.86322 |
| C | -6.18711 | 1.6924 | 1.41971 |
| C | -8.08392 | 1.03743 | -0.50302 |
| H | -6.45481 | 1.02704 | -1.89735 |
| C | -7.52016 | 1.59983 | 1.77376 |
| C | -8.48484 | 1.22316 | 0.82829 |
| H | -8.8289 | 0.79359 | -1.25813 |
| H | -7.82725 | 1.78991 | 2.80053 |
| C | -9.86002 | 1.07917 | 1.24683 |
| C | 2.90028 | 0.2867 | 0.76653 |
| C | 3.78995 | -0.77271 | 0.55788 |
| C | 3.42728 | 1.58469 | 0.78975 |
| C | 5.14151 | -0.5456 | 0.35348 |
| H | 3.40377 | -1.78993 | 0.52556 |
| C | 4.77956 | 1.81318 | 0.60046 |
| H | 2.76481 | 2.42378 | 0.99412 |
| C | 5.66648 | 0.75274 | 0.36577 |
| H | 5.79868 | -1.39098 | 0.15566 |
| H | 5.16331 | 2.82908 | 0.66369 |
| C | 7.08409 | 1.01252 | 0.14026 |
| C | 7.68821 | 2.18668 | -0.23686 |
| S | 8.28032 | -0.24437 | 0.32879 |
| C | 9.09056 | 2.08622 | -0.3715 |
| H | 7.13316 | 3.09914 | -0.43413 |
| C | 9.58214 | 0.83311 | -0.10331 |
| H | 9.72847 | 2.92254 | -0.64204 |
| C | 17.65891 | -1.78147 | -0.54184 |
| C | 16.75528 | -2.4785 | 0.25061 |
| C | 15.42191 | -2.06744 | 0.34411 |
| C | 15.00002 | -0.92332 | -0.38551 |
| C | 15.92951 | -0.21527 | -1.19503 |
| C | 17.25279 | -0.66183 | -1.25766 |
| C | 14.4599 | -2.75836 | 1.15172 |
| C | 13.651 | -0.48819 | -0.30709 |
| C | 12.71658 | -1.19424 | 0.49709 |
| C | 13.1709 | -2.34231 | 1.22625 |
| C | 11.39543 | -0.74906 | 0.5588 |
| H | 10.69449 | -1.28292 | 1.20076 |
| C | 10.9662 | 0.37061 | -0.16153 |
| C | 11.89198 | 1.05637 | -0.9566 |
| C | 13.22412 | 0.65368 | -1.0369 |
| C | 14.18273 | 1.34708 | -1.84785 |
| C | 15.47192 | 0.9328 | -1.92136 |
| H | 16.19023 | 1.46864 | -2.53992 |
| H | 13.84855 | 2.21979 | -2.40665 |
| H | 14.7907 | -3.63309 | 1.70959 |
| H | 18.69212 | -2.11473 | -0.6021 |
| H | 17.07718 | -3.3555 | 0.81003 |
| H | 17.96409 | -0.11863 | -1.8778 |
| H | 12.45107 | -2.87703 | 1.84377 |
| H | 11.56663 | 1.9092 | -1.55065 |
| C | -13.0979 | -0.13762 | 0.1843 |
| C | -12.2901 | -0.99214 | -0.5882 |
| C | -12.8469 | -1.79182 | -1.58154 |
| C | -14.2167 | -1.70776 | -1.77933 |
| C | -15.0317 | -0.87311 | -1.01417 |
| C | -14.4649 | -0.08045 | -0.02168 |
| C | -12.2605 | 0.63178 | 1.12967 |
| C | -10.8486 | 0.27727 | 0.77874 |
| C | -10.8941 | -0.86874 | -0.12118 |
| H | -12.271 | -2.46229 | -2.21038 |
| H | -10.2013 | 1.76395 | 2.03024 |
| C | -9.91016 | -1.80386 | -0.32567 |
| C | -8.66761 | -1.78869 | 0.37642 |
| N | -7.6621 | -1.82215 | 0.96128 |
| C | -10.0947 | -2.93263 | -1.17838 |
| N | -10.2341 | -3.84744 | -1.88435 |
| O | -12.6178 | 1.4223 | 1.97445 |
| H | -4.64336 | -0.3506 | 1.59558 |
| H | -5.44401 | 1.96407 | 2.1663 |
| F | -14.7946 | -2.43272 | -2.72263 |
| F | -16.3325 | -0.8323 | -1.23821 |
| F | -15.2478 | 0.70557 | 0.68884 |

Table S6: Cartesian coordinates of HPPC5

| Atom | X-axis | Y-axis | Z-axis |
| --- | --- | --- | --- |
| C | -3.54603 | -2.2258 | -0.5665 |
| C | -2.25362 | -2.70952 | -0.64254 |
| C | -1.16285 | -1.86097 | -0.43012 |
| C | -1.39733 | -0.49741 | -0.10628 |
| C | -2.73289 | -0.00489 | -0.01247 |
| C | 0.18339 | -2.33189 | -0.50931 |
| C | -0.28855 | 0.36901 | 0.12752 |
| C | 1.04695 | -0.11222 | -0.00802 |
| C | 1.23667 | -1.50093 | -0.30986 |
| C | 2.12801 | 0.775 | 0.19965 |
| C | 1.86286 | 2.0919 | 0.58966 |
| C | 0.56984 | 2.55829 | 0.74169 |
| C | -0.52147 | 1.71879 | 0.50258 |
| C | -1.86748 | 2.17211 | 0.64803 |
| C | -2.92158 | 1.35382 | 0.40542 |
| H | -2.03223 | 3.19784 | 0.97407 |
| H | 0.34674 | -3.38638 | -0.72575 |
| H | -4.38315 | -2.88967 | -0.77333 |
| H | -2.07168 | -3.75509 | -0.88446 |
| H | 2.25048 | -1.8892 | -0.35789 |
| H | 2.70299 | 2.7665 | 0.74228 |
| H | 0.38871 | 3.59135 | 1.03343 |
| C | 3.53782 | 0.37661 | 0.00577 |
| C | 4.49276 | 0.65613 | 0.98961 |
| C | 3.97877 | -0.21971 | -1.18276 |
| C | 5.82885 | 0.33904 | 0.80373 |
| H | 4.17087 | 1.10708 | 1.92668 |
| C | 5.31554 | -0.52516 | -1.37661 |
| H | 3.2635 | -0.40676 | -1.98155 |
| C | 6.26856 | -0.25937 | -0.38358 |
| H | 6.54185 | 0.53651 | 1.60257 |
| H | 5.63843 | -0.94484 | -2.32696 |
| C | 7.67053 | -0.59889 | -0.60218 |
| C | 8.19578 | -1.56332 | -1.42566 |
| S | 8.95024 | 0.26021 | 0.21438 |
| C | 9.60763 | -1.61734 | -1.40631 |
| H | 7.57546 | -2.23078 | -2.017 |
| C | 10.18249 | -0.69447 | -0.56866 |
| H | 10.19272 | -2.30237 | -2.01294 |
| C | 18.47015 | 0.62241 | 0.78172 |
| C | 17.56666 | 1.65557 | 0.99744 |
| C | 16.19736 | 1.46221 | 0.79 |
| C | 15.73913 | 0.18972 | 0.35394 |
| C | 16.66859 | -0.86335 | 0.13616 |
| C | 18.02849 | -0.62424 | 0.35586 |
| C | 15.23472 | 2.50329 | 1.00077 |
| C | 14.35363 | -0.02923 | 0.13479 |
| C | 13.42073 | 1.01963 | 0.35309 |
| C | 13.9109 | 2.29351 | 0.79252 |
| C | 12.06493 | 0.78523 | 0.1224 |
| H | 11.36114 | 1.60567 | 0.2627 |
| C | 11.60143 | -0.46079 | -0.31184 |
| C | 12.52523 | -1.49297 | -0.51158 |
| C | 13.89053 | -1.29905 | -0.30338 |
| C | 14.85006 | -2.34532 | -0.50857 |
| C | 16.17383 | -2.13613 | -0.30035 |
| H | 16.89292 | -2.93769 | -0.46211 |
| H | 14.48766 | -3.31694 | -0.84057 |
| H | 15.59479 | 3.47502 | 1.33526 |
| H | 19.53145 | 0.79064 | 0.94806 |
| H | 17.91737 | 2.6305 | 1.3324 |
| H | 18.74057 | -1.43086 | 0.18877 |
| H | 13.18979 | 3.09279 | 0.95547 |
| H | 12.17515 | -2.47861 | -0.81541 |
| C | -12.901 | 0.33951 | 0.01976 |
| C | -12.4186 | -0.87978 | 0.50456 |
| C | -13.2486 | -1.91193 | 0.89138 |
| C | -14.6217 | -1.72371 | 0.78242 |
| C | -15.1255 | -0.50796 | 0.28945 |
| C | -14.2762 | 0.52939 | -0.09004 |
| C | -11.7511 | 1.21351 | -0.27948 |
| C | -10.5283 | 0.42972 | -0.05359 |
| C | -10.9424 | -0.87667 | 0.52386 |
| H | -3.9319 | 1.72359 | 0.55422 |
| H | -14.7191 | 1.44609 | -0.4649 |
| Cl | -16.831 | -0.26349 | 0.13832 |
| Cl | -15.6849 | -3.00044 | 1.25853 |
| C | -5.21742 | -0.43901 | -0.28964 |
| C | -6.20006 | -1.19541 | 0.36822 |
| C | -5.62681 | 0.70538 | -0.99202 |
| C | -7.53401 | -0.83527 | 0.34621 |
| H | -5.89439 | -2.07406 | 0.9325 |
| C | -6.95583 | 1.07418 | -1.01668 |
| H | -4.89069 | 1.29234 | -1.53619 |
| C | -7.9463 | 0.31543 | -0.35461 |
| H | -8.27295 | -1.43109 | 0.87013 |
| H | -7.25422 | 1.96908 | -1.5619 |
| C | -3.81149 | -0.88163 | -0.27948 |
| C | -11.8543 | 2.53755 | -0.6345 |
| O | -10.2605 | -1.80224 | 0.92392 |
| C | -10.7419 | 3.41232 | -0.82356 |
| N | -9.85515 | 4.14986 | -0.98363 |
| C | -13.1101 | 3.18868 | -0.82138 |
| N | -14.121 | 3.74243 | -0.98389 |
| C | -9.28438 | 0.83735 | -0.45183 |
| H | -9.28326 | 1.78245 | -0.98984 |
| H | -12.8343 | -2.84385 | 1.26808 |

Table S7: Cartesian coordinates of HPPC6

| Atom | X-axis | Y-axis | Z-axis |
| --- | --- | --- | --- |
| C | -2.93398 | -1.07548 | -1.97682 |
| C | -1.61287 | -1.35022 | -2.27555 |
| C | -0.58028 | -0.64252 | -1.65213 |
| C | -0.90273 | 0.35155 | -0.68928 |
| C | -2.26699 | 0.62498 | -0.37433 |
| C | 0.7936 | -0.90938 | -1.9372 |
| C | 0.1476 | 1.06402 | -0.03668 |
| C | 1.51079 | 0.81285 | -0.37318 |
| C | 1.79005 | -0.21922 | -1.32826 |
| C | 2.53094 | 1.5471 | 0.27473 |
| C | 2.18061 | 2.46951 | 1.26656 |
| C | 0.86158 | 2.70451 | 1.60803 |
| C | -0.17241 | 2.02093 | 0.96255 |
| C | -1.54284 | 2.23737 | 1.29869 |
| C | -2.54161 | 1.57223 | 0.66643 |
| H | -1.77136 | 2.94645 | 2.09269 |
| H | 1.02589 | -1.69692 | -2.65214 |
| H | -3.72794 | -1.61164 | -2.49325 |
| H | -1.36354 | -2.1144 | -3.00942 |
| H | 2.82665 | -0.46066 | -1.5467 |
| H | 2.97463 | 3.0302 | 1.75592 |
| H | 0.61486 | 3.43485 | 2.37668 |
| C | 3.9648 | 1.3827 | -0.04345 |
| C | 4.89048 | 1.18982 | 0.98782 |
| C | 4.45519 | 1.47107 | -1.35272 |
| C | 6.24601 | 1.0817 | 0.72492 |
| H | 4.53183 | 1.11463 | 2.0128 |
| C | 5.80992 | 1.35585 | -1.61932 |
| H | 3.75947 | 1.64524 | -2.17153 |
| C | 6.7354 | 1.16139 | -0.58481 |
| H | 6.9423 | 0.94885 | 1.55124 |
| H | 6.161 | 1.40526 | -2.64792 |
| C | 8.16092 | 1.05461 | -0.87434 |
| C | 8.86022 | 1.54966 | -1.94705 |
| S | 9.23591 | 0.20984 | 0.20846 |
| C | 10.24556 | 1.27341 | -1.89649 |
| H | 8.39166 | 2.1367 | -2.73188 |
| C | 10.6249 | 0.56074 | -0.7861 |
| H | 10.95691 | 1.62685 | -2.63732 |
| C | 18.40166 | -2.03431 | 1.45398 |
| C | 17.41838 | -1.88942 | 2.42464 |
| C | 16.13185 | -1.46387 | 2.07999 |
| C | 15.84132 | -1.18034 | 0.71761 |
| C | 16.85168 | -1.33132 | -0.27046 |
| C | 18.12398 | -1.75885 | 0.12062 |
| C | 15.09152 | -1.30129 | 3.05273 |
| C | 14.54209 | -0.74716 | 0.34393 |
| C | 13.52935 | -0.59758 | 1.32846 |
| C | 13.85065 | -0.8872 | 2.69547 |
| C | 12.26125 | -0.16688 | 0.94072 |
| H | 11.50083 | -0.02637 | 1.70896 |
| C | 11.95829 | 0.11124 | -0.39617 |
| C | 12.95897 | -0.04643 | -1.3621 |
| C | 14.24486 | -0.46244 | -1.01671 |
| C | 15.28332 | -0.62737 | -1.99272 |
| C | 16.52493 | -1.04011 | -1.63574 |
| H | 17.30415 | -1.16046 | -2.38686 |
| H | 15.04962 | -0.41062 | -3.0339 |
| H | 15.32327 | -1.52009 | 4.09398 |
| H | 19.39692 | -2.36592 | 1.73996 |
| H | 17.64055 | -2.10716 | 3.46816 |
| H | 18.89765 | -1.87499 | -0.6368 |
| H | 13.06915 | -0.76658 | 3.44389 |
| H | 12.72901 | 0.13638 | -2.41104 |
| C | -12.38 | 0.10706 | 0.32717 |
| C | -11.8204 | -1.17064 | 0.18362 |
| C | -12.6114 | -2.31217 | 0.20373 |
| C | -13.999 | -2.17292 | 0.36932 |
| C | -14.546 | -0.88835 | 0.50807 |
| C | -13.7519 | 0.25327 | 0.49051 |
| C | -11.3029 | 1.11545 | 0.2785 |
| C | -10.0477 | 0.40441 | 0.02521 |
| C | -10.3496 | -1.05118 | 0.01973 |
| H | -3.57181 | 1.73931 | 0.96737 |
| H | -14.2371 | 1.2158 | 0.60197 |
| Cl | -16.2512 | -0.68413 | 0.70711 |
| Cl | -15.0174 | -3.55811 | 0.40126 |
| C | -4.71972 | 0.18192 | -0.83662 |
| C | -5.61184 | -0.88169 | -0.62947 |
| C | -5.24359 | 1.48383 | -0.87156 |
| C | -6.96364 | -0.67159 | -0.43525 |
| H | -5.21859 | -1.8953 | -0.58702 |
| C | -6.5922 | 1.70255 | -0.68256 |
| H | -4.58026 | 2.3229 | -1.0674 |
| C | -7.49057 | 0.63527 | -0.45379 |
| H | -7.62799 | -1.50776 | -0.25532 |
| H | -6.97829 | 2.72119 | -0.70676 |
| C | -3.28648 | -0.08421 | -1.05358 |
| C | -11.4928 | 2.46079 | 0.4968 |
| O | -9.57714 | -1.97975 | -0.10882 |
| C | -10.4468 | 3.43218 | 0.53221 |
| N | -9.62035 | 4.25169 | 0.56983 |
| C | -12.7718 | 3.04404 | 0.74165 |
| N | -13.797 | 3.55763 | 0.94218 |
| C | -8.8565 | 1.0304 | -0.2294 |
| Cl | -11.9209 | -3.8818 | 0.02834 |
| H | -8.93939 | 2.11266 | -0.27431 |

Table S8: Cartesian coordinates of HPPC7

| Atom | X-axis | Y-axis | Z-axis |
| --- | --- | --- | --- |
| C | 3.73374 | -2.0541 | -0.65251 |
| C | 2.4324 | -2.50862 | -0.7389 |
| C | 1.36448 | -1.68002 | -0.38106 |
| C | 1.63299 | -0.37047 | 0.10143 |
| C | 2.97822 | 0.09659 | 0.19035 |
| C | 4.03202 | -0.75576 | -0.21995 |
| C | 0.00808 | -2.10853 | -0.50421 |
| C | 0.54727 | 0.4699 | 0.48859 |
| C | -0.79786 | 0.00713 | 0.38928 |
| C | -1.02304 | -1.30332 | -0.14652 |
| C | -1.85621 | 0.86167 | 0.77488 |
| C | -1.56125 | 2.15617 | 1.21369 |
| C | -0.25795 | 2.60784 | 1.31781 |
| C | 0.81256 | 1.77859 | 0.9718 |
| C | 2.16942 | 2.20138 | 1.1073 |
| C | 3.20216 | 1.39939 | 0.74552 |
| H | 4.22263 | 1.73985 | 0.89572 |
| H | 2.36092 | 3.18802 | 1.52614 |
| H | -0.18196 | -3.10042 | -0.91082 |
| H | 4.55025 | -2.69821 | -0.97249 |
| H | 2.22464 | -3.51172 | -1.10661 |
| H | -2.04623 | -1.64437 | -0.27695 |
| H | -2.38468 | 2.80296 | 1.51026 |
| H | -0.05254 | 3.61155 | 1.68595 |
| C | 5.44362 | -0.33725 | -0.24396 |
| C | 6.4388 | -1.19471 | 0.2547 |
| C | 5.84922 | 0.87987 | -0.81646 |
| C | 7.77872 | -0.86703 | 0.19993 |
| H | 6.13758 | -2.13184 | 0.718 |
| C | 7.18503 | 1.21616 | -0.87453 |
| H | 5.10575 | 1.54758 | -1.24429 |
| C | 8.18832 | 0.35408 | -0.37488 |
| H | 8.5249 | -1.5434 | 0.60053 |
| H | 7.48039 | 2.16486 | -1.32173 |
| C | 9.53159 | 0.84563 | -0.49711 |
| C | -3.27273 | 0.44125 | 0.72781 |
| C | -4.21826 | 1.22479 | 0.05779 |
| C | -3.72333 | -0.71248 | 1.38174 |
| C | -5.55323 | 0.8546 | 0.01152 |
| H | -3.88948 | 2.12145 | -0.46464 |
| C | -5.05916 | -1.07639 | 1.3498 |
| H | -3.01621 | -1.31394 | 1.95037 |
| C | -6.0004 | -0.30897 | 0.64917 |
| H | -6.25642 | 1.46164 | -0.55636 |
| H | -5.3896 | -1.95651 | 1.89725 |
| C | -7.39318 | -0.73839 | 0.58259 |
| C | -7.89164 | -2.01265 | 0.69112 |
| S | -8.6902 | 0.39677 | 0.30998 |
| C | -9.29611 | -2.08567 | 0.55344 |
| H | -7.25555 | -2.88044 | 0.84028 |
| C | -9.89098 | -0.86746 | 0.34068 |
| H | -9.86441 | -3.00842 | 0.62734 |
| C | -18.1529 | 0.6931 | -0.90056 |
| C | -17.3561 | 1.65991 | -0.29991 |
| C | -15.9943 | 1.4287 | -0.0821 |
| C | -15.4324 | 0.18653 | -0.48324 |
| C | -16.2534 | -0.79848 | -1.09631 |
| C | -17.6095 | -0.52332 | -1.2956 |
| C | -15.1392 | 2.40147 | 0.53222 |
| C | -14.052 | -0.07028 | -0.27264 |
| C | -13.2251 | 0.9149 | 0.33102 |
| C | -13.8193 | 2.15781 | 0.72891 |
| C | -11.87 | 0.64271 | 0.52584 |
| H | -11.2488 | 1.39396 | 1.01362 |
| C | -11.3086 | -0.5778 | 0.13751 |
| C | -12.1281 | -1.54167 | -0.45999 |
| C | -13.4876 | -1.31275 | -0.66893 |
| C | -14.3388 | -2.2871 | -1.28777 |
| C | -15.657 | -2.04094 | -1.49069 |
| H | -16.2933 | -2.78889 | -1.96121 |
| H | -13.8984 | -3.23489 | -1.59315 |
| H | -15.5775 | 3.34988 | 0.83914 |
| H | -19.2098 | 0.88996 | -1.06346 |
| H | -17.7854 | 2.61188 | 0.00838 |
| H | -18.2376 | -1.27818 | -1.76602 |
| H | -13.1808 | 2.90637 | 1.1952 |
| H | -11.6926 | -2.48103 | -0.7981 |
| C | 13.16022 | 0.21706 | -0.24981 |
| C | 12.66484 | -1.02674 | 0.15149 |
| C | 13.47529 | -2.10907 | 0.42665 |
| C | 14.85377 | -1.94837 | 0.28622 |
| C | 15.37421 | -0.70046 | -0.12797 |
| C | 14.5358 | 0.38553 | -0.3948 |
| C | 12.01751 | 1.13796 | -0.43459 |
| C | 10.7869 | 0.36715 | -0.21772 |
| C | 11.18646 | -0.99124 | 0.22155 |
| H | 14.98633 | 1.32023 | -0.7115 |
| H | 9.52999 | 1.84114 | -0.9338 |
| O | 10.50464 | -1.93973 | 0.56211 |
| C | 12.14922 | 2.48066 | -0.69589 |
| C | 11.05812 | 3.39758 | -0.78184 |
| N | 10.18966 | 4.16936 | -0.85649 |
| C | 13.41556 | 3.11148 | -0.88152 |
| N | 14.43519 | 3.64977 | -1.03992 |
| H | 13.04172 | -3.05519 | 0.74094 |
| C | 15.73006 | -3.04514 | 0.55735 |
| N | 16.42462 | -3.94914 | 0.78202 |
| C | 16.78727 | -0.53664 | -0.28291 |
| N | 17.93284 | -0.39415 | -0.41322 |

Table S9: Cartesian coordinates of HPPC8

| Atom | X-axis | Y-axis | Z-axis |
| --- | --- | --- | --- |
| C | 3.73172 | -2.29742 | 0.48497 |
| C | 2.43868 | -2.78185 | 0.55108 |
| C | 1.34837 | -1.92833 | 0.35749 |
| C | 1.58401 | -0.55915 | 0.05974 |
| C | 2.91988 | -0.06631 | -0.02532 |
| C | 3.99797 | -0.94809 | 0.22547 |
| C | 0.00137 | -2.39847 | 0.43149 |
| C | 0.4761 | 0.31331 | -0.15515 |
| C | -0.85982 | -0.16825 | -0.02469 |
| C | -1.05119 | -1.56209 | 0.25176 |
| C | -1.93965 | 0.7248 | -0.21206 |
| C | -1.67345 | 2.04815 | -0.57862 |
| C | -0.38004 | 2.51525 | -0.72551 |
| C | 0.71046 | 1.66969 | -0.50474 |
| C | 2.05704 | 2.12434 | -0.6423 |
| C | 3.1102 | 1.30041 | -0.41566 |
| H | 2.2228 | 3.15638 | -0.94725 |
| H | -0.16301 | -3.45664 | 0.62853 |
| H | 4.56872 | -2.96555 | 0.67825 |
| H | 2.25612 | -3.832 | 0.77209 |
| H | -2.06568 | -1.94918 | 0.2961 |
| H | -2.51284 | 2.72707 | -0.71566 |
| H | -0.19785 | 3.55347 | -0.99772 |
| C | 5.40346 | -0.50275 | 0.25159 |
| C | 6.39195 | -1.23656 | -0.42172 |
| C | 5.80444 | 0.62275 | 0.9877 |
| C | 7.7249 | -0.87173 | -0.38288 |
| H | 6.09306 | -2.10101 | -1.01127 |
| C | 7.13234 | 0.99449 | 1.03129 |
| C | 8.12898 | 0.25919 | 0.35299 |
| H | 8.47101 | -1.44751 | -0.91926 |
| H | 7.42469 | 1.87448 | 1.6034 |
| C | 9.46541 | 0.78449 | 0.47635 |
| C | -3.34978 | 0.32744 | -0.01803 |
| C | -4.3087 | 0.62544 | -0.9925 |
| C | -3.78723 | -0.28346 | 1.16444 |
| C | -5.64554 | 0.31389 | -0.80289 |
| H | -3.98943 | 1.08823 | -1.92469 |
| C | -5.12478 | -0.5823 | 1.36272 |
| H | -3.06834 | -0.48576 | 1.95621 |
| C | -6.08231 | -0.2962 | 0.37958 |
| H | -6.3624 | 0.52651 | -1.59438 |
| H | -5.44468 | -1.01226 | 2.30949 |
| C | -7.48596 | -0.62354 | 0.60401 |
| C | -8.01749 | -1.58398 | 1.42854 |
| S | -8.76098 | 0.25982 | -0.19448 |
| C | -9.42994 | -1.62435 | 1.41448 |
| H | -7.40106 | -2.27069 | 2.00162 |
| C | -9.99784 | -0.69552 | 0.57891 |
| H | -10.0199 | -2.34498 | 1.97364 |
| C | -18.2705 | 0.66312 | -0.816 |
| C | -17.3491 | 0.95884 | -1.81299 |
| C | -15.9822 | 0.74615 | -1.60856 |
| C | -15.545 | 0.21969 | -0.3632 |
| C | -16.4929 | -0.08105 | 0.65255 |
| C | -17.8494 | 0.14914 | 0.40428 |
| C | -15.0013 | 1.04055 | -2.6117 |
| C | -14.162 | -0.00515 | -0.13322 |
| C | -13.2102 | 0.30075 | -1.14298 |
| C | -13.6798 | 0.82881 | -2.39069 |
| C | -11.8563 | 0.07003 | -0.89643 |
| H | -11.1354 | 0.28066 | -1.68652 |
| C | -11.4151 | -0.45109 | 0.32396 |
| C | -12.3576 | -0.7427 | 1.31644 |
| C | -13.7209 | -0.53476 | 1.10938 |
| C | -14.699 | -0.82512 | 2.11759 |
| C | -16.0199 | -0.60896 | 1.89864 |
| H | -16.7528 | -0.83324 | 2.67212 |
| H | -14.3525 | -1.22565 | 3.06896 |
| H | -15.3456 | 1.44213 | -3.56355 |
| H | -19.3295 | 0.83592 | -0.99192 |
| H | -17.6838 | 1.36189 | -2.76757 |
| H | -18.575 | -0.08007 | 1.18312 |
| H | -12.945 | 1.05661 | -3.1612 |
| H | -12.0205 | -1.11532 | 2.28288 |
| C | 13.08796 | 0.35519 | -0.00651 |
| C | 12.61307 | -0.86454 | -0.55615 |
| C | 13.44493 | -1.8596 | -0.98187 |
| C | 15.33946 | -0.45572 | -0.3139 |
| C | 14.44475 | 0.55686 | 0.1125 |
| C | 11.92765 | 1.19363 | 0.33444 |
| C | 10.71389 | 0.4064 | 0.06613 |
| C | 11.14077 | -0.86862 | -0.57573 |
| H | 13.02929 | -2.77626 | -1.39804 |
| H | 14.8666 | 1.46617 | 0.53014 |
| O | 10.45603 | -1.77348 | -1.02041 |
| C | 12.00763 | 2.49925 | 0.76657 |
| C | 10.88432 | 3.34583 | 1.00731 |
| N | 9.98818 | 4.06135 | 1.21196 |
| C | 13.25167 | 3.15951 | 0.99261 |
| N | 14.25234 | 3.72149 | 1.18885 |
| C | 14.84362 | -1.67882 | -0.868 |
| C | 15.76506 | -2.66839 | -1.28196 |
| C | 16.73928 | -0.2777 | -0.1988 |
| C | 17.11575 | -2.46323 | -1.15557 |
| H | 15.37944 | -3.59571 | -1.70154 |
| C | 17.60665 | -1.25705 | -0.61 |
| H | 17.11141 | 0.65469 | 0.22153 |
| H | 17.81524 | -3.23059 | -1.47733 |
| H | 18.67925 | -1.10761 | -0.51694 |
| H | 4.12142 | 1.67158 | -0.55503 |
| H | 5.06261 | 1.19227 | 1.54277 |
| H | 9.45414 | 1.70519 | 1.05426 |

Table S10: Calculated energies (E) and energy gap (∆E) for HPPCR, HPPC1, HPPC2, HPPC3, HPPC4, HPPC5, HPPC6, HPPC7 and HPPC8

| Compounds | LUMO+1 E (eV) | HOMO-1 E (eV) | ∆E | LUMO+2 E (eV) | HOMO-2 E (eV) | ∆E |
| --- | --- | --- | --- | --- | --- | --- |
| HPPCR | -2.323 | -6.767 | 4.333 | -1.628 | -6.957 | 5.329 |
| HPPC1 | -1.763 | -5.818 | 4.055 | -1.585 | -5.976 | 4.391 |
| HPPC2 | -2.457 | -5.817 | 3.36 | -1.815 | -5.958 | 4.143 |
| HPPC3 | -2.465 | -5.815 | 3.35 | -1.807 | -5.935 | 4.128 |
| HPPC4 | -2.519 | -5.817 | 3.298 | -1.828 | -5.941 | 4.113 |
| HPPC5 | -2.676 | -5.819 | 3.141 | -1.853 | -5.965 | 4.112 |
| HPPC6 | -2.753 | -5.821 | 3.068 | -1.867 | -5.965 | 4.098 |
| HPPC7 | -3.146 | -5.824 | 2.678 | -1.927 | -5.990 | 4.063 |
| HPPC8 | -2.343 | -5.818 | 3.475 | -1.849 | -5.959 | 4.11 |

E= energy, ∆E(eV)= ELUMO-EHOMO; HOMO= highest occupied molecular orbital; LUMO= lowest unoccupied molecular orbital, MO, molecular orbital

Table S11: Natural bond orbital (NBO) analysis of investigated compound HPPCR by using M06/6-31G(d,p)

| Donor(i) | Type | Acceptor(j) | Type | E(2)a [kcal/mol] | E(J)E(i)b(a.u) | F(I,j)e(a.u) |
| --- | --- | --- | --- | --- | --- | --- |
| C1-C6 | π | C2-C3 | π* | 21.25 | 0.30 | 0.072 |
| C1-C6 | π | C4-C5 | π* | 19.95 | 0.29 | 0.070 |
| C2-C3 | π | C1-C6 | π* | 23.41 | 0.29 | 0.074 |
| C2-C3 | π | C4-C5 | π* | 19.84 | 0.29 | 0.069 |
| C2-C3 | π | C7-C10 | π* | 17.49 | 0.30 | 0.069 |
| C4-C5 | π | C1-C6 | π* | 20.53 | 0.28 | 0.070 |
| C4-C5 | π | C2-C3 | π* | 20.20 | 0.29 | 0.069 |
| C4-C5 | π | C8-C9 | π* | 22.24 | 0.28 | 0.071 |
| C4-C5 | π | C15-C16 | π* | 14.55 | 0.30 | 0.063 |
| C7-C10 | π | C2-C3 | π* | 16.71 | 0.31 | 0.068 |
| C17-C10 | π | C8-C9 | π* | 14.46 | 0.31 | 0.064 |
| C18-C9 | π | C4-C5 | π* | 22.18 | 0.28 | 0.071 |
| C8-C9 | π | C7-C10 | π* | 14.65 | 0.30 | 0.064 |
| C8-C9 | π | C11-C12 | π* | 20.60 | 0.28 | 0.070 |
| C8-C9 | π | C13-C14 | π* | 20.09 | 0.29 | 0.069 |
| C11-C12 | π | C8-C9 | π* | 19.88 | 0.29 | 0.070 |
| C11-C12 | π | C13-C14 | π* | 21.48 | 0.30 | 0.072 |
| C12-H23 | σ | C9-C11 | σ* | 4.62 | 1.10 | 0.064 |
| C15-H18 | σ | C5-C16 | σ* | 4.82 | 1.06 | 0.064 |
| C12-C13 | σ | C11-C12 | σ* | 3.47 | 1.29 | 0.060 |
| C13-H24 | σ | C8-C14 | σ* | 4.75 | 1.10 | 0.065 |
| C15-H18 | σ | C9-C11 | σ* | 4.12 | 1.28 | 0.065 |
| C11-C12 | σ | C8-C14 | σ* | 4.30 | 1.09 | 0.061 |
| C16-H17 | σ | C14-C15 | σ* | 4.66 | 1.08 | 0.063 |
| C13-C14 | π | C8-C9 | π* | 19.96 | 0.29 | 0.069 |
| C13-C14 | π | C11-C12 | π* | 23.12 | 0.29 | 0.074 |
| C13-C14 | π | C15-C16 | π* | 17.62 | 0.30 | 0.069 |
| C15-C16 | π | C4-C5 | π* | 14.59 | 0.31 | 0.064 |
| C15-C16 | π | C13-C14 | π* | 16.60 | 0.31 | 0.067 |
| C25-C26 | π | C27-C30 | π* | 18.03 | 0.30 | 0.067 |
| C27-C30 | π | C25-C26 | π* | 22.76 | 0.30 | 0.074 |
| C27-C30 | π | C28-C32 | π* | 19.06 | 0.29 | 0.068 |
| O41 | LP(2) | C40-O42 | σ* | 34.96 | 0.67 | 0.138 |
| O78 | LP(2) | C77-O79 | σ* | 34.49 | 0.67 | 0.138 |
| O78 | LP(2) | C74-C77 | σ* | 21.33 | 0.71 | 0.112 |
| O41 | LP(2) | C37-C40 | σ* | 21.18 | 0.72 | 0.112 |
| N76 | LP(1) | C74-C75 | σ* | 12.79 | 1.06 | 0.104 |
| O79 | LP(1) | C77-O78 | σ* | 8.89 | 1.17 | 0.091 |
| O42 | LP(1) | C40-O41 | σ* | 8.27 | 1.18 | 0.089 |
| N39 | LP(1) | C37-C38 | σ* | 12.79 | 1.07 | 0.105 |
| O42 | LP(2) | C43-H45 | σ* | 4.79 | 0.76 | 0.056 |

Table S12: Natural bond orbital (NBO) analysis of investigated compound HPPC1 by using M06/6-31G(d,p)

| Donor(i) | Type | Acceptor(j) | Type | E(2)a [kcal/mol] | E(J)E(i)b(a.u) | F(I,j)e(a.u) |
| --- | --- | --- | --- | --- | --- | --- |
| C1-C6 | π | C2-C3 | π* | 21.09 | 0.30 | 0.071 |
| C1-C6 | π | C4-C5 | π* | 19.94 | 0.29 | 0.070 |
| C2-C3 | π | C4-C5 | π* | 19.70 | 0.29 | 0.068 |
| C2-C3 | π | C7-C10 | π* | 17.32 | 0.31 | 0.069 |
| C4-C5 | π | C1-C6 | π* | 20.47 | 0.28 | 0.070 |
| C4-C5 | π | C8-C9 | π* | 22.24 | 0.28 | 0.071 |
| C4-C5 | π | C15-C16 | π* | 14.51 | 0.30 | 0.063 |
| C7-C10 | π | C2-C3 | π* | 16.89 | 0.31 | 0.068 |
| C7-C10 | π | C8-C9 | π* | 14.25 | 0.31 | 0.063 |
| C8-C9 | π | C4-C5 | π* | 22.13 | 0.28 | 0.070 |
| C8-C9 | π | C7-C10 | π* | 14.86 | 0.30 | 0.064 |
| C8-C9 | π | C11-C12 | π* | 20.65 | 0.29 | 0.070 |
| C8-C9 | π | C13-C14 | π* | 19.97 | 0.29 | 0.069 |
| C11-C12 | π | C8-C9 | π* | 19.80 | 0.29 | 0.070 |
| C11-C12 | π | C13-C14 | π* | 22.05 | 0.30 | 0.073 |
| C94-C97 | σ | C83-C95 | σ* | 4.63 | 1.07 | 0.063 |
| C94-C97 | σ | C86-C93 | σ* | 4.15 | 1.09 | 0.060 |
| C92-H103 | σ | C86-C91 | σ* | 4.25 | 1.11 | 0.061 |
| C89-C91 | σ | C91-C92 | σ* | 4.13 | 1.29 | 0.065 |
| C88-H102 | σ | C81-C85 | σ* | 4.63 | 1.07 | 0.063 |
| C88-H102 | σ | C86-C87 | σ* | 4.14 | 1.10 | 0.060 |
| C87-C89 | σ | C86-C87 | σ* | 4.08 | 1.28 | 0.065 |
| C87-C89 | σ | C87-C88 | σ* | 3.30 | 1.25 | 0.057 |
| C13-C14 | π | C8-C9 | π* | 20.08 | 0.29 | 0.069 |
| C13-C14 | π | C11-C12 | π* | 22.63 | 0.29 | 0.073 |
| C13-C14 | π | C15-C16 | π* | 17.89 | 0.30 | 0.070 |
| C82-C83 | π | C79-C84 | π* | 20.28 | 0.28 | 0.070 |
| C82-C83 | π | C80-C81 | π* | 20.03 | 0.29 | 0.069 |
| C82-C83 | π | C86-C93 | π* | 20.41 | 0.28 | 0.068 |
| N39 | LP(1) | C37-C38 | σ* | 12.79 | 1.07 | 0.105 |
| O41 | LP(2) | C37-C40 | σ* | 21.13 | 0.72 | 0.112 |
| O41 | LP(2) | C38-N39 | π* | 1.01 | 0.39 | 0.018 |
| O41 | LP(2) | C40-O42 | σ* | 35.01 | 0.66 | 0.138 |
| O41 | LP(1) | C37-C40 | σ* | 2.54 | 1.16 | 0.049 |
| O41 | LP(1) | C40-O42 | σ* | 1.40 | 1.10 | 0.036 |
| O42 | LP(2) | C43-H45 | σ* | 4.54 | 0.76 | 0.055 |
| O42 | LP(2) | C43-H46 | σ* | 4.65 | 0.76 | 0.056 |
| S74 | LP(1) | C72-C73 | σ* | 2.15 | 1.26 | 0.047 |
| S74 | LP(1) | C75-C77 | σ* | 2.17 | 1.26 | 0.047 |
| S74 | LP(2) | C75-C77 | π* | 23.35 | 0.29 | 0.073 |
| O42 | LP(1) | C40-O41 | σ* | 8.24 | 1.18 | 0.089 |

Table S13: Natural bond orbital (NBO) analysis of investigated compound HPPC2 by using M06/6-31G(d,p)

| Donor(i) | Type | Acceptor(j) | Type | E(2)a [kcal/mol] | E(J)E(i)b(a.u) | F(I,j)e(a.u) |
| --- | --- | --- | --- | --- | --- | --- |
| C1-C97 | π | C2-C3 | π* | 21.10 | 0.30 | 0.071 |
| C1-C97 | π | C4-C5 | π* | 19.95 | 0.29 | 0.070 |
| C2-C3 | π | C1-C97 | π* | 23.74 | 0.29 | 0.075 |
| C2-C3 | π | C4-C5 | π* | 19.69 | 0.29 | 0.068 |
| C2-C3 | π | C6-C9 | π* | 17.27 | 0.31 | 0.069 |
| C4-C5 | π | C1-C97 | π* | 20.42 | 0.28 | 0.070 |
| C4-C5 | π | C2-C3 | π* | 20.31 | 0.29 | 0.069 |
| C4-C5 | π | C7-C8 | π* | 22.27 | 0.28 | 0.071 |
| C72-C81 | π | C72-C81 | π* | 1.91 | 0.32 | 0.022 |
| C7-C8 | π | C4-C5 | π* | 22.14 | 0.28 | 0.070 |
| C7-C8 | π | C6-C9 | π* | 14.86 | 0.30 | 0.064 |
| C7-C8 | π | C10-C11 | π* | 20.67 | 0.29 | 0.070 |
| C7-C8 | π | C12-C13 | π* | 19.94 | 0.29 | 0.069 |
| C12-C13 | π | C7-C8 | π* | 20.06 | 0.29 | 0.069 |
| C12-C13 | π | C10-C11 | π* | 22.54 | 0.29 | 0.073 |
| C12-C13 | π | C14-C15 | π* | 17.89 | 0.30 | 0.070 |
| C23-C73 | π | C72-C81 | π* | 24.08 | 0.30 | 0.076 |
| C23-C79 | σ | C90-C94 | σ* | 5.96 | 1.11 | 0.073 |
| C23-C94 | σ | C23-C73 | σ* | 4.26 | 1.33 | 0.067 |
| C82-N83 | σ | C81-C82 | σ* | 6.17 | 1.57 | 0.089 |
| C29-H33 | σ | C27-C31 | σ* | 4.17 | 1.10 | 0.061 |
| C35-H38 | σ | C34-S36 | σ* | 5.26 | 0.75 | 0.056 |
| C92-H96 | σ | C92-C94 | σ* | 0.80 | 1.09 | 0.026 |
| C56-H59 | σ | C48-C55 | σ* | 4.14 | 1.10 | 0.060 |
| C68-C75 | σ | C66-C67 | σ* | 5.25 | 1.10 | 0.068 |
| C24-C25 | π | C26-C29 | π* | 20.86 | 0.30 | 0.071 |
| C27-C31 | π | C24-C25 | π* | 22.77 | 0.30 | 0.073 |
| C27-C31 | π | C26-C29 | π* | 20.25 | 0.30 | 0.070 |
| C27-C31 | π | C34-C35 | π* | 14.05 | 0.29 | 0.057 |
| C23-C73 | π | C74-O86 | π* | 22.39 | 0.31 | 0.075 |
| S36 | LP(1) | C34-C35 | σ* | 2.15 | 1.26 | 0.047 |
| S36 | LP(1) | C37-C39 | σ* | 2.16 | 1.26 | 0.047 |
| S36 | LP(2) | C34-C35 | π* | 23.28 | 0.29 | 0.073 |
| N83 | LP(1) | C81-C82 | σ* | 13.47 | 1.06 | 0.107 |
| N85 | LP(1) | C81-C84 | σ* | 13.44 | 1.06 | 0.107 |
| O86 | LP(1) | C73-C74 | σ* | 3.50 | 1.17 | 0.058 |
| O86 | LP(1) | C90-H95 | σ* | 3.66 | 1.19 | 0.059 |
| O86 | LP(2) | C67-C74 | σ* | 21.28 | 0.76 | 0.115 |
| O86 | LP(2) | C73-C74 | σ* | 20.87 | 0.74 | 0.112 |
| O86 | LP(2) | C90-H95 | σ* | 4.89 | 0.76 | 0.056 |

Table S14: Natural bond orbital (NBO) analysis of investigated compound HPPC3 by using M06/6-31G(d,p)

| Donor(i) | Type | Acceptor(j) | Type | E(2)a [kcal/mol] | E(J)E(i)b(a.u) | F(I,j)e(a.u) |
| --- | --- | --- | --- | --- | --- | --- |
| C1-C6 | π | C2-C3 | π* | 21.16 | 0.30 | 0.072 |
| C1-C6 | π | C4-C5 | π* | 19.68 | 0.29 | 0.070 |
| C2-C3 | π | C1-C6 | π* | 23.08 | 0.29 | 0.074 |
| C2-C3 | π | C4-C5 | π* | 19.67 | 0.29 | 0.068 |
| C2-C3 | π | C7-C10 | π* | 17.39 | 0.31 | 0.069 |
| C4-C5 | π | C1-C6 | π* | 20.74 | 0.28 | 0.070 |
| C4-C5 | π | C2-C3 | π* | 20.19 | 0.29 | 0.069 |
| C4-C5 | π | C8-C9 | π* | 22.23 | 0.28 | 0.071 |
| C4-C5 | π | C15-C16 | π* | 14.41 | 0.30 | 0.063 |
| C13-C14 | π | C8-C9 | π* | 19.99 | 0.29 | 0.069 |
| C8-C9 | π | C4-C5 | π* | 22.16 | 0.28 | 0.071 |
| C8-C9 | π | C7-C10 | π* | 14.81 | 0.30 | 0.064 |
| C8-C9 | π | C11-C12 | π* | 20.66 | 0.29 | 0.070 |
| C8-C9 | π | C13-C14 | π* | 19.96 | 0.29 | 0.069 |
| C24-C25 | π | C26-C29 | π* | 18.74 | 0.30 | 0.068 |
| C1-C19 | σ | C5-C6 | σ* | 4.70 | 1.10 | 0.064 |
| C2-H20 | σ | C3-C4 | σ* | 4.75 | 1.10 | 0.065 |
| C7-H18 | σ | C3-C4 | σ* | 4.26 | 1.09 | 0.061 |
| C91-N92 | σ | C88-C91 | σ* | 6.21 | 1.57 | 0.089 |
| C88-C91 | σ | C91-N92 | σ* | 5.43 | 1.59 | 0.083 |
| C84-C88 | σ | C91-N92 | σ* | 4.42 | 1.61 | 0.076 |
| C84-C88 | σ | C88-C91 | σ* | 4.23 | 1.29 | 0.066 |
| C2-H20 | σ | C1-C2 | σ* | 1.08 | 1.13 | 0.031 |
| C54-C55 | π | C51-C56 | π* | 20.29 | 0.28 | 0.070 |
| C54-C55 | π | C52-C53 | π* | 20.05 | 0.29 | 0.069 |
| C54-C55 | π | C58-C65 | π* | 20.40 | 0.28 | 0.068 |
| C79-C80 | π | C76-C81 | π* | 21.20 | 0.32 | 0.075 |
| C79-C80 | π | C77-C78 | π* | 21.41 | 0.32 | 0.074 |
| C77-C78 | π | C79-C80 | π* | 24.79 | 0.28 | 0.075 |
| N90 | LP(1) | C88-C89 | σ* | 13.28 | 1.06 | 0.106 |
| N92 | LP(1) | C88-C91 | σ* | 13.37 | 1.06 | 0.106 |
| O93 | LP(2) | C76-C82 | σ* | 22.17 | 0.75 | 0.117 |
| F96 | LP(2) | C78-C79 | σ* | 6.76 | 1.01 | 0.074 |
| F96 | LP(2) | C79-C80 | σ* | 8.27 | 0.97 | 0.080 |
| F96 | LP(3) | C79-C80 | π* | 21.62 | 0.44 | 0.095 |
| F97 | LP(2) | C79-C80 | σ* | 8.36 | 0.97 | 0.080 |
| F97 | LP(2) | C80-C81 | σ* | 6.89 | 1.01 | 0.075 |
| S46 | LP(1) | C44-C45 | σ* | 2.13 | 1.26 | 0.046 |
| S46 | LP(1) | C47-C49 | σ* | 2.15 | 1.26 | 0.046 |
| S46 | LP(2) | C44-C45 | π* | 23.25 | 0.29 | 0.073 |
| F97 | LP(3) | C79-C80 | π* | 21.66 | 0.44 | 0.095 |

Table S15: Natural bond orbital (NBO) analysis of investigated compound HPPC4 by using M06/6-31G(d,p)

| Donor(i) | Type | Acceptor(j) | Type | E(2)a [kcal/mol] | E(J)E(i)b(a.u) | F(I,j)e(a.u) |
| --- | --- | --- | --- | --- | --- | --- |
| C1-C6 | π | C2-C3 | π* | 21.15 | 0.30 | 0.071 |
| C1-C6 | π | C4-C5 | π* | 19.73 | 0.29 | 0.070 |
| C2-C3 | π | C1-C6 | π* | 23.34 | 0.29 | 0.074 |
| C2-C3 | π | C4-C5 | π* | 19.69 | 0.29 | 0.068 |
| C2-C3 | π | C7-C10 | π* | 17.37 | 0.31 | 0.069 |
| C4-C5 | π | C1-C6 | π* | 20.61 | 0.28 | 0.070 |
| C4-C5 | π | C8-C9 | π* | 22.23 | 0.28 | 0.071 |
| C4-C5 | π | C15-C16 | π* | 14.45 | 0.30 | 0.063 |
| C13-C14 | π | C8-C9 | π* | 20.05 | 0.29 | 0.069 |
| C13-C14 | π | C11-C12 | π* | 22.65 | 0.29 | 0.073 |
| C33-C83 | π | C33-C83 | π* | 1.44 | 0.33 | 0.020 |
| C8-C9 | π | C11-C12 | π* | 20.64 | 0.29 | 0.070 |
| C8-C9 | π | C13-C14 | π* | 19.95 | 0.29 | 0.069 |
| C29-C30 | π | C24-C26 | π* | 20.19 | 0.30 | 0.070 |
| C29-C30 | π | C25-C27 | π* | 20.58 | 0.30 | 0.072 |
| C35-H38 | σ | C34-C36 | σ* | 4.21 | 1.10 | 0.061 |
| C45-H48 | σ | C44-S46 | σ* | 5.22 | 0.75 | 0.056 |
| C8-C88 | σ | C88-N89 | σ* | 5.49 | 1.60 | 0.084 |
| C84-C87 | σ | C90-N91 | σ* | 4.38 | 1.61 | 0.076 |
| C63-C64 | σ | C64-C65 | σ* | 3.26 | 1.30 | 0.058 |
| C64-H75 | σ | C58-C65 | σ* | 4.74 | 1.10 | 0.065 |
| C64-H75 | σ | C61-C63 | σ* | 4.19 | 1.11 | 0.061 |
| C63-C64 | σ | C61-C63 | σ* | 4.08 | 1.29 | 0.065 |
| C54-C55 | π | C51-C56 | π* | 20.29 | 0.28 | 0.070 |
| C54-C55 | π | C52-C53 | π* | 20.05 | 0.29 | 0.069 |
| C54-C55 | π | C58-C65 | π* | 20.41 | 0.28 | 0.068 |
| C79-C80 | π | C76-C81 | π* | 23.69 | 0.32 | 0.078 |
| C79-C80 | π | C77-C78 | π* | 19.00 | 0.32 | 0.070 |
| C77-C78 | π | C79-C80 | π* | 25.85 | 0.28 | 0.077 |
| N89 | LP(1) | C87-C88 | σ* | 13.36 | 1.06 | 0.106 |
| N91 | LP(1) | C87-C90 | σ* | 13.40 | 1.06 | 0.107 |
| O92 | LP(2) | C82-C83 | σ* | 22.98 | 0.71 | 0.116 |
| F95 | LP(2) | C78-C79 | σ* | 6.75 | 1.01 | 0.074 |
| F95 | LP(3) | C79-C80 | π* | 22.73 | 0.44 | 0.097 |
| F96 | LP(2) | C79-C80 | σ* | 8.07 | 0.98 | 0.079 |
| F96 | LP(2) | C80-C81 | σ* | 8.05 | 0.98 | 0.079 |
| F97 | LP(2) | C80-C81 | σ* | 8.37 | 0.98 | 0.081 |
| F97 | LP(3) | C76-C81 | π* | 23.22 | 0.46 | 0.100 |
| S46 | LP(2) | C44-C45 | π* | 23.27 | 0.29 | 0.073 |
| S46 | LP(2) | C47-C49 | π* | 23.31 | 0.29 | 0.073 |
| F96 | LP(3) | C79-C80 | π* | 21.09 | 0.44 | 0.094 |

Table S16: Natural bond orbital (NBO) analysis of investigated compound HPPC5 by using M06/6-31G(d,p)

| Donor(i) | Type | Acceptor(j) | Type | E(2)a [kcal/mol] | E(J)E(i)b(a.u) | F(I,j)e(a.u) |
| --- | --- | --- | --- | --- | --- | --- |
| C1-C88 | π | C2-C3 | π* | 21.01 | 0.30 | 0.071 |
| C1-C88 | π | C4-C5 | π* | 19.93 | 0.29 | 0.070 |
| C2-C3 | π | C1-C6 | π* | 23.34 | 0.29 | 0.074 |
| C2-C3 | π | C4-C5 | π* | 19.69 | 0.29 | 0.068 |
| C2-C3 | π | C7-C10 | π* | 17.37 | 0.31 | 0.069 |
| C72-C95 | π | C72-C95 | π* | 1.97 | 0.32 | 0.023 |
| C4-C5 | π | C2-C3 | π* | 20.25 | 0.29 | 0.069 |
| C4-C5 | π | C7-C8 | π* | 22.23 | 0.28 | 0.071 |
| C4-C5 | π | C14-C15 | π* | 14.45 | 0.30 | 0.063 |
| C12-C13 | π | C10-C11 | π* | 22.49 | 0.29 | 0.073 |
| C12-C13 | π | C7-C8 | π* | 20.10 | 0.29 | 0.069 |
| C12-C13 | π | C10-C11 | π* | 22.49 | 0.29 | 0.073 |
| C23-C24 | π | C25-C28 | π* | 20.85 | 0.30 | 0.071 |
| C23-C24 | π | C26-C30 | π* | 22.74 | 0.29 | 0.073 |
| C26-C30 | π | C23-C24 | π* | 22.78 | 0.30 | 0.073 |
| C26-C30 | π | C25-C28 | π* | 20.25 | 0.30 | 0.070 |
| C36-H39 | σ | C35-C38 | σ* | 5.26 | 0.75 | 0.056 |
| C38-C52 | σ | C36-C38 | σ* | 4.37 | 1.29 | 0.067 |
| C45-H62 | σ | C43-C44 | σ* | 4.75 | 1.10 | 0.065 |
| C46-H49 | σ | C42-C43 | σ* | 4.17 | 1.10 | 0.060 |
| C46-C59 | σ | C48-C49 | σ* | 4.66 | 1.07 | 0.063 |
| C48-C50 | σ | C47-C48 | σ* | 4.09 | 1.28 | 0.065 |
| C49-H63 | σ | C42-C46 | σ* | 4.62 | 1.07 | 0.063 |
| C49-H63 | σ | C47-C48 | σ* | 4.14 | 1.16 | 0.037 |
| C52-C53 | π | C47-C54 | π* | 21.31 | 0.30 | 0.073 |
| C52-C53 | π | C48-C50 | π* | 19.94 | 0.30 | 0.069 |
| C65-C70 | π | C66-C67 | π* | 20.86 | 0.31 | 0.073 |
| C65-C70 | π | C68-C69 | π* | 24.13 | 0.26 | 0.071 |
| C66-C67 | π | C68-C69 | π* | 24.03 | 0.25 | 0.071 |
| O90 | LP(1) | C66-C73 | σ* | 21.88 | 0.75 | 0.116 |
| O90 | LP(1) | C72-C73 | σ* | 21.04 | 0.74 | 0.113 |
| O90 | LP(2) | C81-H86 | σ* | 4.40 | 0.76 | 0.053 |
| O92 | LP(2) | C82-C83 | σ* | 22.98 | 0.71 | 0.116 |
| N92 | LP(1) | C89-C91 | σ* | 13.51 | 1.06 | 0.107 |
| N94 | LP(1) | C89-C93 | σ* | 13.46 | 1.06 | 0.107 |
| S35 | LP(1) | C33-C34 | σ* | 2.16 | 1.26 | 0.047 |
| Cl77 | LP(3) | C68-C69 | π* | 16.11 | 0.31 | 0.070 |
| Cl77 | LP(2) | C67-C68 | σ* | 4.00 | 0.89 | 0.053 |
| Cl76 | LP(3) | C68-C69 | π* | 15.85 | 0.31 | 0.070 |
| S35 | LP(2) | C36-C38 | π* | 23.27 | 0.29 | 0.073 |
| Cl76 | LP(2) | C79-C80 | σ* | 5.28 | 0.86 | 0.060 |

Table S17: Natural bond orbital (NBO) analysis of investigated compound HPPC6 by using M06/6-31G(d,p)

| Donor(i) | Type | Acceptor(j) | Type | E(2)a [kcal/mol] | E(J)E(i)b(a.u) | F(I,j)e(a.u) |
| --- | --- | --- | --- | --- | --- | --- |
| C1-C88 | π | C2-C3 | π* | 20.99 | 0.30 | 0.071 |
| C1-C88 | π | C4-C5 | π* | 19.93 | 0.29 | 0.070 |
| C2-C3 | π | C1-C88 | π* | 23.95 | 0.29 | 0.075 |
| C2-C3 | π | C4-C5 | π* | 19.65 | 0.29 | 0.068 |
| C2-C3 | π | C6-C9 | π* | 17.22 | 0.31 | 0.069 |
| C4-C5 | π | C2-C3 | π* | 20.38 | 0.29 | 0.069 |
| C4-C5 | π | C7-C8 | π* | 22.22 | 0.28 | 0.071 |
| C4-C5 | π | C14-C15 | π* | 14.47 | 0.30 | 0.063 |
| C12-C13 | π | C7-C8 | π* | 20.15 | 0.29 | 0.069 |
| C12-C13 | π | C10-C11 | π* | 22.51 | 0.29 | 0.073 |
| C12-C13 | π | C14-C15 | π* | 18.00 | 0.30 | 0.070 |
| C14-C15 | π | C12-C13 | π* | 16.39 | 0.31 | 0.067 |
| C23-C24 | π | C25-C28 | π* | 20.93 | 0.29 | 0.071 |
| C23-C24 | π | C26-C30 | π* | 22.78 | 0.29 | 0.073 |
| C26-C30 | π | C23-C24 | π* | 22.81 | 0.30 | 0.073 |
| C26-C30 | π | C25-C28 | π* | 20.30 | 0.30 | 0.070 |
| C34-H37 | σ | C33-S35 | σ* | 5.26 | 0.75 | 0.056 |
| C36-H39 | σ | S35-C38 | σ* | 5.27 | 0.75 | 0.056 |
| C41-H61 | σ | C42-C43 | σ* | 4.75 | 1.09 | 0.065 |
| C46-H49 | σ | C42-C43 | σ* | 4.17 | 1.10 | 0.060 |
| C46-C59 | σ | C48-C49 | σ* | 4.66 | 1.07 | 0.063 |
| C48-C50 | σ | C47-C48 | σ* | 4.11 | 1.28 | 0.065 |
| C49-H63 | σ | C42-C46 | σ* | 4.62 | 1.07 | 0.063 |
| C49-H63 | σ | C47-C48 | σ* | 4.14 | 1.16 | 0.037 |
| C52-C53 | π | C47-C54 | π* | 21.32 | 0.30 | 0.073 |
| C52-C53 | π | C48-C50 | π* | 19.92 | 0.30 | 0.069 |
| C65-C70 | π | C66-C67 | π* | 23.22 | 0.31 | 0.073 |
| C65-C70 | π | C68-C69 | π* | 25.05 | 0.26 | 0.071 |
| C66-C67 | π | C68-C69 | π* | 21.14 | 0.27 | 0.069 |
| O90 | LP(2) | C72-C73 | σ* | 20.47 | 0.74 | 0.111 |
| O90 | LP(2) | C81-H86 | σ* | 4.47 | 0.77 | 0.054 |
| Cl96 | LP(3) | C66-C67 | π* | 15.95 | 0.34 | 0.071 |
| N92 | LP(1) | C89-C91 | σ* | 13.54 | 1.06 | 0.107 |
| N94 | LP(1) | C89-C93 | σ* | 13.53 | 1.06 | 0.107 |
| S35 | LP(1) | C33-C34 | σ* | 2.16 | 1.26 | 0.047 |
| Cl77 | LP(3) | C68-C69 | π* | 16.66 | 0.31 | 0.071 |
| Cl77 | LP(1) | C68-C69 | σ* | 1.48 | 1.47 | 0.042 |
| Cl76 | LP(3) | C68-C69 | π* | 16.38 | 0.31 | 0.070 |
| S35 | LP(2) | C33-C34 | π* | 23.24 | 0.29 | 0.073 |
| S35 | LP(2) | C36-C38 | π* | 23.24 | 0.29 | 0.073 |
| Cl76 | LP(2) | C79-C80 | σ* | 5.28 | 0.86 | 0.060 |

Table S18: Natural bond orbital (NBO) analysis of investigated compound HPPC7 by using M06/6-31G(d,p)

| Donor(i) | Type | Acceptor(j) | Type | E(2)a [kcal/mol] | E(J)E(i)b(a.u) | F(I,j)e(a.u) |
| --- | --- | --- | --- | --- | --- | --- |
| C1-C2 | π | C3-C4 | π* | 20.22 | 0.30 | 0.072 |
| C3-C4 | π | C1-C2 | π* | 19.08 | 0.29 | 0.069 |
| C3-C4 | π | C5-C6 | π* | 21.02 | 0.28 | 0.070 |
| C3-C4 | π | C7-C10 | π* | 14.24 | 0.30 | 0.063 |
| C3-C4 | π | C8-C9 | π* | 20.52 | 0.28 | 0.068 |
| C5-C6 | π | C1-C2 | π* | 20.89 | 0.29 | 0.072 |
| C5-C6 | π | C3-C4 | π* | 18.82 | 0.29 | 0.067 |
| C5-C6 | π | C15-C16 | π* | 15.81 | 0.31 | 0.066 |
| C13-C14 | π | C7-C8 | π* | 20.15 | 0.29 | 0.069 |
| C12-C13 | π | C10-C11 | π* | 22.51 | 0.29 | 0.073 |
| C12-C13 | π | C14-C15 | π* | 18.00 | 0.30 | 0.070 |
| C25-C27 | π | C12-C13 | π* | 16.08 | 0.30 | 0.065 |
| C84-C90 | π | C84-C90 | π* | 1.50 | 0.32 | 0.020 |
| C26-C28 | π | C30-C32 | π* | 18.16 | 0.29 | 0.066 |
| C30-C32 | π | C35-C85 | π* | 28.11 | 0.28 | 0.084 |
| C35-C85 | π | C84-C90 | π* | 25.26 | 0.30 | 0.077 |
| C35-C85 | π | C86-O89 | π* | 23.98 | 0.30 | 0.078 |
| C35-H88 | σ | C28-C32 | σ* | 6.00 | 1.11 | 0.073 |
| C37-H40 | σ | C36-C38 | σ* | 4.23 | 1.10 | 0.061 |
| C38-H42 | σ | C36-C37 | σ* | 4.16 | 1.11 | 0.061 |
| C38-H42 | σ | C41-C43 | σ* | 4.08 | 1.10 | 0.032 |
| C41-H45 | σ | C36-C38 | σ* | 4.08 | 1.10 | 0.060 |
| C41-H45 | σ | C39-C43 | σ* | 4.16 | 1.10 | 0.061 |
| C53-C58 | π | C54-C55 | π* | 20.94 | 0.30 | 0.071 |
| C53-C58 | π | C56-C57 | π* | 20.36 | 0.30 | 0.072 |
| C54-C55 | π | C53-C58 | π* | 22.00 | 0.29 | 0.073 |
| C54-C55 | π | C56-C57 | π* | 19.54 | 0.29 | 0.069 |
| C56-C57 | π | C53-C58 | π* | 20.27 | 0.28 | 0.070 |
| C56-C57 | π | C54-C55 | π* | 20.04 | 0.29 | 0.069 |
| O89 | LP(1) | C28-H33 | σ* | 3.22 | 1.20 | 0.055 |
| O89 | LP(2) | C28-H33 | σ* | 4.44 | 0.77 | 0.053 |
| O89 | LP(2) | C79-C86 | σ* | 22.36 | 0.74 | 0.117 |
| O89 | LP(2) | C85-C86 | σ* | 20.74 | 0.74 | 0.112 |
| N92 | LP(1) | C90-C91 | σ* | 13.56 | 1.06 | 0.107 |
| N94 | LP(1) | C90-C93 | σ* | 13.53 | 1.06 | 0.107 |
| N97 | LP(1) | C81-C96 | σ* | 13.20 | 1.06 | 0.106 |
| N99 | LP(1) | C82-C98 | σ* | 13.22 | 1.06 | 0.106 |
| S48 | LP(2) | C49-C51 | π* | 23.34 | 0.29 | 0.073 |
| Cl76 | LP(2) | C79-C80 | σ* | 5.28 | 0.86 | 0.060 |

Table S19: Natural bond orbital (NBO) analysis of investigated compound HPPC8 by using M06/6-31G(d,p)

| Donor(i) | Type | Acceptor(j) | Type | E(2)a [kcal/mol] | E(J)E(i)b(a.u) | F(I,j)e(a.u) |
| --- | --- | --- | --- | --- | --- | --- |
| C1-C6 | π | C2-C3 | π* | 21.08 | 0.30 | 0.071 |
| C1-C6 | π | C4-C5 | π* | 19.91 | 0.29 | 0.070 |
| C2-C3 | π | C1-C6 | π* | 23.77 | 0.29 | 0.075 |
| C2-C3 | π | C7-C10 | π* | 17.25 | 0.31 | 0.069 |
| C4-C5 | π | C1-C6 | π* | 20.33 | 0.28 | 0.069 |
| C4-C5 | π | C2-C3 | π* | 20.33 | 0.29 | 0.069 |
| C4-C5 | π | C8-C9 | π* | 22.26 | 0.28 | 0.071 |
| C4-C5 | π | C15-C16 | π* | 14.50 | 0.30 | 0.063 |
| C12-C13 | π | C8-C9 | π* | 20.08 | 0.29 | 0.069 |
| C12-C13 | π | C11-C12 | π* | 22.53 | 0.29 | 0.073 |
| C12-C13 | π | C15-C16 | π* | 17.91 | 0.30 | 0.070 |
| C29-C30 | π | C25-C27 | π* | 20.35 | 0.30 | 0.073 |
| C29-C30 | π | C33-C82 | π* | 25.67 | 0.29 | 0.081 |
| C37-C41 | π | C34-C35 | π* | 22.76 | 0.30 | 0.073 |
| C37-C41 | π | C36-C39 | π* | 20.22 | 0.30 | 0.070 |
| C37-H42 | σ | C34-C35 | σ* | 4.02 | 1.11 | 0.060 |
| C37-H42 | σ | C39-C41 | σ* | 4.24 | 1.10 | 0.061 |
| C44-C45 | σ | C41-C44 | σ* | 4.84 | 1.24 | 0.069 |
| C45-H48 | σ | C44-S46 | σ* | 5.26 | 0.75 | 0.056 |
| C49-C63 | σ | C47-C49 | σ* | 4.38 | 1.29 | 0.067 |
| C51-H71 | σ | C52-C53 | σ* | 4.00 | 1.11 | 0.060 |
| C52-H72 | σ | C53-C54 | σ* | 4.74 | 1.10 | 0.065 |
| C54-C55 | π | C51-C56 | π* | 20.27 | 0.28 | 0.070 |
| C54-C55 | π | C52-C53 | π* | 20.05 | 0.29 | 0.069 |
| C54-C55 | π | C58-C65 | π* | 20.39 | 0.28 | 0.068 |
| C59-C61 | π | C63-C64 | π* | 23.18 | 0.29 | 0.074 |
| C63-C64 | π | C58-C65 | π* | 21.28 | 0.30 | 0.073 |
| C77-C78 | π | C76-C80 | π* | 18.21 | 0.31 | 0.067 |
| C81-C87 | π | C88-N89 | π* | 22.97 | 0.40 | 0.088 |
| C52-C53 | π | C51-C56 | π* | 22.01 | 0.29 | 0.073 |
| C52-C53 | π | C54-C55 | π* | 19.57 | 0.29 | 0.069 |
| C52-C53 | π | C57-C60 | π* | 17.30 | 0.30 | 0.068 |
| O86 | LP(1) | C27-H31 | σ* | 3.35 | 1.19 | 0.056 |
| O86 | LP(2) | C27-H31 | σ* | 4.61 | 0.76 | 0.054 |
| O86 | LP(2) | C77-C83 | σ* | 21.20 | 0.76 | 0.115 |
| O86 | LP(2) | C82-C83 | σ* | 21.12 | 0.73 | 0.112 |
| N89 | LP(1) | C87-C88 | σ* | 13.47 | 1.06 | 0.107 |
| S46 | LP(1) | C47-C49 | σ* | 2.16 | 1.26 | 0.047 |
| S46 | LP(1) | C44-C45 | σ* | 2.15 | 1.26 | 0.046 |
| S46 | LP(2) | C44-C45 | π* | 23.24 | 0.29 | 0.073 |
| N91 | LP(1) | C79-C80 | σ* | 13.39 | 1.06 | 0.107 |

aE(2) means energy of hyper conjugative interaction (stabilization energy in kcal/mol).

bEnergy difference between donor and acceptor i and j NBO orbitals

cF(i;j) is the Fock matrix element between i and j NBO orbitals.

Table S20. Dipole polarizabilities and major contributing tensors (a.u.) of the studied compounds (HPPCR) and (HPPC1- HPPC8)

| Compounds | µx | µy | µz | αxx | αyy | αzz |
| --- | --- | --- | --- | --- | --- | --- |
| HPPCR | 2.2076 | 3.5277 | -0.9766 | 1416.7 | 544.65 | 600.93 |
| HPPC1 | 1.234 | -2.839 | 1.711 | 1937.920 | 900.582 | 429.488 |
| HPPC2 | 1.331 | -2.137 | 0.939 | 2292.460 | 920.050 | 479.458 |
| HPPC3 | 0.234 | -1.875 | 0.500 | 2047.390 | 830.836 | 604.856 |
| HPPC4 | 0.941 | 1.667 | -0.598 | 2106.630 | 798.245 | 628.696 |
| HPPC5 | 2.651 | -1.977 | -0.088 | 2441.300 | 1017.400 | 429.332 |
| HPPC6 | 2.657 | -0.961 | -0.820 | 2420.710 | 820.881 | 728.077 |
| HPPC7 | -5.598 | -0.870 | -0.059 | 2518.530 | 1075.490 | 399.554 |
| HPPC8 | -0.636 | -2.749 | -0.341 | 2550.480 | 879.611 | 602.076 |

Table S21: The computed second-order polarizabilities (βtot) and major contributing tensors (a.u) of (HPPCR) and (HPPC1- HPPC8)

| Compounds | βxxx |  | βxxy |  | βXYY |  | βyyy |  | βxxz |  | βyyz |  | βxzz |  | βyzz |  | βzzz |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HPPCR |  | -8782.8 |  | 772.6 |  | 377.0 |  | -34.9 |  | -162.9 |  | 25.1 |  | -70.2 |  | -99.1 |  | -25.0 |
| HPPC1 |  | 37308.3 |  | -4843.2 |  | 214.1 |  | 187.1 |  | 1618.2 |  | -29.9 |  | 16.5 |  | 12.6 |  | -45.3 |
| HPPC2 |  | 97870.9 |  | -11133.9 |  | 436.4 |  | 335.5 |  | 1418.2 |  | -179.7 |  | -582.0 |  | 72.3 |  | 24.6 |
| HPPC3 |  | 36257.3 |  | -6710.4 |  | 1655.8 |  | -1155.1 |  | 2115.7 |  | -184.5 |  | -339.2 |  | 160.3 |  | 93.9 |
| HPPC4 |  | 53479.0 |  | 8767.2 |  | 1980.4 |  | 1095.5 |  | -1859.1 |  | 461.2 |  | -356.1 |  | 30.3 |  | -80.3 |
| HPPC5 |  | 125866.0 |  | -17680.9 |  | 335.1 |  | -295.4 |  | 2887.4 |  | 157.1 |  | -250.3 |  | -45.8 |  | 25.8 |
| HPPC6 |  | 142639.0 |  | -6515.57 |  | -1470.0 |  | -590.1 |  | -8635.7 |  | 155.0 |  | 295.3 |  | -77.0 |  | -47.8 |
| HPPC7 |  | -196060.0 |  | -18715.6 |  | -2302.8 |  | 1250.4 |  | 11856.6 |  | -212.2 |  | -646.6 |  | 21.8 |  | 11.1 |
| HPPC8 |  | -119052.0 |  | -18355.4 |  | 78.0 |  | 115.5 |  | -4013.5 |  | -8.3 |  | 386.5 |  | 8.1 |  | 10.0 |

Table S22: The computed third-order polarizabilities <γ> and major contributing tensors (a.u) of (HPPCR) and (HPPC1- HPPC8)

| Compounds | γX | γY | γZ |
| --- | --- | --- | --- |
| HPPCR | 5.4780×106 | 4.3388×104 | 2.8403×104 |
| HPPC1 | 7.824x106 | 1.094x105 | 2.919x104 |
| HPPC2 | 1.9289 x107 | 2.1612 x105 | 4.8504 x104 |
| HPPC3 | 1.0149x107 | 2.8738x105 | 6.2586x104 |
| HPPC4 | 1.3278x107 | 2.8872x105 | 7.4497x104 |
| HPPC5 | 2.6116x107 | 4.0798x105 | 3.6029x104 |
| HPPC6 | 2.989 x107 | 3.156 x105 | 1.297 x105 |
| HPPC7 | 4.069 x107 | 4.704 x105 | 1.555 x105 |
| HPPC8 | 2.6065 x107 | 3.7703 x105 | 8.3753 x104 |

Table S23: Wave length, excitation energy and oscillator strength of reference compound (HPPCR)  and investigated compound (HPPC1-HPPC8)

| Compounds | λ (nm) | E (eV) | f | MO contributions |
| --- | --- | --- | --- | --- |
| HPPCR | 430.068 | 2.883 | 0.104 | H→L+1 (97%) |
|  | 358.844 | 3.455 | 0.354 | H-1→L (39%), H→L+2 (40%), H→L+3 (10%), H-1→L+2 (4%) |
|  | 345.244 | 3.591 | 0.141 | H-1→L (25%), H→L+2 (51%), H→L+3 (13%), H-3→L (2%), H-1→L+2 (4%) |
|  | 329.947 | 3.758 | 0.049 | H-2→L (53%), H-1→L+1 (30%), H-3→L+1 (3%), H-2→L+1 (3%), H-1→L (4%), H→L+3 (2%) |
|  | 319.465 | 3.881 | 1.008 | H-3→L (11%), H-2→L+1 (37%), H→L+3 (21%), H-3→L+1 (4%), H-1→L (9%), H-1→L+1 (3%), H-1→L+2 (6%), H-1→L+3 (2%), H→L+2 (2%) |
| HPPC1 | 354.524 | 3.497 | 0.004 | H-3→L (47%), H→L+3 (17%), H→L+4 (14%), H-4→L (3%), H-3→L+1 (6%), H-2→L+1 (3%), H-2→L+4 (3%) |
|  | 395.939 | 3.131 | 0.147 | H-2→L (33%), H-1→L (48%), H→L+1 (14%), |
|  | 393.776 | 3.149 | 0.294 | H-2→L (25%), H-1→L (49%), H→L+1 (22%), |
|  | 389.288 | 3.185 | 1.050 | H-2→L (33%), H→L+1 (52%), H-2→L+3 (3%), H→L (6%) |
|  | 369.506 | 3.355 | 0.001 | H-2→L+2 (25%), H-1→L+1 (16%), H-1→L+3 (22%), H→L+2 (26%), H-4→L+2 (3%), H-1→L+5 (3%) |
| HPPC2 | 475.728 | 2.606 | 0.098 | H-2→L(82%),H-1→L(10%),H→L(5%) |
|  | 481.922 | 2.573 | 0.016 | H-1→L(90%),H-2→L(8%) |
|  | 453.955 | 2.731 | 0.307 | H→L+1(88%),H-2→L(2%),H-2→L+1(5%) |
|  | 412.950 | 3.002 | 1.291 | H-4→L(20%),H-3→L(47%),H→L+2(19%),H-5→L(7%) |
|  | 393.426 | 3.151 | 0.732 | H-3→L(19%),H→L+2(66%),H-4→L(3%),H-2→L+4(4%),H→L+4(2%) |
| HPPC3 | 492.607 | 2.517 | 0.023 | H-2→L (42%), H-1→L (52%), H→L (5%) |
|  | 487.283 | 2.544 | 0.018 | H-2→L (48%), H-1→L (48%), H→L (2%) |
|  | 460.138 | 2.695 | 0.360 | H→L+1 (90%), H-2→L+1 (4%), H→L+2 (2%) |
|  | 425.638 | 2.913 | 0.434 | H-5→L (22%), H-4→L (30%), H-3→L (36%), H-2→L (2%), H→L+2 (6%) |
|  | 401.894 | 3.085 | 1.582 | H→L+2 (81%), H-3→L (5%), H-2→L+4 (4%) |
| HPPC4 | 506.513 | 2.448 | 0.024 | H-2→L (37%), H-1→L (57%), H→L (4%) |
|  | 500.987 | 2.475 | 0.023 | H-2→L (53%), H-1→L (43%), H→L (3%) |
|  | 469.690 | 2.640 | 0.414 | H→L+1 (90%), H-2→L+1 (5%), H→L+2 (2%) |
|  | 432.076 | 2.870 | 0.367 | H-5→L (19%), H-4→L (28%), H-3→L (42%), H-2→L (2%), H→L+2 (4%) |
|  | 403.555 | 3.072 | 1.578 | H→L+2 (82%), H-3→L (6%), H-2→L+4 (4%) |
| HPPC5 | 510.748 | 2.428 | 0.012 | H-1→L (93%), H-2→L (5%) |
|  | 502.815 | 2.466 | 0.121 | H-2→L (83%), H-1→L (6%), H→L (6%), H→L+1 (3%) |
|  | 488.184 | 2.540 | 0.196 | H→L+1 (88%), H-2→L (5%), H-2→L+1 (5%) |
|  | 425.375 | 2.915 | 1.017 | H-5→L (10%), H-4→L (22%), H-3→L (52%), H→L+2 (10%), |
|  | 414.954 | 2.988 | 0.003 | H-1→L+1 (94%), H-2→L+1 (5%) |
| HPPC6 | 526.763 | 2.354 | 0.010 | H-1→L (94%), H-2→L (5%) |
|  | 520.701 | 2.381 | 0.132 | H-2→L (83%), H-1→L (6%), H→L (6%), H→L+1 (3%) |
|  | 503.510 | 2.462 | 0.187 | H→L+1 (88%), H-2→L (5%), H-2→L+1 (5%) |
|  | 432.468 | 2.867 | 0.908 | H-4→L (21%), H-3→L (56%), H-5→L (9%), H→L+2 (8%) |
|  | 425.711 | 2.912 | 0.003 | H-1→L+1 (95%), H-2→L+1 (4%) |
| HPPC7 | 585.273 | 2.118 | 0.321 | H→L+1 (88%), H-2→L+1 (5%), H→L (3%) |
|  | 578.150 | 2.145 | 0.001 | H-1→L (98%), |
|  | 559.344 | 2.217 | 0.019 | H-2→L (92%), H→L (4%), H→L+1 (2%) |
|  | 490.813 | 2.526 | 0.001 | H-1→L+1 (98%), |
|  | 478.316 | 2.592 | 0.033 | H-2→L+1 (91%), H→L+1 (5%) |
| HPPC8 | 493.293 | 2.513 | 0.009 | H-1→L (94%), H-2→L (5%) |
|  | 487.647 | 2.543 | 0.106 | H-2→L (87%), H-1→L (5%), H→L (6%) |
|  | 444.627 | 2.789 | 0.096 | H-3→L (79%), H-4→L (5%), H→L+1 (9%) |
|  | 433.133 | 2.863 | 0.496 | H→L+1 (75%), H-4→L (4%), H-3→L (8%), H-2→L+1 (3%), H→L+2 (4%) |
|  | 418.554 | 2.962 | 1.135 | H-5→L (21%), H-4→L (41%), H→L+2 (12%), H-6→L (9%), H-3→L (7%), H→L+1 (5%) |

MO = molecular orbital, H = HOMO, L = LUMO, f = oscillator strength

| HPPCR |  |  |
| --- | --- | --- |
| HPPC1 |  |  |
| HPPC2 |  |  |
| HPPC3 |  |  |
| HPPC4 |  |  |
| HPPC5 |  |  |
| HPPC6 |  |  |
| HPPC7 |  |  |
| HPPC8 |  |  |

Figure S1: Frontier molecular orbitals of (HPPCR) and (HPPC1-HPPC8).

Figure S2: UV–Vis spectra of (HPPCR) and (HPPC1-HPPC8).