Supplementary materials

For

Tetraphenylethylene-based fluorescent conjugated microporous polymers for fluorescent sensing trinitrophenol

Liying Rena, Xuechun Fangb, Feng qiang Wangb, and Tongmou Gengb,*

a Anqing Medical College, Anqing 246052, China

b AnHui Province Key Laboratory of Optoelectronic and Magnetism Functional Materials; School of Chemistry and Chemical Engineering, Anqing Normal University, Anqing 246011, China

# Corresponding Author:

# Tongmou Geng

Mailing Address: School of Chemistry and Chemical Engineering, Anqing Normal University, Anqing 246011, China

E-mail addresses: gengtongmou@aqnu.edu.cn (TM Geng).

Experimental Section

S1. Synthesis of the CMPs

S1.1. Synthesis of TTTPT

1.6 mmol of cyanuric chloride (TCT or CC) and 0.6 mmol of tetra-triphenylamine-yl-tetraphenyethylene (TTPT) in 12 mL dry o-dichlorobenzene, 16.8 mmol of methylsulfonic acid (MSFA, CH3SO3H) was heated at 140 oC for 48 hours. The precipitate filtered off from the hot reaction mixture was soxhlet extracted 24 hours with methanol, tetrahydrofuran (THF), and acetone and dried in vacuum at 50 oC. The target product was obtained as a brown yellow colored solid (Yield: 60.54 %). Infrared spectra (cm-1): 3447, 1629, 1591, 1495, 1389, 1325, 1272, 819, 749, 685. Solid-state CP/MAS 13C NMR (ppm): 172, 146, 138, 127. Elemental analysis (%): Calculated: C 84.03, N 11.09, H 4.88. Found: C 84.35, N 10.059, H 5.591.

S1.2. Synthesis of TTDAT

TTDATPE was synthesized using the similar procedures as described for TTTPTPE (see 2.1). Tetrakis(2-diphenylamineylazyl)tetraphenyethylene (TDAT, 0.9 mmol), CH3SO3H (25.2 mmol), CC (2.4 mmol), and 18 mL of o-dichlorobenzene were used. TTDAT was obtained as an brown powder (Yield: 69.11%). FT-IR (cm-1): 3433, 1637, 1593, 1490, 1464, 1382, 810, 745, 686. ss 13C NMR (ppm): 175, 145, 137, 129. Anal. calcd. for TTDAT: C 81.37, H 4.91, N 13.72. Found: C 80.40, H 4.807, N 10.194.

Table S1 Specific surface areas, pore valumes, and pore size distributions of TTTPT and TTDAT

| CMPs | SBETa (m2 g-1) | Vtotal (tpv)b (cm3 g-1) | Vmicroc (cm3 g-1) | Vmicro/ Vtotal | DFT pore Diameter (nm) |
| --- | --- | --- | --- | --- | --- |
| TTTPT TTDAT | 564.8 44.1 | 0.549 0.0514 | 0.349 0.0360 | 0.64 0.70 | 1.22 1.22 |

# a Specific surface area is calculated from the adsorption branch of the nitrogen isotherm using the BET method in the relative pressure (P/P0) range from 0.01 to 0.10.

# b Total pore volume is obtained from BET data up to P/P0=0.97 and is defined as the sum of micropore volume and volumes of larger pores.

# c Micropore volume calculated from nitrogen adsorption isotherm using the t-plot method

Table S2 Summary of BET, Ksv and LODs of other CMPs for the determination of TNP.

| materials | BET (m2 g-1) | Methods or Ksv (L mol -1) | LODs (mol L-1) | Refs |
| --- | --- | --- | --- | --- |
| TDPDB | 592.18 | 1.55×104 | 1.93×10-11 | Polym. Adv. Technol. 2020, 31(6), 1388–1394. |
| CK-CMP | - | 9.9×104 | - | Inorg. Chem. Comm., 2019, 107, 107453 |
| iPrTAPB -Azo-COP | 395 | 1.1×104 | - | J. Chem. Sci., 2018. 130(1), 1-14. |
| HPP-2 | 747 | 2.41×104 | 17.67 ppb | Sensor. Actuat. B-Chem., 2018, 265, 476–487. |
| CMP-LS1 CMP-LS2 PNT-4 PNT-5 PNT-6 COP-612 DTF PTPATTh PTPATCz TTPB DCZP DCZN DBQP DBQN COP-401 COP-301 FL-SNWDPP -0.11 polyTPECz film COP-61 COP-62 COP-63 COP-64 COP-65 P2 P3 COP-3 COP-4 HHQ TTTPT TTDAT | 493 1576 1311.54 817.32 433.24 48.80 705.27 594 894 222.25 688 97 355.76 25.48 - - 750 1020 1302 1208 931 716 869 39 143 1869 2015 24.16 564.8 44.1 | 5.05×104 3.70×104 6.22×105 5.08×105 2.38×105 2.51×105 2.08×103 5.00×103 4.28×103 1.29×103 3.94×103 6.63×103 9.02×104 1.79×104 8.3×104 2.6×105 5.3×104 6.4×104 2.40×105 1.82×105 8.04×104 9.79×104 6.80×104 2.1×103 7.6×104 1.45×104 3.93×103 2.30×105 9.13×103 1.31×105 | - - 2.36×10-9 3.12×10-9 5.52×10-9 - 7.22×10-7 3.01×10-9 7.01×10-9 8.14×10-9 - - 3.33×10-13 2.48×10-13 - - - 1 ppm 1 ppm 1 ppm 1 ppm 1 ppm - - - - 1.30×10-11 1.64×10-11 1.15×10-13 | New J. Chem., 2018, 42, 9482–9487. Sensor. Actuat. B-Chem., 2018, 274, 102–109. Sensor. Actuat. B-Chem., 2017, 243, 753–760. Talanta, 2017, 165, 282–288. Sensor. Actuat. B-Chem., 2017,244, 334–343 J. Mater. Chem. A., 2017, 5, 7612–7617. J Mater Sci., 2016, 51, 4104–4114. Micropor.Mesopor. Mater., 2016, 231, 92–99. J. Mater. Chem. A, 2015, 3, 92–96 J. Mater. Chem. C, 2015, 3, 6876–6881 Angew. Chem. Int. Ed. 2015, 54, 11540–11544 J. Mater. Chem. C, 2015, 3, 8490–8494 Polym. Chem., 2015, 6, 3775–3780. Macromol. Rapid Commun. 2012, 33, 1184−1190. New J. Chem., 2021, 45, 3007-3013. This work. |

Table S3 HOMO and LUMO calculations for CMPs and the NCAs and PhOH. All the molecular orbital calculations were performed with the Gaussian 09 program at the B3LYP/6-31G* level.

| MO energy (eV) | TTTPT | TTDAT | TNP | p-DNB | m-DNB |
| --- | --- | --- | --- | --- | --- |
| LUMO | -2.626 | -2.676 | -3.898 | -3.495 | -3.135 |
| HOMO | -2.950 | -2.771 | -8.237 | -8.350 | -8.413 |
| MO energy (eV) | DNT | o-NP | NB | p-NT | PhOH |
| LUMO | -2.977 | -2.711 | -2.428 | -2.318 | -0.3331 |
| HOMO | -8.113 | -6.797 | -7.591 | -7.364 | -6.566 |
| MO energy (eV) | DNP | p-NP | m-NP |  |  |
| LUMO | -3.320 | -2.222 | -2.396 |  |  |
| HOMO | -7.628 | -6.721 | -6.779 |  |  |