Supplementary information

Defect-engineered chiral bubble domains and topological Hall effect in the Kagome ferromagnet Co3+xSn2-xS2

Dilanath Adhikari1, *, Chanyoung Lee2, *, Yusuff Adeyemi Salawu1, Jinyoung Yun2, Yeonkyu Lee2, Jun Zhou3,4, Yuwaraj K. Kshetri5, 6, Geunsik Lee7, Jeehoon Kim2†, Heon-Jung Kim1, 8, †

1Department of Physics, Graduate School, Daegu University, Gyeongbuk 38453, Republic of Korea

2Department of Physics, Pohang University of Science and Technology, Pohang 37673, Republic of Korea

3Future Energy Acceleration & Translation (FEAT), Strategic Research & Translational Thrust (SRTT), A*STAR Research Entities, 1 Fusionopolis Way #20-10 Connexis North Tower, Singapore 138632, Republic of Singapore

4Institute of Materials Research and Engineering (IMRE), Agency for Science, Technology and Research (A*STAR), 2 Fusionopolis Way, Innovis #08-03, Singapore 138634, Republic of Singapore

5Research Center for Green Advanced Materials, Sun Moon University, Chungnam 31460, Republic of Korea

6Department of Semiconductor Materials Engineering, Sun Moon University, Chungnam 31460, Republic of Korea

7Department of Chemistry, College of Natural Science, Ulsan National Institute of Science and Technology, Ulsan 44919, Republic of Korea

8Department of Materials-Energy Science and Engineering, College of Engineering, Daegu University, Gyeongbuk 38453, Republic of Korea.

† jeehoon@postech.ac.kr and hjkim76@daegu.ac.kr

* equal contributions

Supplementary Figure 1 Low field M-H loop for Co3+xSn2-xS2 x = 0.075. a) and b) M-H loop for B//c and B//ab, respectively, at various temperatures below Tc with in ± 0.3 T. The violet arrow shows the magnetic field (B) sweeping direction. The blue arrow in b) shows the metamagnetic-like transition below 110 K.

Supplementary Figure 2 Field ramp rate-dependent M-H and Hall measurement for the x = 0 sample. a)-c) M-H loops at 4.2, 50, and 130 K, respectively, when ramp rates of 0.05 T/min (black), 0.1 T/min (red), 0.25 T/min (blue), and 0.5 T/min (green) were applied. d)-f) Corresponding Hall resistivity.

Supplementary Figure 3 Extraction of topological Hall effect (THE) for the x = 0.075 sample. a)-d) Extraction of THE for 20, 40, 110, and 130 K, respectively. The black is the corrected Hall resistivity after subtraction of the linear ordinary Hall resistivity from the total Hall resistivity. The red is the anomalous Hall resistivity (AHE) estimated from magnetization (M), assuming AHE is proportional to M. And blue is the extracted THE where the AHE is subtracted from the corrected Hall resistivity.

Supplementary Figure 4 Field ramp rate-dependent M-H and Hall measurement for the x = 0.075 sample. a) and b) M-H loops at 50 and 130 K, respectively, when ramp rates of 0.05 T/min (black), 0.1 T/min (red), 0.25 T/min (blue), and 0.5 T/min (green) were applied. c) and d) Corresponding Hall resistivity.