Supporting information

Silk Fibroin-Regulated Biomimetic Mineralization of Ni(OH)2 for Energy Storage Applications

Siva Kumar Ramesh,† Seog Woo Rhee, *,† and Jinkwon Kim*,†

† Department of Chemistry, Kongju National University, 56 Gongjudaehak-ro, Gongju-si, Chungnam-do 32588, Republic of Korea

*Corresponding author.

Tel.: +82-41-850-8496. Fax: +82-41-850-8613.

E-mail: Jinkwon Kim - jkim@kongju.ac.kr, Seog Woo Rhee - jisanrhee@kongju.ac.kr

Fig. S1 High-resolution XPS spectra of (a) Ni 2p, (b) O 1s, (c) C 1s and (d) Raman spectra of Ni(OH)2/SF-0.3.

Fig. S2 XRD patterns of biomineralized Ni(OH)2 using various Ni2+ concentrations with constant silk fibroin concentration (0.3% w/v).

Fig. S3 SEM images of biomineralized Ni(OH)2 using various nickel precusors (a,b) NiCl2.6H2O, (c,d) Ni(CH3CO2)2.4H2O, (e,f) Ni(NO3).6H2O, (g,h) NiSO46H2O, and (i,j) Ni(OCl4)2.6H2O.

Fig. S4 (a) Plot of peak currents vs square root of scan rate, and (b) Plot of log current vs log scan rate obtained from CV curves of Ni(OH)2, Ni(OH)2/SF-0.3, and Ni(OH)2/SF-0.5.

Table S1 Synthesis parameters under different conditions.

| S.No | Ni precursors | Nickel ion concentration | Silk Fibroin concentration | Solvent |
| --- | --- | --- | --- | --- |
| Effect of silk fibroin concentration |  |  |  |  |
| 1 | NiCl2.6H2O | 60 mmol L-1 | 0 | 50 ml DI water |
| 2 | NiCl2.6H2O | 60 mmol L-1 | 0.1% (w/v) | 50 ml DI water |
| 3 | NiCl2.6H2O | 60 mmol L-1 | 0.3% (w/v) | 50 ml DI water |
| 4 | NiCl2.6H2O | 60 mmol L-1 | 0.5% (w/v) | 50 ml DI water |
| Effect of Ni2+ ion concentration |  |  |  |  |
| 5 | NiCl2.6H2O | 20 mmol L-1 | 0.3% (w/v) | 50 ml DI water |
| 6 | NiCl2.6H2O | 30 mmol L-1 | 0.3% (w/v) | 50 ml DI water |
| 7 | NiCl2.6H2O | 40 mmol L-1 | 0.3% (w/v) | 50 ml DI water |
| 8 | NiCl2.6H2O | 60 mmol L-1 | 0.3% (w/v) | 50 ml DI water |
| 9 | NiCl2.6H2O | 80 mmol L-1 | 0.3% (w/v) | 50 ml DI water |
| Effect of organic solvents |  |  |  |  |
| 10 | NiCl2.6H2O | 60 mmol L-1 | 0.1% (w/v) | 20 ml Methanol, 30 ml DI water |
| 11 | NiCl2.6H2O | 60 mmol L-1 | 0.3% (w/v) | 20 ml Ethanol, 30 ml DI water |
| 12 | NiCl2.6H2O | 60 mmol L-1 | 0.5% (w/v) | 20 ml Ethanol, 30 ml DMF |
| Effect of nickel precursors |  |  |  |  |
| 13 | NiCl2.6H2O | 60 mmol L-1 | 0.3% (w/v) | 50 ml DI water |
| 14 | Ni(NO3).6H2O, | 60 mmol L-1 | 0.3% (w/v) | 50 ml DI water |
| 15 | NiSO4.7H2O, | 60 mmol L-1 | 0.3% (w/v) | 50 ml DI water |
| 16 | Ni(OCl4)2.6H2O | 60 mmol L-1 | 0.3% (w/v) | 50 ml DI water |
| 17 | Ni(CH3CO2)2.4H2O | 60 mmol L-1 | 0.3% (w/v) | 50 ml DI water |

Table S2 Specific capacity at different current densities ranging from 0.5 to 1 Ag-1.

| Specific capacity values (mAh g-1) |  |  |  |
| --- | --- | --- | --- |
| Current (A g-1) | Ni(OH)2 | Ni(OH)2/SF-0.3 | Ni(OH)2/SF-0.5 |
| 0.5 | 157.5 | 170 | 127.5 |
| 1 | 135.55 | 168.33 | 88.33 |
| 2 | 120 | 144.44 | 64.44 |
| 3 | 105 | 131.66 | 51.66 |
| 5 | 91.66667 | 111.11 | 41.66 |
| 7 | 81.66 | 108.88 | 35 |
| 10 | 72.22 | 94.44 | 33.33 |

Table S3 Energy storage performances of Ni-based electrodes. The specific capacity (mAh g−1) values with “~” are calculated from specific capacitance or specific capacity (F g-1 or C g-1).

| S.No. | Electrode Material | Electrolyte | Current Density (Ag-1) | Specific Capacity (mAh g-1) | References |
| --- | --- | --- | --- | --- | --- |
| 1 | Ni(OH)2/SF-0.3 | 2 M KOH | 1 | 168.33 | This Work |
| 2 | Ni(OH)2@CoS/NF |  | 1 | 136.25 | 1 |
| 3 | ZnCo2O4@Ni(OH)2 | 3 M KOH | 1 | ~141.8 | 2 |
| 4 | Ni(OH)2-rGO composite-1 Ni(OH)2-rGO composite-5 Ni(OH)2-rGO composite-10 | 6 M KOH | 2 | 83.89 99.44 63.89 | 3 |
| 5 | NiO-CNT | 1 M KOH | 1 | 155 | 4 |
| 6 | NiCo2O4 | 3 M KOH | 1 | 112 | 5 |
| 7 | Ni0.7Co0.2Mn0.1LDH-N Ni0.7Co0.2Mn0.1LDH-A Ni0.7Co0.2Mn0.1LDH-S | 6 M KOH | 1 | ~166.1 ~103.05 ~30.8 | 6 |
| 8 | Ni3S2 | 1 M KOH | 0.2 | 148 | 7 |
| 9 | CuO–NiO/CNT | 2 M KOH | 1 | ~80.73 | 8 |

REFERENCES

(1)	Y. Yang, H. Zhu, H. Meng, W. Ma, C. Wang, F, Ma, Z. Hu, Nickel Foam-Supported Starfish-like Ni(OH)2@CoS Nanostructure with Obvious Core–Shell Heterogeneous Interfaces for Hybrid Supercapacitors Application. J. Mater. Sci. 56 3280–3295 (2021). https://doi.org/10.1007/s10853-020-05407-7.

(2)	X. Han, Y. Yang, J. J. Zhou, Q. Ma, K. Tao, L.  Han, Metal–Organic Framework Templated 3D Hierarchical ZnCo2O4@Ni(OH)2 Core–Shell Nanosheet Arrays for High-Performance Supercapacitors. Chem. Eur. J. 24 18106–18114 (2018). https://doi.org/10.1002/chem.201804327.

(3)	B. Guo, Y. Gao, Y. Li, K. Liu, X. Lv, C. Mi, L. Liu, M. Li, M. Battery-Type-Behavior-Retention Ni(OH)2-RGO Composite for an Ultrahigh-Specific-Capacity Asymmetric Electrochemical Capacitor Electrode. ACS Omega 8 6289–6301 (2023). https://doi.org/10.1021/acsomega.2c06207.

(4)	X. Wang, M. Li, Y. Wang, B.Chen, Y. Zhu, Y. Wu, A Zn-NiO Rechargeable Battery with Long Lifespan and High Energy Density. J. Mater. Chem. A 3 8280–8283 (2015). https://doi.org/10.1039/c5ta01947h.

(5)	J. Wang, Z. Jia, S. Li, Y. Wang, W. Guo, T. Qi, High-Performance Aqueous Rechargeable Batteries Based on Zinc Anode and NiCo2O4 Cathode. Bull. of Mater. Sci. 38 1435–1438 (2015). https://doi.org/10.1007/s12034-015-1033-6.

(6)	M. Goyal, P. Dahiya, S. Kumar, T. K. Rahul; Mandal, Different Metal Precursor Based Rapid Synthesis of α-Ni(OH)2-Type Ni-Co-Mn Layered Double Hydroxides and Its Use as Electrodes for High Performance Energy Storage Devices. J. Energy Storage 72 108622 (2023). https://doi.org/10.1016/j.est.2023.108622.

(7)	P. Hu, T. Wang, J. Zhao, C. Zhang, J. Ma, H. Du, X. Wang, G. Cui, Ultrafast Alkaline Ni/Zn Battery Based on Ni-Foam-Supported Ni3S2 Nanosheets. ACS Appl. Mater. Interfaces 7 26396–26399 (2015). https://doi.org/10.1021/acsami.5b09728.

(8)	S. Veeman, S. Karuppuchamy, H2O2 Assisted Hydrothermal and Microwave Synthesis of CuO–NiO Hybrid MWCNT Composite Electrode Materials for Supercapacitor Applications. Ceram. Int. 48 26806–26817 (2022). https://doi.org/10.1016/j.ceramint.2022.05.380.