Supplementary Material

Outstanding piezoelectricity of (K, Na)(Nb, Sb)O3-SrZrO3-(Bi, Ag)ZrO3 piezoceramics and their application to a planar-type actuator

Su-hwan Goa, †, Jae-min Eum a, †, Dae-Su Kima, Seok-Jun Chaea, Sun-Woo Kima,

Eun-Ji Kima, Yeon-Gyeong Chaea, Jong-Un Woob and Sahn Nahma,b,*

aDepartment of Materials Science and Engineering, Korea University, 145 Anam-ro, Seongbuk-gu, Seoul, 02841, Republic of Korea

b Department of Nano Bio Information Technology, KU-KIST Graduate School of Converging Science and Technology, Korea University, 145 Anam-ro, Seongbuk-gu, Seoul, 02841, Republic of Korea

†These authors contributed equally to this work.

*Corresponding author email address: snahm@korea.ac.kr

1. Experimental procedure for measurement of physical properties of the sample

The crystal structures of the sintered ceramics and thick films were examined using X-ray diffraction analysis (XRD; Shimadzu, XRD-6100, Japan). The peaks at 66.5°, measured by low-speed scanning, were deconvoluted using the Voigt function. For a detailed investigation of the crystal structure of the specimens, XRD patterns were analyzed by the Rietveld method using the FullProf program. The microstructures of the specimens were studied using field-emission scanning electron microscopy (FE-SEM; TESCAN, LYRA3, Czech Republic). Moreover, the domain structures of the specimens were studied using field-emission transmission electron microscopy (FE-TEM; FEI, TECNAI G2 F30, USA) operating at 300 kV. TEM samples were prepared by focused ion beam milling (FIB; Thermo Fisher Scientific, Helios G4 UC, USA). The densities of the sintered specimens were measured using Archimedes’ principle.

Silver electrodes were printed on the surfaces of the sintered specimens and fired at 600 °C for 10 min to measure the electrical properties of the specimens. The specimens were poled by applying a DC electric field of 3 kV/mm for 20 min at various temperatures in a silicone oil bath. The dielectric properties were measured using an impedance analyzer (Agilent Technologies, HP 4194A, USA). Variations in the dielectric constant (εT33/εo) and dielectric loss (tan δ) were measured with respect to temperature and frequency using an impedance analyzer (Agilent Technologies, HP 4294A, USA). The polarization versus electric field (P-E) hysteresis curves were measured using a ferroelectric tester (RT66A, Radiant Co., Ltd.) and a high-voltage amplifier (Trek, 609E-6-L-CE, USA). The piezoelectric charge constant (d33) was measured using a d33 meter (Micro-Epsilon Channel Product, DT-3300, Raleigh, USA).

2. P-E hysteresis curves of KNNS-(0.04-x)SZ-xBAZ piezoceramics

Figures S1(a)–(e) exhibit the P–E hysteresis curves of the KNNS-(0.04-x)SZ-xBAZ piezoceramics (0.0 ≤ x ≤ 0.04), and the variation in saturated polarization (PS), remnant polarization (Pr), and coercive field (EC) with respect to x are displayed in Fig. S1(f). The PS of the sample with x = 0.0 was approximately 22.7 μC/cm2 (Fig. S1(a)); PS decreased slightly with increasing x, but its variation was not significant, as shown in Fig. S1(f). The Pr slightly increased with the addition of BAZ, and it slightly decreased when x exceeded 0.01, but the variation was insignificant (Fig. S1(f)). The EC of the specimen with x = 0.0 was approximately 0.56 kV/mm, which varies negligibly with increasing x, as shown in Fig. S1(f). Therefore, the results suggest that all the samples have good ferroelectric properties and they do not change considerably with the addition of BAZ.

Figure S1. P–E hysteresis curves of the KNNS-(0.04-x)SZ-xBAZ piezoceramics with (a) x = 0.0, (b) x = 0.01, (c) x = 0.02, (d) x = 0.03, and (e) x = 0.04. (f) PS, Pr, and EC values of the KNNS-(0.04-x)SZ-xBAZ piezoceramics with 0.0 ≤ x ≤ 0.04.

3. SEM images of the fractured surface of KNNS-(0.04-x)SZ-xBAZ piezoceramics

Figures S2(a)–(e) show the SEM images of the fractured surface of the KNNS-(0.04-x)SZ-xBAZ piezoceramics with 0.0 ≤ x ≤ 0.04. All samples exhibited dense microstructures. The piezoceramic with x = 0.0 has a microstructure consisting of large and small grains, as shown in Fig. S2(a)), and the inset shows an enlarged SEM image of the small grains. The average grain sizes of the large and small grains are approximately 20 μm and 1 μm, respectively, (Fig. S2(a)). When BAZ was added, the small grains disappeared (Figs. S2(b)-(e)). The size of the large grains did not change with the increase in BAZ content, and the piezoceramics with 0.01 ≤ x ≤ 0.04 exhibited an identical grain size of approximately 23–25 μm. Similar results were observed for the thermally etched samples, as shown in Figs. 2(a)–(e).

Figure S2. SEM images of the KNNS-(0.04-x)SZ-xBAZ ceramics with 0.0 ≤ x ≤ 0.04 sintered at 1090 °C for 3 h: (a) x = 0.0, (b) x = 0.01, (c) x = 0.02, (d) x = 0.03, and (e) x = 0.04

4. XRD patterns of KNNS-(0.04-x)SZ-xBAZ piezoceramics

Figures S3(a)–(e) show the XRD patterns of the KNNS-(0.04-x)SZ-xBAZ piezoceramics with 0.0 ≤ x ≤ 0.04 densified at 1090 °C for 3 h. All the samples have a homogeneous perovskite structure, without secondary phases. Variations in peak position and intensity were not observed with an increase in BAZ content. These results suggest that the addition of BAZ did not change the crystal structure of the samples. However, it is difficult to identify the detailed crystal structures using these normal XRD patterns.

Figure S3. XRD patterns of the KNNS-(0.04-x)SZ-xBAZ piezoceramics sintered at 1090 °C for 3 h: (a) x = 0.0, (b) x = 0.01, (c) x = 0.02, (d) x = 0.03, and (e) x = 0.04.

5. Rietveld refinement XRD profiles of the KNNS-(0.04-x)SZ-xBAZ ceramics

Figures S4(a) and (b) show the Rietveld refinement XRD profile of the KNNS-SZ piezoceramics (x = 0.0) using the O-R multi-structure and T-O-R multi-structure, respectively. The atomic coordinates, site occupancies, lattice parameters, and R-values of these models are listed in Table S1. The R-values of the T-O-R multi-structure were smaller than those of the O-R multi-structure. Therefore, this sample was considered to have a T-O-R multi-structure. The T-O-R multi-structure of this sample consists of 25.2% R3m rhombohedral, 66.2% Amm2 orthorhombic, and 8.6% P4mm tetragonal structures, indicating that the proportion of orthorhombic structure is much larger than those of the rhombohedral and tetragonal structures.

Rietveld analysis was also conducted on the XRD pattern of the piezoceramic with x= 0.01, as shown in Figs. S4(c) and (d). The O-R and T-O-R multi-structures were used for Rietveld analysis, and the atomic coordinates, site occupancies, lattice parameters, and R-values of this model are listed in Table S2. The R-values of the T-O-R multi-structure were smaller than those of the O-R multi-structure. Therefore, this specimen was considered to have a T-O-R multi-structure. The T-O-R multi-structure of this sample consists of 25.6% R3m rhombohedral, 58.1% Amm2 orthorhombic, and 16.3% P4mm tetragonal structures, indicating that the proportion of orthorhombic structure is also much larger than those of the rhombohedral and tetragonal structures.

Figures S4(e) and (f) show the Rietveld refinement XRD profiles of the KNNS-0.02SZ-0.02BAZ piezoceramic (x = 0.02) and the O-R and T-O-R multi-structures were also used for the Rietveld analysis. Table S3 lists the atomic coordinates, site occupancies, lattice parameters, and R-values of these models. This specimen is considered to have a T-O-R multi-structure because the R-values of this structure are smaller than those of the O-R multi-structure. Moreover, the T-O-R multi-structure of this specimen consists of 24.8% R3m rhombohedral, 53.8% Amm2 orthorhombic, and 21.4% P4mm tetragonal structures. Therefore, the proportion of the orthorhombic structure is still larger than that of the rhombohedral and tetragonal structures.

Figure S4. Rietveld refinement XRD profiles of the KNNS-(0.04-x)SZ-xBAZ ceramics with; (a) x = 0.0 (O-R multi-structure), (b) x = 0.0 (T-O-R multi-structure), (c) x = 0.01 (O-R multi-structure), (d) x = 0.01 (T-O-R multi-structure), (e) x = 0.02 (O-R multi-structure), and (f) x = 0.02 (T-O-R multi-structure).

Table S1. Atomic coordinates, site occupancies, lattice parameters, and R-values of the KNNS-0.04SZ ceramic at RT for O-R and T-O-R multi-structures

| Phase | Structural model (SG) | Site label | x | y | z | Site occupancy | Lattice parameter (Å) | R factor |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| O-R multi-structure | Orthorhombic (Amm2) (71%) + Rhombohedral (R3m, H) (29%) | K/Na/Ca | 0(-) | 0(-) | 0(-) | 0.114(-)/0.123(-)/0.010(-) | a=3.9840(1) b=5.6183(1) c=5.6194(1) α = β = γ = 90° | Rp/Rwp/Rexp Rb/Rf 4.28 / 5.51 / 3.05 4.11 / 1.85 |
|  |  | Nb/Sb/Zr | 0.5(-) | 0(-) | 0.5284(19) | 0.224(-)/0.016(-)/0.010(-) |  |  |
|  |  | O1 | 0(-) | 0(-) | 0.5053(89) | 0.250(-) |  |  |
|  |  | O2 | 0.5(-) | 0.2739(-) | 0.3074(50) | 0.500(-) |  |  |
|  |  | K/Na/Ca | 0(-) | 0(-) | 0.5050(37) | 0.076(-)/0.082(-)/0.007(-) | a=b=5.6416(32) c=6.8746(77) α = β = 90° γ = 120° | Rp/Rwp/Rexp Rb/Rf 4.28 / 5.51 / 3.05 3.14 / 1.49 |
|  |  | Nb/Sb/Zr | 0(-) | 0(-) | 0(-) | 0.150(-)/0.010(-)/0.007(-) |  |  |
|  |  | O1 | 0.5109(-) | -0.5109(-) | 0.5184(38) | 0.500(-) |  |  |
| T-O-R multi-structure | Tetragonal (P4mm) (9%) + Orthorhombic (Amm2) (66%) + Rhombohedral (R3m, H) (25%) | K/Na/Ca | 0(-) | 0(-) | 0.0799(403) | 0.057(-)/0.062(-)/0.005(-) | a=b=3.9651(7) c=4.0030(11) α = β = γ = 90° | Rp/Rwp/Rexp Rb/Rf 3.86 / 5.06 / 3.05 3.61 / 2.46 |
|  |  | Nb/Sb/Zr | 0.5(-) | 0.5(-) | 0.5(-) | 0.112(-)/0.008(-)/0.005(-) |  |  |
|  |  | O1 | 0.5(-) | 0.5(-) | 0.0208(-) | 0.125(-) |  |  |
|  |  | O2 | 0.5(-) | 0(-) | 0.5476(168) | 0.250(-) |  |  |
|  |  | K/Na/Ca | 0(-) | 0(-) | 0(-) | 0.114(-)/0.123(-)/0.007(-) | a=3.9697(2) b=5.6253(2) c=5.6339(2) α = β = γ = 90° | Rp/Rwp/Rexp Rb/Rf 3.86 / 5.06 / 3.05 3.53 / 2.40 |
|  |  | Nb/Sb/Zr | 0.5(-) | 0(-) | 0.5135(31) | 0.224(-)/0.016(-)/0.010(-) |  |  |
|  |  | O1 | 0(-) | 0(-) | 0.4730(44) | 0.250(-) |  |  |
|  |  | O2 | 0.5(-) | 0.1816(18) | 0.2429(41) | 0.500(-) |  |  |
|  |  | K/Na/Ca | 0(-) | 0(-) | 0.4885(39) | 0.076(-)/0.082(-)/0.007(-) | a=b=5.6229(19) c=6.9163(42) α = β = 90° γ = 120° | Rp/Rwp/Rexp Rb/Rf 3.86 / 5.06 / 3.05 2.55 / 1.81 |
|  |  | Nb/Sb/Zr | 0(-) | 0(-) | 0(-) | 0.150(-)/0.010(-)/0.007(-) |  |  |
|  |  | O | 0.5109(-) | -0.5109(-) | 0.4869(81) | 0.500(-) |  |  |

Table S2. Atomic coordinates, site occupancies, lattice parameters, and R-values of the KNNS-0.03SZ-0.01BAZ ceramic at RT for O-R and T-O-R multi-structures

| Phase | Structural model (SG) | Site label | x | y | z | Site occupancy | Lattice parameter (Å) | R factor |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| O-R multi-structure | Orthorhombic (Amm2) (67%) + Rhombohedral (R3m, H) (33%) | K/Na/Ca /Bi/Ag | 0(-) | 0(-) | 0(-) | 0.114(-)/0.123(-)/0.007(-) /0.001(-)/(0.001(-) | a=3.9856(1) b=5.6197(1) c=5.6200(1) α = β = γ = 90° | Rp/Rwp/Rexp Rb/Rf 4.13 / 5.42 / 3.07 3.48 / 2.05 |
|  |  | Nb/Sb/Zr | 0.5(-) | 0(-) | 0.5248(33) | 0.224(-)/0.016(-)/0.010(-) |  |  |
|  |  | O1 | 0(-) | 0(-) | 0.6060(59) | 0.250(-) |  |  |
|  |  | O2 | 0.5(-) | 0.2494(40) | 0.2756(-) | 0.500(-) |  |  |
|  |  | K/Na/Ca /Bi/Ag | 0(-) | 0(-) | 0.4683(31) | 0.076(-)/0.082(-)/0.005(-) /0.001(-)/0.001(-) | a=b=5.6360(16) c=6.8874(41) α = β = 90° γ = 120° | Rp/Rwp/Rexp Rb/Rf 4.13 / 5.42 / 3.07 2.97 / 1.36 |
|  |  | Nb/Sb/Zr | 0(-) | 0(-) | 0(-) | 0.150(-)/0.010(-)/0.007(-) |  |  |
|  |  | O1 | 0.5109(-) | -0.5109(-) | 0.4849(35) | 0.500(-) |  |  |
| T-O-R multi-structure | Tetragonal (P4mm) (16%) + Orthorhombic (Amm2) (58%) + Rhombohedral (R3m, H) (26%) | K/Na/Ca /Bi/Ag | 0(-) | 0(-) | 0.0341(85) | 0.057(-)/0.062(-)/0.004(-) /0.001(-)/0.001(-) | a=b=3.9709(6) c=3.9989(5) α = β = γ = 90° | Rp/Rwp/Rexp Rb/Rf 4.01 / 5.24 / 3.07 4.44 / 2.95 |
|  |  | Nb/Sb/Zr | 0.5(-) | 0.5(-) | 0.5(-) | 0.112(-)/0.008(-)/0.005(-) |  |  |
|  |  | O1 | 0.5(-) | 0.5(-) | 0.0208(-) | 0.125(-) |  |  |
|  |  | O2 | 0.5(-) | 0(-) | 0.4711(179) | 0.250(-) |  |  |
|  |  | K/Na/Ca | 0(-) | 0(-) | 0(-) | 0.114(-)/0.123(-)/0.007(-) | a=3.9719(2) b=5.6289(2) c=5.6376(2) α = β = γ = 90° | Rp/Rwp/Rexp Rb/Rf 4.01 / 5.24 / 3.07 3.86 / 2.13 |
|  |  | Nb/Sb/Zr | 0.5(-) | 0(-) | 0.4860(41) | 0.224(-)/0.016(-)/0.010(-) |  |  |
|  |  | O1 | 0(-) | 0(-) | 0.4588(85) | 0.250(-) |  |  |
|  |  | O2 | 0.5(-) | 0.2127(45) | 0.1879(72) | 0.500(-) |  |  |
|  |  | K/Na/Ca /Bi/Ag | 0(-) | 0(-) | 0.4670(51) | 0.076(-)/0.082(-)/0.005(-) /0.001(-)/0.001(-) | a=b=5.6332(15) c=6.8866(37) α = β = 90° γ = 120° | Rp/Rwp/Rexp Rb/Rf 4.01 / 5.24 / 3.07 3.91 / 2.45 |
|  |  | Nb/Sb/Zr | 0(-) | 0(-) | 0(-) | 0.150(-)/0.010(-)/0.007(-) |  |  |
|  |  | O | 0.5109 | -0.5109(-) | 0.4782(51) | 0.500(-) |  |  |

Table S3. Atomic coordinates, site occupancies, lattice parameters, and R-values of the KNNS-0.02SZ-0.02BAZ ceramic at RT for O-R and T-O-R multi-structures

| Phase | Structural model (SG) | Site label | x | y | z | Site occupancy | Lattice parameter (Å) | R factor |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| O-R multi-structure | Orthorhombic (Amm2) (66%) + Rhombohedral (R3m, H) (34%) | K/Na/Ca /Bi/Ag | 0(-) | 0(-) | 0(-) | 0.114(-)/0.123(-)/0.005(-) /0.002(-)/(0.002(-) | a=3.9881(2) b=5.6171(2) c=5.6241(2) α = β = γ = 90° | Rp/Rwp/Rexp Rb/Rf 4.33 / 5.65 / 3.01 4.62 / 2.36 |
|  |  | Nb/Sb/Zr | 0.5(-) | 0(-) | 0.4999(37) | 0.224(-)/0.016(-)/0.010(-) |  |  |
|  |  | O1 | 0(-) | 0(-) | 0.5457(116) | 0.250(-) |  |  |
|  |  | O2 | 0.5(-) | 0.2844(84) | 0.2497(91) | 0.500(-) |  |  |
|  |  | K/Na/Ca /Bi/Ag | 0(-) | 0(-) | 0.4568(26) | 0.076(-)/0.082(-)/0.003(-) /0.002(-)/0.002(-) | a=b=5.6384(26) c=6.8766(62) α = β = 90° γ = 120° | Rp/Rwp/Rexp Rb/Rf 4.33 / 5.65 / 3.01 3.95 / 2.48 |
|  |  | Nb/Sb/Zr | 0(-) | 0(-) | 0(-) | 0.150(-)/0.010(-)/0.007(-) |  |  |
|  |  | O1 | 0.5109(-) | -0.5109(-) | 0.4822(66) | 0.500(-) |  |  |
| T-O-R multi-structure | Tetragonal (P4mm) (21%) + Orthorhombic (Amm2) (54%) + Rhombohedral (R3m, H) (25%) | K/Na/Ca /Bi/Ag | 0(-) | 0(-) | 0.2454(600) | 0.057(-)/0.062(-)/0.002(-) /0.001(-)/0.001(-) | a=b=3.9675(4) c=3.9920(4) α = β = γ = 90° | Rp/Rwp/Rexp Rb/Rf 4.05 / 5.30 / 3.01 3.62 / 1.93 |
|  |  | Nb/Sb/Zr | 0.5(-) | 0.5(-) | 0.5(-) | 0.112(-)/0.008(-)/0.005(-) |  |  |
|  |  | O1 | 0.5(-) | 0.5(-) | 0.0243(-) | 0.125(-) |  |  |
|  |  | O2 | 0.5(-) | 0(-) | 0.3689(421) | 0.250(-) |  |  |
|  |  | K/Na/Ca | 0(-) | 0(-) | 0(-) | 0.114(-)/0.123(-)/0.007(-) | a=3.9697(2) b=5.6253(2) c=5.6339(2) α = β = γ = 90° | Rp/Rwp/Rexp Rb/Rf 3.86 / 5.06 / 3.05 3.53 / 2.40 |
|  |  | Nb/Sb/Zr | 0.5(-) | 0(-) | 0.5135(31) | 0.224(-)/0.016(-)/0.010(-) |  |  |
|  |  | O1 | 0(-) | 0(-) | 0.4730(44) | 0.250(-) |  |  |
|  |  | O2 | 0.5(-) | 0.1816(18) | 0.2429(41) | 0.500(-) |  |  |
|  |  | K/Na/Ca /Bi/Ag | 0(-) | 0(-) | 0.4531(31) | 0.076(-)/0.082(-)/0.003(-) /0.002(-)/0.002(-) | a=b=5.6442(30) c=6.8831(64) α = β = 90° γ = 120° | Rp/Rwp/Rexp Rb/Rf 4.05 / 5.30 / 3.01 2.58 / 1.60 |
|  |  | Nb/Sb/Zr | 0(-) | 0(-) | 0(-) | 0.150(-)/0.010(-)/0.007(-) |  |  |
|  |  | O | 0.5109(-) | -0.5109(-) | 0.5380(67) | 0.500(-) |  |  |

6. Rietveld refinement XRD profiles of the KNNS-0.04 BAZ ceramics

Figures S5(a) and (b) display the Rietveld refinement XRD profiles of the KNNS-0.04BAZ piezoceramic (x = 0.04) using the T-O-R multi-structure and the R-T multi-structure, respectively. The atomic coordinates, site occupancies, lattice parameters, and R-values of these models are listed in Table S4. The R-values of the R-T multi-structure are smaller than those of the T-O-R multi-structure. Hence, this sample is expected to have an R-T multi-structure. This R-T multi-structure consists of 29% R3m rhombohedral and 71% Pm3m tetragonal structures. Therefore, the proportion of the tetragonal structure is larger than that of the rhombohedral structure.

Figure S5. Rietveld refinement XRD profiles of the KNNS-0.04BAZ piezoceramic (x=0.04) using; (a) T-O-R multi-structure and (b) x = R-T multi-structure.

Table S4. Atomic coordinates, site occupancies, lattice parameters, and R-values of the KNNS-0.04BAZ ceramic at RT for T-O-R and R-T multi-structures

| Phase | Structural model (SG) | Site label | x | y | z | Site occupancy | Lattice parameter (Å) | R factor |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| T-O-R multi-structure | Tetragonal (P4mm) (53%) + Orthorhombic (Amm2) (19%) + Rhombohedral (R3m, H) (28%) | K/Na /Bi/Ag | 0(-) | 0(-) | 0.0381(44) | 0.057(-)/0.062(-) /0.002(-)/0.002(-) | a=b=3.9752(1) c=3.9792(1) α = β = γ = 90° | Rp/Rwp/Rexp Rb/Rf 3.93 / 5.22 / 2.86 2.77 / 1.68 |
|  |  | Nb/Sb/Zr | 0.5(-) | 0.5(-) | 0.5(-) | 0.112(-)/0.008(-)/0.005(-) |  |  |
|  |  | O1 | 0.5(-) | 0.5(-) | -0.0381(206) | 0.125(-) |  |  |
|  |  | O2 | 0.5(-) | 0(-) | 0.4449(36) | 0.250(-) |  |  |
|  |  | K/Na /Bi/Ag | 0(-) | 0(-) | 0(-) | 0.114(-)/0.123(-) /0.005(-)/0.005(-) | a=3.9953(3) b=5.5973(4) c=5.6179(3) α = β = γ = 90° | Rp/Rwp/Rexp Rb/Rf 3.93 / 5.22 / 2.86 3.55 / 2.74 |
|  |  | Nb/Sb/Zr | 0.5(-) | 0(-) | 0.4926(36) | 0.224(-)/0.016(-)/0.010(-) |  |  |
|  |  | O1 | 0(-) | 0(-) | 0.4105(115) | 0.250(-) |  |  |
|  |  | O2 | 0.5(-) | 0.2739(-) | 0.2585(-) | 0.500(-) |  |  |
|  |  | K/Na /Bi/Ag | 0(-) | 0(-) | 0.4473(50) | 0.076(-)/0.082(-) /0.003(-)/0.003(-) | a=b=5.6381(33) c=6.8800(82) α = β = 90° γ = 120° | Rp/Rwp/Rexp Rb/Rf 3.93 / 5.22 / 2.86 2.23 / 1.68 |
|  |  | Nb/Sb/Zr | 0(-) | 0(-) | 0(-) | 0.150(-)/0.010(-)/0.007(-) |  |  |
|  |  | O | 0.5109(-) | -0.5109(-) | 0.4841(-) | 0.500(-) |  |  |
| R-T multi-structure | Rhombohedral (R3m, H) (29%) + Tetragonal (P4mm) (71%) | K/Na /Bi/Ag | 0(-) | 0(-) | 0.5173(53) | 0.076(-)/0.082(-) /0.003(-)/0.003(-) | a=b=5.6381(12) c=6.8867(17) α = β = 90° γ = 120° | Rp/Rwp/Rexp Rb/Rf 3.92 / 5.06 / 2.86 2.44 / 1.35 |
|  |  | Nb/Sb/Zr | 0(-) | 0(-) | 0(-) | 0.150(-)/0.010(-)/0.007(-) |  |  |
|  |  | O1 | 0.4951(-) | -0.4951(-) | 0.4629(38) | 0.500(-) |  |  |
|  |  | K/Na /Bi/Ag | 0(-) | 0(-) | 0.0440(48) | 0.057(-)/0.062(-) /0.002(-)/0.002(-) | a=b=3.9701(2) c=3.9881(2) α = β = γ = 90° | Rp/Rwp/Rexp Rb/Rf 3.92 / 5.06 / 2.86 2.10 / 1.54 |
|  |  | Nb/Sb/Zr | 0.5(-) | 0.5(-) | 0.5(-) | 0.112(-)/0.008(-)/0.005(-) |  |  |
|  |  | O1 | 0.5(-) | 0.5(-) | 0.0588(74) | 0.125(-) |  |  |
|  |  | O2 | 0.5(-) | 0(-) | 0.4703(62) | 0.250(-) |  |  |

7. εT33/εo versus temperature curves measured at various frequencies for the KNNS-(0.04-x)SZ-xBAZ ceramics

Figure S6(a) shows the εT33/εo versus temperature curves measured at various frequencies for the specimen with x = 0.01, near a TT-O-R peak. The εT33/εo value decreased with increasing frequency. Moreover, the TT-O-R increased with an increase in the frequency, and ΔT was approximately 4.5 °C. Therefore, the specimen with x = 0.01 shows a relaxor characteristic near the TT-O-R that corresponds to the ferroelectric-to-ferroelectric phase transition temperature. Similar results were observed for the specimen with x = 0.02, and ΔT slightly increased to 5.7 °C, as displayed in Fig. S6(b). Hence, the specimen with x = 0.02 also shows relaxor characteristics near the TT-O. Figure S6(c) shows the εT33/εo versus temperature curves measured at various frequencies for the specimen with x = 0.04. They were measured near the TR-T peak, which is also a ferroelectric-to-ferroelectric phase transition temperature. The TR-T peak increased with an increase in frequency, and the ΔT was approximately 14 °C. Therefore, it can be concluded that the specimen with x = 0.04 also shows the relaxor characteristic near the TR-T.

The above results show that ΔT increased with an increase in x, indicating that the addition of BAZ increased the relaxor properties of the samples. Moreover, relaxor properties, which are found in the samples with 0.01 ≤ x ≤ 0.04, are observed at the ferroelectric-to-ferroelectric transition temperatures, such as TT-O-R and TR-T. Therefore, they are different from the traditional relaxor properties that were found near TC, that is, the ferroelectric-to-paraelectric phase transition temperature.

Figure S6. εT33/εo versus temperature curves measured at various frequencies for the KNNS-(0.04-x)SZ-xBAZ ceramics with (a) x = 0.01, (b) x = 0.02, and (c) x = 0.04.

8 . SEM images of the thermally etched KNNS-0.01SZ-0.03BAZ thick films

Figure S7(a) shows an SEM image of the thermally etched surface of the KNNS-0.01SZ-0.03BAZ thick film sintered at 1080 °C for 6 h. Two types of grains were developed in this thick film: large grains and small grains, with average grain sizes of 25 μm and 0.5 μm, respectively. The inset shows an enlarged SEM image of the small-sized grains. The relative density of this thick film was low, at 89% of the theoretical density (Fig. 7(c)). However, when the sintering temperature increased, small grains disappeared, and large grains with an average grain size of approximately 25 μm appeared only in the KNNS-0.01SZ-0.03BAZ thick films, as shown in Figs. S7(b) and (c). The microstructures of these thick films are similar to those of the KNNS-0.01SZ-0.03BAZ piezoceramic sintered at 1090 °C. Moreover, these thick films showed high relative densities (≥ 93% of the theoretical density), as shown in Fig. 7(c). Therefore, it is possible that the presence of the small grains can be explained by the insufficient sintering of the thick film, suggesting that the KNNS-0.01SZ-0.03BAZ thick films should be sintered at temperatures higher than 1080 °C.

Figure S7. SEM images of the KNNS-0.01SZ-0.03BAZ thick films sintered at various temperatures; (a) 1080oC, (b) 1100oC and (c) 1110oC.

9. Simulation of actuating properties of planar-type KNNS-0.01SZ-0.03BAZ actuator

The actuating characteristics of the planar-type KNNS-0.01SZ-0.03BAZ actuator were simulated using the COMSOL program, and the parameters used for the measurement of the actuating properties of this actuator were also employed in the simulation. Figure S8(a) shows the variation in the acceleration with respect to the frequency. The maximum acceleration was observed at a resonance frequency of 620 Hz and it increased with an increase in the applied electric field; the largest acceleration of 330 G was obtained at an electric field of 120 V/mm (36 V). A similar resonance frequency of 610 Hz was obtained from the measurement, as shown in Fig. 8(c), and the calculated maximum accelerations at various applied electric fields are displayed as red circles in the inset of Fig. 8(c). The calculated accelerations were similar to the measured accelerations.

Figure S8(b) shows the variation in the simulated displacement of this actuator with respect to the frequency at various applied electric fields. The maximum displacement was also obtained at 620 Hz and it increased with an increase in the electric field, as indicated by the red circles in the inset of Fig. 8(d). When an electric field of 120 V/mm (36 V) was used for the simulation, the largest displacement of 213 μm was obtained, which is similar to the largest measured displacement (231 μm). The above results clearly show that the simulated results are in good agreement with the measured results.

Figure S8. Variations of (a) the acceleration and (b) displacement with respect to the frequency calculated at various electric fields for the KNNS-0.01SZ-0.03BAZ planar-type actuator.