APPENDIX

Fig.3 and Table 1 attached in the appendix are from the data collection from the pilot study that later informed the MDTL framework.

Fig. 3: Categorization of Selected Recyclable Waste

|  | # Material Type | # Before | # After | # Test Results | # Proposed Use |
| --- | --- | --- | --- | --- | --- |
| # Food | # Orange Peel |  |  | # Moderate strength, water resistant, moderate smooth surface, non recyclable. | # Wall tiles, accessories, decorative. |
|  | # Potato Skin |  |  | # Moderate strength, water resistance, tactile surface, non recyclable. | # Wall tiles, accessories, decorative. |
|  | # Peanut Shell |  |  | # Moderate strength, biodegradable, non water proof, tactile surface, biodegradable. | # Acoustic panel, insulation. |
|  | # Coffee Grounds |  |  | # Low strength, non water proof, tactile surface, strong smell, biodegradable. | # Acoustic panel, accessories. |
|  | # Egg Shell |  |  | # Moderate strength, water resistance, smooth surface, non recyclable. | # Wall tiles, accessories, decorative. |
|  | # Banana Peel |  |  | # Very low strength, non water proof, tactile surface, strong smell, biodegradable. | # Not for design use. |
| # Agricultural Waste | # PFL |  |  | # Very low strength, non water proof, tactile surface, strong smell, biodegradable. | # Not for design use. |
|  | # Coconut Husk |  |  | # Low strength, biodegradable, non water proof, tactile surface, biodegradable. | # Acoustic panel, insulation. |
|  | # Cork |  |  | # Moderate Strength, non water proof, smooth surface, biodegradable. | # Acoustic panel, insulation, decorative. |
| # Manufacturing | # PET |  |  | # Moderate strength, waterproof, smooth surface, recyclable. | # Wall tiles, surface tops, accessories, decorative. |
|  | # HDPE |  |  | # Moderate strength, waterproof, tactile surface, recyclable. | # Wall tiles, accessories, decorative. |
|  | # LDPE |  |  | # Low strength, waterproof, soft surface, recyclable. | # Decorative. |
|  | # Paper |  |  | # Moderate strength, non waterproof, tactile surface, recyclable. | # Acoustic panel, insulation, decorative. |
|  | # Egg Tray |  |  | # Low strength, non waterproof, smooth surface, recyclable. | # Wall panel, decorative, accessories. |
|  | # Sawdust |  |  | # Moderate strength, waterproof, smooth surface, non recycleable. | # Blocks, wall tiles, insulation. |

Table 1: New Material Sample, basic testing and proposed use