Supplementary Information

Voltage-driven gigahertz frequency tuning of spin Hall nano-oscillators

Jong-Guk Choi1†, Jaehyeon Park2†, Min-Gu Kang1, Doyoon Kim3, Jae-Sung Rieh3, Kyung-Jin Lee2, Kab-Jin Kim2★ and Byong-Guk Park1★

1 Department of Materials Science and Engineering, KAIST, Daejeon 34141, Korea

2 Department of Physics, KAIST, Daejeon 34141, Korea

3 School of Electrical Engineering, Korea University, Seoul 02841, Korea

- Contents -

Note 1. ST-FMR spectra for various frequencies

Note 2. Voltage-driven frequency modulation in Co/Ni sample with a different thickness

Note 3. Gate voltage effect on the current-induced SOT

Note 4. Threshold current for current-induced magnetization auto-oscillation

Note1. ST-FMR spectra for various frequencies

Figure S1a shows the schematic illustration of the ST-FMR measurement [S1, S2], of which details are discussed in the Method section of the main text. Figures S1b-S1d show the ST-FMR spectra of the Co/Ni sample with different Vg’s for various frequencies ranging from 10 to 21 GHz, measured while sweeping magnetic fields along the z-direction.

Figure S1. ST-FMR measurement of Co/Ni sample for various frequencies. a, Schematic diagram of the device structure of the ST-FMR measurement set-up. b-d, ST-FMR spectra of the Co/Ni sample for various frequencies ranging from 10 to 21 GHz with sequentially applied gate voltages Vg = 0 V (initial) (b), Vg = +5 V (c), and Vg = -5 V (d). The dotted lines are the fitting curves based on Eq. (2) of the main text.

Note 2. Voltage-driven frequency modulation in Co/Ni sample with a different thickness

To show the reproducibility of the voltage-driven frequency modulation, we fabricated another Co/Ni device of Ta (3 nm)/Pt (5 nm)/[Co (0.4 nm)/Ni (0.6 nm)]7/Co (0.4 nm)/AlOx (2 nm), where a slightly thinner Co (0.4 nm) is used compared to the sample used in the main text has a [Ta (3 nm)/Pt (5 nm)/[Co (0.45 nm)/Ni (0.6 nm)]7/Co (0.45 nm)/AlOx (2 nm)]. We first check PMA of the sample using the ST-FMR measurement with the same procedure used in Fig. 2 of the main text. Figure S2 shows the resonance frequency (fres,z) of ST-FMR spectra as a function of the resonance field (Bres,z) for two Co/Ni samples having different Co thicknesses. As the y-intercept indicates the PMA field (Bk) according to the Kittel formula fres,z=γ2π(Bres, z+Bk) [S3], demonstrating that the sample with a thinner Co has a stronger PMA.

We then fabricate an SHNO with a constriction width of 100 nm. The experimental procedure for the power spectral density (PSD) measurement is the same as used in Fig. 3 of the main text, except for a dc current (Idc) of 1.8 mA used. Figures S3a-S3c show the color plots of PSD as a function of a magnetic field (B), where gate voltages of +5 V and -3V were sequentially applied. The auto-oscillation peak is clearly observed, and its frequency is increased by the positive voltage and restored by the subsequent negative voltage. Figure S3d shows the auto-oscillation spectra for a magnetic field of B=0.9 T for different gate voltages, extracted from Figs. S3c-S3g. The frequency modulation of the sample with a thinner Co is about a few GHz, confirming the reproducibility of the voltage-driven frequency modulation of the SHNO.

Figure S2. ST-FMR measurement. Resonance frequency (fres,z) of ST-FMR spectra as a function of the resonance field (Bres,z) for the samples of Ta (3 nm)/Pt (5 nm)/[Co (0.45 nm)/Ni (0.6 nm)]7/Co (0.45 nm)/AlOx (2 nm) (black squares) and Ta (3 nm)/Pt (5 nm)/[Co (0.4 nm)/Ni (0.6 nm)]7/Co (0.4 nm)/AlOx (2 nm) structures (red circles).

Figure S3. Voltage-driven frequency modulation in SHNO of Ta (3 nm)/Pt (5 nm)/[Co (0.4 nm)/Ni (0.6 nm)]7/Co (0.4 nm)/AlOx (2 nm). a-c, PSDs versus a magnetic field for sequentially applied gate voltages, Vg = 0 V (initial state) (a), Vg = +5 V (b), and Vg = -3 V (c). Idc= 1.8 mA. d, Auto-oscillation spectra for B=0.9 T for different gate voltages, extracted from Figs. S3c-S3g. The yellow line is the Lorentz fit of the auto-oscillation spectra.

Note 3. Gate voltage effect on the current-induced SOT

We investigated the gate voltage effect on current-induced spin-orbit torque (SOT) using in-plane harmonic measurements. For the measurement, we fabricated a Hall bar device with a 10 μm × 10 μm cross using the Ta (3 nm)/Pt (5 nm)/[Co (0.45 nm)/Ni (0.6 nm)]7/Co (0.45 nm)/AlOx (2 nm) film. The first and second harmonic Hall resistance (R1ω and R2ω) were simultaneously measured with an a.c. current of 15 mA and a frequency of 11 Hz while rotating the sample (azimuthal angle φ) under an in-plane magnetic field (Bext). The Bext ranges from 0.3 T to 4.0 T, which is larger than the perpendicular magnetic anisotropy field (Bk), so the magnetization is aligned in the magnetic field direction. The gate voltage was applied to the top electrode for 5 minutes at 150 ℃ before the measurement. Figure S4a shows the R2ω as a function of φ under a magnetic field of 0.6 T for various gate voltages. The R2ω can be expressed as [S4, S5],

R2ωφ=RAHEBDLTBeff+R∇Tcosφ+2RPHEBFLTBext2cos3φ-cosφ,   (2)

where RAHE, RPHE and R∇T2ω are the anomalous Hall resistance, planar Hall resistance and thermal effect contribution, respectively; BDLT and BFLT are the damping-like effective field and field-like effective field including Oersted field, respectively; Beff is the effective magnetic field (Beff=Bext-Bk). Figures S4b and S4c show the magnetic field-dependence of the cosφ and (2cos3φ-cosφ) components of R2ω, respectively. Figure S4d demonstrates that the extracted BDLT and BFLT values of the sample, which are not changed by the gate voltage.

Figure S4. Gate voltage effect on current-induced SOT. a, Second-harmonic Hall resistance R2ω versus azimuthal angle φ under an in-plane magnetic field of 0.6 T for sequentially applied gate voltages. b, cosφ component of R2ω as a function of 1/Beff for sequentially applied gate voltages. c, (2cos3φ-cosφ) component of R2ω as a function of 1/Bext for sequentially applied gate voltages. The gate voltages were applied in the sequence indicated by the black arrows in Figs. S4a-S4c. d, The variation of the SOT-induced BDLT (black square) and BFLT (black triangle) values with sequentially applied gate voltages.

Note 4. Threshold current for current-induced magnetization auto-oscillation

We determine the threshold current (Ith) at which auto-oscillation begins to occur by a linear fit of the inverse of the PSD integral. Figures S5a-S5e show the (integral of PSD)-1 versus current for sequentially applied gate voltages, where Ith is obtained by the x-intercept of the linear fit (solid red lines) [S6, S7]. Figure S4f displays the variation of Ith with gate voltages, which is the same as Fig. 4f in the main text.

Figure S5. Threshold current for current-induced magnetization auto-oscillation. a-e, (integral of PSD)-1 as a function of current for sequentially applied gate voltages, Vg = 0V (initial) (a), Vg = +4 V (b), Vg = +5 V (c), Vg = -2 V (d), and Vg = -3 V (e). B=0.52 T. f,  Ith according to the sequentially applied gate voltages, extracted from Figs. S5a-S5e.

References

- Liu, L., Moriyama, T., Ralph, D. C. & Buhrman, R. A. Spin-torque ferromagnetic resonance induced by the spin Hall effect. Phys. Rev. Lett. 106, 306601 (2011).

- Kim, J. H. et al. Spin-orbit torques associated with ferrimagnetic order in Pt/GdFeCo/MgO layers. Sci. Rep. 8, 6017 (2018).

- Beaujour, J.-M., Ravelosona, D., Tudosa, I., Fullerton, E. E. & Kent, A. D. Ferromagnetic resonance linewidth in ultrathin films with perpendicular magnetic anisotropy. Phys. Rev. B 80, 180415(R) (2009).

- Hayashi, M., Kim, J., Yamanouchi, M. & Ohno, H. Quantitative characterization of the spin-orbit torque using harmonic Hall voltage measurements. Phys. Rev. B 89, 144425 (2014).

- Avci, C. O. et al. Interplay of spin-orbit torque and thermoelectric effects in ferromagnet/normal-metal bilayers. Phys. Rev. B 90, 224427 (2014).

- Tiberkevich, V., Slavin, A. & Kim, J. Von. Microwave power generated by a spin-torque oscillator in the presence of noise. Appl. Phys. Lett. 91, 192506 (2007).

- Awad, A. A., Houshang, A., Zahedinejad, M., Khymyn, R. & Åkerman, J. Width dependent auto-oscillating properties of constriction based spin Hall nano-oscillators. Appl. Phys. Lett. 116, 232401 (2020).