Supporting Information

Development of a multifunctional nanocomposite film with record-high ultralow temperature toughness and unprecedented fatigue-resistance

Shuaicheng Jianga, Yanqiang Weia, Jiongjiong Lia, Xiaona Lia, Kaili Wanga, Kuang Lia, Sheldon Q. Shib, Jianzhang Li*,c and Zhen Fang*,d,e

aCollege of Materials Science and Engineering, Nanjing Forestry University, Nanjing, Jiangsu 210037, China

bDepartment of Mechanical Engineering, University of North Texas, Denton, 76203, United States

cCollege of Materials Science and Engineering, Beijing Forestry University, Beijing 100083, China

dDepartment of Biochemistry & Molecular Biology, Michigan State University, 603 Wilson Road, East Lansing, Michigan, 48824, United States

eGreat Lakes Bioenergy Research Center - Michigan State University, 1129 Farm Lane, East Lansing, Michigan 48824, United States

*Corresponding authors: lijzh@bjfu.edu.cn (J. Li); fangzhe8@msu.edu (Z. Fang)

Experimental Section

Materials: SPI (95 % protein), hydrogen peroxide (30 wt%), sodium hydroxide (NaOH, AR), D (+)-glucose (AR), boron nitride (99.9% metals basis, 1-2μm), poly(vinyl alcohol) 1788 (87.0-89.0%), glutaraldehyde (25 wt% BR), polyethylene glycol 200 (H(OCH2CH2)nOH) were supplied by Nanjing Chemical Reagents Co., Ltd. (Nanjing, China). Deionized water was used for all experiments.

Exfoliation of h-BN: The liquid phase exfoliation of h-BN was prepared according to a previous work1. Briefly, 10 g of h-BN powders was added into 500 mL of deionized water. The suspension was sonicated in a FS-450N model sonication bath (Shanghai ShengXi Ultrasonic Instrument Co., LTD) for 3 h with a frequency of 200 kHz. The resulting dispersion was centrifuged using TGL-15B supercentrifuge (Shanghai MeiYingPu Instrument Manufacturing Co., LTD, China) at 6000 rpm for 8 min to remove nonexfoliated h-BN. The supernatants were collected and centrifuged at 10000 rpm for 25 min to collect the exfoliated BN nanosheets.

Preparation of SPI-lignin: Firstly, lignin was extracted from poplar by ethanol following the method reported by Pan et al2. Then, 2 g of lignin and N, N-dimethyl formamide (DMF, 50 mL) was added into a three necked flask. After stirring for 5 min, the pH was adjusted to about 10 and the temperature was raised to 80-90 °C, then glutaraldehyde solution (4 g, 25 wt%) and SPI solution (10 g, 1 wt%) were slowly added into the three necked flasks, in which the dropping was completed within 10-20 min. The mixture was stirred for 3 h then cooled to collect SPI-lignin (yield: 40%, brown).

Preparation of D (+)-glucose quantum dots (QDs): QDs were prepared according to a previous work3. Firstly, 2 g of glucose and 10 mL of PEG-200 were dissolved into 3 mL of distilled water to form a clear solution. Then the solution was put into a domestic microwave oven for 2 min. Transmission electron microscopy (TEM) were carried out with JEM-2000 FX operating at 200 kV accelerating voltage.

Preparation of HBPA-1, HBPA-2, and QDs-CHO: The HBPA-1, HBPA-2, and QDs-CHO were prepared according to a previous work4-6. Hydroxyl-containing hyperbranched polysiloxane fabrication (HBPA-1): Firstly, glycerol (46 g, 0.5 mol) and maleic anhydride (49 g, 0.5 mol) were mixed in a three-necked glass reactor flask at 75 °C under N2 while stirring continuously for 1 h. Secondly, pentaerythritol (0.454 g, 0.005 mol) was dissolved in a small volume of water, added it to the intermediate, and the resulting solution was maintained at 100 °C for 2 h, 120 °C for 2 h, and 140 °C for 4 h. Hydroxyl and primary amine-containing hyperbranched polysiloxane fabrication (HBPA-2): Firstly, 1.0 mol of (3-Aminopropyl) triethoxysilane (APTES) and 1.9 mol of 2-methyl-1,3-propanediol (MPD) were added into a three-necked flask with a mechanical stirrer and a thermometer under nitrogen condition. Then the mixture was heated to about 110 °C for a certain time till some distillate was distilled off. After that, the mixture was continuously heated to around 160 °C (the distillate temperature was kept below 78 °C). Finally, the hydroxyl and primary amine-containing hyperbranched polysiloxane was obtained after the distillate temperature dropped below 55 °C. QDs-CHO fabrication: Glutaraldehyde (300 µL) and ethanol (600 µL) were added to a pressure vessel and heated in an oven at 150 °C for 2 h. After cooling down, the resultant brown solid was redispersed in acetone and chloroform and centrifuged at 10 000 rpm for 15 min to remove high-weight carbon aggregates. The whole procedure was repeated three times for each solvent and finally the solution was evaporated under reduced pressure to obtain a brown solid.

Preparation of bioinspired self-assembled bio-nanocomposite films: A mixture of 10% PVA dispersion (50 g) and 2% BN nanosheets dispersion (50 g) was mechanically stirred for 1 h, and then SPI-lignin (0.2 g) was added. After stirring for an additional 0.5 h, QDs (0.2 g) were added into the resulting mixture, and the stirring was continued for 1 h until a uniform mixed solution was obtained. After 30 minutes of ultrasonic degassing, the mixed solution was poured into a disposable culture dish and dried in an oven at 55 °C for 12 h. The bionanocomposite films were stored in a desiccator (25 °C and 50% RH) for 7 days, and then the subsequent tests were carried out.

Mechanical property measurements: The mechanical performance of the composites was evaluated using an electron universal testing machine (AGS-X, Japan). The samples were conditioned (50 ± 2% relative humidity, 25 ± 2 °C) in a desiccator for 48 h before tests. Film samples with dimensions of 10 mm × 80 mm (width × length) were tested at a tensile speed of 20 mm/min. The thickness of the films was determined with a digimatic micrometer. The result for each sample was recorded by testing specimens in quintuplicate. The dynamic mechanical behavior of the composites was analyzed on a dynamic thermomechanical analysis analyzer (DMA, Q850, TA Instruments, USA) from 20 to 180 °C at a heating rate of 5 °C min-1 under an air atmosphere. The average values were obtained by measuring at least five samples.

Self-healing property measurements: Firstly, a 1 cm notch was drawn in the PVA-BN-QDs-SPI-lignin strip with a knife, and then moistened with deionized water. The self-healing conditions of the sample at 25 °C (humidity was 50%) were recorded using a camera. The tensile test of the sample after self-healing was measured. Each test type was repeated at least six times and averaged results were reported.

Folding fatigue-resistant property measurements: The folding fatigue-resistant performance of the composites was evaluated using an MIT folding tester (Shenzhen PuYu Electronic Co. Ltd). The samples were conditioned (50 ± 2% relative humidity, 25 ± 2 °C) in a desiccator for 48 h before tests. Film samples with dimensions of 10 mm × 80 mm (width × length) were tested at a folding speed of 200 times/min. The thickness of the films was determined with a digimatic micrometer. The result for each sample was recorded by testing specimens in quintuplicate.

Characterizations: The bonding characteristics were examined using Fourier transform infrared spectroscopy (FTIR, Nicolet iS50 Thermo Fisher Scientific Co., Ltd, USA). FTIR spectra were recorded from 500 to 4000 cm-1 with a resolution of 4 cm-1 at ambient temperature for 32 scans. Rheological test was carried out on an RST-CPS rheometer using a 50 mm parallel-plate at room temperature. The elemental compositions and chemical structures of PVA-BN-QDs-SPI-lignin were examined by X-ray photoelectron spectroscopy (XPS, AXIS UltraDLD, Britain) and X-ray diffraction patterns (XRD, Ultima IV analyzer, Rigaku, Japan). Thermogravimetric analysis (TGA) of the SPI-based nanocomposite film (around 5 mg) was performed on a TGA55 instrument (Waters, USA) in the temperature range of 25 - 800 °C at a heating rate of 10 °C min-1 under N2 with a flow rate of 100 mL min-1. The UV-vis absorption spectra were obtained in the 200-800 nm range using a UV lamp (PE Lambda950). The samples were cut into rectangles (5 cm × 2 cm). Morphology and structure of films were observed with scanning electron microscope (SEM, Quanta 200, USA). The morphology of the BN nanosheets were also observed by a TEM (JEM-2010, JEOL, Japan) at an acceleration voltage of 200 kV and AFM (Nanoscope IIIa, Multimode apparatus, Veeco Instruments). The TEM samples were prepared by dropping a few drops of the BN nanosheets solution on a carbon-coated cooper grid and air-dried before measurement. AFM samples were prepared by dropping a few drops of the BN nanosheets aqueous solutions onto freshly exfoliated mica substrates and drying. Small-angle X-ray scattering (SAXS) analyses of the as-fabricated and stretched composite films were carried out using a SAXSess mc2 nanostructure analyzer (Anton Paar, Austria), using Cu Kα radiation (λ = 0.15406 nm) with a voltage at 40 kV and current at 30 mA.

Biodegradable performance: The oven-dried composite films (20 mm × 20 mm, width × length) were wrapped by plastic mesh and immersed in the soil inoculation source. Finally, the films were weighted every 7 days and the weight residue was calculated based on the weight ratio between the degraded film and the original film.

Mechanical property measurements in wet conditions: The mechanical performance of the composites was evaluated using an electron universal testing machine (AGS-X, Japan). Firstly, the films were stored at RH 80% for 30 days, and then films with dimensions of 10 mm × 80 mm (width × length) were tested at a tensile speed of 20 mm/min. The thickness of the films was determined with a digimatic micrometer. The average values were obtained by measuring at least five samples.

Mechanical property measurements in liquid N2:  The mechanical performance of the films was examined in liquid N2 by an electron universal testing machine (AGS-X, Japan) with a tensile speed of 20 mm/min. The thickness of the films was determined with a digimatic micrometer. The average values were obtained by measuring at least five samples.

Cryogenic tolerance of the films: The cryogenic tolerance experiments were carried out by testing the mechanical property of the films suffering from different cryogenic temperature. Firstly, the mechanical performance of the films was tested in different cryogenic temperature by an electron universal testing machine (AGS-X, Japan) with a tensile speed of 20 mm/min. During the test, liquid N2 was used to maintain the temperature, and a digital thermometer (DTM-280) was used to monitor the temperature in real time. The thickness of the films was determined with a digimatic micrometer. The average values were obtained by measuring at least five samples.

Differential Scanning Calorimetry (DSC) curves: Differential scanning calorimetry (DSC) analysis was operated on a DSC 250 (TA instruments, USA) under nitrogen atmosphere. The temperature ranged from -140 to 40 °C and the heating rate was set at 20 °C min-1.

Variable-temperature X-ray diffraction (XRD) patterns: The BRUKER D8-Discover diffractometer with Cu Kα radiation (λ = 1.5406 Å, operation voltage 40 kV, current 40 mA) was employed to obtain the variable-temperature XRD patterns of films with the scan speed of 5°/min and the scan range from 10° to 50°.

Figure S1. Synthesis of SPI-lignin and a schematic illustration of three-dimensional (3D) chain microstructure of SPI-lignin.

Figure S2. a FTIR spectra and b TGA curves of BN and functionalized BN-OH. c The SEM image of BN nanosheet.

Figure S3. The TEM image of QDs.

Figure S4. a Tensile stress-strain curves, b tensile strength, and c toughness of films made by pure PVA and PVA-BN.

Figure S5. a Large-sized PVA-BN-QDs-SPI-Lignin nanocomposite with a volume of 250× 250 × 0.2 mm. b The external packing produced from the PVA-BN-QDs-SPI-Lignin nanocomposite.

Figure S6. SAXS scattering profiles of PVA-BN, PVA-BN-QDs, PVA-BN-SPI-lignin, PVA-BN-QDs-SPI-lignin, and PVA-BN-QDs-SPI-lignin-200%. The sample shows an arc-like scattering feature on the 2D pattern of SAXS. The 2D SAXS patterns are gradually elongated, and the prestrain increases from 0 to 200%. The corresponding scattering peak increases gradually which demonstrates that stretching the film can improve the molecular orientation of the PVA-BN-QDs-SPI-lignin.

Figure S7. a Tensile strength of PVA-BN-QDs-SPI-lignin treated with different conditions, including repeated folding for 0, 500, 1000, 10 000 times, after self-healing, and storage at RH:80% for 30 days. b Typical strain-stress curves of PVA-BN-QDs, PVA-BN-SPI-lignin, and PVA-BN-QDs-SPI-lignin maintained at RH 80% for 30 days.

Figure S8. Optical photographs of the stability of PVA-BN-QDs, PVA-BN-SPI-lignin, and PVA-BN-QDs-SPI-lignin (order: left to right) nanocomposite samples in oil and ethyl acetate. At t= 96 h, PVA-BN-QDs, PVA-BN-SPI-lignin were already fully solubilized in oil, while PVA-BN-QDs-SPI-lignin demonstrated an excellent oil resistance and stability.

Figure S9. a-c Typical strain-stress curves of PVA-BN-SPI-lignin, PVA-BN-QDs, and PVA-BN-QDs-SPI-lignin ranged from -196 °C to 25 °C. and d-e Typical strain-stress curves of PVA-BN-HBPA-1, PVA-BN-HBPA-2, PVA-BN-QDs-CHO, and Pure-PVA at -196 °C and 25 °C.

Table S1. Mechanical properties of the nanocomposites.

| Samples | Strain at break (%) | Tensile strength (MPa) | Young’s modulus (MPa) | Tensile toughness (MJ/m3) |
| --- | --- | --- | --- | --- |
| PVA-BN-QDs | 339.4 | 45 | 320 | 77.9 |
| PVA-BN- SPI-Lignin | 169.9 | 24.9 | 80.5 | 21.3 |
| PVA-BN-QDs-SPI-Lignin | 480 | 53.3 | 219.3 | 182.8 |

Table S2. Comparison of the mechanical properties of PVA-BN-QDs-SPI-Lignin with other nanocomposite materials.

| Samples | Tensile strength (MPa) | strain at break (%) | Reference |
| --- | --- | --- | --- |
| Cellulose-polyurethane acrylate | 55 | 58 | 7 |
| Lignocellulosic | 38.3 | 4.40 | 8 |
| Starch/AEEP | 21.6 | 40 | 9 |
| SPI-PEI-PDA | 10.01 | 115 | 10 |
| PS/BNNS | 37.8 | 3.5 | 11 |
| BN/PVA | 30 | 2.5 | 12 |
| PVA/BNNS | 5.2 | 28 | 13 |
| CNF/BNNS | 38.8 | 2 | 14 |
| CNF/EOH-BNNS | 45.54 | 14.25 | 15 |
| GNS/PBONF | 137.5 | 30.7 | 16 |
| VPVA | 48.2 | 15.4 | 17 |
| VPVA–HA | 55.6 | 59.7 | 17 |
| SPI/CNC-CHO | 14 | 145 | 18 |
| PVA-BN-QDs-SPI-Lignin | 53.3 | 480 | This work |

Table S3. Toughness and strain of PVA-BN-QDs-SPI-Lignin nanocomposite and other nanocomposite materials.

| Composites | Strain at break (%) | Tensile toughness (MJ/m3) | Reference |
| --- | --- | --- | --- |
| MTM/PVA 70/30 | 1.7 | 2.1 | 19 |
| MTM/PVA-PVAm 50/50 | 40.8 | 21.0 | 20 |
| LAP/PVA 42/58 | 22.0 | 12.5 | 21 |
| RGO/PVA 58/42 | 10.4 | 8.5 | 22 |
| RGO/PAPB 92/8 | 4.3 | 7.5 | 23 |
| GO/PDA-UPy 85/15 | 5.3 | 11.1 | 24 |
| GO/PAA 95/5 | 7.9 | 8.9 | 25 |
| MTM/NFC 50/50 | 2.8 | 2.3 | 26 |
| GNS/PBONF-X 60/40 | 34.0 | 34.4 | 16 |
| PVA/LA-5 | 282 | 219.2 | 27 |
| PVA/LA-10 | 129 | 80.4 | 27 |
| RGO/CS | 10.4 | 17.7 | 28 |
| MXene/NFC | 16.7 | 14.8 | 29 |
| SPI/BN | 13.3 | 2.58 | 30 |
| PVA-BN-QDs-SPI-Lignin | 480 | 182.8 | This work |

Table S4. Mechanical properties of the PVA-BN-QDs-SPI-Lignin nanocomposite after repeated folding for 0, 500, 1000, and 10 000 times.

| Folding times | Strain at break (%) | Tensile strength (MPa) | Young’s modulus (MPa) | Tensile toughness (MJ/m3) |
| --- | --- | --- | --- | --- |
| 0 | 480 | 53.3 | 219.3 | 182.8 |
| 500 | 426.2 | 49.5 | 493.6 | 182.2 |
| 1000 | 317 | 48 | 360 | 115.9 |
| 10000 | 211.2 | 28.8 | 108.3 | 34 |

Table S5. Tensile strength, stress, healing conditions, and healing efficiency of the PVA-BN-QDs-SPI-Lignin self-healable nanocomposite and other self-healable polymers.

| Substances | Strain at break (%) | Tensile strength (MPa) | Healing conditions | Healing efficiency | Reference |
| --- | --- | --- | --- | --- | --- |
| Boronic esters | 4.4 | 58 | 25 °C/72 h (85% humidity) | ≈90 | 31 |
| Chitosan | 0.026 | 76.1 | 25 °C/2 h | 100 | 32 |
| Polybutadiene | 3.25 | 380 | 110 °C/12 h | 75 | 33 |
| DFTPA-PI-MA | 3 | 118 | 110 °C/3 min and 60 °C/24 h | 90.7 | 34 |
| Polybenzoxazine | 0.12 | 100 | 25 °C/12 h (pressure) | 96 | 35 |
| Poly(urethane urea)s | 0.93 | 301 | 37 °C/12 h | 87 | 36 |
| PDMS | 0.7 | 115 | 25 °C/4 h | 75 | 37 |
| PDMS-boroxine | 9.46 | 9.72 | 70 °C/5 h | 95 | 38 |
| Polycyclooctene | 1.85 | 345 | 50 °C/16 h | ≈100 | 39 |
| Polyurethane | 6.76 | 923 | 25 °C/2 h | ≈80 | 40 |
| Polyacrylate | 17.89 | 38.92 | 60 °C/24 h | 95.81 | 41 |
| Polysaccharide | 0.12 | 600 | 25 °C/24 h | 87.7 | 42 |
| PAA/CS | 3.7 | 1200 | 70 °C/24 h | 58.33 | 43 |
| PAA/agar/PVA | 0.45 | 497 | 25 °C/24 h | 84 | 44 |
| 1NDI/CNC | 0.5-3.25 | 10-20 | 85 °C/5-20 min | ≈100 | 45 |
| PVA-BN-QDs-SPI-Lignin | 49.1 | 434.5 | 25 °C/2 min (H2O) | ≈100 | This work |

Table S6. Comparison of stress and toughness of PVA-BN-QDs-SPI-Lignin with other nanocomposites materials.

| Types | Materials | Strain at break (%) | Tensile strength (MPa) | Reference |
| --- | --- | --- | --- | --- |
| Platelet/polymer | MTM/PVA 70/30 | 1.7 | 2.1 | 19 |
|  | MTM/CS 65/35 | 2.3 | 1.3 | 46 |
|  | MTM/PDDA 70/30 | 2.1 | 1.4 | 47 |
|  | NHT/EG-UPy 50/50 | 1.3 | 3.2 | 48 |
|  | MTM/PVA-PVAm 50/50 | 40.8 | 21.0 | 20 |
|  | LAP/PVA 42/58 | 22.0 | 12.5 | 21 |
|  | RGO/PDA 95/5 | 5 | 4 | 49 |
|  | RGO/CS 95/5 | 10.4 | 17.7 | 28 |
|  | RGO/MoS2-TPU 86/14 | 5.8 | 6.9 | 50 |
|  | RGO/CS-Cu+ 91/9 | 4.4 | 14.0 | 51 |
|  | RGO/PVA 58/42 | 10.4 | 8.5 | 22 |
|  | RGO/PAPB 92/8 | 4.3 | 7.5 | 23 |
|  | GO/PDA-UPy 85/15 | 5.3 | 11.1 | 24 |
|  | GO/Al2O3-CMC 8/92 | 5 | 8.2 | 52 |
|  | GO/PAA 95/5 | 7.9 | 8.9 | 25 |
| Platelet/nanofiber | MTM/NFC 50/50 | 2.8 | 2.3 | 26 |
|  | MXene/NFC 50/50 | 16.7 | 14.8 | 29 |
|  | Aminoclay/TOCN 33/67 | 11.7 | 20 | 53 |
|  | RGO/TOCN 95/5 | 6.2 | 15.6 | 54 |
|  | RGO/DWNT-PCDO 95/5 | 7.9 | 9.2 | 55 |
| Platelet/3D | CaCO3/chitin 95/5 | 2 | 1.8 | 56 |
| nanofiber network | GNS/PBONF-X 60/40 | 34.0 | 34.4 | 16 |
| PVA-BN-QDs-SPI-Lignin | Folding 0 | 480 | 182.8 | This work |
|  | Folding 500 | 426.2 | 182.2 | This work |
|  | Folding 1000 | 317 | 115.9 | This work |
|  | Folding 10000 | 211.2 | 34 | This work |
|  | Self-healing | 434.5 | 130.5 | This work |

Note: MTM: montmorillonite, PVA: poly(vinyl alcohol), CS: chitosan, PDDA: poly(diallyldimethyl-ammonium chloride), NHT: sodium fluorohectorite, EG-UPy: ureidopyrimidinone-containing poly(ethylene glycol methacrylate) copolymer, LAP: Laponite, PVAm: polyvinylamine, RGO: reduced graphene oxide, PDA: poly(dopamine), TPU: thermoplastic polyurethane, CMC: sodium carboxymethyl Cellulose, GO: graphene oxide, PDA-UPy: ureidopyrimidinone-containing poly(dopamine), PAPB: poly(acrylic acid-co-(4-acrylamidophenyl) boronic acid), PAA: polyacrylic acid, NFC: nanofibrillar cellulose, DWNT: double-walled carbon nanotube, TOCN: TEMPO-oxidized cellulose nanofibril.

Table S7. Comparison of tensile strength of PVA-BN-QDs-SPI-Lignin nanocomposite (folding 1000 times or after self-healing) with typical polymers.

| Typical polymers | Tensile strength (MPa) |
| --- | --- |
| ABS | 27.6-55.2 |
| Polycarbonate (PC) | 60-72.4 |
| Polyethylene (PE) | 20.7-44.8 |
| PET | 48.3-72.4 |
| Acrylic (PMMA) | 48.3-79.6 |
| Acetal (POM) | 60-89.6 |
| Polypropylene (PP) | 27.6-41.4 |
| Cellulose polymers (CA) | 25-50 |
| Polystyrene (PS) | 35.9-56.5 |
| Polyurethane thermoplastics (TPU) | 31-62 |
| PVC | 40.7-65.1 |
| Teflon (PTFE) | 20-30 |
| Epoxies | 45-89.6 |
| Phenolics | 34.5-62.1 |
| Polyester | 41.4-89.6 |
| Folding 1000 times | 48±2 |
| After self-healing | 49.1±1 |

References

1.	Qi, X., Yang, L., Zhu, J., Hou, Y. & Yang, M. Stiffer but more healable exponential layered assemblies with boron nitride nanoplatelets. ACS Nano 10, 9434-9445 (2016).

2.	Pan, X. J., Kadla, J. F., Ehara, K., Gilkes, N. & Saddler, J. N. Organosolv ethanol lignin from hybrid poplar as a radical scavenger: relationship between lignin structure, extraction conditions, and antioxidant activity. J. Agric. Food Chem. 54, 5806-5813 (2006).

3.	Zhu, H. et al. Microwave synthesis of fluorescent carbon nanoparticles with electrochemiluminescence properties. Chem. Commun. 34, 5118-5120 (2009).

4.	Gu, W. et al. Tough, strong, and biodegradable composite film with excellent UV barrier performance comprising soy protein isolate, hyperbranched polyester, and cardanol derivative. Green Chem. 21, 3651-3665 (2019).

5.	Li, J. et al. Facile fabrication of tough, strong, and biodegradable soy protein-based composite films with excellent UV-blocking performance. Compos. Part B 211, 108645 (2021).

6.	Chen, S., Sun, T., Zheng, M. & Xie, Z. Carbon dots based nanoscale covalent organic frameworks for photodynamic therapy. Adv. Funct. Mater. 30, 2004680 (2020).

7.	Li, W., Wu, Y., Liang, W., Li, B. & Liu, S. Reduction of the water wettability of cellulose film through controlled heterogeneous modification. ACS Appl. Mater. Interfaces 6, 5726-5734 (2014).

8.	Chen, M., Zhang, X., Liu, C., Sun, R. & Lu, F. Approach to renewable lignocellulosic biomass film directly from bagasse. ACS Sustain. Chem. Eng. 2, 1164-1168 (2014).

9.	Soeyler, Z. & Meier, M. A. R. Sustainable functionalization of cellulose and starch with diallyl carbonate in ionic liquids. Green Chem. 19, 3899-3907 (2017).

10.	Chang, Z. et al. Self-healable and biodegradable soy protein-based protective functional film with low cytotoxicity and high mechanical strength. Chem. Eng. J. 404, 126505 (2021).

11.	Wang, X. & Wu, P. Preparation of highly thermally conductive polymer composite at low filler content via a self-assembly process between polystyrene microspheres and boron nitride nanosheets. ACS Appl. Mater. Interfaces 9, 19934-19944 (2017).

12.	Wang, J. et al. Super-compatible functional boron nitride nanosheets/polymer films with excellent mechanical properties and ultra-high thermal conductivity for thermal management. J. Mater. Chem. C 6, 1363-1369 (2018).

13.	Chen, J., Wei, H., Bao, H., Jiang, P. & Huang, X. Millefeuille-inspired thermally conductive polymer nanocomposites with overlapping BN nanosheets for thermal management applications. ACS Appl. Mater. Interfaces 11, 31402-31410 (2019).

14.	Wu, K. et al. Achieving a collapsible, strong, and highly thermally conductive film based on oriented functionalized boron nitride nanosheets and cellulose nanofiber. ACS Appl. Mater. Interfaces 9, 30035-30045 (2017).

15.	Wu, K. et al. Preparation of a thermally conductive biodegradable cellulose nanofiber/hydroxylated boron nitride nanosheet film: the critical role of edge-hydroxylation. J. Mater. Chem. A 6, 11863-11873 (2018).

16.	Wang, Y., Xia, S., Li, H. & Wang, J. Unprecedentedly tough, folding-endurance, and multifunctional graphene-based artificial nacre with predesigned 3D nanofiber network as matrix. Adv. Funct. Mater. 29, 1903876 (2019).

17.	Li, Y., Li, S. & Sun, J. Degradable poly(vinyl alcohol)-based supramolecular plastics with high mechanical strength in a watery environment. Adv. Mater. 33, 2007371 (2021).

18.	Xie, D.-Y., Qian, D., Song, F., Wang, X.-L. & Wang, Y.-Z. A fully biobased encapsulant constructed of soy protein and cellulose nanocrystals for flexible electromechanical sensing. ACS Sustain. Chem. Eng. 5, 7063-7070 (2017).

19.	Walther, A. et al. Large-area, lightweight and thick biomimetic composites with superior material properties via fast, economic, and green pathways. Nano Lett. 10, 2742-2748 (2010).

20.	Eckert, A., Rudolph, T., Guo, J., Mang, T. & Walther, A. Exceptionally ductile and tough biomimetic artificial nacre with gas barrier function. Adv. Mater. 30, 1802477 (2018).

21.	Das, P. et al. Nacre-mimetics with synthetic nanoclays up to ultrahigh aspect ratios. Nat. Commun. 6, 5967 (2015).

22.	Zhao, N. et al. Superstretchable nacre-mimetic graphene/poly(vinyl alcohol) composite film based on interfacial architectural engineering. ACS Nano 11, 4777-4784 (2017).

23.	Zhang, M., Huang, L., Chen, J., Li, C. & Shi, G. Ultratough, ultrastrong, and highly conductive graphene films with arbitrary sizes. Adv. Mater. 26, 7588-7592 (2014).

24.	Wang, Y. et al. Artificial nacre from supramolecular assembly of graphene oxide. ACS Nano 12, 6228-6235 (2018).

25.	Wan, S. et al. Nacre-inspired integrated strong and tough reduced graphene oxide-poly(acrylic acid) nanocomposites. Nanoscale 8, 5649-5656 (2016).

26.	Liu, A., Walther, A., Ikkala, O., Belova, L. & Berglund, L. A. Clay nanopaper with tough cellulose nanofiber matrix for fire retardancy and gas barrier functions. Biomacromolecules 12, 633-641 (2011).

27.	Zhang, X., Liu, W., Yang, D. & Qiu, X. Biomimetic supertough and strong biodegradable polymeric materials with improved thermal properties and excellent uv-blocking performance. Adv. Funct. Mater. 29, 1806912 (2019).

28.	Wan, S. et al. Use of synergistic interactions to fabricate strong, tough, and conductive artificial nacre based on graphene oxide and chitosan. ACS Nano 9, 9830-9836 (2015).

29.	Cao, W.-T. et al. Binary strengthening and toughening of mxene/cellulose nanofiber composite paper with nacre-inspired structure and superior electromagnetic interference shielding properties. ACS Nano 12, 4583-4593 (2018).

30.	Jiang, S. et al. Nacre-inspired strong and multifunctional soy protein-based nanocomposite materials for easy heat-dissipative mobile phone shell. Nano Lett. 21, 3254-3261 (2021).

31.	Cash, J. J., Kubo, T., Bapat, A. P. & Sumerlin, B. S. Room-temperature self-healing polymers based on dynamic-covalent boronic esters. Macromolecules 48, 2098-2106 (2015).

32.	Qu, J. et al. Antibacterial adhesive injectable hydrogels with rapid self-healing, extensibility and compressibility as wound dressing for joints skin wound healing. Biomaterials 183, 185-199 (2018).

33.	Xiang, H. P., Qian, H. J., Lu, Z. Y., Rong, M. Z. & Zhang, M. Q. Crack healing and reclaiming of vulcanized rubber by triggering the rearrangement of inherent sulfur crosslinked networks. Green Chem. 17, 4315-4325 (2015).

34.	Zheng, R. et al. Intelligent biomimetic chameleon skin with excellent self-healing and electrochromic properties. ACS Appl. Mater. Interfaces 10, 35533-35538 (2018).

35.	Arslan, M., Kiskan, B. & Yagci, Y. Benzoxazine-based thermosets with autonomous self-healing ability. Macromolecules 48, 1329-1334 (2015).

36.	Ying, H., Zhang, Y. & Cheng, J. Dynamic urea bond for the design of reversible and self-healing polymers. Nat. Commun. 5, 3218 (2014).

37.	Roy, N., Buhler, E. & Lehn, J.-M. Double dynamic self-healing polymers: supramolecular and covalent dynamic polymers based on the bis-iminocarbohydrazide motif. Polym. Int. 63, 1400-1405 (2014).

38.	Lai, J.-C. et al. A stiff and healable polymer based on dynamic-covalent boroxine bonds. Adv. Mater. 28, 8277-8282 (2016).

39.	Cromwell, O. R., Chung, J. & Guan, Z. Malleable and self-healing covalent polymer networks through tunable dynamic boronic ester bonds. J. Am. Chem. Soc. 137, 6492-6495 (2015).

40.	Barthel, M. J. et al. Self-healing materials via reversible crosslinking of poly(ethylene oxide)-block-poly(furfuryl glycidyl ether) (PEO-b-PFGE) block copolymer films. Adv. Funct. Mater. 23, 4921-4932 (2013).

41.	Zhang, Y., Yuan, L., Guan, Q., Liang, G. & Gu, A. Developing self-healable and antibacterial polyacrylate coatings with high mechanical strength through crosslinking by multi-amine hyperbranched polysiloxane via dynamic vinylogous urethane. J. Mater. Chem. A 5, 16889-16897 (2017).

42.	Wang, X.-H. et al. Strong and tough fully physically crosslinked double network hydrogels with tunable mechanics and high self-healing performance. Chem. Eng. J. 349, 588-594 (2018).

43.	Kim, J. R. & Netravali, A. N. Self-healing properties of protein resin with soy protein isolate-loaded poly(d,l-lactide-co-glycolide) microcapsules. Adv. Funct. Mater. 26, 4786-4796 (2016).

44.	Wang, Y. et al. A novel design strategy for triple-network structure hydrogels with high-strength, tough and self-healing properties. Polymer 135, 16-24 (2018).

45.	Fox, J. et al. High-strength, healable, supramolecular polymer nanocomposites. J. Am. Chem. Soc. 134, 5362-5368 (2012).

46.	Yao, H.-B., Tan, Z.-H., Fang, H.-Y. & Yu, S.-H. Artificial nacre-like bionanocomposite films from the self-assembly of chitosan-montmorillonite hybrid building blocks. Angew. Chem. Int. Edit. 49, 10127-10131 (2010).

47.	Walther, A. et al. Supramolecular control of stiffness and strength in lightweight high-performance nacre-mimetic paper with fire-shielding properties. Angew. Chem. Int. Edit. 49, 6448-6453 (2010).

48.	Zhu, B. et al. Hierarchical nacre mimetics with synergistic mechanical properties by control of molecular interactions in self-healing polymers. Angew. Chem. Int. Edit. 54, 8653-8657 (2015).

49.	Cui, W. et al. A strong integrated strength and toughness artificial nacre based on dopamine cross-linked graphene oxide. ACS Nano 8, 9511-9517 (2014).

50.	Wan, S. et al. Synergistic toughening of graphene oxide-molybdenum disulfide-thermoplastic polyurethane ternary artificial nacre. ACS Nano 9, 708-714 (2015).

51.	Cheng, Y., Peng, J., Xu, H. & Cheng, Q. Glycera-inspired synergistic interfacial interactions for constructing ultrastrong graphene-based nanocomposites. Adv. Funct. Mater. 28, 1800924 (2018).

52.	Zhao, H., Yue, Y., Zhang, Y., Li, L. & Guo, L. Ternary artificial nacre reinforced by ultrathin amorphous alumina with exceptional mechanical properties. Adv. Mater. 28, 2037-2042 (2016).

53.	Liu, Y., Yu, S.-H. & Bergstrom, L. Transparent and flexible nacre-like hybrid films of aminoclays and carboxylated cellulose nanofibrils. Adv. Funct. Mater. 28, 1703277 (2018).

54.	Wen, Y., Wu, M., Zhang, M., Li, C. & Shi, G. Topological design of ultrastrong and highly conductive graphene films. Adv. Mater. 29, 1702831 (2017).

55.	Gong, S. et al. Integrated ternary bioinspired nanocomposites via synergistic toughening of reduced graphene oxide and double-walled carbon nanotubes. ACS Nano 9, 11568-11573 (2015).

56.	Wang, R. Z., Suo, Z., Evans, A. G., Yao, N. & Aksay, I. A. Deformation mechanisms in nacre. J. Mater. Res. 16, 2485-2493 (2001).