Supporting Information

Resiquimod-encapsulated MOF525 for Sustained Immunostimulant Release and Synergistic Photodynamic–Immunotherapy in Colorectal Cancer

Na Kyeong Lee, Nea Young Chun, Yu Jin Oh, Ulziituya Batjargal, Min-Seok Kim, WonJun Jang, Tae-Eun Park , Han-Jun Kim, Wooram Park*, Chun Gwon Park*, Se-Na Kim*

Figure S1. Hydrodynamic stability of MOF525 in serum-containing conditions. The Z-average diameter and polydispersity index of MOF525 were measured by DLS to assess colloidal stability in PBS supplemented with 5% FBS. MOF525 maintained stable size distribution with minimal aggregation over the measured time points (n = 3).

Figure S1. Hydrodynamic stability of MOF525 in serum-containing conditions. The Z-average diameter and polydispersity index of MOF525 were measured by DLS to assess colloidal stability in PBS supplemented with 5% FBS. MOF525 maintained stable size distribution with minimal aggregation over the measured time points (n = 3).

Figure S2. XPS spectra in the Zr 3d region of (A) MOF525 and (B) R848@MOF525. In the pristine MOF525, the Zr 3d spectrum shows a characteristic Zr–O bonding peak. After loading R848, R848@MOF525 displays an additional signal corresponding to O–Zr–N bonding, suggesting that the amine-containing functional group of R848 coordinates to the open metal sites of Zr in MOF525.

Figure S2. XPS spectra in the Zr 3d region of (A) MOF525 and (B) R848@MOF525. In the pristine MOF525, the Zr 3d spectrum shows a characteristic Zr–O bonding peak. After loading R848, R848@MOF525 displays an additional signal corresponding to O–Zr–N bonding, suggesting that the amine-containing functional group of R848 coordinates to the open metal sites of Zr in MOF525.

Figure S3. Quantification of ATP release as a DAMP signal following different treatment conditions. ATP levels were measured using a colorimetric ATP assay to evaluate extracellular ATP release. CT26 cells were assigned to four groups: non-treated control, laser irradiation only, MOF525 only, and MOF525 with laser irradiation. Combined treatment with MOF525 and laser irradiation induced the highest ATP release compared with other groups (n=5). ***P < 0.001 compared to MOF525 treated group.

Figure S3. Quantification of ATP release as a DAMP signal following different treatment conditions. ATP levels were measured using a colorimetric ATP assay to evaluate extracellular ATP release. CT26 cells were assigned to four groups: non-treated control, laser irradiation only, MOF525 only, and MOF525 with laser irradiation. Combined treatment with MOF525 and laser irradiation induced the highest ATP release compared with other groups (n=5). ***P < 0.001 compared to MOF525 treated group.

Figure S4. Gating strategy for BMDC.

Figure S4. Gating strategy for BMDC.

Figure S5. CD86 expression in BMDCs at different MOF treatment concentrations in vitro (n=5). ****P < 0.0001 compared to LPS treated group.

Figure S5. CD86 expression in BMDCs at different MOF treatment concentrations in vitro (n=5). ****P < 0.0001 compared to LPS treated group.

Figure S6. CD40 expression in BMDCs at different MOF treatment concentrations in vitro (n=5). ####P < 0.0001 compared to non- treated group.

Figure S6. CD40 expression in BMDCs at different MOF treatment concentrations in vitro (n=5). ####P < 0.0001 compared to non- treated group.

Figure S7. MHCII expression in BMDCs at different MOF treatment concentrations in vitro (n=5). ****P < 0.0001 compared to the LPS-treated group.

Figure S7. MHCII expression in BMDCs at different MOF treatment concentrations in vitro (n=5). ****P < 0.0001 compared to the LPS-treated group.

Figure S8. Expression of BMDCs maturation cell markers at treatment concentrations of below 10 µg/mL (n=5). ***P < 0.001, *P < 0.05.

Figure S8. Expression of BMDCs maturation cell markers at treatment concentrations of below 10 µg/mL (n=5). ***P < 0.001, *P < 0.05.

Figure S9. Tumor rechallenge test evaluating long-term immune memory and protective effects of MOF. Representative image of a mouse 3 weeks after tumor rechallenge.

Figure S9. Tumor rechallenge test evaluating long-term immune memory and protective effects of MOF. Representative image of a mouse 3 weeks after tumor rechallenge.

Figure S10. Histopathological assessment of vital organs following tumor rechallenge. Representative H&E stained sections of heart, lung, liver, kidney, and spleen (Scale bar=100 μm).

Figure S10. Histopathological assessment of vital organs following tumor rechallenge. Representative H&E stained sections of heart, lung, liver, kidney, and spleen (Scale bar=100 μm).

Figure S11. Body weight in the different groups of mouse (n=5). n.s, not significant.

Figure S11. Body weight in the different groups of mouse (n=5). n.s, not significant.