Gradient Copolymerization towards High-performance Monocomponent Polymers for Energy and Charge Storages

Yuanwei Zhu1, Wanlong Lu1, Nan Qiao1, Huize Cui1, Zhipeng Hu1,3, Zichao Shen1, Jinde Yu1, Bo Liu2*, Shuwen Zhang4, Yongjie Nie5, Guochang Li6, Shengtao Li1*, Guanghao Lu1*

Supplementary information

Table S1  Copolymerization of ethylene and styrene catalyzed by complex 1 under various initial concentration of styrene.a

| copolymer | E /atm | [St]0 /mol·L–1 | Time /min | Yield /g | fSt / mol%b | Mn ×10-4c | PDIc |
| --- | --- | --- | --- | --- | --- | --- | --- |
| PESt15 | 1 | 0.20 | 15 | 3.6 | 14.7 | 4.2 | 3.7 |
| PESt37 | 1 | 0.40 | 15 | 4.3 | 36.7 | 32.2 | 1.3 |
| PESt59 | 1 | 1.50 | 9 | 4.7 | 59.2 | 65.2 | 1.6 |

a1: 20 μmol, 1:[Ph3C][B(C6F5)4]:AliBu3 = 1:1:2, toluene: 75 mL, temperature: 40 °C. b Determined by 1H NMR spectrum in C2D2Cl4 at 110 °C (fSt = 4Aar/(5Aal + Aar)×100%, where Aar = area of aromatic protons and Aal = area of aliphatic protons). c Determined by GPC in 1,2,4-trichlorobenzene at 150 °C against polystyrene standard.

Table S2  Kinetic study of co-polymerization of ethylene and styrene catalyzed by 1.a

| Entry | Time /min | Yield /g | fSt / mol%b | Mn ×10-4c | PDIc |
| --- | --- | --- | --- | --- | --- |
| 1 | 2 | 0.60 | 59.7 | 25.1 | 2.6 |
| 2 | 5 | 0.89 | 58.0 | 51.2 | 1.6 |
| 3 | 15 | 1.71 | 50.3 | 56.8 | 1.7 |
| 6 | 40 | 2.08 | 40.8 | 60.5 | 1.7 |

a1: 10 μmol, 1:[Ph3C][B(C6F5)4]:AliBu3 = 1:1:2, [St]0 = 0.45 /mol·L–1, toluene: 35 mL, ethylene: 1 atm, temperature: 40 °C. b Determined by 1H NMR spectrum in C2D2Cl4 at 110 °C (fSt = 4Aar/(5Aal + Aar)×100%, where Aar = area of aromatic protons and Aal = area of aliphatic protons). c Determined by GPC in 1,2,4-trichlorobenzene at 150 °C against polystyrene standard.

Table S3  Performance of C12-BTBT/PS and C12-BTBT/PESt OFET on 10 devices

|  | C12-BTBT/PS | C12-BTBT/ PESt15 | C12-BTBT/ PESt37 | C12-BTBT/ PESt59 |
| --- | --- | --- | --- | --- |
| max | 12.3 | 9.8 | 11.8 | 14.2 |
| average | 11.2 | 8.7 | 10.1 | 12.8 |
| Ion/Ioff (average) | 3×106 | 3×105 | 5×105 | 2×106 |
| Vth-average | -28 | -36 | -33 | -26 |

Figure S1  The 1H NMR spectra of PESt (PESt15, PESt37 and PESt59).

Figure S2  The 13C NMR spectra of PESt (PESt15, PESt37 and PESt59).

b

a

Figure S3  Frequency dependent dielectric spectra of a) PE and b) s-PS.

a

c

b

Figure S4  Weibull distributions of DC breakdown strength of PE, PESt15, PESt37, PESt59 and s-PS at a) 40 oC, b) 70 oC c) 100 oC on 15 samples.

a

b

c

Figure S5  Output characteristics of C12-BTBT OFETs with a) PESt15, b) PESt37 and c) PESt59 gate dielectrics.

Figure S6  Voltage transfer characteristics of the C12-BTBT/PS inverter.

Figure S7  Charging voltage dependent (0~10 kV) particulate filtration efficiency (PFE) of PESt coated nylon fiber membrane.