Table 1: Synthetic polymers tested for epifluorescence upon excitation at 390nm and an emission recorded >420nm using a Long Pass filter. This was done on a Nikon microscope equipped with the PARISS® hyperspectral imaging system. Plastics used are standards from the PolymerKit 1.0; Hawaii Pacific University.

| Synthetic polymer | Abbreviation | Wavelength (color) of epifluorescence (nm) |  |
| --- | --- | --- | --- |
| Acrylonitrile Butadiene Styrene | ABS | 530 (Blue/Green) |  |
| Cellulose Acetate | CA | 505 (Blue) |  |
| Crumb Rubber (tire) | CR | None |  |
| Ethylene Vinyl Acetate | EVA | None |  |
| Polyamide 66 (nylon) | PA66 | 495 (Blue/Green) |  |
| Polyester | PEST | 460 (Blue) |  |
| Polyester (with line dyed black) | PEST | None for black line |  |
| Polyethylene Terephthalate | PET | 475 (Blue/Green) |  |
| Polypropylene | PP | 465 (Blue) |  |
| Polystyrene | PS | 475 (Blue) |  |
| Polyurethane (Elastane/Spandex) | EA/SP | 450 (Blue) |  |
| Polyvinyl Chloride | PVC | 530 (Blue/Green) |  |