Supplementary Information

Title: Near-atomic size highly positive silver nanoparticles are bactericidal targeting cell wall and adherent fimbriae expression

Lok R. Pokhrel1,2,*, Zachary L. Jacobs3, Dmitriy Dikin4, Shaw M. Akula5

1Department of Public Health, The Brody School of Medicine, East Carolina University, Greenville, NC, USA.

2Department of Health Education and Promotion, College of Health and Human Performance, East Carolina University, Greenville, NC, USA.

3School of Law, University of California, Berkeley, Berkeley, CA, USA.

4Department of Mechanical Engineering, College of Engineering, Temple University, Philadelphia, PA, USA.

5Department of Microbiology and Immunology, The Brody School of Medicine, East Carolina University, Greenville, NC, USA.

*Correspondence: LR Pokhrel, Phone: 252-737-5587; Email: pokhrell18@ecu.edu.

Table S1. Representative protocol for the purification of AgNPs using the Tangential Flow Filtration (TFF) system.

| Purification of unclean AgNPs | Electrical Conductivity (µS/cm) |
| --- | --- |
| Started Volume = 500 ml | 1095 |
| Ended Volume = 70 ml | 1162 |
| Volume increased to 500 ml adding Milli-Q water | 185 |
| Ended Volume = 100 ml | 283 |
| Volume increased to 500 ml adding Milli-Q water | 36 |
| Ended Volume = 75 ml | 68 |
| Volume increased to 500 ml adding Milli-Q water | 11 |
| Ended Volume = 150 ml | 20 |
| Volume increased to 500 ml adding Milli-Q water | 10* |

* obtained as purified AgNPs suspension with electrical conductivity of 10 µS/cm.

Table S2. Impact of incubation time (72 h) and temperature (35 °C) on the stability of nanoparticles in the carrier medium, i.e., moderately hard water (MHW), evaluated by measuring average hydrodynamic diameter (HDD) and zeta potential.

| Parameters | Citrate-AgNPs |  | NH2-AgNPs |  |
| --- | --- | --- | --- | --- |
|  | Pre-incubation | Post-incubation | Pre-incubation | Post-incubation |
| HDD ± SD (nm)* | 11.0 ± 0.7 | 11.2 ± 1.3 | 4.3 ± 0.8 | 5.1 ± 0.3 |
| Zeta potential (mV) | -23.47 | -18.41 | +41.6 | +39.2 |

* Volume weighted hydrodynamic diameter (HDD) measured using DLS, and all size measurements were 100% by volume.

Table S3 General linear model showing significant association between E. coli cell length and diameter (top table), followed by model parameters (bottom table).

| Dependent Variable: Cell Length |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Source | Type III Sum of Squares |  | df |  | Mean Square |  |  | F | Sig. |  |  |
| Model | 2006.904a |  | 1 |  | 2006.904 |  |  | 1386.473 | .000 |  |  |
| Diameter | 2006.904 |  | 1 |  | 2006.904 |  |  | 1386.473 | .000 |  |  |
| Error | 396.612 |  | 274 |  | 1.447 |  |  |  |  |  |  |
| Total | 2403.516 |  | 275 |  |  |  |  |  |  |  |  |
| a. R Squared = .835 (Adjusted R Squared = .834) |  |  |  |  |  |  |  |  |  |  |  |
| b. Computed using alpha = .05 |  |  |  |  |  |  |  |  |  |  |  |
| Parameter | B | Std. Error |  | t |  | Sig. | 95% Confidence Interval |  |  |  |  |
|  |  |  |  |  |  |  | Lower Bound |  |  | Upper Bound |  |
| Diameter | 2.924 | .079 |  | 37.235 |  | .000 | 2.769 |  |  | 3.079 |  |
| a. Computed using alpha = .05 |  |  |  |  |  |  |  |  |  |  |

Fig. S1. UV-Visible spectra of purified NH2-AgNPs (1 µg/mL and 10 µg/mL) and Citrate-AgNPs (1 µg/mL and 10 µg/mL) used in this study showing no change in localized surface plasmon resonance (λmax) of both the AgNPs with dilution in Milli-Q water.

Fig. S2. Energy dispersive spectroscopy (EDS) elemental mapping of silver and other background elements (C, O, Na, Cl, and K) on the E. coli surfaces upon exposure to 10 µg/mL Citrate-AgNPs for 72 h. Scale bar denotes 5 µm for all images, except for A (scale bar = 4 µm).