Supplementary Information

Flexible Laser-Induced Graphene Biosensor Enables Real-Time, In Vivo Profiling of Wound Healing Cytokine Dynamics

Jonghee Eun1‡, A-Hyeon Lee1,2‡, Seungjun Lee1,3‡, Jimin Lee1,5, Hyogeun Shin1,3, Ja Wook Koo1,2*, Namsun Chou1,4*.

1 Emotion, Cognition & Behavior Research Group, Korera Brain Research Institute (KBRI), Daegu 41062, Korea

2 Department of Brain Sciences, Daegu Gyeongbuk Institute of Science and Technology (DGIST), Daegu 42988, Republic of Korea

3 School of Electronics Engineering, College of IT Engineering, Kyungpook National University, Daegu 41566, Republic of Korea

4 Graduate School, Daegu Gyeongbuk Institute of Science and Technology (DGIST), Daegu 42988, Republic of Korea

5 Department of Robotics and Mechatronics Engineering, Daegu Gyeongbuk Institute of Science and Technology (DIGST), Daegu, 42988, Republic of Korea

* Corresponding author at: Emotion, Cognition & Behavior Research Group, Korera Brain Research Institute (KBRI), Daegu 41062, Korea. E-mail address: jawook.koo@kbri.re.kr (J. W. Koo), nschou@kbri.re.kr (N. Chou).

Fig. S1. Laser parameter optimization of LIG formed on SU8 substrate

(a) Optical images of laser-patterned SU8 surfaces generated under varying laser powers (10%–100%) and scan speeds (10%–100%).  (b) Corresponding sheet resistance (Rₛ) heatmap showing conductive windows and non-conductive regions before transfer onto PDMS. Gray regions indicate conditions where no graphene was formed, whereas white regions correspond to graphene visible optically but lacking measurable conductivity.

Fig. S2. Raman spectra of substrates and LIG-transferred hybrids

Raman spectra of bare SU8 (black) and PDMS (red) substrates compared with SU8/LIG (blue) and PDMS/LIG (green) hybrids. The appearance of characteristic D, G, and 2D bands in SU8/LIG and PDMS/LIG confirms graphitic domain formation after laser-induced carbonization and successful transfer onto PDMS.

Fig. S3. SEM and EDS characterization of optimized LIG on PDMS (90% power, 40% speed)

(a) Top-view SEM image of SU8-derived LIG transferred onto PDMS. (b) Side-view SEM image showing the interface between porous LIG layer and the underlying substrate. (c) Merged EDS elemental mapping of the analyzed region, illustrating the distribution of silicon (Si), carbon (C), and oxygen (O). (d–f) Individual EDS elemental maps of Si (magenta), C (red), and O (green), highlighting carbon-rich domains of the graphene network. (g) EDS spectrum and quantified elemental composition confirming high carbon content (75.84 at%), reduced oxygen content (14.20 at%), and residual silicon content (9.98 at%), consistent with effective graphitization under optimized laser processing.

Fig. S4 SEM and EDS analysis of non-graphitized control (30% power, 40% speed)

(a) Top-view and (b) cross-sectional SEM images of SU8 after laser processing under suboptimal conditions (30% power, 40% speed), showing no porous graphene formation. (c) Merged EDS elemental mapping and individual distributions of (d) Si, (e) C, and (f) O, confirming incomplete carbonization with high oxygen and silicon signals. (g) EDS spectrum and quantified elemental composition from the mapped region, indicating reduced carbon content (~37 at%) and elevated oxygen (~26 at%) and silicon (~22 at%) compared with optimized LIG conditions.

Fig. S5. Schematic diagrams of mechanical test configurations

(a) Bending test setup showing bend angle (θ), bend radius (R), and PDMS thickness. (b) Roller-assisted bending setup with the lubricant-coated configuration. (c) Tape-peeling test schematic illustrating applied force and direction of graphene detachment direction.

Fig. S6. TIRF imaging of LIG surface prior to antigen binding

TIRF microscopy images of antibody-functionalized LIG electrodes before IL-6 exposure. Both panels (a-1, a-2) show uniform, low-level background fluorescence without distinct localized signals, confirming minimal nonspecific interactions on the antibody-functionalized graphene surface.

Fig. S7. Morphological and compositional analysis of LIG

(a–c) SEM images of LIG at different magnifications, highlighting its porous morphology. (d–h) EDS elemental maps of Si, C, O, and Sb, showing carbon-rich graphene domains. (i) EDS spectrum and (j) quantified elemental composition from the mapped region, confirming predominant carbon content (~70 at%), with minor oxygen and silicon, as well as trace Sb signals.

Fig. S8. In vitro characterization of IL-6 binding on LIG electrodes

(a–c) SEM images of the LIG surface after IL-6 exposure, showing nanoscale aggregates associated with antigen–antibody complex formation. (d–l) EDS elemental maps of C, O, P, Cl, and Na, confirming protein-related elements distributed across the porous graphene network after IL-6 binding. (m) EDS spectrum and quantified composition from the analyzed region, further verifying IL-6-specific adsorption on the LIG surface under in vitro conditions.