Multiscale Structural Engineering Enables Superior Energy Storage in Tetragonal Tungsten Bronze Relaxor Ferroelectrics

Saifei Wang1, Juntao Huang1, Guangyao Li1, Tao Yang1, Haihua Huang1*, Yajie Han1 Wei Li1*, Zhenxiang Cheng2*, He Qi3, Mahesh Kumar Joshi4, Peng Fu1*

1-School of Materials Science and Engineering, Liaocheng University, Liaocheng 252059, PR

2-Institute for Superconducting and Electronic Materials, University of Wollongong, Innovation Campus, North Wollongong, NSW 2500, Australia

3-School of Materials Science and Technology, Hainan University, Hainan 570228, China

4-Central Department of Chemistry, Tribhuvan University, Kathmandu 44613, Nepal

Fig. S1| Rietveld correction of X–ray diffraction data for BLBTN–x ceramics (a) x=0.35, (b) x=0.40, (c) x=0.45, (d) x=0.55.

| Samples | 0.35 | 0.4 | 0.45 | 0.5 | 0.55 |
| --- | --- | --- | --- | --- | --- |
| Space group | P4bm | P4bm | P4bm | P4bm | P4bm |
| a | 12.447250 | 12.430459 | 12.446912 | 12.443444 | 12.428993 |
| b | 12.447250 | 12.430459 | 12.446912 | 12.443444 | 12.428993 |
| c | 3.933159 | 3.928861 | 3.934113 | 3.932960 | 3.928716 |
| alpha | 90 | 90 | 90 | 90 | 90 |
| beta | 90 | 90 | 90 | 90 | 90 |
| gamma | 90 | 90 | 90 | 90 | 90 |
| c/a | 0.315986 | 0.316067 | 0.316071 | 0.316067 | 0.3160929 |
| volume | 609.380 | 607.073 | 609.495 | 608.977 | 606.905 |

Table S1 Crystal Phase Data of BLBTN–x Ceramics Calculated by X–ray Rietveld Method

Fig. S2| Images of grains with different axes. (a) ; (b) [100]. c [100]c crystal plane atomic matching diagram. d High resolution TEM image. e High resolution image of  crystal plane. f Lattice model along the [110] axis direction.

Fig. S3| Local morphology of ceramics. a–e Surface SEM images and particle size distribution of the BLBTN–x ceramics (x = 0.35, 0.40, 0.45, 0.50, 0.55); f surface element distribution of the BLBTN-0.5 ceramic.

Fig. S4| Electric field distribution diagram: a x=0.35, b x = 0.50. Local electric field distribution: c x=0.35 d x = 0.50.