Supporting Information

Atom-precise fluorescent copper cluster for tumor microenvironment targeting and transient chemodynamic cancer therapy

Zhenzhen Yang 1, #, Anli Yang3, #, Wang Ma1, Kai Ma2, Ya-Kun Lv2, Peng Peng1, 2, *, Bingjie Li1, 2,* , Shuang-Quan Zang2,*

1 Department of Oncology, The First Affiliated Hospital of Zhengzhou University, 450052, China

2 Henan Key Laboratory of Crystalline Molecular Functional Materials, Henan International Joint Laboratory of Tumor Theranostical Cluster Materials, Green Catalysis Center, and College of Chemistry, Zhengzhou University, 450001, China

3 Department of Breast Oncology, Sun Yat-sen University Cancer Center, State Key Laboratory of Oncology in South China, Collaborative Innovation Center for Cancer Medicine, 510060, China

#These authors contributed equally to the work.

*Corresponding authors.

E-mail: ppeng@zzu.edu.cn; bingjieli1991@outlook.com; zangsqzg@zzu.edu.cn

Supporting Tables

Table S1. Crystal data and structure refinement information for Cu6NC.

| Compound | Cu6NC |
| --- | --- |
| CCDC number | 2083549 |
| Empirical formula | C30H32Cu6N14O2S6. |
| Formula weight | 1194.29 |
| Temperature / K | 199.99(10) |
| Crystal system | triclinic |
| Space group | P-1 |
| a /Å | 10.0702(2) |
| b /Å | 11.7425(2) |
| c /Å | 17.9207(3) |
| α /° | 90.4010(10) |
| β /° | 105.473(2) |
| γ /° | 92.479(2) |
| Volume /Å3 | 2040.02(7) |
| Z | 2.000 |
| ρcalc g/cm3 | 1.944 |
| μ /mm-1 | 6.705 |
| F(000) | 1192.0 |
| Crystal size/mm3 | 0.12 × 0.11 × 0.1 |
| Radiation | CuKα (λ = 1.54184) |
| 2Θ range for data collection /° | 5.118 to 148.216 |
| Index ranges | -12 ≤ h ≤ 12,-13 ≤ k ≤ 14,-11 ≤ l ≤ 22 |
| Reflections collected | 21566 |
| Independent reflections | 8008 [Rint = 0.0337, Rsigma= 0.0405] |
| Data/restraints/parameters | 8008/78/556 |
| Goodness-of-fit on F2 | 1.051 |
| Final R indexes [I>=2σ (I)] | R1= 0.0539, wR2= 0.1580 |
| Final R indexes [all data] | R1= 0.0628, wR2= 0.1662 |
| Largest diff. peak/hole / e Å-3 | 1.47/-0.75 |

Supporting Figures

Figure S1. XPS analysis of Cu6NC. a) Survey of all elements. b), c) and d) High-resolution XPS for Cu 2p, N 1s and S 2p, respectively.

Figure S2. FTIR spectra of 2-mercaptopyrimidine (black line) and Cu6NC (red line).

Figure S3. TGA curves for Cu6NC. The first stage of the weight loss indicated the evaporation of the DMF, which was used as the solution during the synthesis.

Figure S4. Solid-state emission spectra of Cu6NC at 365 nm.

Figure S5. DLS analysis of Cu6NC.

Figure S6. Solid-state UV-vis test of Cu6NC.

Figure S7. The PXRD patterns of Cu6NC before and after the treatment of HCl (pH~6).

Figure S8. The SEM associated EDS images of crystalline Cu6NC. Cu, N, C and S elements were homogenously dispersed along the ctrystals.

Figure S9. The SEM associated EDS images of the Cu6NC treated by acidic solution (pH~6). The Cu, N, C and S could still be observed with homogenous distribution, while the Cl was from the the addition of HCl solution (pH~6). The crystals were totally pulverized.

Figure S10. CCK-8 results of the viability of tumor cells cultured with Cu6NC for 24 h.

Figure S11. Statistical results of apoptosis ratio in A735 cells after different concentrations (0, 2, 8 and16 μM) of Cu6NC treatment.

Figure S12. Statistical results of cell cycle in A735 cells after different concentrations (0, 2, 8 and16 μM) of Cu6NC treatment.

Figure S13. The live/dead status of A375 cells after different treatments detected by flow cytometry.

Figure S14. The live/dead status of A375 cells after different treatments analyzed by FlowJo software.

Figure S15. The statistical results of the migration number were counted with ImageJ software, after A375 cells were processed differently.

Figure S16. Quantitative analysis of the number of colonies for A375 cells undergo different treatments.

Figure S17. Quantitative analysis of ROS generation in A375 cells after Cu6NC treatment, detected by the DCFH-DA probe.

Figure S18. GSH/GSSG ratio in A375 cells after treatment different concentrations of Cu6NC.

Figure S19. Quantitative analysis of blood parameters in mice injected with different concentrations of Cu6NC to assess the long-term toxicity. ALT, Alanine aminotransferase; AST, Aspartate aminotransferase; BUN, Blood urea nitrogen; CREA, Creatinine; CK, Creatine kinase; CK-MB, Creatine Kinase, MB Form.