Supplementary Information (SI)

Biosynthesis of 3D/2D CeO2/MoS2 nanocomposites with enhanced photocatalytic activity to degrade organic dye in wastewater and statistical optimization of reaction parameters

Yogesh Sharmaa,#, Mohammad Ahmed Khana,#, Thangapandi Chellapandib, Magdum Tejas Sukumara, Gunabalan Madhumithab, Md. Maksudur Rahman Khanc, Mohammed Danishd, Sagadevan Velua, Selvaraj Mohana Roopanb,*

aSchool of Chemical Engineering, Vellore Institute of Technology, Vellore 632014, Tamilnadu, India

bChemistry of Heterocycles & Natural Research Laboratory, Department of Chemistry, School of Advanced Sciences, Vellore Institute of Technology, Vellore 632014, Tamilnadu, India

cDepartment of Chemical Engineering, College of Engineering, Universiti Malaysia Pahang, Gambang 26300, Pahang, Malaysia.

dSchool of Industrial Technology, Universi Sains Malaysia, Penang 11800, Malaysia

*Corresponding author E-mail address: mohanaroopan.s@vit.ac.in (S.M. Roopan)

#Equal contribution to this work

S1.	Experimental Section

S1.1. 	Synthesis of 2D MoS2 sheet

In this study, molybdenum disulphide nanosheets was prepared using analytical grade chemicals. The solution has been prepared by mixing 12 mL (10%) hydrazine hydrate, 5 mL (0.1M) tartaric acid, 10 mL (0.1M) of ammonium molybdate, and 15 mL ammonia in a beaker. Then 20 mL (0.1M) thiourea solution was added to the prepared solution. In order to make the volume of the reaction mixture 150 mL, distilled water was added. Then, the reaction vessel was heated indirectly using an oil bath at 90C for 90 min. After heating, the solution was transferred to an autoclave and kept in a hot air oven at 120C for 18 h. This process was known as hydrothermal. The solution was then taken out and centrifugation was done at 6000 rpm. The colloidal suspension was rinsed several times using organic solvent and water. Lastly, the obtained product was set to dry for 24 h using a vacuum oven at 60C. The dried product thus obtained was exfoliated 2D MoS2, which was black in colour.

S2.	Results and discussion

S2.1.	UV-Visible Diffuse Reflectance Spectra

Optical absorption properties of the synthesized MoS2, CeO2 and CeO2/MoS2 nanocomposites samples were analysed by observing UV-spectra. Fig. S1 displays the UV−Vis spectrum of MoS2, CeO2 and CeO2/MoS2. Pristine CeO2 has a typical absorption peak of around 430 nm.  Observationally, it is noted that weight of MoS2 is increased (in nanocomposite), the absorption peak intensity of composite samples also increased significantly. The reason for this could be the blackish colour of original MoS2 and the change in colour of the composite. As the weight percentage of MoS2 in the composite increased, a change appeared in the composite’s absorbance intensity at the edge that corresponded with the colour change from greenish-yellow to light brown [1]. The absorption of light of CeO2, in visible spectrum (440-800 nm), significantly rises after the addition of black MoS2catalyst and therefore, the CeO2/MoS2 nanocomposites can absorb a higher number of photons for the photocatalytic reactions [2].

Moreover, the bandgap energies for the MoS2, CeO2 and CeO2/MoS2 nanocomposites were computed by the use of Tauc’s formula (ahv) = A(hv - Eg)n/2, where “h” was the Planck’s constant,“Eg” was the band gap energy, “a” was the absorption coefficient, “v” is the frequency of light and “n” varies with the properties of the transition [3]. Subsequently, the values of Eg are assessed, i.e., 1.81, 2.66, 2.41, 2.50, 2.57 and 2.61 eV for MoS2, CeO2, CMS-2, CMS-4, CMS-6 and CMS-8 respectively (Fig. S2).

Fig. S1. UV-Vis DRS of MoS2, CeO2 and CMS (CeO2/MoS2 nanocomposites).

Fig. S2. Tauc’s plot photon energy of MoS2, CeO2 and CMS (CeO2/MoS2 nanocomposites).

S2.2.   EDAX Analysis

The presences of all elements are identified from selected area EDAX studies and the presence MoS2, CeO2 and CMS-4 composite elements are shown in Fig. S3a-c respectively. The spectra obtained by the EDAX data shows peaks corresponding to elements making up the composition of the sample being analysed. The analysis disclosed the presence of Mo, S, Ce and O in the formed nanocomposite. No more other peak is present, and this shows that the green synthesized CeO2 nanoparticles decorated MoS2 is indeed a pure composite (Fig. S3c).

Fig. S3. EDAX Spectrum of a) MoS2, b) CeO2 c) CMS-4.

S2.3.	Photoluminescence Spectra

The concept of Photoluminescence emission stems from the radiative recombination of photogenerated excitons (such as electron-hole pairs) which was employed to estimate the charge separation and transfer [4]. Fig. S4 depicts that CeO2 indicates an intense photoluminescence signal with an emission band centred at 470 nm under 360 nm, which attributes to its prompt charge recombination. A solid blue emission peak noted at 470nm was because of the development of extra surface defect energy levels amongst band levels between O 2p and Ce 4f. As the percentage of CeO2 in the composite decreases, the fall in the steadiness of peak was observed. Effective interfacial transfer of electron between excited MoS2 and CeO2 energy level was attributed to the removal of a photoluminescent peak in the CMS-4 photo catalyst. Based on the photoluminescence results, we can say CMS-4 nanocomposite has better charge separation compared with other samples.  Due to the this it leaves more redox electrons hole pair, which is the responsible for enhances in degradation behavior.

Fig. S4. Photoluminescence spectrum of MoS2, CeO2 and CeO2/MoS2 nanocomposites.

S2.4.	Fourier Transform Infrared Spectroscopy (FT-IR Analysis)

In order to analyze the functional groups present on the surface, an FT-IR study was carried out. The MoS2, CeO2 and CeO2/MoS2 nanocomposite FT-IR spectrum is shown in Fig. S5. The O-Ce-O bonding character of the nanoparticles CeO2 was a prominent peak at 841 cm-1.  The band at 1290 cm-1 ultimately corresponds to the vibration of oxygen atom in N-O stretching which was present in the CeO2 nanoparticles. The small bands formed at 710 and 431 cm-1 corresponds to Ce-O straighten mode. According to the MoS2 range, the band with its 450 cm-1 vibration can be assigned to the Mo–S range.  The band at 3413 cm-1 which can be observed in CeO2 and CeO2/MoS2 nanocomposites was mainly attributed to stretching vibrations of O-H bonds. Hence, the FT-IR spectra provide the evidence that CeO2 nanoparticles were successfully composited with MoS2 sheets [5].

Fig. S5. FT-IR spectrum of MoS2, CeO2 and CMS (CeO2/MoS2 nanocomposites).

S2.5.	Zeta Potential

The high zeta potential symbolizes that the nanocomposites prepared are stable. The zeta potential values for CMS-2, CMS-4, CMS-6 and CMS-8 nanocomposites are -34.7, -66.7, -52.7 and -43.3 mV respectively (illustrated in Fig. S6) and therefore suggests high stability. The nanocomposite of CMS-4 was remarkably stable. The values of zeta potential signify the establishment of a balanced system. Furthermore, negatively charged surfaces of the nanocomposites offer electrostatic repulsive forces and affords greater stability by restraining the nanocomposites from accumulating in the colloidal state [6].

Fig. S6. Zeta potential of a) CMS-2, b) CMS-4, c) CMS-6 and d) CMS-8 nanocomposite.

Fig. S7. The experimental data versus the predicted data for MV degradation (in %).

Fig. S8. Contour plot as a function of (a) amount of photocatalyst (Z1) and concentration of MV dye (Z2), (b) amount of photocatalyst (Z1) and time for degradation (Z3), (c) concentration of MV dye (Z2) and time for degradation (Z3)

Table S1. Performance of various photocatalysts for degrading methyl violet

| Photocatalyst | Preparation method | Degradation Percentage | Amount of photocatalyst | Vol. and conc. of MV | Time for degradation (min) | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| ZnO | Precipitation method | 66.5 | 0.08 g | 40 mL of 7.1 mgL-1 | 60 | [7] |
| TiO2/Pt | Incipient wetness method | 78 | 0.02 g | 10 mL of 15 mgL-1 | 20 | [8] |
| Fe0@Guar gum-crosslinked-soya lecithin nanocomposite hydrogel | Ultrasonication method | 81 | 30 mg | 100 mL of 30 mgL-1 | 120 | [9] |
| TiSiW12O40/TiO2 | - | 82.4 | 0.3 g | 20 mgL-1 | 180 | [10] |
| Bi doped ZnO | Precipitation method | 82.5 | 0.08 g | 40 mL | 60 | [7] |
| Ho2O3 (Holmium oxide) | Precipitation method | 82.8 | 120 mg | 3 mg | 90 | [11] |
| Cation exchange membrane | - | 84-93 | 2.0 g/L | 20 mL of 15 mgL-1 | 120 | [12] |
| SnO2-activated carbon fiber hybrid catalyst | Pore-fabrication and self-assembly processes | 87 | 0.05 g | 150 mL | 12 | [13] |
| Activated charcoal supported bismuth doped ZnO nanocomposite | Precipitation method | 94.5 | 0.08 g | 40 mL of 7.1 mgL-1 | 60 | [7] |
| TiO2/Pd | Incipient wetness method | 95 | 0.02 g | 10 mL of 15 mgL-1 | 20 | [8] |
| Pu-erh tea powder | - | 95 | 0.2 g | 100 mL of 100 mgL-1 | 300 | [14] |
| Hybrid hydrogel | Suspension and heating–cooling cyclic processes | 95.7 | 0.5 mL | 4.5 mg of 1 mgL-1 | 240 | [15] |
| Fertilizer plant waste carbon | - | 96 | 1.0 g/L | 100 mL of 20 mgL-1 | 300 | [16] |
| CeO2/MoS2 nanocomposite (4%) | Biosynthetic microwave assisted process | 96.25 | 20 mg | 100 mL of 20 mgL-1 | 90 | Present Study |

Table S2. The design factors and respective parameters with coded levels

| Parameters | Units | Levels |  |  |
| --- | --- | --- | --- | --- |
|  |  | -1 | 0 | +1 |
| Amount of photocatalyst (Z1) | mg | 10 | 20 | 30 |
| Concentration of MV dye (Z2) | mgL-1 | 10 | 20 | 30 |
| Time for degradation (Z3) | min | 75 | 90 | 105 |

Table S3. Analysis of Variance and multiple regression results

| Source | DF | Adj SS | Adj MS | F-Value | P-Value |
| --- | --- | --- | --- | --- | --- |
| Model | 10 | 461.683 | 46.168 | 12.41 | 0.000 |
| Blocks | 1 | 25.759 | 25.759 | 6.92 | 0.027 |
| Linear | 3 | 133.814 | 44.605 | 11.99 | 0.002 |
| Z1 | 1 | 54.943 | 54.943 | 14.76 | 0.004 |
| Z2 | 1 | 14.811 | 14.811 | 3.98 | 0.077 |
| Z3 | 1 | 64.060 | 64.060 | 17.21 | 0.002 |
| Square | 3 | 311.558 | 103.853 | 27.91 | 0.000 |
| Z1*Z1 | 1 | 31.731 | 31.731 | 8.53 | 0.017 |
| Z2*Z2 | 1 | 10.241 | 10.241 | 2.75 | 0.132 |
| Z3*Z3 | 1 | 65.590 | 65.590 | 17.62 | 0.002 |
| 2-Way Interaction | 3 | 2.912 | 0.971 | 0.26 | 0.852 |
| Z1*Z2 | 1 | 0.031 | 0.031 | 0.01 | 0.929 |
| Z1*Z3 | 1 | 0.281 | 0.281 | 0.08 | 0.790 |
| Z2*Z3 | 1 | 2.599 | 2.599 | 0.70 | 0.425 |
| Error | 9 | 33.493 | 3.721 |  |  |
| Lack-of-Fit | 5 | 33.493 | 6.699 | * | * |
| Pure Error | 4 | 0.000 | 0.000 |  |  |
| Total | 19 | 495.176 |  |  |  |

References

[1] Y. Song, Y. Lei, H. Xu, C. Wang, J. Yan, H. Zhao, Y. Xu, J. Xia, S. Yin, H. Li, Synthesis of few-layer MoS2 nanosheet-loaded Ag3PO4 for enhanced photocatalytic activity, Dalton Trans. 44 (2015) 3057-3066, https://doi.org/10.1039/c4dt03242j.

[2] G. Swain, S. Sultana, B. Naik, K. Parida, Coupling of Crumpled-Type Novel MoS2 with CeO2 Nanoparticles: A Noble-Metal-Free p–n Heterojunction Composite for Visible Light Photocatalytic H2 Production, ACS Omega 2 (2017) 3745-3753, https://doi.org/10.1021/acsomega.7b00492.

[3] Y. Li, Z. Wang, H. Zhao, X. Huang, M. Yang, 3D MoS2@TiO2@poly(methyl methacrylate) nanocomposite with enhanced photocatalytic activity, J. Colloid Interf. Sci. 557 (2019) 709-721, https://doi.org/10.1016/j.jcis.2019.09.074.

[4] S.R. Kande, U.G. Ghoshir, J.K. Khedkar, G.G. Muley, A.B. Gambhire, Nanocrystalline B/C/S-Doped ZnO-SnO2 Photocatalysts: Preparation, Characterization and Photocatalytic Performance, Asian J. Chem. 31 (2019) 1971-1978, https://doi.org/10.14233/ajchem.2019.22047.

[5] S. Ding, P. He, W. Feng, L. Li, G. Zhang, J. Chen, F. Dong, H. He, Novel molybdenum disulfide nanosheets–decorated polyaniline: Preparation, characterization and enhanced electrocatalytic activity for hydrogen evolution reaction, J. Phys. Chem. Solids. 91 (2016) 41-47, https://doi.org/10.1016/j.jpcs.2015.12.009.

[6] P. Singh, H. Singh, V.C. Aceituno, S. Ahn, Y.J. Kim, D.C. Yang, Bovine serum albumin as a nanocarrier for the efficient delivery of ginsenoside compound K: preparation, physicochemical characterizations and in vitro biological studies, RSC Adv. 7 (2017) 15397-15407, https://doi.org/10.1039/C6RA25264H

[7] V.L. Chandraboss, J. Kamalakkannan, S. Prabha, S. Senthilvelan, An efficient removal of methyl violet from aqueous solution by an AC-Bi/ZnO nanocomposite material, RSC Adv. 5 (2015) 25857–25869, https://doi.org/10.1039/C4RA14463E.

[8] K. Saeed, I. Khan, T. Gul, M. Sadiq, Efficient photodegradation of methyl violet dye using TiO2/Pt and TiO2/Pd photocatalysts, Appl Water Sci. 7 (2017) 3841–3848, https://doi.org/10.1007/s13201-017-0535-3.

[9] G. Sharma, A. Kumar, S. Sharma, A.H. Al-Muhtaseb, Mu. Naushad, A.A. Ghfar, T. Ahamad, F.J. Stadler, Fabrication and characterization of novel Fe0@Guar gum-crosslinked-soya lecithin nanocomposite hydrogel for photocatalytic degradation of methyl violet dye, Sep. Purif. Technol. 211 (2019) 895–908, https://doi.org/10.1016/j.seppur.2018.10.028.

[10] S. Yang, Y. Xu, Y. Huang, G. Zhou, Z. Yang, Y. Yang, G. Wang, Photocatalytic Degradation of Methyl Violet with TiSiW12O40/TiO2, Int. J. Photoenergy (2013) 1–5, https://doi.org/10.1155/2013/191340.

[11] S. Zinatloo-Ajabshir, S. Mortazavi-Derazkola, M. Salavati-Niasari, Preparation, characterization and photocatalytic degradation of methyl violet pollutant of holmium oxide nanostructures prepared through a facile precipitation method, J. Mol. Liq. 231 (2017) 306–313, https://doi.org/10.1016/j.molliq.2017.02.002.

[12] J.-S. Wu, C.H. Liu, K.H. Chu, S.Y. Suen, Removal of cationic dye methyl violet 2B from water by cation exchange membranes, J. Membr. Sci. 309 (2008) 239–245, https://doi.org/10.1016/j.memsci.2007.10.035.

[13] J. Li, D.H.L. Ng, P. Song, C. Kong, Y. Song, Synthesis of SnO2-activated carbon fiber hybrid catalyst for the removal of methyl violet from wate, Mater. Sci. Eng. B. 194 (2015) 1–8, https://doi.org/10.1016/j.mseb.2014.12.007.

[14] P. Li, Y.J. Su, Y. Wang, B. Liu, L.M. Sun, Bioadsorption of methyl violet from aqueous solution onto Pu-erh tea powder, J. Hazard. Mater. 179 (2010) 43–48, https://doi.org/10.1016/j.jhazmat.2010.02.054.

[15] J. Wang, H. Wang, Z. Song, D. Kong, X. Chen, Z. Yang, A hybrid hydrogel for efficient removal of methyl violet from aqueous solutions, Colloids Surf. B. 80 (2010) 155–160, https://doi.org/10.1016/j.colsurfb.2010.05.042.

[16] I.D. Mall, V.C. Srivastava, G.V.A. Kumar, I.M. Mishra, Characterization and utilization of mesoporous fertilizer plant waste carbon for adsorptive removal of dyes from aqueous solution, Colloids Surf. A: Surf Physicochem Eng Aspect 278 (2006) 175–187, https://doi.org/10.1016/j.colsurfa.2005.12.017.