Supporting information

A Computational Study of Optoelectronic and Charge Transport Properties of Purine Nucleobases Dinucleotides

Kimberly Madison, Wojciech Kolodziejczyk, Karina Kapusta, Glake A. Hill*

Interdisciplinary Center for Nanotoxicity,

Department of Chemistry, Physics and Atmospheric Sciences,

Jackson State University, Jackson, MS, 39217, USA

*Corresponding author:

E-mail addresses: glakeh@icnanotox.org (Glake A. Hill);

Phone: +1 (601) 979-1699; Fax: +1 (601) 979-3674

GAS PHASE

C3

C1

C2

C5

C6

C4

C7

C8

WATER PHASE

C3

C2

C1

C6

C4

C5

C7

C8

THF PHASE

C3

C2

C1

C6

C5

C4

C7

C8

DCM PHASE

C3

C2

C1

C6

C5

C4

C8

C7

Figure 1S. Optimized geometries of compounds C1-C8 in gas, water, THF, and DCM phases. The green arrows indicate bending of O-P-O-P dihedral angles.

Table 1S. Absorption spectra characteristics which includes the wavelength (nm), excitation energy (eV), major percent contributions, and the electronic transitions for gas, water, THF, and DCM phases.

| Gas Excitation |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | λ-max (nm) | Excitation Energy (eV) | Major Contributions (%) | Electronic Transitions |
| C1 | 605 | 2.05 | 86 | HOMO - LUMO |
| C2 | 614 | 2.02 | 84 | HOMO - LUMO |
| C3 | 605 | 2.05 | 86 | HOMO-1 - LUMO |
| C4 | 613 | 2.02 | 83 | HOMO-1 - LUMO |
| C5 | 638 | 1.94 | 77 | HOMO - LUMO |
| C6 | 639 | 1.94 | 55 | HOMO - LUMO |
| C7 | 652 | 1.90 | 53 | HOMO - LUMO |
| C8 | 642 | 1.93 | 76 | HOMO - LUMO |
| Water Excitation |  |  |  |  |
|  | λ-max (nm) | Excitation Energy (eV) | Major Contributions (%) | Electronic Transitions |
| C1 | 572 | 2.17 | 91 | HOMO - LUMO |
| C2 | 582 | 2.13 | 90 | HOMO - LUMO |
| C3 | 579 | 2.14 | 91 | HOMO - LUMO |
| C4 | 584 | 2.12 | 90 | HOMO - LUMO |
| C5 | 603 | 2.06 | 78 | HOMO - LUMO |
| C6 | 609 | 2.04 | 72 | HOMO - LUMO |
| C7 | 610 | 2.03 | 70 | HOMO - LUMO |
| C8 | 612 | 2.03 | 75 | HOMO - LUMO |
| THF Excitation |  |  |  |  |
|  | λ-max (nm) | Excitation Energy (eV) | Major Contributions (%) | Electronic Transitions |
| C1 | 584 | 2.12 | 91 | HOMO - LUMO |
| C2 | 614 | 2.02 | 84 | HOMO - LUMO |
| C3 | 579 | 2.14 | 91 | HOMO - LUMO |
| C4 | 613 | 2.02 | 83 | HOMO - LUMO |
| C5 | 616 | 2.01 | 77 | HOMO - LUMO |
| C6 | 639 | 1.94 | 55 | HOMO - LUMO |
| C7 | 615 | 2.02 | 66 | HOMO - LUMO |
| C8 | 643 | 1.93 | 76 | HOMO - LUMO |
| DCM Excitation |  |  |  |  |
|  | λ-max (nm) | Excitation Energy (eV) | Major Contributions (%) | Electronic Transitions |
| C1 | 578 | 2.14 | 90 | HOMO - LUMO |
| C2 | 588 | 2.11 | 88 | HOMO - LUMO |
| C3 | 580 | 2.14 | 91 | HOMO - LUMO |
| C4 | 589 | 2.11 | 89 | HOMO - LUMO |
| C5 | 614 | 2.02 | 76 | HOMO - LUMO |
| C6 | 617 | 2.01 | 72 | HOMO - LUMO |
| C7 | 614 | 2.02 | 67 | HOMO - LUMO |
| C8 | 613 | 2.02 | 77 | HOMO - LUMO |

Table 2S. The reorganization energy, ionization potential energy, and the global chemical reactivity descriptors of all compounds in their gas, water, THF, and DCM phases.

| Gas Phase |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Reorganization energy (eV) | Ionization potential (eV) | Hardness (eV) | Chemical potential (eV) | Electronegativity (eV) | Electrophilicity (eV) |
| C1 | 0.64 | 6.33 | 1.27 | -4.31 | 4.31 | 7.33 |
| C2 | 0.81 | 6.34 | 1.24 | -4.36 | 4.36 | 7.65 |
| C3 | 0.76 | 6.15 | 1.26 | -4.32 | 4.32 | 7.08 |
| C4 | 0.73 | 6.16 | 1.23 | -4.27 | 4.27 | 7.42 |
| C5 | 0.55 | 6.07 | 1.19 | -4.29 | 4.29 | 7.75 |
| C6 | 0.63 | 6.08 | 1.18 | -4.32 | 4.32 | 7.93 |
| C7 | 0.39 | 5.75 | 1.10 | -4.03 | 4.03 | 7.39 |
| C8 | 0.56 | 5.86 | 1.17 | -4.17 | 4.17 | 7.41 |
| Water Phase |  |  |  |  |  |  |
|  | Reorganization energy (eV) | Ionization potential (eV) | Hardness (eV) | Chemical potential (eV) | Electronegativity (eV) | Electrophilicity (eV) |
| C1 | 0.26 | 5.13 | 1.32 | -3.94 | 3.94 | 5.86 |
| C2 | 0.24 | 5.13 | 1.30 | -3.96 | 3.96 | 6.04 |
| C3 | 0.21 | 5.15 | 1.31 | -3.96 | 3.96 | 5.99 |
| C4 | 0.21 | 5.11 | 1.29 | -3.95 | 3.95 | 6.02 |
| C5 | 0.18 | 5.02 | 1.24 | -3.89 | 3.89 | 6.09 |
| C6 | 0.20 | 5.03 | 1.23 | -3.91 | 3.91 | 6.23 |
| C7 | 0.18 | 5.04 | 1.23 | -3.91 | 3.91 | 6.25 |
| C8 | 0.18 | 5.04 | 1.22 | -3.92 | 3.92 | 6.27 |
| THF Phase |  |  |  |  |  |  |
|  | Reorganization energy (eV) | Ionization potential (eV) | Hardness (eV) | Chemical potential (eV) | Electronegativity (eV) | Electrophilicity (eV) |
| C1 | 0.35 | 5.32 | 1.30 | -4.01 | 4.01 | 6.16 |
| C2 | 0.27 | 5.26 | 1.30 | -3.95 | 3.95 | 5.99 |
| C3 | 0.27 | 5.28 | 1.31 | -3.96 | 3.96 | 5.98 |
| C4 | 0.37 | 5.32 | 1.29 | -4.02 | 4.02 | 6.29 |
| C5 | 0.21 | 5.19 | 1.22 | -3.97 | 3.97 | 6.45 |
| C6 | 0.19 | 5.20 | 1.22 | -3.99 | 3.99 | 6.52 |
| C7 | 0.17 | 5.13 | 1.21 | -3.92 | 3.92 | 6.33 |
| C8 | 0.18 | 5.17 | 1.23 | -3.95 | 3.95 | 6.35 |
| DCM Phase |  |  |  |  |  |  |
|  | Reorganization energy (eV) | Ionization potential (eV) | Hardness (eV) | Chemical potential (eV) | Electronegativity (eV) | Electrophilicity (eV) |
| C1 | 0.27 | 5.26 | 1.31 | -3.96 | 3.96 | 5.97 |
| C2 | 0.26 | 5.26 | 1.29 | -3.99 | 3.99 | 6.20 |
| C3 | 0.27 | 5.26 | 1.31 | -3.96 | 3.96 | 6.00 |
| C4 | 0.26 | 5.26 | 1.29 | -3.99 | 3.99 | 6.19 |
| C5 | 0.25 | 5.17 | 1.23 | -3.96 | 3.96 | 6.41 |
| C6 | 0.28 | 5.17 | 1.22 | -3.97 | 3.97 | 6.48 |
| C7 | 0.17 | 5.11 | 1.22 | -3.92 | 3.92 | 6.31 |
| C8 | 0.17 | 5.15 | 1.23 | -3.94 | 3.94 | 6.32 |