Table 1. Experimental conditions for isotherm studies on adsorptive removal of As(III) and As(V) using Fe3O4 particles.

| Parameters | Adsorption isotherm | Effect of solution pH | Unit |
| --- | --- | --- | --- |
| Initial As(III) & (V) conc. | 0.5-70 | 10 | mg/L |
| Fe3O4 dosage | 1 | 1 | g |
| Adsorption time | 24 | 24 | h |
| pH | 7 | 2-10 | - |
| Fe3O4 size | 45-75 | 45-75 | µm |
| Mixing speed | 250 | 250 | rpm |
| Solution volume | 1 | 1 | L |
| Temperature | 20±1 | 20±1 | ˚C |

Table 2. Packed-bed column design for arsenate removal with magnetite particles.

| Design of packed-bed column using Fe₃O₄ for As(V) removal |  |  |
| --- | --- | --- |
| Total Height | 40.0 | cm |
| Height of Magnetite layer | 20.0 | cm |
| Height of glass bead layer | 10.0 each (Top and bottom) | cm |
| Inner diameter | 2.0 | cm |
| Cross-sectional area | 3.14 | cm2 |
| Column volume | 125.6 | cm3 |
| Packing volume of Fe3O4 | 62.83 | cm3 |
| Density of Fe3O4 | 5.0 | g/cm3 |
| Weight of Fe3O4 | 80.0 | g |

Table 3. Packed-bed column operations on arsenate removal by adsorption onto magnetite particles.

| Operational design of packed-bed column using Fe₃O₄ for As(V) removal |  |  |
| --- | --- | --- |
| Input arsenic concentration | 1.0 | mg/L |
| Removal efficiency | 99.0 | % |
| Treat. volume until breakthrough | 0.44 | m3 |
| Empty bed contact time (EBCT) | 0.25 | h |
| Input flowrate | 251.4 | mL/h |
| Input flowrate | 4.19 | mL/min |
| Empty bed volume (EBV) | 80.00 | cm/h |
| Daily treatment capacity | 6.03 | L/d |
| Daily adsorption amount | 5.43 | mgAs/d |
| Duration until breakthrough | 74 | days |

Table 4. Particle size distribution of synthesized magnetite

| Sieving time: 15min | Quantity (Kg) | Recovery (%) |
| --- | --- | --- |
| Particle size |  |  |
| < 75 µm | 0.09 | 2.25 |
| 75-150 µm | 0.61 | 15.25 |
| 150-300 µm | 0.81 | 20.25 |
| 300-425 µm | 0.78 | 19.50 |
| 425-600 µm | 1.09 | 27.25 |
| > 600 µm | 0.55 | 13.75 |
| Total | 4.00 | 100 |