Supplementary Information

Engineering a BSA-templated Iridium Oxide Nanozyme for Colorimetric Evaluation of Total Antioxidant Capacity in Food Samples
Shuangshuang Yana,d,1, Dongying Ana,c,1, Yutian Zhoua,c,1, Xinli Guoa,c, Zhihang Qinc, Li Yuanc, Mengmeng Wanga,*, Yang Zhanga,b,*

aShenyang Key Laboratory of Medical Molecular Theranostic Probes in School of Pharmacy, Shenyang Medical College, 146 Huanghe North Avenue, Shenyang 110034, China
bLiaoning Province Key Laboratory for Phenomics of Human Ethnic Specificity and Critical Illness, Shenyang Medical College, 146 Huanghe North Avenue, Shenyang 110034, China
cSchool of Basic Medicine, Shenyang Medical College, 146 Huanghe North Avenue, Shenyang 110034, China
dSchool of Public Health, Shenyang Medical College, 146 Huanghe North Avenue, Shenyang 110034, China
Corresponding Author

*E-mail: wangmengmeng@symc.edu.cn; zhangyang@symc.edu.cn

Tel: +86 24 62215711; Fax: +86 24 62215711
1These authors contributed equally to this work

Kinetic assays with variable TMB concentration. H2O2 concentration was 5 mM, while TMB concentration was varied within the range of 0-1.5 mM. The reaction system was prepared by sequentially mixing 10 μL b-IrOx (50 μg/mL), variable-volume TMB solution, and 10 μL H2O2 (5 mM), followed by adding NaAc-HAc buffer addition to 200 μL. After incubation at 25 °C, the change of absorbance at 652 nm was recorded every 2 min for 30 min. The V was derived from the linear segment of the absorbance-time curve.
Kinetic assays with variable H2O2. TMB was 1 mM, while H2O2 concentration varied from 0 to 16 mM. The reaction system contained 10 μL b-IrOx (50 μg/mL), 30 μL TMB (1 mM), and variable-volume H2O2 solution, followed by adding NaAc-HAc buffer addition to 200 μL. Absorbance at 652 nm was measured as above, with V calculated from linear curves.

Kinetic parameter calculation. Kinetic parameters including Michaelis constant (Km) and maximum reaction velocity (Vmax) were calculated as follows.
V = Vmax [S] / (Km + [S])                         (1)
Where V, Vmax, [S], and Km represent the initial reaction velocity, maximum velocity, substrate concentration (TMB or H2O2), and Michaelis constant, respectively.
[image: image1.png]A 07
0.6
0.5

£03
02
0.1
0.0

10

L6
14
12
1.0
208
<06
0.4
0.2
0.0

10

20 30 40
Temperature (°C)

50

60




Figure S1. The catalytic activity of b-IrOx. The effect of (A) pH 3.0-10.0 and (B) Temperature (10-60◦C). 
[image: image2.png]A B

1.4 0.8
[

1.2 0.7
. 1.0 0.6
508 a
M 20.5

< 0.6 -

04 0.4

0.2 0.3

0.0k 0.2

0 50 100 150 200 250 0 10 20 30 40 50 60

b-IrOx (ug/mL) Time (min)




Figure S2. The catalytic activity of b-IrOx. The effect of (A) Concentration (5–250 μg/mL) of b-IrOx and (B) Reaction time (1–60 min).

[image: image3.png]1.5
1.0

2.5
2.0
0.5
0.0

v v




Figure S3. Selectivity studies of b-IrOx nanozyme-based TMB colorimetric sensor towards different substances. 
Table S1. Linear detection performance of the b-IrOx-based TMB colorimetric method for different antioxidants.
	Antioxidant
	Linear equation
	Range

(μM)
	R2
	LOD
(μM)

	Trolox
	y = 0.0065x+0.0201
	0.1-100
	0.9954
	0.27

	GSH
	y =0.0221x+0.0638

y =0.0037x+0.2717
	0.2-90
	0.9900

0.9907
	0.35

	AA
	y = 0.0173x+0.1154
	0.5-20
	0.9935
	0.53

	Caffeic acid
	y = 0.0116x+0.0937
	0.1-40
	0.9977
	0.15


Table S2. Recovery study of standard Trolox in different samples by using TMB as substrate. (n=3)
	Sample
	Added Trolox (µM)
	Found
(µM)
	Recovery

(%)
	RSD

(%)

	Yellow peach juice
	10
	48.47 ± 1.89
	96.31
	1.31

	
	20
	57.41 ± 0.42
	90.49
	0.95

	
	30
	69.37 ± 0.77
	101.78
	2.91

	Apple juice
	10
	17.64 ± 2.11
	98.97
	2.51

	
	20
	29.05 ± 1.56
	106.79
	1.83

	
	30
	40.92 ± 0.39
	110.62
	0.65

	Mango juice
	10
	57.71 ± 0.84
	102.97
	1.67

	
	20
	67.16 ± 0.41
	99.62
	1.04

	
	30
	80.48 ± 0.91
	110.21
	1.05


