Mechanism of moisture adsorption in plant fibers surface-modified with glycerol evaluated by LF-NMR relaxation technique

Lili Fu, Ke Zhang, Mingjian Zhang, Le Wang, Songjin Zheng, Ze Liu, Shanzhai Shang, Yue Sun, Feng Huang, Shuang Wang, Qi Zhang, Bing Wang, Bin Li, Yan Cao, Zhongya Guo*

Fig. S1  Adsorption isotherms of the samples (a. ZZP0; b. ZZP1; c. ZZP2; d. ZZP3) at 0-95 % RH for the cycle of adsorption-desorption

Fig. S2  SEM photograph of the samples (a) ZZP0, (b) ZZP1, (c) ZZP2, (d) ZZP3

Fig. S3  IR spectra of hygroscopic samples: (a) ZZP0; (b) ZZP1; (c) ZZP2; (d) ZZP3

Table S1  Element content of the plant fiber samples

| Element | Content /At% |  |  |  |
| --- | --- | --- | --- | --- |
|  | ZZP0 | ZZP1 | ZZP2 | ZZP3 |
| C | 42.97 | 46.39 | 48.22 | 47.45 |
| N | 14.17 | 4.98 | 4.61 | 4.11 |
| O | 42.86 | 48.64 | 47.17 | 48.44 |

*Corresponding authors, https://orcid.org/0000-0001-8160-4866, E-mail address: zhongyaguo@126.com

Phone numbers: +86-0371-67672972

Zhengzhou Tobacco Research Institute of CNTC, 450001, Zhengzhou, China

Lili Fu, Ke Zhang, Mingjian Zhang, Le Wang, Yue Sun, Feng Huang, Shuang Wang, Qi Zhang, Bing Wang, Bin Li, Zhongya Guo

China Tobacco Hebei Industrial Co. Ltd, 050051, Shijiazhuang, China

Songjin Zheng

China Tobacco Yunnan Industrial Co. Ltd, 650202, Kunming, China

Ze Liu, Shanzhai Shang

Guangzhou Institute of Energy Conversion, Chinese Academy of Sciences, 510640, Guangzhou,China

Yan Cao