Comparative Study on Cathode Delamination for Efficient Lithium-ion Battery Recycling with Industrial Relevance

(Supporting Information)

Varun Kumar Sarwa, Neha Shukla*

School of Mechanical and Materials Engineering, Indian Institute of Technology, Mandi, Himachal Pradesh-175005, India

*Corresponding author: +919617585140; nehashukla@iitmandi.ac.in

- Cost and Energy Analysis:

Reagents Used (according to used proportion)

Reagent Cost Reagent Cost

Total Cost Reagent Cost

Electricity Cost Cost Reagent Cost

Energy Consumption (as per equipment consumption)

Reagent Regeneration

Table S1: Detailed cost and energy analysis, including reagent, electricity, and solvent regeneration costs.

| Process | Reagents Used | Reagent Cost/ Cell (INR) | Equipment Used | Time for Equipment Used | Energy Consumption (Wh) | Electricity Cost/ Cell (INR) | Reagent Regeneration/ Effluent Treatment Cost (INR) | Total Cost/ Cell (INR) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Direct Calcination | - | - | Tube Furnace (4.5 kW) | ~1h | ~53 | ~0.424 | ~10 | ~10.4 |
| Molten Salt Delamination | AlCl3 (~129 g) + NaCl (~56 g) | ~293 | Tube Furnace (4.5 kW) | ~40 min | ~3000 | ~24 | ~11 | ~328 |
| Electrochemical Delamination | Na2SO4 (~28 g) | ~11 | Electrolysis Setup (20W) + Tube Furnace (For binder decomposition) | ~20 sec (electrolysis) and ~1h (thermal treatment for PVDF decomposition) | ~168 | ~1.34 | ~10 | ~11.3 |
| NMP Dissolution | ~370 mL | ~407 | Ultra-sonicator (200W) | ~30 min | ~75 | ~1 | ~9 | ~417 |
| DMI | ~740 mL | ~808 | Hot plate stirrer (500W) | ~5h | ~2500 | ~20 | ~17 | ~845 |
| Cyrene | ~93 mL | ~2232 | Overhead stirrer (200W) | ~1h | ~600 | ~5 | ~23 | ~2260 |
| GVL | ~180 mL | ~113 | Hot plate stirrer (500W) | ~30 min | ~258 | ~2 | ~3 | ~118 |

  - Important Considerations:

- Standard NMC18650 cell has a total weight of ~45 g, the cathode strip weight of ~18.5 g, and PVDF 4 wt% coating (~0.7 g). The net Active material fraction of the coating is ~90%, i.e., 15.75 g [1].

- The total surface area of the cathode strip is ~720 (2*360) cm2 [2].

- The cost of electricity for industrial use is around ~INR8 [3].

- The whole calculation is performed for the delamination of one NMC18650 cell.

- The electricity cost is calculated for the equipment available in the corresponding laboratory.

- The reagent regeneration/ effluent treatment cost is determined by the energy input and the cost of reagent loss for the process.

- The direct depreciation cost for reagents is not included, but the depreciation during use is indirectly expressed through the cost associated with solvent loss in the reaction.

- Quantitative Environmental Analysis:

The simplified base formula, which is also mentioned in the main manuscript, is shown in the equation below.

Enet ​= Eavoided​ − Eprocess

The expanded form of the above formula is shown in the equation below.

Enet ​= (m1​⋅EF1​+m2​⋅EF2​+m3​⋅EF3​) − [Eelec​⋅EFelec​+(L1​⋅EFL1​+L2​⋅EFL2​) + (M⋅erecov​⋅EFelec​) + Eother

Where,

- Enet​: Net carbon impact (kg CO₂e).

- m1, m2, m3​: Mass of recovered materials (e.g., cathode active material, binder, aluminium).

- EFAM and EFPVDF​: Emission factors for virgin production of active cathode materials and PVDF, respectively (kg CO₂e/kg).

- Eelec: Electricity consumed by the process (kWh).

- EFelec: Carbon intensity of electricity (kg CO₂e/kWh).

- L1, L2: Net losses of solvents or reagents (kg).

- EFL1, EFL2​: Production emission factors of those solvents/reagents (kg CO₂e/kg).

- M: Mass of solvent recovered (kg).

- erecov​: Energy needed to recover 1 kg of solvent (kWh/kg).

- Eother: Other emissions (transport, fugitive, heating, etc.).

Additionally,

- Sign convention: Enet > 0 = net savings (benefit); Enet < 0 = net burden.

  - Key Factors for Calculations

- 2% of Li volatization loss % in direct calcination or thermal treatment for PVDF decomposition is also incorporated [4].

- EFs of avoided emission because of the prevention of use of Virgin cathode EFAM = 42.8 kgCO₂/kg. and EFPVDF = 55.8 kgCO₂/kg. [5].

- 99% of solvent or reagent recovery during regeneration is assumed as all the referred literatures show complete regeneration (qualitative, not quantitative).

- EFelec is referred to as 0.727 kgCO2e/kWh for the Indian grid [6]. The carbon intensity of the grid (EFelec) varies greatly by region.

- The assumption of a pilot scale “proxy industrial” scenario for direct calcination or thermal treatment for PVDF decomposition is made, in which a furnace with 30kW of rating is used to treat 10 Kg of active material batch loading at a time. This pilot-scale calculation is applied only to the commonly practiced thermal processes, such as direct calcination and electrochemical delamination (which also requires a subsequent thermal step for PVDF decomposition). In contrast, emerging solvent-based routes are evaluated using parameters drawn directly from the literature, as comprehensive batch-size data for these methods are not yet available.

Table S2:  Quantitative environmental impact analysis for CDPs.

| Process | Energy (Wh) | Energy emission (kg CO₂ eq) | Reagent emission (kg CO₂ eq) | Solvent recovery/energy emission (kg CO₂ eq) | Eprocess (kg CO₂ eq) | Eavoided (kg CO₂ eq) | Enet (kg CO₂ eq) | Hazadrouseffluent generation (g) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Direct calcination | 53 | 0.0386 | 0.00000 | 0.00000 | 0.0386 | 0.6606 | +0.622 | 0.19 g HF |
| Molten-salt (AlCl₃+NaCl) | 3000 | 2.181 | 0.0052 | 0.1982 | 2.3844 | 0.7132 | -1.67 | - |
| Electrochemical (Na₂SO₄) | 168 | 0.122 | 0.00280 | 0.0953 | 0.2201 | 0.6997 | +0.480 | 0.19 g HF |
| NMP dissolution | 75 | 0.0545 | 0.004 (net solvent loss) | 0.037108 | 0.0960 | 0.7132 | +0.6172 | - |
| DMI dissolution | 2500 | 1.818 | 0.003 (net solvent loss) | 0.188574 | 1.373 | 0.7132 | -0.659 | - |
| Cyrene | 600 | 0.436 | 0.001 (net solvent loss) | 0.027558 | 0.465 | 0.7132 | +0.248 | - |
| GVL | 258 | 0.1876 | 0.001 (net solvent loss) | 0.0004 | 0.189 | 0.7132 | +0.524 | - |

- Toxicity Index

Table S3:  Toxicity index of the compared solvents [3].

| Solvent | IC₅₀ (µM) | Toxicity Models | Comments |
| --- | --- | --- | --- |
| Dimethyl isosorbide | >100000 | Very low toxicity | One of the least toxic solvents in the table |
| NMP | 24700 | Moderate toxicity | Known reproductive toxin; included in REACH SVHC list |
| Cyrene | 1000 | High toxicity (IC₅₀ low) | Biogenic but more toxic than some assume |
| GVL | 6600 | Moderate-low toxicity | Biodegradable, often considered green |

Note:

- IC₅₀ (µM): Concentration required to inhibit 50% of the biological activity in a given assay. Lower = more toxic.

Reference

[1]	“18650 Lithium Battery Specs-mAh and Important Specs-battery-knowledge | Large Power.” Accessed: Jul. 10, 2025. [Online]. Available: https://www.large.net/news/8mu43p8.html

[2]	Nigel, “LG INR 18650 MJ1,” Battery Design. Accessed: Jul. 10, 2025. [Online]. Available: https://www.batterydesign.net/lg-18650/

[3]	“Book_2023 (1).”, Assessed: Dec. 08, 2025. [Online]. Available: http://www.cea.in/, CEA COVER FINAL 2024.cdr

[4]	C. Wu, J. Ban, T. Chen, J. Wang, Y. He, and Z. Wu, “Evolution Path of Precursor-Induced High-Temperature Lithiation Reaction during the Synthesis of Lithium-Rich Cathode Materials,” ACS Omega, vol. 9, no. 13, pp. 15191–15201, Apr. 2024, doi: 10.1021/acsomega.3c09567.

[5]	“Ecoinvent | GHG Protocol.” Accessed: Dec. 08, 2025. [Online]. Available: https://ghgprotocol.org/ecoinvent

[6]	“Emission Factor: Electricity supplied from grid - weighted average (for net effective injection into grid) | Energy | Electricity | India | Climatiq.” Accessed: Dec. 08, 2025. [Online]. Available: https://www.climatiq.io/data/emission-factor/404c5385-0f7a-4267-8d3c-56866bf10156