Supporting Information

Multidimensional Bidirectional Functional Ordering Strategy for Deep-Ultraviolet Nonlinear Optical Crystals

Meng Chenga, b#, Linlin Liua, b#, Abudukadi Tudia, b#, Chenxu Lia, b, Xueling Houa, b, Zhihua Yang a, b* & Shilie Pana, b*

a Research Center for Crystal Materials; CAS Key Laboratory of Functional Materials and Devices for Special Environmental Conditions; Xinjiang Key Laboratory of Functional Crystal Materials; Xinjiang Technical Institute of Physics and Chemistry, Chinese Academy of Sciences, 40-1 South Beijing Road, Urumqi 830011, China

b Center of Materials Science and Optoelectronics Engineering, University of Chinese Academy of Sciences, Beijing 100049, China

# These authors contributed equally.

* Corresponding authors, E-mails: zhyang@ms.xjb.ac.cn and slpan@ms.xjb.ac.cn

Contents

Table S1 Crystallographic data for [C(NH2)3]B6O9F.

Table S2 Atomic coordinates (× 104), equivalent isotropic displacement parameters (Å2 × 103) and bond valence sum (BVS) calculation for C(NH2)3B6O9F. U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

Table S3 Selected bond distances (Å) and angles (deg) for C(NH2)3B6O9F.

Table S4 The atom charges for LiB6O9F obtained from the electron density by the Bader method.

Table S5 The atom charges for [C(NH2)3]B6O9F obtained from the electron density by the Bader method.

Table S6 The data of HOMO-LUMO energy gap, polarizability anisotropy for [B6O11F] groups and hyperpolarizability with torsion angle.

Table S7 Basic information (energy above the hull (Eₕᵤₗₗ, in eV/atom), space group (SG), band gap (Eg, in eV) calculated at the HSE06 level) and key parameters (SHG (pm/V), birefringence (Δn) at 1064 nm, and shortest SHG phase-matching wavelength (λPM)) of [C(NH2)3]B6O9F (designated GBOF-i, where i = 1-30). FWPM denotes full-wavelength phase-matching.

Table S8 Birefringence among all anhydrous and ordered fluorooxoborate compounds with deep-UV cut-off edges.

Figure S1 The 2D [B6O9F]∞ layers for [C(NH2)3]B6O9F(up) and LiB6O9F(down) in ac plane.

Figure S2 The Powder X-ray diffraction patterns for [C(NH2)3]B6O9F at different temperature.

Figure S3 The IR Spectra of [C(NH2)3]B6O9F.

Figure S4 The TG-DSC curve of [C(NH2)3]B6O9F.

Figure S5 The ELF map of [C(NH2)3] group in [C(NH2)3]B6O9F.

Figure S6 The ELF map of 2D [B6O9F]∞ anion layer in [C(NH2)3]B6O9F.

Figure S7. The low-lying allotropes of [C(NH2)3]B6O9F. Top and side views of crystal structures for [C(NH2)3]B6O9F with the same anionic frameworks [B6O9F] and different cation [C(NH2)3] functional motifs are presented.

Figure S8. Phonon dispersion spectra for predicted stable GBOF-i (i=1-30) calculated with linear response method.

Figure S9. The SHG density maps of occupied and unoccupied orbitals of the largest effective NLO coefficient d33 in a virtual-electron process of GBOF-i (i=1, 3, 4, 5, 12).

Table S1. Crystallographic data for [C(NH2)3]B6O9F.

| Formula | [C(NH2)3]B6O9F |
| --- | --- |
| Formula weight | 287.95 |
| Temperature / K | 273.15 |
| CCDC number | 2523050 |
| Crystal system | orthorhombic |
| Space group | Pna21 |
| a / Å | 7.8420(11) |
| b / Å | 15.1862(19) |
| c / Å | 8.5762(9) |
| α / ° | 90 |
| β / ° | 90 |
| γ / ° | 90 |
| Volume / Å3 | 1021.3(2) |
| Z | 4 |
| ρcalc g/cm3 | 1.873 |
| μ / mm-1 | 0.179 |
| F (000) | 576.0 |
| Radiation | Mo Kα (λ = 0.71073) |
| 2θ range for date collection/ ° | 5.456 to 55.046 |
| Index ranges | -10 ≤ h ≤ 10, -19 ≤ k ≤ 19, -10 ≤ l ≤ 11 |
| Reflections collected | 7276 |
| Independent reflections | 2293 [Rint = 0.0644, Rsigma = 0.0559] |
| Data / restraints / parameters | 2293 / 1 / 182 |
| Goodness-of-fit on F2 | 1.071 |
| Final R indices [I ≥ 2σ (I)]a | R1= 0.0468, wR2= 0.1096 |
| Final R indices (all data)a | R1= 0.0653, wR2= 0.1270 |
| Largest diff. peak / hole /e Å-3 | 0.21 / - 0.23 |

aR1 = Fo - Fc/Fo and wR2 = [w(Fo2 – Fc2)2 / wFo4]1/2 for Fo2> 2( Fo2)

Table S2. Atomic coordinates (×104) and equivalent isotropic displacement parameters (Å2 ×103) for [C(NH2)3]B6O9F. U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

| Atoms | x | y | z | U(eq) | BVS |
| --- | --- | --- | --- | --- | --- |
| B1 | 7626(6) | 4890(3) | 4522(6) | 25.7(9) | 3.04 |
| B2 | 8315(6) | 4386(3) | 1984(6) | 25.0(9) | 3.04 |
| B3 | 7599(7) | 3350(3) | 3929(5) | 29.3(11) | 3.05 |
| B4 | 7491(7) | 1693(3) | 3903(6) | 31.5(11) | 3.09 |
| B5 | 7003(6) | 182(3) | 4442(5) | 26.0(10) | 3.08 |
| B6 | 8398(6) | 592(3) | 2005(6) | 27.0(10) | 3.10 |
| C1 | 4780(7) | 2574(3) | 8321(7) | 41.5(13) | 4.45 |
| N1 | 3911(11) | 2531(4) | 9604(7) | 89(2) |  |
| N2 | 5124(8) | 3332(4) | 7678(9) | 90(2) |  |
| N3 | 5192(9) | 1857(4) | 7615(8) | 88(2) |  |
| O1 | 7347(4) | 5570.6(18) | 5456(4) | 30.9(7) | 1.93 |
| O2 | 8298(4) | 5050.0(18) | 3049(3) | 27.4(7) | 1.98 |
| O3 | 7258(4) | 4029(2) | 4933(3) | 33.1(8) | 1.97 |
| O4 | 8522(4) | 4512.8(18) | 430(3) | 29.1(7) | 2.00 |
| O5 | 8224(4) | 3518.1(19) | 2470(3) | 32.3(8) | 1.97 |
| O6 | 7272(5) | 2529.4(18) | 4475(4) | 38.9(9) | 2.04 |
| O7 | 8264(4) | 1495.3(19) | 2582(3) | 33.2(8) | 1.93 |
| O8 | 6845(5) | 1045(2) | 4889(4) | 36.1(8) | 1.94 |
| O9 | 7609(5) | -40(2) | 3049(4) | 36.6(8) | 1.93 |
| F1 | 10133(3) | 366(2) | 1874(5) | 52.4(9) | 1.71 |
| H1A | 3617 | 2028 | 9975 | 107 |  |
| H1B | 3629 | 3007 | 10085 | 107 |  |
| H3A | 4891 | 1356 | 7996 | 106 |  |
| H3B | 5768 | 1877 | 6762 | 106 |  |
| H2A | 5625 | 3352 | 6787 | 108 |  |
| H2B | 4851 | 3813 | 8146 | 108 |  |

Table S3. Bond lengths[Å] and angles [deg] for [C(NH2)3]B6O9F.

| Bond | Bond length (Å) | Bond | Bond length (Å) |
| --- | --- | --- | --- |
| B1-O2 | 1.390(6) | B4-O7 | 1.319(6) |
| B2-O2 | 1.360(5) | B1-O3 | 1.385(5) |
| B6-F1 | 1.408(6) | B3-O3 | 1.370(6) |
| B1-O1 | 1.325(5) | B4-O6 | 1.372(6) |
| B61-O1 | 1.452(6) | B3-O6 | 1.355(6) |
| B2-O4 | 1.356(6) | B5-O8 | 1.372(5) |
| B52-O4 | 1.386(5) | B4-O8 | 1.393(6) |
| B2-O5 | 1.385(5) | C1-N1 | 1.296(8) |
| B3-O5 | 1.368(6) | C1-N3 | 1.288(7) |
| B5-O9 | 1.329(6) | C1-N2 | 1.304(7) |
| B6-O9 | 1.452(6) | B5-O43 | 1.386(5) |
| B6-O7 | 1.462(5) | B6-O14 | 1.452(6) |
|  | Bond angle (degree) |  | Bond angle (degree) |
| N1-C1-N2 | 120.8(6) | F1-B6-O14 | 108.1(4) |
| N3-C1-N1 | 119.2(6) | F1-B6-O9 | 107.5(4) |
| N3-C1-N2 | 119.8(6) | F1-B6-O7 | 109.0(4) |
| O1-B1-O2 | 118.4(4) | O14-B6-O9 | 112.2(4) |
| O1-B1-O3 | 123.2(4) | O14-B6-O7 | 107.6(3) |
| O3-B1-O2 | 118.4(4) | O9-B6-O7 | 112.4(4) |
| O2-B2-O5 | 120.2(4) | O7-B4-O6 | 125.1(4) |
| O4-B2-O2 | 123.8(4) | O7-B4-O8 | 121.8(4) |
| O4-B2-O5 | 115.9(4) | O6-B4-O8 | 113.0(4) |
| O9-B5-O43 | 118.0(4) | O5-B3-O3 | 120.3(4) |
| O9-B5-O8 | 121.8(4) | O6-B3-O5 | 123.8(4) |
| O8-B5-O43 | 120.2(4) | O6-B3O3 | 116.0(4) |

Symmetry transformations used to generate equivalent atoms:

13/2-X,1/2+Y,1/2+Z; 23/2-X,1/2+Y,-1/2+Z; 33/2-X,-1/2+Y,1/2+Z; 43/2-X,-1/2+Y,-1/2+Z

Table S4. The atom charges for [C(NH2)3]B6O9F obtained from the electron density by the Bader method.

| Atoms | U11 | U22 | U33 | U23 | U13 | U12 |
| --- | --- | --- | --- | --- | --- | --- |
| B1 | 41(2) | 18(2) | 18(2) | 0.0(18) | -2(2) | -1.0(18) |
| B2 | 35(2) | 20(2) | 20(2) | 1(2) | 0.8(18) | 2.8(18) |
| B3 | 53(3) | 16(2) | 18(2) | 0.6(18) | 1(2) | 3(2) |
| B4 | 55(3) | 18(2) | 22(2) | -2.1(19) | 3(2) | -4(2) |
| B5 | 39(2) | 19(2) | 20(2) | 1.5(19) | -2(2) | -0.2(17) |
| B6 | 38(2) | 21(2) | 22(2) | -2(2) | 2.7(19) | -0.9(19) |
| C1 | 66(3) | 25(2) | 34(3) | 2(2) | 15(2) | 1(2) |
| N1 | 139(6) | 83(5) | 46(3) | -14(3) | 47(4) | -20(4) |
| N2 | 97(5) | 48(3) | 125(6) | 41(4) | 22(4) | -9(3) |
| N3 | 141(6) | 59(4) | 64(4) | -23(3) | 7(4) | 45(4) |
| O1 | 54.1(19) | 16.8(14) | 21.7(15) | -1.7(13) | 2.7(14) | 2.0(13) |
| O2 | 44.5(17) | 19.3(14) | 18.5(14) | -0.5(12) | 2.4(14) | -3.7(12) |
| O3 | 63(2) | 17.1(14) | 18.8(14) | -0.6(12) | 9.6(15) | -0.4(13) |
| O4 | 48.1(18) | 20.7(15) | 18.6(14) | 2.3(13) | 5.9(13) | 5.5(12) |
| O5 | 57.4(19) | 19.6(16) | 19.8(15) | 1.1(13) | 7.5(13) | 2.6(13) |
| O6 | 81(3) | 15.4(15) | 20.8(15) | -1.2(12) | 16.0(16) | -2.4(14) |
| O7 | 56.6(19) | 20.3(16) | 22.6(16) | -3.2(13) | 11.0(13) | -7.2(13) |
| O8 | 66(2) | 18.7(15) | 23.8(15) | -0.8(13) | 13.9(15) | -2.4(14) |
| O9 | 70(2) | 19.8(15) | 19.8(14) | -1.5(13) | 6.1(16) | -2.2(14) |
| F1 | 37.8(14) | 57.4(19) | 62(2) | -12.0(17) | -1.4(15) | 6.9(14) |

Table S4. The atom charges for LiB6O9F obtained from the electron density by the Bader method.

| Atoms | Get Charge | Atoms | Get Charge |
| --- | --- | --- | --- |
| Li1 | -0.8214 | O3 | 1.626014 |
| Li2 | -0.82108 | O4 | 1.627108 |
| Li3 | -0.82266 | O5 | 1.618611 |
| Li4 | -0.81983 | O6 | 1.615519 |
| B1 | -2.43724 | O7 | 1.61902 |
| B2 | -2.4286 | O8 | 1.619386 |
| B3 | -2.43275 | O9 | 1.564053 |
| B4 | -2.43312 | O10 | 1.55716 |
| B5 | -2.34191 | O11 | 1.553209 |
| B6 | -2.33961 | O12 | 1.56433 |
| B7 | -2.34556 | O13 | 1.592112 |
| B8 | -2.34001 | O14 | 1.591771 |
| B9 | -2.41061 | O15 | 1.590184 |
| B10 | -2.41241 | O16 | 1.594011 |
| B11 | -2.40773 | O17 | 1.574316 |
| B12 | -2.41234 | O18 | 1.597406 |
| B13 | -2.37244 | O19 | 1.595508 |
| B14 | -2.38391 | O20 | 1.581235 |
| B15 | -2.38564 | O21 | 1.593958 |
| B16 | -2.37434 | O22 | 1.595771 |
| B17 | -2.41769 | O23 | 1.593349 |
| B18 | -2.42832 | O24 | 1.5961 |
| B19 | -2.42797 | O25 | 1.58661 |
| B20 | -2.41752 | O26 | 1.587389 |
| B21 | -2.35993 | O27 | 1.58206 |
| B22 | -2.37663 | O28 | 1.59111 |
| B23 | -2.38254 | O29 | 1.608737 |
| B24 | -2.35551 | O30 | 1.592474 |
| F1 | 0.853821 | O31 | 1.594934 |
| F2 | 0.849068 | O32 | 1.607113 |
| F3 | 0.852417 | O33 | 1.554524 |
| F4 | 0.851512 | O34 | 1.559325 |
| O1 | 1.622172 | O35 | 1.561975 |
| O2 | 1.624739 | O36 | 1.549097 |

The analysis of Bader charges indicates that Li lost 0.821 charges.

Table S5. The atom charges for [C(NH2)3]B6O9F obtained from the electron density by the Bader method.

| Atoms | Get Charge | Atoms | Get Charge | Atoms | Get Charge |
| --- | --- | --- | --- | --- | --- |
| B1 | -2.23083 | N9 | 1.065713 | O33 | 1.480361 |
| B2 | -2.22613 | N10 | 1.053079 | O34 | 1.466143 |
| B3 | -2.22563 | N11 | 1.047494 | O35 | 1.461008 |
| B4 | -2.23568 | N12 | 1.067506 | O36 | 1.484986 |
| B5 | -2.21601 | O1 | 1.462293 | F1 | 0.80242 |
| B6 | -2.22453 | O2 | 1.471739 | F2 | 0.805624 |
| B7 | -2.2137 | O3 | 1.461868 | F3 | 0.799705 |
| B8 | -2.22371 | O4 | 1.472753 | F4 | 0.804257 |
| B9 | -2.23672 | O5 | 1.426246 | H1 | -0.32062 |
| B10 | -2.22178 | O6 | 1.42529 | H2 | -0.34815 |
| B11 | -2.21299 | O7 | 1.432158 | H3 | -0.3618 |
| B12 | -2.2371 | O8 | 1.418659 | H4 | -0.31585 |
| B13 | -2.24388 | O9 | 1.43262 | H5 | -0.38021 |
| B14 | -2.23291 | O10 | 1.426728 | H6 | -0.37545 |
| B15 | -2.23634 | O11 | 1.433286 | H7 | -0.3754 |
| B16 | -2.24574 | O12 | 1.440859 | H8 | -0.38139 |
| B17 | -2.31171 | O13 | 1.55274 | H9 | -0.40636 |
| B18 | -2.30755 | O14 | 1.5227 | H10 | -0.40913 |
| B19 | -2.3059 | O15 | 1.540123 | H11 | -0.41041 |
| B20 | -2.31355 | O16 | 1.559394 | H12 | -0.41055 |
| B21 | -2.38131 | O17 | 1.493699 | H13 | -0.41417 |
| B22 | -2.36197 | O18 | 1.479211 | H14 | -0.40256 |
| B23 | -2.38348 | O19 | 1.491242 | H15 | -0.4109 |
| B24 | -2.38666 | O20 | 1.488899 | H16 | -0.40961 |
| C1 | -1.81486 | O21 | 1.529833 | H17 | -0.40215 |
| C2 | -1.81893 | O22 | 1.52009 | H18 | -0.41206 |
| C3 | -1.82088 | O23 | 1.522231 | H19 | -0.40712 |
| C4 | -1.81984 | O24 | 1.530493 | H20 | -0.40399 |
| N1 | 1.075813 | O25 | 1.524347 | H21 | -0.29886 |
| N2 | 1.100801 | O26 | 1.527708 | H22 | -0.27402 |
| N3 | 1.112914 | O27 | 1.524166 | H23 | -0.27124 |
| N4 | 1.076585 | O28 | 1.522022 | H24 | -0.2971 |
| N5 | 1.195094 | O29 | 1.61196 |  |  |
| N6 | 1.17253 | O30 | 1.621828 |  |  |
| N7 | 1.187657 | O31 | 1.620961 |  |  |
| N8 | 1.194438 | O32 | 1.616858 |  |  |

The analysis of Bader charges indicates that [C(NH2)3] lost 0.706 charges.

Table S6. The data of HOMO-LUMO energy gap, polarizability anisotropy for [B6O11F] groups and hyperpolarizability with torsion angle.

| Torsion angle (°) | HOMO-LUMO（eV） | Polarizability anisotropy | Hyperpolarizability |
| --- | --- | --- | --- |
| 0 | 5.59111 | 36.99413 | 136.5524 |
| 10 | 5.63057 | 39.7077 | 134.008 |
| 29.1 | 5.74566 | 43.32994 | 126.8629 |
| 33.04 | 5.77233 | 43.78615 | 125.2404 |
| 40 | 5.82076 | 44.34164 | 123.027 |
| 50.49 | 5.89396 | 44.58087 | 122.711 |
| 70 | 6.02239 | 43.39696 | 134.6375 |
| 90.25 | 6.13123 | 40.55963 | 163.042 |
| 100.11 | 6.17068 | 38.86582 | 176.9565 |
| 110.96 | 6.19844 | 36.99535 | 187.3831 |
| 115 | 6.20442 | 36.33857 | 189.5156 |
| 120 | 6.20905 | 35.58677 | 190.417 |
| 125 | 6.21095 | 34.91798 | 189.5454 |
| 130 | 6.20851 | 34.34793 | 187.2889 |
| 140.55 | 6.17098 | 33.5669 | 178.7235 |
| 160 | 6.1198 | 33.77973 | 159.3755 |
| 180 | 6.00171 | 35.61299 | 150.3658 |

Table S7 Basic information (energy above the hull (Eₕᵤₗₗ, in eV/atom), space group (SG), band gap (Eg, in eV) calculated at the HSE06 level) and key parameters (SHG (pm/V), birefringence (Δn) at 1064 nm, and shortest SHG phase-matching wavelength (λPM)) of [C(NH₂)₃]B₆O₉F (designated GBOF-i, where i = 1-30). FWPM denotes full-wavelength phase-matching.

| Crystal | Ehull | SG | Eg | SHG | ∆n | λPM |
| --- | --- | --- | --- | --- | --- | --- |
| GBOF-1 | 16.81 | Pna21 | 6.65 | d24=0.89, d33=-1.00, d15=-0.07 | 0.143 | FWPM |
| GBOF-2 | 17.45 | P21/c | 6.51 |  | 0.162 |  |
| GBOF-3 | 17.73 | Pna21 | 6.71 | d24=0.22, d33=-0.40, d15=-0.0036 | 0.137 | 192 |
| GBOF-4 | 18.23 | Pna21 | 6.47 | d24=-0.49, d33=0.72, d15=-0.19 | 0.152 | FWPM |
| GBOF-5 | 18.30 | Pc | 6.82 | d15=-0.42, d12=-0.17, d13=-0.12, d24=0.05, d33=-0.69 | 0.134 | 190 |
| GBOF-6 | 18.35 | P21/c | 7.26 |  | 0.109 |  |
| GBOF-7 | 18.39 | P21/c | 6.84 |  | 0.165 |  |
| GBOF-8 | 18.44 | Pna21 | 6.89 | d24=-0.12, d33=-0.20, d15=0.07 | 0.129 | 209 |
| GBOF-9 | 18.66 | P21/c | 7.09 |  | 0.112 |  |
| GBOF-10 | 18.77 | Pc | 6.12 | d11=-0.53, d12=0.27, d13=0.27, d15=0.08, d24=-0.15, d33=0.13 | 0.120 | 203 |
| GBOF-11 | 18.80 | P21/c | 6.72 |  | 0.093 |  |
| GBOF-12 | 18.80 | Pna21 | 6.42 | d24=0.34, d33=-0.73, d15=0.15 | 0.141 | FWPM |
| GBOF-13 | 18.94 | Pna21 | 6.60 | d33=0.25, d15=-0.25 | 0.159 | FWPM |
| GBOF-14 | 19.23 | Cc | 7.06 | d11=0.25, d12=-0.32, d13=0.08, d15=-0.17, d24=0.31, d33=0.11 | 0.171 | FWPM |
| GBOF-15 | 19.33 | Pc | 6.60 | d12=0.2, d13=-0.2, d24=0.54, d33=0.50 | 0.137 | 195 |
| GBOF-16 | 19.40 | Cc | 6.65 | d11=0.11, d12=-0.06, d13=0.19, d24=0.27, d33=-0.38 | 0.147 | FWPM |
| GBOF-17 | 19.60 | Pna21 | 6.36 | d15=0.08, d33=-0.12 | 0.158 | FWPM |
| GBOF-18 | 19.91 | Pc | 6.60 | d11=0.36,d12=-0.08,d13=-0.32, d15=-0.76,d24=0.25,d33=0.54 | 0.022 | 417 |
| GBOF-19 | 19.91 | P21/c | 6.98 |  | 0.133 |  |
| GBOF-20 | 20.06 | P21 | 6.76 |  | 0.159 |  |
| GBOF-21 | 20.10 | P21/c | 6.77 |  | 0.160 |  |
| GBOF-22 | 20.22 | Cc | 6.92 | d11=0.2, d15=-0.22, d13=-0.05, d24=-0.25, d33=-0.31 | 0.153 | FWPM |
| GBOF-23 | 20.26 | P21/c | 6.47 |  | 0.143 |  |
| GBOF-24 | 20.29 | Cc | 6.92 | d11=0.52, d12=-0.56, d13=-0.13, d24=-0.27, d33=-0.12 | 0.153 | FWPM |
| GBOF-25 | 20.37 | Pna21 | 6.71 | d24=-0.6, d33=-0.27, d15=0.07 | 0.132 | 199 |
| GBOF-26 | 20.62 | P21/c | 7.08 |  | 0.133 |  |
| GBOF-27 | 21.46 | Pc | 6.50 | d11=0.13,d12=-0.15,d15=-0.43, d24=0.16, d33=0.57 | 0.153 | FWPM |
| GBOF-28 | 21.72 | Pna21 | 6.78 | d24=-0.17, d33=0.62, d15=0.62 | 0.096 | 225 |
| GBOF-29 | 22.04 | Pc | 6.64 | d11=0.31, d12=-0.19, d13=0.11, d15=0.13, d24=-0.29, d33=0.3 | 0.167 | FWPM |
| GBOF-30 | 22.24 | Pna21 | 6.71 | d24=-0.39, d33=0.28, d15=0.20 | 0.155 | 196 |

Table S8 Birefringence among all anhydrous and ordered fluorooxoborate compounds with deep-UV cut-off edges.

| Compounds | Space group | Cut-off edge (nm) | Birefringence (@ 1064 nm) |
| --- | --- | --- | --- |
| Cs4B4O3F10 | P21/c | ＜200 | / |
| Na3B7O11F2 | Pnma | ＜200 | 0.083@193nm |
| K10B13O15F19 | R3m | ＜190 | 0.03 |
| Rb10B13O15F19 | R3m | ＜190 | 0.026 |
| [C(NH2)3][BF4] | R3m | 193 | 0.11 |
| Na3B3O3F6 | C2/c | 7.83 eV | / |
| Rb3B3O3F6 | P21/c | ＜190 | / |
| K2RbB3O3F6 | Pbcn | / | / |
| KCs2B3O3F6 | P21/c | ＜190 | / |
| Cs3B3O3F6 | Pbcn | ＜190 | 0.0069 |
| Na4B8O9F10 | Pna21 | ＜200 | 0.036 |
| Ba2B9O13F4•BF4 | P-1 | ＜ 190 nm | 0.052 |
| β-KB3O4F2 | P21/n | 7.88 eV | 0.096 @ 546 nm |
| α-KB3O4F2 | P21/n | 6.45 | 0.011 @ 546 nm |
| RbB3O4F2 | P21/c | ＜190 | 0.09 |
| Cs2B3O4F3 | P21/c | 6.63 | 0.016 |
| KNaB3O4F3 | Pbcn | ＜200 | 0.04 |
| K2B3O4F3 | Pbcn | ＜200 | 0.031 |
| KCsB3O4F3 | Pbcn | ＜200 | 0.032 |
| NaRbB3O4F3 | P21/c | ＜175 | / |
| Li2B3O4F3 | P212121 | 8.425 eV | 0.05 |
| α-BaBOF3 | P21 | ＞6.53 | / |
| β-BaBOF3 | P21/c | ＞6.53 | / |
| γ-BaBOF3 | P21/c | ＞6.53 | / |
| α-BaB4O5F4 | P21 | 8.4 eV | 0.044 |
| β-BaB4O5F4 | P21/c | ＞6.72 | 0.047 |
| Ba3B10O17F2·0.1KF | P-1 | ＜200 | 0.054 |
| K6B12O19F4 | Pnma | 5.6 eV | / |
| LiB6O9F | Pna21 | 8.37 eV | 0.04 |
| (NH4)2B6O9F2 | P21/c | ＜ 180 | 0.050 |
| K2B6O9F2 | Pbcn | 7.41 eV | 0.053 |
| NaKB6O9F2 | P21/c | ＞ 6.5 eV | 0.096-0.053@190-2000nm |
| NaRbB6O9F2 | P21/n | ＜180 | 0.064 |
| Na2B6O9F2 | P21/c | 7.34 | / |
| NaB4O6F | C2/c | ＜ 200 | 0.124 |
| NaB4O6F | C2 | ＜180 | 0.12 |
| NH4B4O6F | Pna21 | 7.87 eV | 0.107 |
| RbB4O6F | Pna21 | ＜200 | 0.102 |
| CsB4O6F | Pna21 | 8.01 eV | 0.0976 |
| CsKB8O12F2 | P321 | ＜200 | 0.105 |
| CsRbB8O12F2 | P-62c | ＜200 | / |
| CsNH4B8O12F2 | P321 | ＜190 | 0.127 |
| RbNH4B8O12F2 | Pna21 | ＜190 | 0.104 |
| CaB4O6F2 | P-1 | ＜190 | 0.091 |
| SrB4O6F2 | P-1 | ＜190 | 0.089 |
| BaB4O6F2 | P21/n | ＜190 | 0.085 |
| BaB8O12F2 | R-3c | ＜180 | 0.116 |
| K3B6O9F3 | P21/c | 6.98 eV | / |
| α-K3B6O9F3 | Pc | 6.8 eV | / |
| BaB2O3F2 | P21 | ＜180 | / |
| Rb3B5O8F2 | P21 | ＜200 | / |
| Li2NaB5O8F2 | Pbcn | 7.48 eV | 0.047 |
| Li2KB5O8F2 | Pbcn | ＜196 | 0.049 |
| MgB5O7F3 | Cmc21 | ＜200 | 0.07 |
| CaB5O7F3 | Cmc21 | ＜180 | 0.07 |
| SrB5O7F3 | Cmc21 | ＜180 | 0.07 |
| Ba2B7O12F | C2/c | 6.67 eV | / |
| LiNaB6O9F2 | Pnn2 | ＜ 190 | 0.067 |
| Na2BaB12O18F4 | Pbcn | ＜ 190 | 0.054 |
| Li2B6O9F2 | Cc | ＜190 | 0.07 |
| K3NaB10O16F2 | C2/c | 6.93 eV | 0.047 |
| [C(NH2)3]B6O9F | Pna21 | ＜190 | 0.133 |

“/” Indicates not reported.

Figure S1. The 2D [B6O9F]∞ layers for [C(NH2)3]B6O9F(up) and LiB6O9F(down) in ac plane.

Figure S2. The Powder X-ray diffraction patterns for [C(NH2)3]B6O9F at different temperature.

Figure S3. The IR Spectra of [C(NH2)3]B6O9F.

Figure S4. The TG-DSC curve of [C(NH2)3]B6O9F.

Figure S5. The ELF map of [C(NH2)3] group in [C(NH2)3]B6O9F.

Figure S6. The ELF map of 2D [B6O9F]∞ anion layer in [C(NH2)3]B6O9F.

Figure S7. The low-lying allotropes of [C(NH2)3]B6O9F. Top and side views of crystal structures for [C(NH2)3]B6O9F with the same anionic frameworks [B6O9F] and different cation [C(NH2)3] functional motifs are presented. Their structure number and convex hull values are below corresponding [C(NH2)3] functional motifs.

Figure S8. Phonon dispersion spectra for predicted stable GBOF-i (i=1-30) calculated with linear response method.

Figure S9. The SHG density maps of occupied and unoccupied orbitals of the largest effective NLO coefficient d33 in a virtual-electron process of GBOF-i (i=1, 3, 4, 5, 12).