Supplementary Information for Ran, et al., “Terahertz response of monolayer and few layer WTe2 at the nanoscale”

Supplementary Note 1: Comparison between topography and near-field images

Supplementary Figure 1|Comparison between topography and near-field images. a The topography image of the field-of-view shown in Fig. 1b and c of the main text. The dashed lines, indicating the boundaries between different regions, are determined by topographical contrast of monolayer (1L), bilayer (2L) and trilayer (3L) regions. b The near-field S1 image taken simultaneously with the topography image.

A side-by-side comparison between topography and near-field images helps better locate different regions on the sample surface. The micrometer-sized white dots in topography images, corresponding to the black dots in the near-field images, result from bubbles between WTe2 sample and hBN encapsulation layers. Because the existence of the top layer hBN and bubbles, locating different regions in atomic force microscopy (AFM) images is challenging. Nevertheless, we can still track the boundary by taking line-cuts and compare with the near-field image and the optical inspection image.

Supplementary Note 2. Spatial resolution and approach Curve of S1 and S2 near-field signal

To illustrate how localized the signal is above the sample surface, we measured the dependence of near-field signal on the tip-sample distance. In the Fig. S2, S2 signal is much more localized than S1. More than 90% of S2 signal is contributed within 150nm above the sample surface. For S1 signal, this length scale of signal decay is ~700nm. In terms of full width half maximum, the decay length scale for S1 and S2 signal are <100nm and <50nm. The in-plane length scale of E-field localization of near-field signal equals that of out-of-plan [1]. Hence, the resolution of S1 (S2) image is no larger than 200nm (100nm).

Supplementary Figure 2|Near-field Approach Curve of S1 and S2 signal. The approach curve is measured by varying the tip-sample distance. S1 signal is mainly contributed by E field within 700nm above the sample surface, whereas S2 signal is confined within 150nm above the sample surface.

Supplementary Note 3: Zoomed-in images of monolayer WTe2

Supplementary Figure 3|Zoomed-in images of monolayer WTe2. a THz near-field S1 image of the whole sample area at room temperature. We mark the boundaries of terraces with different number of WTe2 layers (1L, 2L, 3L) with dashed lines. The red frame indicates the area where the monolayer images are taken. b Zoomed-in S1 image around monolayer region. c Zoomed-in S2 image around monolayer region.

Monolayer WTe2 is confirmed to support quantum spin Hall state below 100K [2] [3] [4] [5] [6] [7] with edge conduction channels. At the lowest temperature of the experiment 44K, THz response near images around monolayer WTe2 was measured in more detail (Fig. S3). The location of the zoomed-in field-of-view is indicated in Fig. S3a with a red frame. In this field-of-view, we can see the boundaries between monolayer WTe2 and substrate and between monolayer and bi-layer WTe2. With our current signal to noise ratio, no clear feature arising from the topological edge state is observed, despite previous observation of the edge state at DC [8] and microwave frequencies [3]. It is possible that the increase of conductivity due to edge state does not extend to THz range. However, the low conductivity [8] of the edge state is also challenging for nano-THz technology.

Supplementary Note 4: The influence of in-plane anisotropy of WTe2 on near-field modeling.

Supplementary Figure 4|Temperature dependent normalized S2 from experiment and modeling.  Experimental data points are indicated with solid squares. Near-field modeling are indicated with empty diamonds. Three different sets of parameters: ϵ∥=ϵb, ϵ∥=ϵa and ϵ∥=(ϵa+ϵb)/2 are configured for 3L WTe2 modeling. Bi-layer and monolayer results are achieved by setting the thickness of WTe2 to 1.4 nm and 0.7 nm.

The near-field modeling mainly follows the procedure described in Ref. [1]. One assumption is that the material can be treated as isotropic or uniaxial material with a unique out-of-plane axis. On the contrary, WTe2 reveals notable in-plane anisotropy with distinct plasma frequencies between a and b axes within the WTe2 plane [9] [10]. We assumed that tri-layer WTe2 can be reasonably described as a uniaxial material with its in-plane relative permittivity represented by that of b-axis of bulk WTe2. Nevertheless, the finite in-plane anisotropy is evident only at much higher frequencies (~12 THz) [9] and gives rise to minor quantitative change in the observed near-field response, as demonstrated below. We first performed calculations with both a purely a-axis response and an effective dielectric function averaging between a-axis and b-axis data. In Fig. S4, three different configurations are displayed. Modeling with ϵ∥=ϵb has the highest increase of near-field signal at low temperature. The increase is lower in ϵ∥=(ϵb+ϵa)/2 and the lowest in ϵ∥=ϵa, despite the overall differences are small enough to neglect.

We also performed modeling to see whether bi-layer and monolayer results can be explained. We tuned the thickness of WTe2 down from 2.1 nm 1.4 nm to 0.7 nm. As is shown in Fig. S4, as long as the bulk conductivity is used in the modeling, the near-field signal always increases significantly at low temperature due to the existence of SPPs. Therefore, the conductivity of bi- and monolayer WTe2 cannot be characterized by bulk conductivity.

Supplementary Note 5: Mid-IR response of monolayer and few layer WTe2 at the nanoscale.

Supplementary Figure 5|Near-field nano-imaging on multi-terraced encapsulated WTe2 micro-crystal in the mid-infrared. Image of the normalized near-field S3 signal (ω=27 THz) at a 250 K and b 57K. c Layout of the sample measured in the mid-IR near-field experiments. d Temperature dependence of mid-IR near-field signal for regions with different number of layers.

For completeness, we also acquired near-field data in the frequency range higher than the plasma frequency of bulk WTe2. The experiment is carried out in the mid-IR range with a 27 THz CO2 laser. Here, a third (S3) or higher harmonic of the near-field signal must be measured to suppress the far-field contribution [11]. The WTe2-based structure investigated in this experiment shares common elements with the devices in the main text Fig.1a. The major difference is that there is another layer of graphite in between the SiO2/Si substrate and bottom layer hBN. This latter architecture is only suitable for mid-IR experiments: the graphite beneath the sample saturates the near-field signal in THz range but not in mid-IR range. Images acquired at 250K and 57K are shown in Fig. S4a&b. The temperature dependence of nano-IR signals is plotted in Fig. S4d. WTe2 shows a much weaker nano-IR signal compared to the signal produced by the platinum electrodes. Regions with more WTe2 layers show systematically higher mid-IR signal levels and the temperature dependence for all layers is insignificant (Fig. S4d). This temperature independent behavior is well explained by our model result shown in the main text Fig. 3d.

Supplementary Note 5: Near-field electrodynamics of thermally activated carriers of bi-layer WTe2

In calculating the near-field signal of bi-layer WTe2, we mainly consider the Drude response of its thermally activated carriers. The carrier density is computed assuming WTe2 has quadratic bands with effective electron mass at the conduction and valence band edge:

n2D=EC-EF∞2fFDEg2DEdE=2kTmC*πℏ2ln⁡(e-EC-EFkT+1)

p2D=|ED-EF|∞2fFDEg2DEdE=2kTmV*πℏ2ln⁡(e-|EV-EF|kT+1)

Here, mC* and mV* are the effective electron mass at the band edge of conduction and valence band. EC, EV and EF are the energy of conduction band edge, valence band edge and Fermi energy of bi-layer WTe2. The Fermi energy is determined by the neutrality condition n2D=p2D of the investigated system. The permittivity of the model bi-layer:

ϵ=ϵ∞-ωP2ω(ω-iγ)

Here ωP is the plasma frequency determined by the thermally activated carrier density:

ωp,n=n2de2dm*ϵ0=2e2kTdπℏ2ϵ0ln⁡(e-EC-EFkT+1)

ωp,p=p2de2dm*ϵ0=2e2kTdπℏ2ϵ0ln⁡(e-|EV-EF|kT+1)

Here d = 1.4 nm, nbulk and ωP are the carrier density and the plasma frequency of the bulk WTe2. The scattering rate γ of the model bi-layer is assumed to be the average of the two scattering rate of two Drude components in the bulk [12] γ=(γ1+γ2)/2.

Supplementary Note 6: Real-space near-field modeling of SPP structures

To generate predicted real-space images shown in the main text, we apply a semi-analytic method that approximates the near-field scattering signal from a 2D material as proportionate (to first-order) by the z-polarization of a polarizable dipole raster-scanned (at a height z=zdp) some tens of nanometers over the surface of a sample (at z=0):

Sρdp ~ pz≈αEref,  z (ρdp,z=zdp).	(S1)

Here α denotes the dipole polarizability, Eref,  z denotes the z-component of the electric near-field reflected by the sample in response to the incident dipole field, and ρdp denotes evaluation at the in-plane coordinate of the probe.  Although this expression represents only the first term in a Born expansion of the full self-consistent dipole polarization [13] a similar conceptual treatment was previously shown to faithfully replicate the polaritonic near-field response of two-dimensional materials as measured by scanning near-field optical microscopy [14].  Here we summarize the key points enabling our calculation of Eq. S1 in the quasi-electrostatic approximation, and defer more detailed discussion to forthcoming work.

We recast Eq. S1 in a form reminiscent of the local photonic density of states [15] measured at the location rdp=(ρdp,zdp) of our dipole probe:

Sρdp ~ z>0 dV jdp⋅Eref=z>0 dV ∇⋅jdp Φref∝z>0 dV -ϱdp⋅Φref	(S2)

Here jdp denotes the unit vector oriented along the direction of the point dipole current, ϱdp denotes the instantaneous charge distribution associated with the dipole, and Φref is the electrostatic potential for the reflected field given by Eref=-∇Φref.  Now Sρdp can be evaluated entirely in the plane z=0 by identifying the “incident” electrostatic potential generated by the dipole through ϱdp=-14π∇2Φdp and integrating Eq. S2 by parts, yielding:

z>0 dV -ϱdp⋅Φref=14πz=0+ dA (-z⋅∇Φdp )Φref-z>0 dV∇Φdp⋅∇Φref
                                      =14πz=0+ dA Φdp∂zΦref-∂zΦdpΦref.                      (S3)

Here we have applied the source-free condition ∇2Φref=0 in the volume z>0.  Eq. (S3) represents an approximation for the signal Sρdp when Φdp is produced from a dipole-like probe at rdp.  Further simplification is admitted by the fact that Φref=-RΦdp≡-ΦR, with R a generalized reflection operator.  Moreover, for scalar potentials Φ1,2 harmonic (viz. source-free) in the plane of integration, dAΦ1∂zΦ2=±d2q q Φ1Φ2, where tilde quantities represent in-plane Fourier transforms with respect to the momentum q, and   ± correspond to the cases where Φ2 is sourced from z>0 or z<0, respectively.  With these considerations, Eq. (S3) reduces to:

Sρdp~12πd2q q ΦdpΦR = 12π dA(q*Φdp)RΦdp	(S4)

where (q*Φdp) represents the incident scalar potential spatially convolved at z=0+ with a sharpening function with Fourier kernel q.  Eq. (S4) represents a norm of the function Φdp in the plane z=0 with respect to the composite reflection operator q* R.  By way of demonstration, we can consider cases where the reflected field is given by ΦR=rp(q)Φdp(q), with rp the momentum-resolved Fresnel coefficient for e.g. a layered medium with in-plane translational invariance.  Applying the in-plane Fourier transform of the dipole potential Φdpq=e-qzdp at z=0, for such cases Eq. S4 evaluates to S∝dq rpq q2e-2qzdp.  This is indeed the first-order term in a Born series expansion of the point dipole model widely used to predict near-field observables in the case of multilayered systems [16] [17].  Meanwhile, whereas the real-space counterpart that we present in Eq. S4 remains underreported, it provides a powerful means to predict images recorded by scanning near-field optical microscopy.

We now briefly describe our method for evaluating RΦdp in the case of a spatially inhomogeneous 2D material at z=0 described by a (piecewise) optical conductivity σ2D(ρ) upon a substrate with isotropic reflectivity βsubs.   We first consider the integro-differential equation for the scalar potential Φref generated by σ2D in response to the potential Φdp of our quasi-dipolar probe [18], in absence of a substrate:

|  | 1+V*m 12πqp,m∇⋅σmρ ∇Φρ=Φdpρ, with Φ=Φdp+Φref. | (S5) |
| --- | --- | --- |

Here m indexes the piecewise homogeneous domains of our 2D material (i.e. in our case domains of mono-, bi-, and tri-layer WTe2), qp,m denotes the complex plasmon wavevector associated with each domain, and σmρ are piecewise homogeneous functions equal to zero or 1 marking the lateral regions ρ∈Ωm occupied by each domain.  Meanwhile, V(r,r')=1/|r-r'| is the Coulomb kernel, and the asterisk (*) denotes spatial convolution over the in-plane coordinate ρ=(x,y).  We solve Eq. S5 by expanding Φref(ρ)=mnϕmnrefΦmn(ρ) into an orthonormal basis of eigenfunctions specified on the domains ∂Ωm by ∇⋅σmρ ∇Φmnρ=-qmn2Φmnρ and subject to the “zero current” boundary conditions n⋅∇Φmn on the domain edges ∂Ωm.  These functions are obtained with the finite element solver FEniCs [19] after meshing the experimentally relevant domain configurations shown in Figure 5a of the main text.

Values for the plasmon wave-vectors are inferred from the respective layer thicknesses dm and complex in-plane optical permittivities εm of each domain in Ωm according to qp,m=21-εm-1 dm-1; see Supplementary Table 1 for the values used in our simulations.  Although WTe2 is known to exhibit biaxial in-plane permittivity, for simplicity in our simulations we apply an isotropic approximation as earlier discussed in this supplement.

| Domain (indexed m) | Thickness dm (nm) | Optical permittivity εm (ω≈1 THz) | Plasmon wave-vector qp,m (cm-1) |
| --- | --- | --- | --- |
| Monolayer (70 K) | 0.7 | 41 | -710000 |
| Monolayer (295 K) | 0.7 | 41 | -710000 |
| Bilayer (70 K) | 1.4 | -1056+1056i | 6764+6758i |
| Bilayer (295 K) | 1.4 | -223+1482i | 1424+9424i |
| Trilayer (70 K) | 2.1 | -28265+28265i | 168.47+168.47i |
| Trilayer (295 K) | 2.1 | -1226+6146i | 296.5+1490i |

Supplementary Table 1| Parameters for modeling real-space near-field images of WTe2 monolayer, bilayer, and trilayer domains at 70 K and 295 K.  Layer thickness and the complex-valued optical permittivity ε=ε1+iε2 determines the plasmon wave-vector.  Permittivities are estimated according to discussion in the main test.

Assembling the expansion coefficients ϕmnref into a vector ϕref (taking mn as a composite index), we solve Eq. (S5) by the matrix equation:

ϕref=--Vmqm2/(2πqp,m)1-Vmqm2/(2πqp,m)ϕdp

(S6)

As with ϕref, here ϕdp represents the vector of expansion coefficients for Φdp(ρ).  Meanwhile, each qm2 denotes a diagonal matrix of eigenvalues qmn2 acting in the vector subspace spanned by Φmn ∀n at fixed domain index m, and V is the coulomb matrix whose elements are given by Vkl,mn=z=0 dA Φklρ V*Φmnρ.  The term in brackets in Eq. (S6) represents the generalized reflection operator R for the system in the Φmn basis.  (The denominator is understood in the sense of a matrix inverse applied before pre-multiplication by the numerator.)  While we defer the derivation to forthcoming work, this reflection operator generalizes to the case of our 2D materials upon a substrate with isotropic reflectivity βsubs as follows:

R=βsubs-Vnqn2/(2πκqp,n)1-Vnqn2/(2πκqp,n)

(S7)

Here κ=(εsubs+1)/2 and βsubs=(εsubs-1)/(εsubs+1), with εsubs the substrate permittivity; in this work the substrate includes 20nm hBN and bulk SiO2.

We also define a symmetric matrix Q in the Φmn basis corresponding to the spatial convolution in Eq. S4, with elements given by Qkl,mn=z=0 dA Φklρ q*Φmnρ.  Since the Φmn are orthonormal, Eq. S4 reduces to:

S(ρdp)~12πϕdp(ρdp)T QR ϕdp(ρdp).		(S8)

This represents a vector norm of ϕdp with respect to the matrix QR.

In summary, after computing eigenfunctions Φmn associated with our sample geometry, we compute symmetric matrices V and Q and the generalized reflectance operator R.  Then, in order to predict a spatial map S(ρdp), we simply project the incident potential emitted by our quasi-dipolar probe at each location ρdp into the Φnm basis by evaluating the vector of coefficients ϕdp,mn(ρdp)=dA Φdp(ρ)Φmn(ρ) and successively applying Eq. S8.  Although the eigenbasis {Φmn} is of infinite size, projections into ϕdp decay exponentially with n when Φmn are sorted by increasing eigenvalue qmn2, so a truncated basis of size N≈103 is in our case sufficient for a converged map of near-field scattering amplitude |Sρdp|.   In this way, the observables of near-field microscopy can be predicted entirely by evaluating functions in the plane of the sample (z=0).  This computational method may be suitable for qualitative and quantitative modeling of near-field response of other spatially inhomogeneous 2D heterostructures. Such applications and details of their unique numerical implementation will be reported elsewhere.

# References

| [1] | A. S. McLeod, P. Kelly, M. D. Goldflam, Z. Gainsforth, A. J. Westphal, G. Dominguez, M. H. Thiemens, M. M. Fogler and D. N. Basov, "Model for quantitative tip-enhanced spectroscopy and the extraction of nanoscale-resolved optical constants," Physical Review B, vol. 90, p. 085136, 2014. |
| --- | --- |
| [2] | Z. Fei, M. D. Goldflam, J.-S. Wu, S. Dai, M. Wagner, A. S. McLeod, M. K. Liu, K. W. Post, S. Zhu, G. C. A. M. Janssen and others, "Edge and surface plasmons in graphene nanoribbons," Nano letters, vol. 15, p. 8271–8276, 2015. |
| [3] | Y. Shi, J. Kahn, B. Niu, Z. Fei, B. Sun, X. Cai, B. A. Francisco, D. Wu, Z.-X. Shen, X. Xu and others, "Imaging quantum spin Hall edges in monolayer WTe2," Science advances, vol. 5, p. eaat8799, 2019. |
| [4] | L. Peng, Y. Yuan, G. Li, X. Yang, J.-J. Xian, C.-J. Yi, Y.-G. Shi and Y.-S. Fu, "Observation of topological states residing at step edges of WTe 2," Nature communications, vol. 8, p. 659, 2017. |
| [5] | S. Tang, C. Zhang, D. Wong, Z. Pedramrazi, H.-Z. Tsai, C. Jia, B. Moritz, M. Claassen, H. Ryu, S. Kahn and others, "Quantum spin Hall state in monolayer 1T'-WTe 2," Nature Physics, vol. 13, p. 683, 2017. |
| [6] | S. Wu, V. Fatemi, Q. D. Gibson, K. Watanabe, T. Taniguchi, R. J. Cava and P. Jarillo-Herrero, "Observation of the quantum spin Hall effect up to 100 kelvin in a monolayer crystal," Science, vol. 359, p. 76–79, 2018. |
| [7] | X. Qian, J. Liu, L. Fu and J. Li, "Quantum spin Hall effect in two-dimensional transition metal dichalcogenides," Science, vol. 346, p. 1344–1347, 2014. |
| [8] | Z. Fei, T. Palomaki, S. Wu, W. Zhao, X. Cai, B. Sun, P. Nguyen, J. Finney, X. Xu and D. H. Cobden, "Edge conduction in monolayer WTe 2," Nature Physics, vol. 13, p. 677, 2017. |
| [9] | A. J. Frenzel, C. C. Homes, Q. D. Gibson, Y. M. Shao, K. W. Post, A. Charnukha, R. J. Cava and D. N. Basov, "Anisotropic electrodynamics of type-II Weyl semimetal candidate WTe 2," Physical Review B, vol. 95, p. 245140, 2017. |
| [10] | C. Wang, S. Huang, Q. Xing, Y. Xie, C. Song, F. Wang and H. Yan, "Van der Waals thin films of WTe 2 for natural hyperbolic plasmonic surfaces," Nature communications, vol. 11, p. 1–9, 2020. |
| [11] | A. J. Sternbach, J. Hinton, T. Slusar, A. S. McLeod, M. K. Liu, A. Frenzel, M. Wagner, R. Iraheta, F. Keilmann, A. Leitenstorfer and others, "Artifact free time resolved near-field spectroscopy," Optics Express, vol. 25, p. 28589–28611, 2017. |
| [12] | C. C. Homes, M. N. Ali and R. J. Cava, "Optical properties of the perfectly compensated semimetal WTe 2," Physical Review B, vol. 92, p. 161109, 2015. |
| [13] | R. Hillenbrand, B. Knoll and F. Keilmann, "Pure optical contrast in scattering-type scanning near-field microscopy," Journal of microscopy, vol. 202, p. 77–83, 2001. |
| [14] | A. Y. Nikitin, P. Alonso-González, S. Vélez, S. Mastel, A. Centeno, A. Pesquera, A. Zurutuza, F. Casanova, L. E. Hueso, F. H. L. Koppens and others, "Real-space mapping of tailored sheet and edge plasmons in graphene nanoresonators," Nature Photonics, vol. 10, p. 239–243, 2016. |
| [15] | L. Novotny and B. Hecht, Principles of nano-optics, Cambridge university press, 2012. |
| [16] | Z. Fei, G. O. Andreev, W. Bao, L. M. Zhang, A. S. McLeod, C. Wang, M. K. Stewart, Z. Zhao, G. Dominguez, M. Thiemens and others, "Infrared nanoscopy of Dirac plasmons at the graphene–SiO2 interface," Nano letters, vol. 11, p. 4701–4705, 2011. |
| [17] | J. Aizpurua, T. Taubner, F. J. G. de Abajo, M. Brehm and R. Hillenbrand, "Substrate-enhanced infrared near-field spectroscopy," Optics Express, vol. 16, p. 1529–1545, 2008. |
| [18] | B. Rejaei and A. Khavasi, "Scattering of surface plasmons on graphene by a discontinuity in surface conductivity," Journal of Optics, vol. 17, p. 075002, 2015. |
| [19] | M. Alnæs, J. Blechta, J. Hake, A. Johansson, B. Kehlet, A. Logg, C. Richardson, J. Ring, M. E. Rognes and G. N. Wells, "The FEniCS project version 1.5," Archive of Numerical Software, vol. 3, 2015. |