Tables

Table (1): Mean and standard deviation (SD) values of microtensile bond strength test of all tested groups.

| Subgroups | Main groups |  |  |  | T test | P value |
| --- | --- | --- | --- | --- | --- | --- |
|  | Superficial |  | Deep |  |  |  |
|  | mean | SD | mean | SD |  |  |
| Control (T0) | 26.78aA | 6.11 | 16.06cB | 4.29 | 9.08 | <0.001** |
| Sodium hypochlorite (T1) | 20.55bB | 4.82 | 23.02aA | 5.35 | 2.17 | 0.033** |
| Bromelain (T2) | 19.55bA | 4.22 | 20.86bA | 3.61 | 1.50 | 0.138 ns |
| F test | 23.49 |  | 25.35 |  |  |  |
| P value | <0.001** |  | <0.001** |  |  |  |
| Test used: one-way ANOVA at P<0.05 **; means significant difference, (ns): means non-significant difference. values that share the same superscript letter indicate there is no significant difference between groups. Values with different superscript letter indicate a statistically significant difference. small letters for comparison of different values for each group (column). capital letters for comparison of different values for each group (row). (a & A): represent the highest mean values followed by (b & B). (c): represent the lowest mean values. |  |  |  |  |  |  |

Table (2): Failure Mode Analysis

|  |  | Control subgroup |  | Sodium hypochlorite subgroup |  | Bromelain Enzyme subgroup |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | N | % | N | % | N | % | P value |
| Superficial dentin | Adhesive Failure | 7 | 17.5 | 17 | 42.5 | 20 | 50.0 | 0.0424** |
|  | Dentin Cohesive Failure | 6 | 15.0 | 5 | 12.5 | 3 | 7.5 | 0.6066 |
|  | Composite Cohesive Failure | 25 | 62.5 | 12 | 30 | 11 | 27.5 | 0.0221** |
|  | Mixed Failure | 2 | 5.0 | 6 | 15.0 | 6 | 15.0 | 0.3189 |
|  | P value | <0.001** |  | 0.0244** |  | <0.001** |  |  |
|  | overall p value | 0.008** |  |  |  |  |  |  |
| Deep dentin | Adhesive Failure | 24 | 60.0 | 8 | 20.0 | 20 | 50.0 | 0.0047** |
|  | Dentin Cohesive Failure | 4 | 10.0 | 6 | 15.0 | 3 | 7.5 | 0.583 |
|  | Composite Cohesive Failure | 5 | 12.5 | 24 | 60.0 | 6 | 15.0 | <0.001** |
|  | Mixed Failure | 7 | 17.5 | 2 | 5.0 | 11 | 27.5 | 0.0473** |
|  | P value | <0.001** |  | <0.001** |  | <0.001** |  |  |
|  | overall p value | <0.001** |  |  |  |  |  |  |
| **; mean significant at t P<0.05. |  |  |  |  |  |  |  |  |