Supporting Information

# Self-healing Co3O4@Fe3O4/cellulose blend membranes efficient degrade perfluorooctanoic acid in the visible light-driven photo-Fenton system

Wenqiang Chen a, Chen Hou a, *, Yang Wang a, Linhui Fu a, Sufeng Zhang a, Jianzhi Wang b

a College of Bioresources Chemical and Materials Engineering, Shaanxi University of Science and Technology, Shaanxi Provincial Key Laboratory of Papermaking Technology and Specialty Paper Development, Key Laboratory of Paper Based Functional Materials of China National Light Industry, National Demonstration Center for Experimental Light Chemistry Engineering Education, Xi’an 710021, China

b Key Laboratory for Green Chemical Process of Ministry of Education, School of Chemical Engineering and Pharmacy, Wuhan Institute of Technology, Wuhan 430205, P.R. China

# The Synthesis of Fe-MOF:

# For the synthesis of the MOF-derived Fe3O4, FeCl3 6H2O (5 mmol) was dissolved in 30 mL deionized water. Subsequently, fumaric acid (7 mmol) was tardily added under stirring for 30 min, which the mixture was heated at 65°C in a 100 mL Teflon stainless autoclave for 12 h. After cooling naturally, the product was washed with deionized water and methanol three times by centrifugation and vacuum dried at 65°C overnight (Liang et al. 2020).

# Bis-cyclic Carbonate (BCC) Synthesis:

# Di(trimethylopropane) (10 g, 39.9 mmol) and diphenyl carbonate (85.7 g, 400 mmol) were mixed together and then heated to 140°C for reactions. After 48 h, the reaction mixture was cooled to ambient temperature and washed with diethyl ether to remove unreacted diphenyl carbonate. The resultant white solid powder was then recrystallized in tetrahydrofuran three times to yield monomer BCC as a white crystal (6 g, 60%).

# Drying of tris (2-aminoethyl) amine:

# A high purity tris (2-aminoethyl) amine was obtained by adding a proper amount of calcium hydride to tris (2-aminoethyl) amine, stirring for 12 h, and then distillation at 120°C with a stirring rate of 100 rpm.

# Synthesis of vitrimer:

# As shown in Fig. S1, the synthesized bicyclic precursor and tris (2-aminoethyl) amine are dissolved in a proper amount of CH2Cl2 in a ratio of 1:0.75 mol, then dried in an oven at 90°C for 12 h. Vitrimer with shape plasticity is obtained (Xiong et al. 2020; Zhao et al. 2019).

Fig. S1. The synthesis route of vitrimer, vitrimer material.

# SEM, FTIR, XRD, XPS and VU-vis DRS analysis:

# Morphological analysis was carried out with field emission scanning electron microscopy (FESEM, Quanta FEG, 250). The detection of specific chemical bonds within the catalysts was achieved by FTIR (Vectory-22 spectrometer) with KBr powder. The XRD patterns for phase and crystallite analysis were collected (10-80°, 0.02°/step, 0.06 seconds/step) using Cu Kα radiation at room temperature. The XPS data were obtained with a thermo Fisher K-Alpha equipped with a monochromatic Al Kα X-ray source (150 W, 15kV, 10mA). The binding energy of the C1s peak at 284.6 eV was used as the reference for calibration. The UV–vis DRS were obtained by a UV–vis spectrophotometer (UV-VIS-NIR, Cary 5000) using BaSO4 powder as blank from 800 nm to 200 nm.

# The concentration of PFOA and intermediates analysis:

The PFOA concentration was measured by high-performance liquid chromatography (HPLC-UV, Waters 1525) with a reverse phase C18 column (4.6mm×250 mm, 5 μm). The following operating conditions were employed: isocratic elution of acetonitrile/20 mM NaH2PO4 (pH =3) (60:40, v/v), flow rate of 1mL min−1, injection volume of 40 μL, and UV detector of 210 nm (Wang et al. 2019).

The determination of the degradation intermediates of PFOA were conducted by Ultra Performance Liquid Chromatography coupled with quadrupole Q Exavtive mass spectrometry (Q-Exactive UHPLC-MS). The solution after reaction was extracted by SPE. The sample was analyzed by Ultra Performance Liquid Chromatography with waters cortecs C18 (2.1×50 mm, 1.77 µm), followed by a quadrupole Q Exavtive mass spectrometry. The measurement for intermediates was performed in negative mode and gradient eluted HPLC-grade acetonitrile (A) and water (B) as mobile phase at a flow rate of 0.3 mL/min. The A linear solvent gradient was as follows: 0–1 min, 0%–10%; 1–8 min, 10%–90% and hold for 4 min; 12–12.1 min, 90%–10% and hold for 1 min. The column was kept at 25°C during the sample analysis. A 1.00 µl of sample was injected by the auto sample system. The mass spectrometry conditions were as follows: the ionization mode was negative electrospray (ESI−); the source temperature was set at 120°C; the desolvation gas flow was 350 L h−1. The mass range parameters value was set from 50 to 600 amu.

IC analysis:

Fluoride was analyzed by ion chromatography (940 Metrohm) provided with an IonPac As-HC column and using a 9 mM Na2CO3 solution as eluent, which was circulated at a flow rate of 1 mL min−1.

EPR analysis:

To evaluating the instantaneous intensity of radicals, the EPR analysis was conducted by the following procedures. Briefly, 250 mg DMPO was dissolved in 2.5 mL deionized water prior to use. The catalytic process was activated by composite membranes and H2O2 (30 mM) simultaneously in solution. 1 mL water sample was obtained and rapidly mixed with 100 μL DMPO solution and rigorously stirred for 5 seconds. The mixture was analyzed by Bruker EMXmicro-6/1 EPR spectrometer immediately and the instantaneous intensity of radicals at different conditions can be obtained. The EPR spectra were obtained with a center field at 3515 G and a sweep width of 100 G at 20°C.

Electrochemical measurements:

The electrochemical measurements of the working electrodes containing the catalysts were carried out on a computer–controlled electrochemical station using traditional three–electrode system in 0.5 M Na2SO4 solution.

Fig. S2. The SEM of Co3O4 in different magnification.

Fig. S3. The XPS survey pattern of Co3O4@ Fe3O4/cellulose.

Fig. S4. The fitting of degradation curves and rate constant (k) derived.

Table S1. Comparison of light driven AOPs for PFOA removal by different catalysts.

| catalyst | Light source |  |  | C0 (PFOA) | Reaction time | Removal | Refs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| lignin/PVA/bi-MOFs/PMS |  | λ = 185 nm |  | 20 mg L-1 | 2.5 h | 100% | Hou et al |
| Ga2O3/PMS |  |  | λ = 185/254 nm | 50 mg L-1 | 1 h & 2 h | 100% | Xu et al |
| Ga2O3/PMS |  |  | Visible light | 50 mg L-1 | 2 h | 10% |  |
| Fe3+/H2O2 & PS |  |  | Sunlight | 20 mg L-1 | 28 d | 74.8% & 88.9% | Liu et al |
| BiOI@Bi5O7I |  |  | Simulated Sunlight | 15 mg L-1 | 6 h | 98% | Wang et al |
| TiO2/PMS |  |  | λ=400-770 nm | 50 mg L-1 | 8 h | 100% | Xu et al |
| lignin/PVA/bi-MOFs/PMS |  |  | Sunlight | 20 mg L-1 | 3 h | 89.6% | Hou et al |
| Co3O4@Fe3O4/cellulose/H2O2 |  |  | Visible light | 20 mg L-1 | 3 h | 94.5% | This work |
| Co3O4@Fe3O4/cellulose/V/H2O2 |  |  | Visible light | 20 mg L-1 | 3 h | 80.4% | This work |

Fig. S5. The metal leaching of Fe and Co.

Table S2. Identified reaction intermediates of PFOA in the H2O2/ membrane/visible light system.

| Acronym | Name | Formula | m/z | Retention time / min |
| --- | --- | --- | --- | --- |
| PFHpA | Perfluoroheptanoic acid | C6F13COOH | 362.9 | 7.8 |
| PFPeA | Perfluoropentanoic acid | C4F9COOH | 266.9 | 7.6 |
| PFBA | Perfluorobutyric acid | C3F7COOH | 216.9 | 7.3 |
| TFA | Trifluoroacetic acid | CF3COOH | 112.9 | 7.9 |

Fig. S6. LC-MS/MS spectra of the intermediates.

References

Hou C, Chen WQ, Fu LH, Zhang SF, Liang C, Wang Y (2021) Efficient degradation of perfluorooctanoic acid by electrospun lignin-based bimetallic MOFs nanofibers composite membranes with peroxymonosulfate under solar light irradiation. Int J Biol Macromol 174: 319-329. https://doi.org/10.1016/j.ijbiomac.2021.01.184

Liang Q, Gao W, Liu C, Xu S, Li Z (2020) A novel 2D/1D core-shell heterostructures coupling MOF-derived iron oxides with ZnIn2S4 for enhanced photocatalytic activity. J Hazard Mater 392: 122500. https://doi.org/10.1016/j.jhazmat.2020.122500

Liu D, Xiu Z, Liu F, Wu G, Adamson D, Newell C (2013) Perfluorooctanoic acid degradation in the presence of Fe (III) under natural sunlight. J hazard mater 262: 456-463. https://doi:10.1016/j.jhazmat.2013.09.001

Wang J, Cao C, Wang Y, Wang Y, Sun B, Zhu L (2020) In situ preparation of p-n BiOI@Bi5O7I heterojunction for enhanced PFOA photocatalytic degradation under simulated solar light irradiation. Chem Eng J 319: 123530. https://doi.org/10.1016/j.cej.2019.123530

Wang Q, Liu M, Zhao H, Chen Y, Xiao F, Chu W, Zhao G (2019) Efficiently degradation of perfluorooctanoic acid in synergic electrochemical process combining cathodic electro-Fenton and anodic oxidation. Chem Eng J 378: 122071. https://doi.org/10.1016/j.cej.2019.122071

Xu B, Ahmed MB, Zhou JL, Altaee A (2020) Visible and UV photocatalysis of aqueous perfluorooctanoic acid by TiO2 and peroxymonosulfate: Process kinetics and mechanistic insights, Chemosphere 243: 125366. https://doi:10.1016/j.chemosphere.2019.125366

Xu B, Zhou JL, Altaee A, Ahmed MB, Johir MAH, Ren J, Li X (2020) Improved photocatalysis of perfluorooctanoic acid in water and wastewater by Ga2O3/UV system assisted by peroxymonosulfate. Chemosphere 239: 124722. https://doi.org/10.1016/j.chemosphere.2019.124722

Xiong C, Li M, Zhao W, Duan C, Dai L, Shen M, Xu Y, Ni, Y (2020) A smart porous wood-supported flower-like NiS/Ni conjunction with vitrimer co-effect as a multifunctional material with reshaping, shape-memory, and self-healing properties for applications in high-performance supercapacitors, catalysts, and sensors. Chem Eng J 396: 125318. http://dx.doi.org/10.1016/j.cej.2020.125318

Zhao W, Feng Z, Liang Z, Lv Y, Xiang F, Xiong C, Ni Y (2019) Vitrimer-Cellulose Paper Composites: A New Class of Strong, Smart, Green, and Sustainable Materials. ACS Appl Mater Inter 11: 36090–36099. https://doi.org/10.1021/acsami.9b11991