A Near-Infrared Excited FRET-Based Fluorescent Sensor Using Core–Shell Upconversion Nanoparticles Functionalized with Rhodamine B Derivative for Highly Selective Detection of Hg²⁺

Yanmei Zhang1, Rui Jiang1, Hongze Yang1, Cheng Zhou1, Mengxi Sun1, Hong Chen1, Donghai Lin2,*, Liming Huang3,*, Guosong Chen1
1.School of Chemistry and Molecular Engineering, Nanjing Tech University, Nanjing 211816, China

2.School of Energy and Materials, Shanghai Thermophysical Properties Big Data Professional Technical Service Platform, Shanghai Engineering Research Center of Advanced Thermal Functional Materials, Shanghai Key Laboratory of Engineering Materials Application and Evaluation, Shanghai Polytechnic University, Shanghai 201209, China

3. Department of Microbiology and Immunology, School of Medicine, University of Nevada, Reno, Nevada 89557, United States

* Corresponding Authors 

E-mail: dhlin@sspu.edu.cn (Dong-Hai Lin); huang@med.unr.edu (Li-Ming Huang)

[image: image1.jpg]16
616”
26501

11901
608017

e
L€zl
S6ECL

snele ise decovpled ated NOF
0

LLF-JRe
S

a)

(

i 60 50 40 30 2 10

30

18 170 160 150 140 130 120 110 100
£1 (ppm)

190

=007

F 929

58
28
e

(AL

w

£

€1
107
2

Nl





Figure S1. (a) 13C NMR (101 MHz, chloroform-d) and (b) 1H NMR (CDCl3, 400 MHz) spectra of RBDA

13C NMR (101 MHz, CDCl3): δ 191.94, 153.34, 151.67, 149.09, 145.25, 141.32, 136.69, 133.79, 129.79, 128.56, 128.11, 124.13, 123.61, 108.09, 105.92, 97.95, 44.41, 12.69. 
1H NMR (400 MHz, Chloroform‐d): δ 9.94 (s, 1H), 8.74 (s, 1H), 8.00‐7.97 (m, 1H), 7.77‐7.66 (m, 3H), 7.55‐7.45 (m, 2H), 7.15‐7.12(m, 1H), 6.52 (d, J = 8.9 Hz, 2H), 6.44 (d, J = 2.6Hz, 2H), 6.24 (dd, J = 8.9, 2.6 Hz, 2H), 3.32 (q, J = 7.1 Hz, 8H), 1.15 (t, J = 7.0 Hz, 12H) 
[image: image2.jpg]Intensity(a.u.)

|CS-UCNP@mSiO,-RBPA

CS-UCNP@mSIO,

A

CS-UCNP

B

@

A Mo A A

A Mo AN

JCPDS No. 16-0334

10 20 30

40 50

20/degree

60 70 80




Figure S2. XRD patterns of UCNP, CS-UCNP, CS-UCNP@mSiO2 and CS-UCNP@mSiO2-RBPA along with the standard card (JCPDS No. 16-0334)

[image: image3.jpg]Transmittance (%)

AN

(554 cm™)
3(Si-0)

CS-UCNP

CS-UCNP@mSIO,

CS-UCNP@mSiO,-RBPA

(1398 cml)| (1590 cm™) W(C=N)
(1445 cm™)W(C=C) (aromatic ring)

— (1082 cm!)
o(S1-O-S1)

(2910 cm™)
§(-CH2

(2910 cm™)

o-cHz) (2

) (2980 cm™)

480 cm™)

N 1
(3410 cm™)

S(-NH)

500

1000 1500 2000

2500

Wavenumber (cm'l)

3000

3500

4000




Figure S3. FT-IR spectra of CS-UCNP, CS-UCNP@mSiO2, and CS-UCNP@mSiO2-RBPA

[image: image4.jpg](a)

o]

O N—NH; OCHO

N
O O N S CH;0H , COOHCF3, 60°C ™
24h reflux )





Figure S4. (a) Synthetic route of RBPA and its (b) reaction with Hg2+

