Supplementary Materials

S1. Gaussian Simulation Parameters

The absorption and emission spectra of P3HT were modeled using Gaussian components to capture the vibronic progression (0-0, 0-1, 0-2). The following parameters were used for simulations:

Solution Phase:

- 0-0 peak: λ = 455 nm, σ = 25–30 nm, I = 1.0

- 0-1 shoulder: λ = 495 nm, σ = 25–30 nm, I = 0.3

Aggregated Phase:

- 0-0 peak: λ = 520 nm, σ = 15–20 nm, I = 1.0

- 0-1 peak: λ = 560 nm, σ = 15–20 nm, I = 0.75

- 0-2 peak: λ = 610 nm, σ = 15–20 nm, I = 0.65

Linewidths (σ) were adjusted to reflect disorder, crystallinity, and π-π stacking in different aggregation states.

S2. Crystallization Conditions

The effects of temperature, time, and polymer concentration on vibronic peaks were modeled as follows:

- Temperature (T): 25, 50, 75, 100, 125 °C

- Crystallization Time (t): 1–8 h

- Polymer Concentration (C): 0.5–2.5 a.u.

Gaussian peak positions and intensities were systematically modified according to:

σ=18-0.5(t-1)
λ0-0=530+0.05(C-1)
R(T)=I0-2(T)I0-1(T)

These relations simulate the evolution of molecular ordering, aggregation, and vibronic intensity ratios.

S3. Solvent Effects

Solvent quality was simulated using a dimensionless aggregation parameter (0–1) to account for differences in chain solubility:

- Good solvents: chloroform, chlorobenzene → broad, disordered spectra, lower 0-2/0-1 ratios (~0.8–0.9)

- Poor solvents: toluene, acetone, hexylthiophene → sharper, red-shifted spectra, higher 0-2/0-1 ratios (~1.2–1.3)

Normalized Gaussian spectra were generated to quantify the impact of solvent on aggregation-induced vibronic progression.

S4. Stokes Shift Calculations

Stokes shifts (ΔE_Stokes) were computed from the Gaussian-fitted absorption (λ_abs) and emission (λ_em) maxima using:

ΔEStokes=1240(1λabs-1λem)eV

- Solution: ΔE_Stokes = 0.35 eV (λ_abs = 550 nm, λ_em = 650 nm)

- Aggregates: ΔE_Stokes = 0.477 eV (λ_abs = 520 nm, λ_em = 650 nm)

S5. Python Simulation Scripts

All simulations were executed using Python 3 with the following packages:

- NumPy: array handling and numerical computations

- Matplotlib: plotting absorption and emission spectra

- SciPy: Gaussian fitting and peak analysis

Annotated scripts are available from the corresponding author upon request.

S6. Data Availability

All Gaussian-fitted spectra, peak parameters, and Python scripts used for the simulations are available from the corresponding author upon reasonable request.