Supplementary Information

Pt/CeO2 with residual chloride as reusable soft Lewis acid catalysts: application to highly efficient isomerization of allylic esters

Qi-An Huang,1 Asahi Haruta,1 Yuhya Kumamoto,1 Haruno Murayama,*1 Eiji Yamamoto,1 Tetsuo Honma,2 Mitsutaka Okumura,3 Hiroki Nobutou,3 Makoto Tokunaga*1

1Department of Chemistry, Graduate School of Science, Kyushu University, 744 Motooka, Nishi-ku, Fukuoka 819-0395, Japan

2Japan Synchrotron Radiation Research Institute (JASRI), SPring-8, Sayo, Hyogo 679-8198, Japan

3Department of Chemistry, Osaka University, Toyonaka, Osaka 560-0043, Japan

*Corresponding author: haruno9@chem.kyushu-univ.jp, mtok@chem.kyushu-univ.jp

Table of Contents

1. Optimization of reaction 	S2

1-1. Catalyst screening 	S2

1-2. Effect of Pt loading	S2

1-3. Details for evaluation of catalytic activity	S3

1-4. Time course of catalytic isomerization	S4

1-5. Effect of supports on catalytic isomerization 	S4

2. Characterization of the catalysts 	S5

2-1. HADDF-STEM images 	S5

2-2. XPS analysis 	S6

2-3. XAFS analysis 	S7

2-4. H2-TPR profiles	S10

3. Catalytic isomerization of allylic esters	S12

3-1. Substrate scope 	S12

3-2. Isomerization with homogeneous catalysts 	S14

3-3. Proposed catalytic cycle 	S15

4. Computational Details 	S16

5. Details for substrates discussion 	S20

5-1. Characterization of the products	S20

5-2. 1H and 13C NMR charts of compounds 	S22

- Optimization of the reaction conditions

1-1 Catalysts screening

Supplementary Table 1. Supporting effect of metal oxide-supported Pt catalysts in the catalytic isomerization of 3,4-DABE.

| Entry | Catalyst | Conv. (%)a | Yield (%)a |  |  | TON |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | (E)-2 | (Z)-2 |  |  |
| 1b | Pd/ZrO2 | 0 | 0 |  | 0 | 0 |
| 2c | Pd/CeO2 | 18 | 0 |  | 0 | 0 |
| 3 | Ir/CeO2 | 0 | 0 |  | 0 | 0 |
| 4 | Au/ZrO2 | 14 | 10 |  | 1 | 67 |
| 5 | Pt/CeO2 | 63 | 51 |  | 1 | 347 |
| 6 | Pt/ZrO2 | 57 | 49 |  | 2 | 327 |
| 7 | Pt/TiO2 | 63 | 47 |  | 1 | 320 |
| 8 | Pt/Al2O3 | 49 | 40 |  | 0 | 267 |
| 9 | Pt/MgO | 39 | 27 |  | 0 | 180 |
| 10d | Pt/CeO2 | 55 | 52 |  | 1 | 5300 |
| 11d,e | Pt/CeO2 | 56 | 51 |  | 1 | 5200 |
| 12d,e,f | Pt/CeO2 | 60 | 53 |  | 1 | 5400 |
| 13g | Mont-K10 | 18 | 12 |  | 1 | / |
| 14g | ZSM-5 | 27 | 7 |  | 1 | / |

aDetermined by gas chromatography (GC) analysis using tridecane as an internal standard. bUsing 10 wt% Pd/ZrO2 (2 mol%), THF as the solvent, reacting for 14 h. cUsing 5 wt% Pd/CeO2 (2 mol%), DMSO as the solvent, reacting for 18 h. dReacting in 0.01 mol%. eReacting under an air atmosphere. fReacting at the feedstock scale of 10 mmol. cUsing 30 mg catalysts under an air atmosphere, reacting for 5 h.

1-1 Effect of the Pt loading

Supplementary Table 2. Effect of the Pt loading on the catalytic isomerization of allylic esters.

| Entry | Catalyst | Conv. (%)a | Yield (%)a |  |
| --- | --- | --- | --- | --- |
|  |  |  | (E)-2 | (Z)-2 |
| 1 | 1 wt% Pt/CeO2 | 51 | 49 | 1 |
| 2 | 3 wt% Pt/CeO2 | 57 | 50 | 1 |
| 3 | 5 wt% Pt/CeO2 | 48 | 43 | 1 |
| 4 | 10 wt% Pt/CeO2 | 27 | 18 | 0 |

a Determined by GC analysis using tridecane as an internal standard.

1-3. Details for evaluation of the catalytic activity

Supplementary Table 3. Effect of the Pt loading on the catalytic isomerization of allylic esters.

| Entry | Catalyst | TON | Mechanism | Ref. |
| --- | --- | --- | --- | --- |
| 1 | Co(II) ligand | 9a | -allyl | 1 |
| 2 | Pd(0) ligand | 13 | -allyl | 2 |
| 3 | Pd(II) ligand | 13 | soft Lewis acid | 3 |
| 4 | Au(I) ligand | 33a | soft Lewis acid | 4 |
| 5b | Au/ZrO2 | 67d | soft Lewis acid | this study |
| 6c | Pt/CeO2 | 5400d | soft Lewis acid | this study |

aMaximum TON of discussed allylic esters substrates. bUsing 1 wt% Au/ZrO2 (0.15 mol%), reacting for 2 h. cUsing 1 wt% Pt/CeO2 (0.01 mol%) , reacting for 2 h under an air atmosphere. dCalculated by gas chromatography (GC) analysis using tridecane as an internal standard.

(1) Mukhopadhyay, M.; Reddy, M. M.; Maikap, G. C.; Iqbal, J. Cobalt(II)-Catalyzed Conversion of Allylic Alcohols/Acetates to Allylic Amides in the Presence of Nitriles. J. Org. Chem.60, 2670–2676 (1995).

(2) Bouquillon, S.; Muzart, J. Palladium(0)-Catalyzed Isomerization of (Z)-1,4-Diacetoxy-2-Butene - Dependence of η1- or η3-Allylpalladium as a Key Intermediate on the Solvent Polarity. Eur. J. Org. Chem. 17, 3301–3305 (2001).

(3) Zawisza, A. M.; Bouquillon, S.; Muzart, J. Palladium(II)-Catalyzed Isomerization of (Z)-1,4-Diacetoxy-2-Butene: Solvent Effects. Eur. J. Org. Chem. 2, 3901-3904 (2007).

(4) Marion, N.; Gealageas, R.; Nolan, S. P. [(NHC)Au1]-Catalyzed Rearrangement of Allylic Acetates. Org. 9, 2653–2656 (2007).

1-2 Time course of catalytic isomerization

Supplementary Figure 1. Reaction time course of the catalytic isomerization of allylic esters within 2 hours.

The time course of the catalytic isomerization of 3,4-DABE over the optimal Pt/CeO2 catalysts was conducted with a Pt loading of 0.05 mol% at 150 °C within 2 h. After reacting for 30 minutes, few changes in the conversion and yields could be seen during the following process.

1-3 Effect of supports on catalytic isomerization

Pt/CeO2   Pt/ZrO2   Pt/TiO2   Pt/Al2O3  Pt/MgO

Supplementary Figure 2. Reusability of Pt catalysts supported by different metal oxides for the catalytic isomerization of allylic esters.

The reusability of the catalysts was evaluated with the Pt catalysts supported by different metal oxide supports. After the Pt/CeO2 catalysts were used 3 times, no obvious deactivation occurred in the conversions or yields. Nevertheless, a marked decrease in conversions and yields was observed when using the other catalysts.

The reaction solution of the Pt/CeO2 catalysts was analyzed with MP-AES, and the leaching of the Pt species was detected as around 2 %, which was within the normal range of supported catalysts.

- Characterization of the catalysts

2-1. HADDF-STEM images

Supplementary Figure 3. HADDF-STEM images coupled with EDS mapping of 1 wt% Pt/CeO2 prepared from H2PtCl6·6H2O.

2-2. XPS analysis

Supplementary Table 4. Summary of the XPS measurement results for Pt/CeO2 prepared from various precursors or as-prepared catalysts after HCl treatment.

| Sample | Pt 4f XPS (at%) |  |  | Pt/Ce ratio (at%) | Cl/Pt ratio |
| --- | --- | --- | --- | --- | --- |
|  | Pt2+ (72.7 eV) | Pt4+ (74.1 eV) | Pt4+ (Cl) (74.8 eV) |  | (at%) |
| Pt/CeO2_Cl | 85.61% | 6.99% | 7.39% | 0.84 | 6.66 |
| Pt/CeO2_A | 94.36% | 5.64% | ̶ | 0.75 | ̶ |
| Pt/CeO2_N | 87.64% | 12.36% | ̶ | 0.87 | ̶ |
| Pt/CeO2_A_HCl | 75.86% | 1.46% | 22.68% | 0.54 | 15.23 |
| Pt/CeO2_N_HCl | 74.03% | 14.40% | 11.57% | 0.72 | 10.13 |

Supplementary Figure 4. Ce 3d XPS spectra of (a) 1 wt% Pt/CeO2 prepared from various precursors or as-prepared catalysts after HCl treatment and (b) amplification of the peaks.

The Ce 3d peaks of the catalysts prepared from H2PtCl6 and HCl-treated catalysts prepared from Pt(acac)2 or Pt(NH3)4(NO3)2 shifted by 0.2 eV to higher binding energy compared with that of the catalysts containing no chlorine. The peak shift can be considered as the positive charge effect from chlorine, revealing the strong interaction between CeO2 and Pt.

2-3. XAFS analysis

Supplementary Figure 5. The k3-weighted Pt LIII-edge EXAFS oscillations of Pt/CeO2_Cl, Pt/CeO2_A_HCl, and Pt/CeO2_N_HCl.

Supplementary Figure 6. (a) Pt LIII-edge XANES spectra and (b) Fourier transform magnitude EXAFS spectra of Pt catalysts supported by different metal oxides (k = 313 Å-1).

Supplementary Figure 7. (a) Pt LI-edge XANES spectra and (b) edge energy plots of Pt/CeO2 and Pt/Al2O3 prepared from H2PtCl6·6H2O.

Supplementary Figure 7 shows the Pt LI-edge XANES spectra of Pt0 foil, Pt2+(acac)2, Pt4+O2, and the as-prepared catalysts. The energy differences from the edge energy of the Pt foil are shown as ΔE. The ΔEs are found to vary linearly with the oxidation state of Pt. From the relationship, the oxidation states of Pt in Pt/CeO2_Cl were nearly 4+ and higher compared with those of Pt/Al2O3_Cl.

Supplementary Table 5. EXAFS fit parameters of Pt/CeO2.a

| Catalyst | Scattering path | CNb | R (Å)c | Δ2 (Å2)d | ΔE0 (eV) e | R-factorf |
| --- | --- | --- | --- | --- | --- | --- |
| Pt/CeO2 from Pt(acac)2 | PtO | 3.75 0.48 | 2.01 0.009 | 0.003 0.001 | 16.1 1.58 | 0.018 |
| Pt/CeO2 from Pt(NO3)2(NH3)4 | PtO | 3.14 0.29 | 1.99 0.006 | 0.003 0.001 | 14.7 1.16 | 0.009 |
| Pt/CeO2 from H2PtCl6 | PtO PtCl | 3.62 0.49 1.49 0.78 | 1.99 0.011 2.32 0.012 | 0.004 0.001 0.006 0.005 | 11.3 2.26 20.1 0.21 | 0.013 |
| Pt/CeO2 from Pt(acac)2_HCl | PtO PtCl | 4.24 1.03 1.76 1.03 | 2.01 0.038 2.32 0.026 | 0.008 0.002 0.001 0.003 | 12.3 3.91 18.0 6.07 | 0.021 |
| Pt/CeO2 from Pt(NO3)2(NH3)4_HCl | PtO PtCl | 2.17 0.28 1.79 0.27 | 1.97 0.013 2.29 0.019 | 0.001 0.001 0.001 0.001 | 12.2 3.52 11.1 4.82 | 0.018 |
| Pt/ZrO2 | PtO PtCl | 2.30 0.31 1.49 0.23 | 2.00 0.012 2.32 0.018 | 0.001 0.001 0.001 0.001 | 10.7 3.43 12.7 4.91 | 0.028 |
| Pt/MgO | PtO PtCl | 2.83 0.74 1.08 0.46 | 2.00 0.025 2.29 0.036 | 0.005 0.003 0.005 0.003 | 13.4 3.17 13.4 3.17 | 0.031 |
| Pt/Al2O3 | PtO PtCl PtPt | 1.72 0.70 1.62 0.26 3.80 0.71 | 1.99 0.016 2.32 0.023 2.75 0.007 | 0.006 0.003 0.006 0.001 0.006 0.001 | 8.20 2.06 18.2 4.73 8.20 2.06 | 0.015 |

a k3: k-range = 3–13 Å-1, Intrinsic loss factor, S02 = 1.21 (Pt–O) , 0.83 (Pt–Cl), and 0.84 (Pt–Pt).

b Coordination number.

c Bond length.

d Debye-Waller factor.

e Energy differences in the absorption threshold.

f Goodness-of-fit index.

2-4. H2-TPR profiles

Temperature programmed reduction with hydrogen (H2-TPR) was carried out in a BELCATII system (MicrotracBEL Corp.) equipped with a thermal conductivity detector (TCD) to quantify the consumed H2. The samples (100 mg) mounted in a quartz vessel were pretreated in an Ar atmosphere at 200 °C for 30 min to remove the physisorbed water and then cooled to room temperature. TPR profiles were collected by heating the samples from room temperature to 800 °C at a heating rate of 5 °C/min under a 50 mL/min flow of 5% H2/Ar.

Supplementary Figure 8. Temperature programmed reduction (TPR) profiles of 1 wt% Pt/CeO2 (prepared from an H2PtCl6·6H2O precursor, red line) and CeO2 (black line).

CeO2 usually gave a peak at 550 ℃, which belonged to the reduction of the surface of CeO2.5 Also, Pt/CeO2_Cl only showed an intense reduction peak at 220 ℃ below 600 ℃, which might be related to the Pt(OH)xCly species directly connected to the surface of CeO2 (Supplementary Figure 8).6 Also, the disappearance of the reduction peak of CeO2 in the curve of the prepared catalysts revealed a strong metal-support interaction (SMSI) between Pt and CeO2. Pt/CeO2_A showed a peak at 80 ℃, and Pt/CeO2_N showed a peak at 190 ℃ (Supplementary Figure 9a). The difference in the reduction peaks of the prepared Cl-free catalysts might be related to the surface PtOx of different sizes and Pt/O ratios as well as the strong interaction between Pt and CeO2.7-9 Pt/CeO2_Cl was calcined at 300 ℃ and 500 ℃ in the preparation process to obtain Pt(OH)xCly and PtOxCly as reference peaks.6 After HCl treatment, the peak of Pt/CeO2_A_HCl was mainly observed at approximately 220 ℃ (Supplementary Figure 9b). The peak of Pt/CeO2_N_HCl shifted to 250 ℃. Therefore, Pt species after HCl treatment were mainly considered Pt(OH)xCly and PtOxCly with the reference peaks obtained. This result was consistent with the result of the EXAFS spectra. The shift in the temperature may be related to the difference in the ratio of x/y of the species; the main reduction temperature increased along with a decrease in the x/y ratio, which meant that the sample contained a greater amount of Pt–Cl coordination. Hence, the weak reduction peaks occurred at the high temperature in Pt/CeO2_A_HCl, probably related to the large Pt–Cl coordination numbers or smaller clusters containing stronger Pt–O–Ce bonding.

Supplementary Figure 9. Temperature programmed reduction (TPR) profiles of 1 wt% Pt/CeO2 prepared (a) from different precursors at different calcination temperatures or (b) with HCl posttreatment.

(a) Different precursors: 1 wt% Pt/CeO2 catalysts prepared from three kinds of precursors were detected by TPR measurement. The catalyst prepared from Pt(acac)2 showed a peak at 80 ℃ (red). The catalysts prepared from Pt(NH3)4(NO3)2 gave a peak at 190 ℃ (blue). The catalyst prepared from H2PtCl6·6H2O was calcined at 300 ℃ (black) and 500 ℃ (yellow).

(b) HCl posttreatment: After the HCl treatment, the peak of the Pt catalyst prepared from Pt(acac)2 turned into three peaks at 215 ℃, 250 ℃, and 275 ℃ (red). The peak of the Pt catalyst prepared from Pt(NH3)4(NO3)2 shifted to 250 ℃ (blue).

(5) Lee, J.; Ryou, Y.; Chan, X.; Kim, T. J.; Kim, D. H. How Pt Interacts with CeO2 under the Reducing and Oxidizing Environments at Elevated Temperature: The Origin of Improved Thermal Stability of Pt/CeO2 Compared to CeO2. J. Phys. Chem. C 120, 25870-25879 (2016).

(6) Lieske, H.; Lietz, G.; Spindler, H.; Völter, J. Reactions of Platinum in Oxygen- and Hydrogen-Treated Pt γ-Al2O3 catalysts. I. Temperature-Programmed Reduction, Adsorption, and Redispersion of Platinum. J. Catal. 81, 8-16 (1983).

(7) Gao, Y.; Wang, W.; Chang, S.; Huang, W. Morphology Effect of CeO2 Support in the Preparation, Metal-Support Interaction, and Catalytic Performance of Pt/CeO2 Catalysts. ChemCatChem 5, 3610-3620 (2013).

(8) Acerbi, N.; Tsang, S. C.; Golunski, S.; Collier, P. A Practical Demonstration of Electronic Promotion in the Reduction of Ceria Coated PGM Catalysts. Chem. Commun. 13, 1578-1580 (2008).

(9) Acerbi, N.; Tsang, S. C. E.; Jones, G.; Golunski, S.; Collier, P. Rationalization of Interactions in Precious Metal/Ceria Catalysts Using the d-Band Center Model. Angew. Chem. Int. Ed. 52, 7737-7741 (2013).

- Catalytic isomerization of allylic esters

3-1 Discussion on substrate scope

Supplementary Figure 10. Pt/CeO2-catalyzed isomerization of allylic acetates. aDetermined by GC analysis using tridecane as an internal standard. b 0.25 mol% Pt/CeO2 added. c 71:29 ratio of E/Z isomers.

When allylic acetates derived from tertiary alcohol were tested, a yield of 48% was achieved (entry 1). The substrates with pentyl or cyclo-hexyl groups showed similar yields to the model reaction discussed above (entries 2 and 3). Particularly, the substrate with the phenyl group provided a higher transformation rate than the others, which might be because of the stable conjugated structure in the product (entry 4). Low transformation and low Z-isomer amounts were detected when using linalyl acetate derived from tertiary alcohols, which might be due to the strong steric effect on the surface (entry 5).

Supplementary Figure 11. Pt/CeO2-catalyzed isomerization of allylic benzoates. aDetermined by NMR analysis using mesitylene as an internal standard. b The experiment was conducted under an air atmosphere.

Regardless of the presence of the electron-donating methoxy or electron-withdrawing nitryl group on the phenyl, the detected yields were almost 5767% (entries 13), revealing the weak electron effect in this reaction system. Furthermore, allylic benzoate with a 2,4,6-trimethylphenyl group was used to confirm the steric effect of the substrates (entry 4). A 33% yield revealed that the steric effect plays a more important role than the electron effect in this reaction.

3-2 Isormerization with homogeneous catalysts.

Supplementary Table 6. Catalytic isomerization of oct-1-en-3-yl benzoate with homogeneous catalysts.

| entry | catalyst | solvent | Yield (%)b |  |  | TONc |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 1 | 2 | 3 |  |
| 1 | Pd(PPh3)4 (10 mol%) | THF | 0 | 63 | 31 | 0 |
| 2 | PdCl2(MeCN)2 (10 mol%) | THF | 64 | 0 | 0 | 6 |
| 3 | Pt(PPh3)4 (10 mol%) | THF | 0 | 70 | 29 | 0 |
| 4 | PtCl2(PhCN)2 (10 mol%) | THF | 59 | 0 | 0 | 6 |
| 5 | Pt(acac)2 (10 mol%) | THF | 0 | 0 | 0 | 0 |
| 6 | H2PtCl6∙6H2O (10 mol%) | THF | 42 | 0 | 0 | 4 |
| 7a | Pt/CeO2 (0.01 mol%) | neat | 50 | 0 | 0 | 5000 |

a Reaction condition: 150 °C, 4 h.

b Determined by NMR analysis using mesitylene as an internal standard

c Turnover numbers of catalytic isomerization of allylic esters.

Homogeneous Pt and Pd catalysts were also used to investigate the reaction mechanism and effect of PtCl bonding by oct-1-en-3-yl benzoate. It was reported that Pd(PPh3)4 can catalyze the isomerization of allylic esters through a -allyl intermediate. However, only dienes were detected in this reaction, which might be due to the relatively low nucleophilicity of the carbonyl oxygen atom in the benzoyl ester group. Hence, the isomerization of substrates such as oct-1-en-3-yl benzoate could only proceed by the soft Lewis acid mechanism. Apart from Pt(PPh3)4 and Pt(acac)2, PtCl2(PhCN)2 and H2PtCl6∙6H2O both showed activity in the isomerization reaction with a low TON. An elimination reaction was observed when using Pt(PPh3)4, and no products were detected when using Pt(acac)2. This result proved that catalysts containing PtCl bonds can act as soft Lewis acids and promote the isomerization of allylic esters.

3-3 Proposed catalytic cycle

Supplementary Figure 12. Proposed catalytic cycle of the isomerization of allylic esters.

- Details of the calculations and structural models

Supplementary Figure 14. Optimized structural models of the CeO2-supported Pt catalysts and the calculated charges on the Pt species.

Structural models in which chlorine atoms were bonded with platinum on the CeO2 surface were hypothesized and calculated for the whole 3,4-DABE isomerization reaction. Optimized structural models for each state are shown in Supplementary Figure 15.

Supplementary Figure 15. Optimized structural models for the reaction path of the isomerization of 3,4-DABE over CeO2 supported Pt catalysts containing Pt–Cl bonds.

Isomerization of 3,4-DABE on the surface of PtO2/CeO2 was also hypothesized and calculated. A structural model of Pt1O3/CeO2 was created and the binding between the surface of the catalyst and 3,4-DABE was thought to be generated via a di–σ (Pt–O) bond instead of a –bond. Optimized structural models for each state are shown in Supplementary Figure 16.

Supplementary Figure 16. Optimized structural models for the reaction path of the isomerization of 3,4-DABE over Pt1O3/CeO2 catalysts.

The calculation result for the isomerization of 3,4-DABE on the bulk surface (011) of PtO2 catalyst was shown in Supplementary Figure 17. The adsorption of 3,4-DABE should also occur via di–σ (Pt–O) bonding instead of the –bond. Because of the high desorption energy (1.66 eV), bulk PtO2 is also inactive for the isomerization of 3,4-DABE.

Supplementary Figure 17. Diagram of the energy calculation of the transition states on the model catalyst PtO2 (011).

Supplementary Figure 18. Optimized structural models for the reaction path of the isomerization of 3,4-DABE over PtO2 (011) catalysts.

Both the bulk PtO2 and the supported PtO2 catalysts were proved to adsorb C=C via di-σ (Pt–O) bonding at INI and FIN. Since the di–σ (Pt–O) bonding is stable, the desorption of the substrate does not proceed. In order to investigate the basic adsorption site of C=C structure, the adsorption states of ethylene on bulk PtO2 were compared in Supplementary Figure 19.

Supplementary Figure 19. Comparison of the adsorption states of ethylene on bulk PtO2.

The adsorption energies of ethylene on optimized structures of discussed Pt catalysts were compared based on di–σ (Pt–O) bonding and di–σ (Pt–Cl) bonding (Supplementary Table 7). The results show that on the model of the listed catalysts, di–σ (Pt–O) bonding is more stable than the π-bond and tends to be difficult to process the desorption. Also, for the calculation over Pt1O1Cl2/CeO2 and Pt1Cl4/CeO2, di–σ (Pt–Cl) bonding is less stable than the π-bond.

Supplementary Table 7. Adsorption energy for ethylene on discussed structures.

| Catalyst | Ead (eV) | di (PtO) |  | di (PtCl) |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Ead (eV) | Ead (eV) | Ead (eV) | Ead (eV) |
| Pt1O3/CeO2 | -1.05 | -1.86 | -0.81 | - | - |
| Pt1O1Cl2/CeO2 | -1.02 | -1.29 | -0.27 | -0.54 | 0.48 |
| Pt1Cl4/CeO2 | -1.19 | - | - | -1.02 | 0.17 |
| PtO2 (011) | -0.81 | -1.67 | -0.86 | - | - |

- Substrates Discussion

5-1. Characterization of the Products

3-methylbut-2-en-1-yl acetate

1H NMR (600 MHz, CDCl3) δ 5.33–5.30 (1 H, m), 4.54 (2 H, d, J = 7.6 Hz), 2.03 (3 H, s), 1.74 (3 H, s), 1.68 (3 H, s).

13C NMR (151MHz, CDCl3) δ 171.4, 139.3, 118.6, 61.5, 25.9, 21.1, 18.1.

(E)-Oct-2-en-1-yl acetate

1H NMR (400 MHz, CD3OD) δ 5.80–5.73 (1 H, m), 5.56–5.51 (1 H, m), 4.46 (2 H, d, J = 6.9 Hz), 2.05–1.99 (5 H, m), 1.40–1.24 (6 H, m), 0.90–0.86 (3 H, m).

13C NMR (151MHz, CD3OD) δ 171.3, 136.0, 123.9, 64.9, 31.9, 31.2, 28.5, 22.2, 19.5, 13.1.

(E)-3-cyclohexylallyl acetate

1H NMR (600 MHz, CDCl3) δ 5.76–5.68 (1H, m), 5.52–5.47 (1 H, m), 4.49 (2 H, d, J = 6.2 Hz), 2.05 (3 H, m), 1.98–1.94 (1 H, m), 1.72–1.62 (5 H, m) 1.28–0.94 (5 H, m).

13C NMR (151MHz, CDCl3) δ 171.1, 142.3, 121.3, 65.7, 40.4, 32.6, 26.2, 26.0, 21.2.

Cinnamyl acetate

1H NMR (400MHz, CD2Cl2) δ 7.37–7.19 (5 H, m), 6.60 (1 H, d, J = 15.6 Hz), 6.25 (1 H, dt, J = 15.7, 6.3 Hz), 4.66 (2 H, dd, J = 6.4, 1.4 Hz), 2.03 (3 H, s).

13C NMR (151MHz, CD2Cl2) δ 170.6, 136.3, 133.6, 128.6, 128.0, 126.5, 123.6, 64.9, 20.8.

(a) Geranyl acetate, (b) Neryl acetate

(a)                 (b)

1H NMR (600 MHz, CD3OD) δ 5.33–5.28 (1H, m), 5.15–5.06 (1 H, m), 4.56–4.51 (2 H, m), 2.11–1.94 (7 H, m), 1.89–1.64 (6 H, m), 1.59–1.57 (3 H, m).

13C NMR (151MHz, CD3OD) (a) δ 170.5, 141.8, 131.3, 123.6, 118.5, 60.9, 39.2, 26.0, 24.5, 19.5, 16.3, 15.1. (b) δ 170.5, 141.8, 131.3, 123.6, 119.2, 60.7, 31.7, 26.3, 24.5, 22.8, 19.5, 16.3.

(E)-Oct-2-en-1-yl benzoate

1H NMR (400 MHz, CDCl3) δ 8.04–8.01 (2H, m), 7.54–7.50 (1 H, m), 7.43–7.38 (2 H, m), 5.90–5.79 (1 H, m), 5.68–5.61 (1 H, m), 4.73 (2 H, d, J = 6.4 Hz), 2.04 (2 H, q, J = 7.2 Hz), 1.41–1.23 (6 H, m), 0.87–0.83 (3 H, m).

13C NMR (151 MHz, CDCl3) δ 166.6, 136.9, 132.9, 130.5, 129.7, 128.4, 123.8, 65.9, 32.4, 31.5, 28.7, 22.6, 14.1.

(E)-Oct-2-en-1-yl p-nitrobenzoate

1H NMR (600 MHz, CDCl3) δ 8.29–8.27 (2H, m), 8.22–8.20 (2 H, m), 5.91–5.85 (1 H, m), 5.69–5.64 (1 H, m), 4.80 (2 H, d, J = 5.5 Hz), 2.08 (2 H, q, J = 7.1 Hz), 1.43–1.25 (6 H, m), 0.89–0.87 (3 H, m).

13C NMR (151 MHz, CDCl3) δ 164.6, 150.6, 138.0, 135.9, 130.8, 123.6, 123.1, 66.8, 32.4, 31.5, 28.6, 22.6, 14.1.

(E)-Oct-2-en-1-yl p-methoxybenzoate

1H NMR (400 MHz, CDCl3) δ 7.99–7.96 (2H, m), 6.90–6.86 (2 H, m), 5.89–5.77 (1 H, m), 5.67–5.60 (1 H, m), 4.69 (2 H, d, J = 6.4 Hz), 3.82 (3H, m), 2.03 (2 H, q, J = 7.0 Hz), 1.40–1.23 (6 H, m), 0.87–0.82 (3 H, m).

13C NMR (151 MHz, CDCl3) δ 166.3, 163.4, 136.6, 131.7, 124.0, 122.9, 113.6, 65.6, 55.5, 32.4, 31.5, 28.7, 22.6, 14.1.

(E)-Oct-2-en-1-yl 2,4,6-trimethylbenzoate

1H NMR (600 MHz, CDCl3) δ 6.83 (2H, m), 5.88–5.82 (1 H, m), 5.68–5.63 (1 H, m), 4.73 (2 H, d, J = 6.9 Hz), 2.27–2.26 (9 H, m), 2.05 (2 H, q, J = 7.1 Hz), 1.43–1.23 (6 H, m), 0.89–0.86 (3 H, m).

13C NMR (151 MHz, CDCl3) δ 170.1, 139.3, 137.4, 135.1, 131.1, 128.4, 123.6, 65.8, 32.3, 31.4, 28.6, 22.6, 21.2, 19.7, 14.1.

5-2. 1H and 13C NMR charts of compounds

(some charts contained both substrates and products because of the difficulty in separation)

1H NMR charts of byproducts dienes of isomerization of oct-1-en-3-yl benzoate with homogeneous catalyst.

Engman, L.; Bystrom, S. E. Tellurolate-Induced 1,4-Elimination of 1,4-Dibromo 2-Enes. Syntheses of 1,3-Dienes. J. Org. Chem. 1985, 50, 3170–3174.