Supporting

Room Temperature long-wavelength infrared Sensitive Imaging Photodetection based on topological insulator Bi2Te3 nanoflakes

Sihang Liu1, Dongbo Wang1, ✉ lijuan Liang7, ✉, Chenchen Zhao2, ✉, Donghao Liu1, Bingke Zhang3, Jingwen Pan9, Xiangqun Chen1, Xuxuan Yang1, Hao Dang1, Dong Li1, Gang Liu4, ✉, Dengkui Wang5, Dan Fang5, Fujun Liu5,✉, Jiamu cao10, Ling Li10, Yufeng Zhang10, Dongwei Jiang6,✉, Xuan Fang5, ✉, Jiehe Sui1, Liancheng Zhao1, Zhichuan Niu6, Jiaqi Zhu8, ✉

1School of Materials Science and Engineering, Harbin Institute of Technology, Harbin 150001, China.

2School of Chemistry and Chemical Engineering, Henan University of Science and Technology, Luoyang, Henan 471023,China

3School of Materials Science and Engineering, University of Jinan, Jinan 250000, China.

4Center for High Pressure Science and Technology Advanced Research Shanghai 201203, China

5Changchun University Science and Technology, Sch Sci, State Key Lab High Power Semicond Lasers, Changchun 130022, People’s Republic of China

6Key Laboratory of Optoelectronic Materials and Devices, Chinese Academy of Sciences, institute of semiconductors, Beijing 100083, China

7Shanghai Institute of Microsystem and Information Technology, Chinese Academy of Sciences, Shanghai 200050, China

8Harbin Inst Technol, Ctr Composite Mat & Struct, Harbin 150080, Peoples R China

9School of Materials Science and Engineering, Henan University of Technology, Zhengzhou 450001, China

10Harbin Inst Technol, Sch Astronaut, Harbin 150001, Heilongjiang, Peoples R China

✉e-mail: wangdongbo@hit.edu.cn; llj@mail.sim.ac.cn; cczhaophd@haust.edu.cn; liugang@hpstar.ac.cn; fjliu@cust.edu.cn; jdw@semi.ac.cn; fangx@cust.edu.cn; zhujq@hit.edu.cn

Appendix 1: Calculation of single-particle eigen-energy and eigen-wavefunction from a tight-binding model

With the energies and wavefunctions obtained from DFT calculation, we develop a tight-binding (TB) model using the Wannier90 package [Mostofi A A, Yates J R, Pizzi G, Lee Y-S, Souza I, Vanderbilt D and Marzari N 2014 Computer Physics Communications 185 2309-10]. This maps the ground-state wave functions from the plane wave basis set onto a maximally localized Wannier function basis Wik, where i=I,α is the composite index of the atomic orbit α of an atom with atom site R. R = Raa + Rbb + Rcc is the Bravais lattice vector with Ra/b/c being the Bravais lattice vector component in the direction of the unit cell lattice vector a/b/c. The Bloch function of TB model is thus given by:

ϕik=1NRe-ik⋅RWik(r)	(A1)

and elements of the TB Hamiltonian HTB are given by:

HijTBk=Re-ik⋅RtijR	(A2)

where tijR=Wi0HKSWjk are the matrix element extracted from the Wannier90 output file, with HKS being the Hamiltonian of the Kohn-Sham equation.

Appendix 2: Calculation of excitonic bandstructure

With single-particle eigenvalues and wavefunctions of the single particle from TB model, we calculate excitonic states through many-body problem using Bethe–Salpeter equation (BSE) [Cutkosky R E 1954 Phys Rev 96 1135-41; Carbonell J and Karmanov V A 2010 The European Physical Journal A 46 387-97]. An exciton state|ΨsQ is a coherent superposition of hole (with crystal momentum k) and electron (with crystal momentum k+Q) states from band-pairs (υ, c) in the reciprocal space and can be written as:

|ΨsQ=c,υ,kAc,υ,k,QSϕc,k+Q|ϕυ,k⟩	(A3)

where S and Q are the exciton band index and the center-of-mass momentum, respectively, and Ac,υ,k,QS is the coordinate. The exciton eigenvalue problem in the basis displayed in Eq. (A3) leads to the following BSE:

ES(Q)=(Ec,k,+Q-Eυ,k)k,υ,ck',υ',c'+1Ak',υ',c'Wk,υ,ck',υ',c',QAc',υ',k',QS	(A4)

where A=AcNk2 is the total area of the crystal, with Ac=3a22 and a being the lattice constant, Ec/v,k is the eigenvalue of TB model with the momentum k, Wk,υ,ck',υ',c',Q represents the matrix element of the many-body Coulomb potential including direct W dand W x exchange terms, and ES(Q) is the exciton energy of the Sth state with the center-of-mass momentum Q.

To simplify the calculation, we apply the Tamm-Dancoff approximation [ So Hirata and Head-Gordon M 1999 Chem Phys Lett 314 291-299] to the many-body Coulomb potential, which neglects the orbital character of the Coulomb interaction. In this case Wk,υ,ck',υ',c',Qd and Wk,υ,ck',υ',c',Qx are given by

Wk,υ,ck',υ',c',Qd=Vk-k'c,k+Qc',k'+Qυ,kυ',k'	(A5)

and

Wk,υ,ck',υ',c',Qx=VQc,k+Qυ,kυ',k'υ',k'+Q	(A6)

with

VQ=-e22ε0εdQ1+r0Q	(A7)

where ε0/d is the vacuum/effective dielectric constant, and r0represents a characteristic length.

Appendix 3: Calculations of the surface local density of states.(LDOS) of related energy spectrum

To investigate the superconducting or magnetic proximity effects in Bi₂Te₃ crystals, it is necessary to adopt open boundary conditions to model the material’s surface or interface. For convenience, the three-dimensional vector R is decomposed into a longitudinal component R⊥, perpendicular to the material surface, and a transverse component R∥, parallel to the surface. After applying open boundary conditions along the R⊥ direction, a two-dimensional thin-film system is formed, in which only the in-plane R⊥ direction remains periodic.

In general, experimentally cleavable planes often conflict with the primitive lattice vectors obtained from first-principles calculations. Therefore, it becomes necessary to redefine the basis vectors R′₁, R′₂, and R′₃ as follows:

R′1 = U11R1 + U12R2 + U13R3

R′2 = U21R1 + U22R2 + U23R3

R′3 = U31R1 + U32R2 + U33R3	(A8)

where R′₁ and R′₂ form the transverse vector R⊥, while R′₃ corresponds to R⊥. Using the basis vector transformation matrix U, the physical properties of arbitrary cleavage surfaces can be systematically studied.

In this project, the Hamiltonian of the resulting two-dimensional Bi₂Te₃ crystal is obtained by imposing open boundary conditions along the R′₃ direction and performing a Fourier transform along the periodic directions:

Hij2Dk‖=R'HijTBR'e-ik‖R' 	(A9)

Figure S1 (a, b)TEM and (c, d) multi-element mappings of the synthesis samples of Bi2Te3.

Figure S2 (a)SEM and (b, c) AFM of the synthesis samples of Bi2Te3.

Figure S3 (a) XPS survey of Bi2Te3. (b, c) XPS fine spectra of elemental Bi and Te in Bi2Te3.

Figure S4 (a, c, e) Variable temperature PL of Bi2Te3 and (b, d, f) Variable power PL of Bi2Te3 which be prepared in different batches.

Figure S5 Absorption spectra of Bi2Te3 (a) in the visible light and (b) in the infrared light.

Figure S6 Under the excitation of a 447 nm laser (a) I-V characteristics. (b) photocurrent response of the Bi2Te3-based device. (c) Response time characteristics of the device.

Figure S7 Under the excitation of a 470 nm laser (a) I-V characteristics. (b) photocurrent response of the Bi2Te3-based device. (c) Response time characteristics of the device.

Figure S8 Under the excitation of a 520 nm laser (a) I-V characteristics. (b) photocurrent response of the Bi2Te3-based device. (c) Response time characteristics of the device.

Figure S9 Under the excitation of a 808 nm laser (a) I-V characteristics at different temperature. (b) I-V characteristics at different power. (c) Photocurrent response of the Bi2Te3-based device. (d) Response time characteristics of the device.

Figure S10 Under the excitation of a 980 nm laser (a) I-V characteristics at different temperature. (b) I-V characteristics at different power. (c) Photocurrent response of the Bi2Te3-based device. (d) Response time characteristics of the device.

Figure S11 Under the excitation of a 1064 nm laser (a) I-V characteristics. (b) Photocurrent response of the Bi2Te3-based device. (c) Response time characteristics of the device. (d) Cycling test of photocurrent response.

Table S1 The on/off ratio, Ri, D* and EQE values of each laser at different temperatures.

| Laser | Temperature (K) | on/off ratio | Ri (mA/W) | D* (Jones) | EQE (%) |
| --- | --- | --- | --- | --- | --- |
| 447 nm 100 mW 0.1 V | 75 | 1844 | 5.75938E-5 | 1.82127E9 | 6.75029E-4 |
|  | 100 | 2060 | 6.43438E-5 | 2.03473E9 | 7.54142E-4 |
|  | 150 | 2280 | 7.12188E-5 | 2.25213E9 | 8.34721E-4 |
|  | 200 | 236 | 7.34375E-5 | 7.34375E8 | 8.60726E-4 |
|  | 250 | 30.20833 | 8.7625E-5 | 2.82808E8 | 1.02701E-3 |
|  | 300 | 3.98214 | 1.04375E-4 | 9.86251E7 | 1.22333E-3 |
| 808 nm 100 mW 0.1 V | 15 | 13008.13008 | 9.99923E-5 | 6.37528E9 | 1.17196E-3 |
|  | 50 | 9847.32824 | 8.06168E-5 | 4.98052E9 | 9.44871E-4 |
|  | 100 | 9310.34483 | 8.43659E-5 | 4.95414E9 | 9.88813E-4 |
|  | 150 | 2572.46377 | 8.87155E-5 | 2.67002E9 | 1.03979E-3 |
|  | 200 | 309.61538 | 1.003E-4 | 9.83522E8 | 1.17557E-3 |
|  | 250 | 27.74123 | 1.52425E-4 | 3.56898E8 | 1.7865E-3 |
|  | 300 | 5.01661 | 1.51125E-4 | 1.37728E8 | 1.77126E-3 |
| 980 nm 100 mW 0.1 V | 15 | 12053.57143 | 8.4368E-5 | 5.63707E9 | 9.88837E-4 |
|  | 50 | 12248.06202 | 9.87419E-5 | 6.1474E9 | 1.15731E-3 |
|  | 100 | 11586.2069 | 1.04991E-4 | 6.16528E9 | 1.23055E-3 |
|  | 150 | 3955.82329 | 1.23094E-4 | 3.90038E9 | 1.44272E-3 |
|  | 200 | 479.21225 | 1.36589E-4 | 1.42871E9 | 1.6009E-3 |
|  | 250 | 34.97653 | 1.80925E-4 | 4.38292E8 | 2.12053E-3 |
|  | 300 | 6.05128 | 1.84688E-4 | 1.70744E8 | 2.16463E-3 |

Table S2 The on/off ratio, Ri, D* and EQE values of each laser at different power.

| Laser | Power density | on/off ratio | Ri (mA/W) | D* (Jones) | EQE (%) |
| --- | --- | --- | --- | --- | --- |
| 470 nm 300 K 0.1 V | 167.6 μW | 7.21667 | 0.1391 | 1.26977E11 | 1.63 |
|  | 5891.5 μW | 16.71667 | 0.01 | 9.1322E9 | 0.117 |
|  | 9047.1 μW | 23.15 | 0.00918 | 8.38118E9 | 0.108 |
|  | 10704.2 μW | 24.91667 | 0.00838 | 7.64869E9 | 9.8203E-2 |
| 520 nm 300 K 0.1 V | 6.8 mW | 1.78333 | 4.31985E-4 | 3.94347E8 | 5.06309E-3 |
|  | 25 mW | 2.16667 | 1.75E-4 | 1.59752E8 | 2.05109E-3 |
|  | 43.5 mW | 2.35 | 1.16379E-4 | 1.06239E8 | 1.36403E-3 |
|  | 60.3 mW | 2.5 | 9.32836E-5 | 8.51559E7 | 1.09333E-3 |
|  | 77.2 mW | 2.61667 | 7.85298E-5 | 7.16876E7 | 9.2041E-4 |
| 808 nm 300 K 0.1 V | 40 mW | 4.16667 | 2.96875E-4 | 2.71009E8 | 3.47953E-3 |
|  | 60 mW | 4.46667 | 2.16667E-4 | 1.97789E8 | 2.53945E-3 |
|  | 80 mW | 4.73333 | 1.75E-4 | 1.59752E8 | 2.05109E-3 |
|  | 100 mW | 5.01667 | 1.50625E-4 | 1.37501E8 | 1.7654E-3 |
|  | 120 mW | 5.3 | 1.34375E-4 | 1.22667E8 | 1.57494E-3 |
| 980 nm 300 K 0.1 V | 40 mW | 4.58333 | 3.35937E-4 | 3.06668E8 | 3.93736E-3 |
|  | 60 mW | 5 | 2.5E-4 | 2.28218E8 | 2.93013E-3 |
|  | 80 mW | 5.46667 | 2.09375E-4 | 1.91132E8 | 2.45398E-3 |
|  | 100 mW | 5.88333 | 1.83125E-4 | 1.67169E8 | 2.14632E-3 |
|  | 120 mW | 6.41667 | 1.69271E-4 | 1.54522E8 | 1.98394E-3 |
| 1064 nm 300 K 0.1 V | 7.5 μW | 4.1 | 3.35937E-4 | 1.1553E12 | 12.111 |
|  | 375.8μW | 11.75 | 2.5E-4 | 7.99552E10 | 0.838 |
|  | 637.6μW | 19.33333 | 2.09375E-4 | 9.84314E10 | 1.264 |
|  | 787.4μW | 23.66667 | 1.83125E-4 | 9.85446E10 | 1.265 |
| 10.6 μm 300 K 1 V | 60 mW | 1.86408 | 0.00221 | 3.1503E8 | 2.58462E-2 |
|  | 80 mW | 1.89879 | 0.00173 | 2.46763E8 | 2.03278E-2 |
|  | 100 mW | 1.93952 | 0.00146 | 2.07612E8 | 1.7068E-2 |
|  | 120 mW | 1.94444 | 0.00124 | 1.74607E8 | 1.45286E-2 |
|  | 140 mW | 1.95402 | 0.00111 | 1.53857E8 | 1.30286E-2 |
|  | 160 mW | 2.04183 | 0.00107 | 1.47577E8 | 1.25446E-2 |

Figure S11 Picture of the Bi2Te3-based device. (b) Optical photograph of the electrode. (c) “HIT” pixel images under the excitation of a 1064 nm laser.

Figure S12 Response spectrum.

Figure S13 (a) Picture of the Bi2Te3-based 64×64 focal plane array. (b) Picture of the Bi2Te3-based 64×64 focal plane device. (c) Imaging system under the excitation of visible light.

Video S1 Imaging process under the excitation of visible light.