Supporting information

The structural stability of ARuO3 perovskites is quantified by the Goldschmidt Tolerance Factor (t):

t= rA+rO2rRu+rO

While Sr2+ (rA = 1.44 Å) results in t ~ 0.96 (closer to an ideal cubic structure), the smaller Ca2+ radius (rA = 1.34 Å) leads to t ~ 0.92, necessitating significant structural distortions to stabilize the lattice [3].

Therefore, the octahedral configuration of the tensile-strained CRO thin film was confirmed to be a0a0c+ and octahedral anisotropic distortion, in-plane elongation of bond lengths contraction along cPC-axis.

Simultaneously, the out-of-plane connectivity is completely linearized to 180°. This linearization of the apical bonds leads to a compressed bond length of 1.918 Å, driven by the c-axis contraction. The dramatic increase in the octahedral distortion parameter (Δ = 1.68 x 10–3) and the anomalously low effective Poisson's ratio (ν = 0.13) reflect a structural hardening along the apical cpc-axis. Once linearized, these apical bonds act as rigid structural pillars, making the vertical axis significantly stiffer than the bulk hinge-like configuration. [ref]

The extreme in-plane structural distortion explains the high in-plane effective mass (m* = 4.12 m0) and the observed Non-Fermi Liquid behavior, as the narrowed in-plane bandwidth enhances electron-electron correlations and prevents coherent quasiparticle formation.