Electronic Supplementary Information

Photocapacitors Integrating Binder-Free MXene Microsupercapacitor and Carbon Perovskite Solar Cell for Indoor Applications

Abhinandan Patra1$, Samyuktha Noola1,2$, Giulio Koch1, Ebin Joseph1, Thomas Meredith Brown1, Francesca De Rossi1, Claudia Barolo2, Chandra Sekhar Rout3,* Francesca Brunetti1,*

1C.H.O.S.E. (Centre for Hybrid and Organic Solar Energy), Department of Electronic Engineering, University of Rome Tor Vergata, via del Politecnico 1, 00133, Rome, Italy.

2 Department of Chemistry, NIS Interdepartmental Centre and INSTM Reference Centre, Università Degli Studì di Torino, Via Pietro Giuria 7, 10125, Torino, Italy.

3Centre for Nano and Material Sciences, Jain (Deemed–to–be University), Jain Global Campus, Kanakapura Road, Bangalore – 562112, Karnataka, India

$ The authors have contributed equally.

Corresponding authors: francesca.brunetti@uniroma2.it, r.chandrasekhar@jainuniversity.ac.in

Figure S1: Exposed area for EDS along with elemental mapping of Ti and C.

Figure S2: XPS survey spectra of exfoliated Ti3C2Tx MXene.

Figure S3: PV parameters of C-PSCs in forward and reverse scan directions; (a) open-circuit voltage (VOC) (b) short-circuit current density (JSC); (c) fill factor (FF); (d) power conversion efficiency (PCE).

| Scan | Voc(V) | Jsc(mA/cm2) | Fill factor (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| FW | 0.99 ± 0.02 | 16.16 ± 2.3 | 32.5 ± 4.6 | 5.23 ± 1.1 |
| RV | 0.98 ± 0.02 | 16.17 ± 2.4 | 32.43 ± 8.1 | 5.21 ± 1.5 |

Table S1:  Average values of PV parameters of C-PSCs in forward and reverse scan directions.

Figure S4: (a) Dark JV and (b) Current vs light Intensity for the best performing C-PSC device.

Figure S5: (a) Comparative GCD of the integrated photocapacitor under various light intensities, i.e. 1 sun, 1000 lx, 500 lx, 200 lx; (b) Power variation with time of the device under various light conditions, (c) GCD of the device under 1 sun and constant current mode; (d), (e) and (f) Power variation of the integrated photocapacitor under different indoor light conditions, i.e. 1000 lx, 500 lx, 200 lx, respectively.

Figure S6: Diagram illustrating the synthesis process for Ti3C2Tx MXenes exfoliation.

Figure S7: (a) MXene inks of different concentrations and (b) all blade coated MXene/ITO/glass in a 10 × 8 cm2 of large area.

| Light intensities (Outdoor and indoor) | Load Resistances |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1 MΩ |  |  |  | 3 MΩ |  |  |  | 6 MΩ |  |  |  |  |
|  | Vcap (V) | Pcap (µW) | tc (s) | td (s) | Vcap (V) | Pcap (µW) | tc (s) | td (s) | Vcap (V) | Pcap (µW) | tc (s) | td (s) |
| 1 sun | 0.85 | 0.75 | 5.1 | ≈67 | 0.86 | 0.25 | 5 | ≈68 | 0.87 | 0.13 | 4.9 | ≈70 |
| 1000 lx | 0.78 | 0.63 | 5.1 | ≈65 | 0.79 | 0.21 | 5 | ≈67 | 0.8 | 0.10 | 4.9 | ≈68 |
| 500 lx | 0.76 | 0.60 | 5.1 | ≈62 | 0.77 | 0.20 | 5 | ≈65 | 0.78 | 0.09 | 4.9 | ≈66 |
| 200 lx | 0.72 | 0.54 | 5.1 | ≈60 | 0.73 | 0.18 | 5 | ≈63 | 0.74 | 0.09 | 4.9 | ≈64 |

Table S2: All the information regarding photocharging, discharging time, voltage and power acquired at various light intensities and resistances.

| Supercapacitor electrode | Device layout | Type of PV device | Operational voltage (Vcap) | ηoverall (%) (illumination) | Mode of measurement | Stability | Coulombic efficiency (%) | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MWCNT-PPy | 3T | Glass/FTO/TiO2/MAPbI3/ Spiro-OMeTAD/gold | 0.6 in 300 s | 10 (1 sun) | Constant current mode | - | - | 1 |
| carbon-AC/rGO-PEDOT (Microsupercapacitor) | 2T | Glass/FTO/SnO2/MAPbI3/ carbon-AC/rGO-PEDOT | 0.85 in 20 s | 3.6 (1 sun) | Constant current mode | 51.6% after 6000 cycles | - | 2 |
| PEDOT-C | 2T | Perovskite solar cell | 0.96 in 10 s | 5.6 (1 sun) | Constant current mode | 100% after 460 cycles | - | 3 |
| PANI@CNT (Sandwiched type) | 3T | Glass/FTO/TiO2/MAPbI3- MWCNT/PANI@CNT/PMMA | 0.7 in 100 s | 0.76 (1 sun) | Constant current mode | 70% after 500 cycles | 96 | 4 |
| Activated carbon (sandwiched type) | 3T | Glass/FTO/WOx/MAPbI3/ Spiro-OMeTAD/Au | 0.65 in 25 s | 2.13 (1 sun) | Constant current mode | 85% after 2000 cycles | - | 1 |
| Carbon (sandwiched type) | 3T | Glass/FTO/c-TiO2/ m-TiO2/MAPbI3/Carbon | 0.91 in 10 s | 7.1% (1 sun) | Constant current mode | 85% after 3000 cycles | - | 6 |
| MoO3 (Sandwiched type) | 3T | Glass/FTO/TiO2/MAPbI3− xCl x/ spiro-OMeTAD/MoO3/Au | 0.6 in 100 s | 2.3% (1 sun) | Constant current mode | - | - | 7 |
| MXene (Sandwiched type) | 2T | PET/Ti3C2Tx/PEI/P3HT:ICBA/PEDOT:PSS/Ti3C2Tx | 0.8 V in 50 s | 2.2% (1 sun) | Constant current mode | 95% after 10000 cycles | 97% after 10000 cycles | 8 |
| MXene (Microsupercapacitor) | 3T | Glass/ITO/SnO2/ Cs0.06FA0.78MA0.16Pb(I0.84Br0.16)3/PTAA/C | 1.15 in 4.9 s | 8.5% (1 sun) | Constant current mode | 87% after 6000 cycles | 99 | This Work |
| MXene (Microsupercapacitor) | 3T | Glass/ITO/SnO2/ Cs0.06FA0.78MA0.16Pb(I0.84Br0.16)3/PTAA/C | 0.87 in 4.9 s | 3.8% (1 sun) 8.05 (1000 lx) | Open circuit voltage | 87% after 6000 cycles | 99 | This Work |

Table S3: Comparative analysis of photocapacitors combining supercapacitors with different layouts and electrode materials and perovskite solar cells with different cell stacks.

References

1. Xu, X. et al. A Power Pack Based on Organometallic Perovskite Solar Cell and Supercapacitor. ACS Nano 9, 1782–1787 (2015).

2. Sun, J. et al. Laser-Assisted Fabrication of Microphotocapacitors with High Energy Density and Output Voltage. ACS Appl. Mater. Interfaces 13, 419–428 (2021).

3. Gao, K., Ti, D. & Zhang, Z. A photocapacitor with high working voltage and energy density. Sustainable Energy Fuels 3, 1937–1942 (2019).

4. Liu, R., Liu, C. & Fan, S. A photocapacitor based on organometal halide perovskite and PANI/CNT composites integrated using a CNT bridge. J. Mater. Chem. A 5, 23078–23084 (2017).

5. Yang, Y. et al. Self-charging flexible solar capacitors based on integrated perovskite solar cells and quasi-solid-state supercapacitors fabricated at low temperature. Journal of Power Sources 479, 229046 (2020).

6. Liang, J. et al. Integrated perovskite solar capacitors with high energy conversion efficiency and fast photo-charging rate. J. Mater. Chem. A 6, 2047–2052 (2018).

7. Zhou, F. et al. Perovskite Photovoltachromic Supercapacitor with All-Transparent Electrodes. ACS Nano 10, 5900–5908 (2016)

8. Qin, L. et al. A flexible semitransparent photovoltaic supercapacitor based on water-processed MXene electrodes. Journal of Materials Chemistry A 8, 5467–5475 (2020).