Table 1. Engine oil technical specifications in the current study.

| Result | Test | Unit | Physical and chemical characteristics |
| --- | --- | --- | --- |
| SAE 10W40 | J 300 | unit | SAE Grade |
| 15.4 | ASTM D445 | cSt | Kinematic Viscosity at 100°C |
| 155 | ASTM D2270 | - | Viscosity Index |
| 0.856 | ASTM D1298 | gr/cm3 | Density at 15°C |
| 220 | ASTM D92 | °C | Flash Point |
| -36 | ASTM D97 | °C | Pour Point |

Table 2. Independent variables and coded levels used in CCD.

| Name | Units | Type | Min. | Max. | Mean | Coded Level |  |  |  |  | Std. Dev. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | -α | -1 | 0 | +1 | +α |  |
| Concentration TiO2 NPs(A) | %wt | Numeric | 0.0 | 0.4 | 0.2 | 0.0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.1 |
| Applied weight(load)(B) | Kg | Numeric | 1.0 | 9.0 | 5.0 | 1.0 | 3.0 | 5.0 | 7.0 | 9.0 | 2.0 |
| Sliding Speed(C) | Hz | Numeric | 10.0 | 50.0 | 30.0 | 10.0 | 20.0 | 30.0 | 40.0 | 50.0 | 10.0 |

Table 3. Dependent (response) variables used in CCD.

| Response Name | Units | Analysis | Min. | Max. | Mean | Std. Dev. | Ratio | Transform | Model |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Weight Loss(R1) | mg | Polynomial | 0.25 | 1.3 | 0.6741 | 0.3065 | 5.20 | None | Reduced Quadratic |
| Average friction coefficient(R2) | - | Polynomial | 0.068 | 0.162 | 0.1164 | 0.0242 | 2.38 | None | Reduced Quadratic |

Table 4. Experimental results for Weight Loss and Average COF.

| Std | Factors |  |  | Responses |  |
| --- | --- | --- | --- | --- | --- |
|  | A: Concentration TiO2 NPs(%wt) | B: Applied weight(load)(Kg) | C: Sliding Speed (Hz) | Weight Loss(mg) | Average friction coefficient(K) |
| 1 | 0.1 | 3 | 20 | 0.4 | 0.136 |
| 2 | 0.3 | 3 | 20 | 0.5 | 0.113 |
| 3 | 0.1 | 7 | 20 | 0.95 | 0.132 |
| 4 | 0.3 | 7 | 20 | 1.1 | 0.121 |
| 5 | 0.1 | 3 | 40 | 0.33 | 0.105 |
| 6 | 0.3 | 3 | 40 | 0.6 | 0.092 |
| 7 | 0.1 | 7 | 40 | 0.7 | 0.112 |
| 8 | 0.3 | 7 | 40 | 0.9 | 0.125 |
| 9 | 0 | 5 | 30 | 1 | 0.162 |
| 10 | 0.4 | 5 | 30 | 1.3 | 0.152 |
| 11 | 0.2 | 1 | 30 | 0.25 | 0.068 |
| 12 | 0.2 | 9 | 30 | 0.97 | 0.116 |
| 13 | 0.2 | 5 | 10 | 0.6 | 0.146 |
| 14 | 0.2 | 5 | 50 | 0.35 | 0.108 |
| 15 | 0.2 | 5 | 30 | 0.5 | 0.099 |
| 16 | 0.2 | 5 | 30 | 0.48 | 0.091 |
| 17 | 0.2 | 5 | 30 | 0.53 | 0.1 |

Table 5. ANOVA Results for Weight Loss.

| Source | Adj SS | DF | Adj MS | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 1.49 | 9 | 0.1655 | 86.52 | < 0.0001 | significant |
| A-Concentration TiO2 NPs | 0.1089 | 1 | 0.1089 | 56.92 | 0.0001 |  |
| B-Applied weight(load) | 0.6642 | 1 | 0.6642 | 347.18 | < 0.0001 |  |
| C-Sliding Speed | 0.0529 | 1 | 0.0529 | 27.65 | 0.0012 |  |
| AB | 0.0000 | 1 | 0.0000 | 0.0261 | 0.8761 |  |
| AC | 0.0060 | 1 | 0.0060 | 3.16 | 0.1186 |  |
| BC | 0.0288 | 1 | 0.0288 | 15.05 | 0.0061 |  |
| A² | 0.5063 | 1 | 0.5063 | 264.65 | < 0.0001 |  |
| B² | 0.0138 | 1 | 0.0138 | 7.21 | 0.0313 |  |
| C² | 0.0010 | 1 | 0.0010 | 0.5053 | 0.5002 |  |
| Residual | 0.0134 | 7 | 0.0019 |  |  |  |
| Lack of Fit | 0.0121 | 5 | 0.0024 | 3.83 | 0.2199 | not significant |
| Pure Error | 0.0013 | 2 | 0.0006 |  |  |  |
| Cor Total | 1.50 | 16 |  |  |  |  |
| R²=99.11%, R2(adj)=97.96%, R2(pred)=93.12%, Std. Dev=0.0437, Adequate Precision=33.16, PRESS=0.1034, C.V%=6.49, Mean=0.6741, DF=degree of freedom, Adj SS: adjusted sum of squares, Adj MS: adjusted mean squares. |  |  |  |  |  |  |

Table 6. ANOVA Results for Average COF.

| Source | Adj SS | DF | Adj MS | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 0.0091 | 9 | 0.0010 | 26.70 | 0.0001 | significant |
| A-Concentration TiO2 NPs | 0.0002 | 1 | 0.0002 | 4.83 | 0.0639 |  |
| B-Applied weight(load) | 0.0012 | 1 | 0.0012 | 32.47 | 0.0007 |  |
| C-Sliding Speed | 0.0013 | 1 | 0.0013 | 34.35 | 0.0006 |  |
| AB | 0.0002 | 1 | 0.0002 | 4.78 | 0.0649 |  |
| AC | 0.0001 | 1 | 0.0001 | 3.83 | 0.0912 |  |
| BC | 0.0002 | 1 | 0.0002 | 4.29 | 0.0770 |  |
| A² | 0.0044 | 1 | 0.0044 | 116.01 | < 0.0001 |  |
| B² | 0.0000 | 1 | 0.0000 | 0.7608 | 0.4120 |  |
| C² | 0.0011 | 1 | 0.0011 | 29.13 | 0.0010 |  |
| Residual | 0.0003 | 7 | 0.0000 |  |  |  |
| Lack of Fit | 0.0002 | 5 | 0.0000 | 1.77 | 0.3990 | not significant |
| Pure Error | 0.0000 | 2 | 0.0000 |  |  |  |
| Cor Total | 0.0093 | 16 |  |  |  |  |
| R²=97.17%, R2(adj)=93.53%, R2(pred)=79.66%, Std. Dev=0.0061, Adequate Precision=18.94, PRESS=0.0019, C.V%=5.28, Mean=0.1164, DF=degree of freedom, Adj SS: adjusted sum of squares, Adj MS: adjusted mean squares. |  |  |  |  |  |  |