Cu-Fe Oxide Nanozymes with Enhanced Peroxidase-like Activity for Sensitive H2O2 Colorimetric Detection

Pengfei Jiang1, #, Yifan Hao1, #, Mingxi Jia2, Cun Liu1,*

1College of Chemistry and Chemical Engineering, Xinjiang Agricultural University, 311 East Nongda Road, Urumqi 830052, China.

2College of Food Science and Pharmacy, Xinjiang Agricultural University, China. 311 East Nongda Road, Urumqi 830052, China.

# These authors contributed equally to this work.

* Corresponding Author

*E-mail: liucun0910@163.com

Fig. S1. SEM images of (a) Cu2FeOx (b) CuFeOx (c) CuFe2Ox.

Fig. S2. Energy-dispersive X-ray (EDX) spectroscopy of (a, b) Cu2FeOx, (c, d) CuFeOx, (e, f) CuFe2Ox.

Fig. S3. UV-Vis absorption spectra of TMB oxides in the presence and absence of CuFeOx, CuxO, and Fe2O3.

Fig. S4. Effect of Cu-Fe oxide nanozyme dosage on the catalytic oxidation of TMB for H2O2 detection. (a) UV-Vis absorption spectra obtained at different Cu-Fe oxide nanozyme dosages. (b) Comparison of the absorbance at 652 nm extracted from the spectra in (a).

Fig. S5. Effect of solution pH on the catalytic oxidation of TMB for H2O2 detection. (a) UV-Vis absorption spectra obtained at different pH values. (b) Comparison of the absorbance at 652 nm extracted from the spectra in (a).

Fig. S6. Effect of reaction temperature on the catalytic oxidation of TMB for H2O2 detection. (a) UV-Vis absorption spectra obtained at different temperatures. (b) Comparison of the absorbance at 652 nm extracted from the spectra in (a).

Fig. S7. (a) UV-Vis absorption spectra obtained at various H2O2 concentrations for CuxO. (b) Corresponding absorbance values at 652 nm as a function of H2O2 concentration, with the linear fitting curves shown as insets.

Fig. S8. (a) UV-Vis absorption spectra obtained at various H2O2 concentrations for Fe2O3. (b) Corresponding absorbance values at 652 nm as a function of H2O2 concentration, with the linear fitting curves shown as insets.

Fig. S9. Light microscopic observation of HCC827 cell.

Fig. S10. UV-Vis absorption spectra of Cu2FeOx in two systems: “nanozyme + TMB + standard H2O2” system and “nanozyme + TMB + AA-stimulated HCC827 cell” system.

Table S1. ICP-OES data of Cu-Fe oxides with different molar ratios.

| Sample | Test components | Sample element content W (%) | Cu : Fe molar ratio |
| --- | --- | --- | --- |
| Cu2FeOx | Cu | 51.8824 | 1.96 : 1 |
|  | Fe | 23.2633 |  |
| CuFeOx | Cu | 41.2708 | 1.03 : 1 |
|  | Fe | 35.2516 |  |
| CuFe2Ox | Cu | 23.6357 | 0.52 : 1 |
|  | Fe | 40.3440 |  |

Table S2. Comparison of enzymatic kinetic parameters for three Cu-Fe oxide nanozymes.

| Sample | Km (mM) | Vmax*10-8 (Ms-1) |
| --- | --- | --- |
| Cu2FeOx | 1.85401 | 1.08055 |
| CuFeOx | 2.28712 | 0.99709 |
| CuFe2Ox | 1.93308 | 1.04619 |

Table S3. Analytical parameters of H2O2 detection in previous papers

| Materials | Linear range | LOD | references |
| --- | --- | --- | --- |
| TreHOAuC | 0-20 μM | 0.5 μM | [1] |
| CdV2O6 nanorods | 50-100 μM | 36.5 μM | [2] |
| Fe3O4 @COFs | 0.1-4 mM | 2.6 μM | [3] |
| InCex | 10–100 mM | 5 mM | [4] |
| CuBTC@PW12 | 0.01-1.0 mM | 2.67μM | [5] |
| Fe1.5-N-GDY | 100-800 μM | 52.96 μM | [6] |
| Cu2O–CuO/O–g-C3N4 | 2.5–250 µM | 1 µM | [7] |
| FeSx/SiO2 | 1.0 μM-100 μM | 0.2 μM | [8] |
| AuNCs/Fe-MIL | 5-1000 μM | 2.78 μM | [9] |
| Cu2FeOx | 10-200μM | 0.572 μM | This work |
| CuFeOx | 10-200μM | 0.636 μM | This work |
| CuFe2Ox | 10-200μM | 0.591 μM | This work |

References

[1] Y. Liu, F. Wang, Y. Liu, L. Cao, H. Hu, X. Yao, J. Zheng, H. Liu, A label-free plasmonic nanosensor driven by horseradish peroxidase-assisted tetramethylbenzidine redox catalysis for colorimetric sensing H2O2 and cholesterol, Sensors and Actuators B: Chemical, 389 (2023) 133893. https:/doi.org/10.1016/j.snb.2023.133893

[2] Y. Liu, P. Hao, L. Wang, G. Li, G. Fan, T. Wu, X. Zhu, Q. Liu, N,N-dicarboxymethyl Perylene-diimide-modified CdV2O6 Nanorods for Colorimetric Sensing of H2O2 and Pyrogallol, Microchimica Acta, 190 (2023) 270. https://doi.org/10.1007/s00604-023-05846-4

[3] L. Tian, B. Zhao, J. Zhang, X. Luo, F. Wu, Magnetic covalent organic framework nanospheres with enhanced peroxidase-like activity for colorimetric detection of H2O2 and glucose, Colloids and Surfaces A: Physicochemical and Engineering Aspects, 666 (2023) 131309. https:/doi.org/10.1016/j.colsurfa.2023.131309

[4] B. Liu, H. Ruan, C. Li, J. Yao, B. Wei, L. Wang, S. Ban, J. Xie, Ce-doped indium oxide nanozymes with peroxidase-like activity induced by cerium–indium synergy for colourimetric detection of H2O2, New Journal of Chemistry, 47 (2023) 18476-18484. https://doi.org/10.1039/D3NJ02985A

[5] W. Song, P. Sun, J. Zhou, X. Han, Q. Dai, F. Chai, The fabrication of CuBTC@PW12 with prominent peroxidase-mimicking activity for colorimetric detection of H2O2 and ascorbic acid via “on–off” switch, New Journal of Chemistry, 47 (2023) 15721-15730. https://doi.org/10.1039/D3NJ02611F

[6] J. Liu, X. Guo, H. Huang, R. Cui, D. Wang, Y. Chen, Y. Chai, J. Dong, B. Sun, Y. Lian, Enhanced Peroxidase-like Activity of Graphdiyne-Based Nanozymes by Fe and N Codoping for Colorimetric Determination of H2O2 and Ascorbic Acid, ACS Applied Nano Materials, 6 (2023) 22142-22151. https://doi.org/10.1021/acsanm.3c04348

[7] S. Mullakkattuthodi, B.N. Narayanan, Mesoporous Cu2O–CuO/O–g-C3N4 nanocomposite with enhanced peroxidase-like activity for the colorimetric H2O2 sensing, Research on Chemical Intermediates, 50 (2024) 4025-4047. https://doi.org/10.1007/s11164-024-05333-2

[8] C. Gu, L. Bai, T. Hou, L. Zhang, P. Gai, F. Li, Dual-mode colorimetric and homogeneous electrochemical detection of intracellular/extracellular H2O2 based on FeSx/SiO2 nanoparticles with high peroxidase-like activity, Analytica Chimica Acta, 1265 (2023) 341332. https:/doi.org/10.1016/j.aca.2023.341332

[9] Y.-S. Li, Q.-Y. Lv, Z.-D. Ding, X. Song, J. Chen, H.-F. Cui, Luminescent gold nanoclusters loaded on iron metal–organic framework with enhanced peroxidase-like activity for the colorimetric/fluorescent determination of H2O2, Microchemical Journal, 201 (2024) 110675. https:/doi.org/10.1016/j.microc.2024.110675