Supplementary Materials

Biosynthesis of polyhydroxyalkanoates from polyethylene terephthalate monomers by newly isolated bacterium Kosakonia cowanii EP30

Muhammad Zia Ul Haqa,†, Salah Ud Dina,†, Muhammad Usman Qamara, Cancan Jiangb, Fariha Hasana, Samiullah Khana, Malik Badshaha, Aamer Ali Shaha,b*

a Department of Microbiology, Faculty of Biological Sciences, Quaid-i-Azam University, Islamabad 45320, Pakistan.

bResearch Center for Eco-Environmental Sciences, Chinese Academy of Sciences, Beijing 100085, China.

†First and second authors equally contributed in this manuscript

*Corresponding author:

Prof. Dr. Aamer Ali Shah

Department of Microbiology, Faculty of Biological Sciences,

Quaid-i-Azam University, Islamabad 45320, Pakistan.

Email: alishah@qau.edu.pk

Telephone No.: +92-51-90643116

Table S1. Growth (CDW) and PHA yield Response of K. cowanii EP30 determined by Plackett Burman Design for medium optimization using TPA as a carbon source

|  | Factor 1 | Factor 2 | Factor 3 | Factor 4 | Factor 5 | Factor 6 | Factor 7 | Factor 8 | Factor 9 | Response 1 | Response 2 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Run | A: (NH₄)₂SO₄ (g/L) | B: KH₂PO₄ (g/L) | C: K₂HPO₄ (g/L) | D: MgSO₄·7H₂O (g/L) | E: CaCl₂·2H₂O (g/L) | F: FeSO₄·7H₂O (g/L) | G: NaH₂PO₄ (g/L) | H: ZnSO₄ (g/L) | J: TPA (g/L) | CDW (g/L) | PHA (g/L) | PHA (%) |
| 1 | 1.00 | 3.70 | 3.00 | 0.10 | 0.30 | 0.50 | 3.00 | 0.01 | 1.30 | 1.3 | 0.07 | 5.38 |
| 2 | 1.00 | 3.70 | 1.00 | 1.20 | 0.30 | 0.10 | 3.00 | 0.10 | 3.30 | 2.0 | 0.12 | 6.00 |
| 3 | 2.00 | 3.70 | 3.00 | 0.10 | 0.10 | 0.10 | 3.00 | 0.01 | 3.30 | 2.3 | 0.14 | 6.09 |
| 4 | 1.50 | 2.60 | 2.00 | 0.65 | 0.20 | 0.30 | 2.00 | 0.06 | 2.30 | 2.5 | 0.14 | 5.60 |
| 5 | 1.50 | 2.60 | 2.00 | 0.65 | 0.20 | 0.30 | 2.00 | 0.06 | 2.30 | 2.4 | 0.14 | 5.83 |
| 6 | 2.00 | 3.70 | 1.00 | 0.10 | 0.10 | 0.50 | 1.00 | 0.10 | 3.30 | 1.6 | 0.10 | 6.25 |
| 7 | 2.00 | 1.50 | 3.00 | 1.20 | 0.10 | 0.50 | 3.00 | 0.10 | 1.30 | 1.6 | 0.09 | 5.63 |
| 8 | 1.00 | 1.50 | 3.00 | 0.10 | 0.30 | 0.50 | 1.00 | 0.10 | 3.30 | 2.7 | 0.14 | 5.19 |
| 9 | 1.50 | 2.60 | 2.00 | 0.65 | 0.20 | 0.30 | 2.00 | 0.06 | 2.30 | 2.2 | 0.13 | 5.91 |
| 10 | 2.00 | 1.50 | 3.00 | 1.20 | 0.30 | 0.10 | 1.00 | 0.01 | 3.30 | 2.0 | 0.11 | 5.50 |
| 11 | 1.00 | 1.50 | 1.00 | 0.10 | 0.10 | 0.10 | 1.00 | 0.01 | 1.30 | 1.4 | 0.08 | 5.71 |
| 12 | 2.00 | 1.50 | 1.00 | 0.10 | 0.30 | 0.10 | 3.00 | 0.10 | 1.30 | 2.1 | 0.12 | 5.71 |
| 13 | 1.00 | 1.50 | 1.00 | 1.20 | 0.10 | 0.50 | 3.00 | 0.01 | 3.30 | 1.7 | 0.10 | 5.88 |
| 14 | 1.00 | 3.70 | 3.00 | 1.20 | 0.10 | 0.10 | 1.00 | 0.10 | 1.30 | 2.2 | 0.13 | 5.91 |
| 15 | 2.00 | 3.70 | 1.00 | 1.20 | 0.30 | 0.50 | 1.00 | 0.01 | 1.30 | 2.1 | 0.12 | 5.71 |

Table S2. Growth (CDW) and PHA yield Response of K. cowanii EP30 determined by Plackett Burman Design for medium optimization using EG as a carbon source

|  | Factor 1 | Factor 2 | Factor 3 | Factor 4 | Factor 5 | Factor 6 | Factor 7 | Factor 8 | Factor 9 | Response 1 |  | Response 2 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Run | A: (NH₄)₂SO₄ (g/L) | B: KH₂PO₄ (g/L) | C: K₂HPO₄ (g/L) | D: MgSO₄·7H₂O (g/L) | E: CaCl₂·2H₂O (g/L) | F: FeSO₄·7H₂O (g/L) | G: NaH₂PO₄ (g/L) | H: ZnSO₄ (g/L) | J: EG (g/L) | CDW (g/L) | PHA (g/L) |  | PHA (%) |  |
| 1 | 1.00 | 1.50 | 1.00 | 1.20 | 0.10 | 0.50 | 3.00 | 0.01 | 1.86 | 1.80 | 0.081 |  | 4.50 |  |
| 2 | 1.50 | 2.60 | 2.00 | 0.65 | 0.20 | 0.30 | 2.00 | 0.06 | 1.24 | 2.10 | 0.095 |  | 4.52 |  |
| 3 | 1.00 | 1.50 | 3.00 | 0.10 | 0.30 | 0.50 | 1.00 | 0.10 | 1.86 | 1.85 | 0.071 |  | 3.84 |  |
| 4 | 1.50 | 2.60 | 2.00 | 0.65 | 0.20 | 0.30 | 2.00 | 0.06 | 1.24 | 2.15 | 0.099 |  | 4.60 |  |
| 5 | 2.00 | 3.70 | 3.00 | 0.10 | 0.10 | 0.10 | 3.00 | 0.01 | 1.86 | 2.31 | 0.103 |  | 4.46 |  |
| 6 | 2.00 | 1.50 | 3.00 | 1.20 | 0.10 | 0.50 | 3.00 | 0.10 | 0.62 | 2.00 | 0.081 |  | 4.05 |  |
| 7 | 1.00 | 3.70 | 3.00 | 1.20 | 0.10 | 0.10 | 1.00 | 0.10 | 0.62 | 2.05 | 0.097 |  | 4.73 |  |
| 8 | 2.00 | 1.50 | 1.00 | 0.10 | 0.30 | 0.10 | 3.00 | 0.10 | 0.62 | 1.90 | 0.071 |  | 3.74 |  |
| 9 | 2.00 | 1.50 | 3.00 | 1.20 | 0.30 | 0.10 | 1.00 | 0.01 | 1.86 | 2.10 | 0.098 |  | 4.67 |  |
| 10 | 2.00 | 3.70 | 1.00 | 0.10 | 0.10 | 0.50 | 1.00 | 0.10 | 1.86 | 2.25 | 0.101 |  | 4.49 |  |
| 11 | 1.00 | 1.50 | 1.00 | 0.10 | 0.10 | 0.10 | 1.00 | 0.01 | 0.62 | 1.75 | 0.071 |  | 4.06 |  |
| 12 | 2.00 | 3.70 | 1.00 | 1.20 | 0.30 | 0.50 | 1.00 | 0.01 | 0.62 | 2.05 | 0.082 |  | 4.00 |  |
| 13 | 1.50 | 2.60 | 2.00 | 0.65 | 0.20 | 0.30 | 2.00 | 0.06 | 1.24 | 2.20 | 0.094 |  | 4.27 |  |
| 14 | 1.00 | 3.70 | 3.00 | 0.10 | 0.30 | 0.50 | 3.00 | 0.01 | 0.62 | 2.15 | 0.091 |  | 4.23 |  |
| 15 | 1.00 | 3.70 | 1.00 | 1.20 | 0.30 | 0.10 | 3.00 | 0.10 | 1.86 | 2.30 | 0.100 |  | 4.35 |  |

Table S3. ANOVA from the experimental design of Plackett Burmann showed significant factors of TPA medium for CDW by of K. cowanii EP30.

| Source | Sum of Squares | Df | Mean Square | F Value | p-value (Prob > F) |
| --- | --- | --- | --- | --- | --- |
| Model | 1.73 | 10 | 0.17 | 11.10 | 0.0362 |
| A-(NH₄)₂SO₄ | 0.030 | 1 | 0.030 | 1.93 | 0.2591 |
| B-KH₂PO₄ | 0.00333 | 1 | 0.00333 | 0.21 | 0.6749 |
| C-K₂HPO₄ | 0.083 | 1 | 0.083 | 5.36 | 0.1036 |
| E-CaCl₂·2H₂O | 0.12 | 1 | 0.12 | 7.71 | 0.0691 |
| F-FeSO₄·7H₂O | 0.053 | 1 | 0.053 | 3.43 | 0.1612 |
| G-NaH₂PO₄ | 0.12 | 1 | 0.12 | 7.71 | 0.0691 |
| H-ZnSO₄ | 0.21 | 1 | 0.21 | 13.71 | 0.0342 |
| J-TPA | 0.27 | 1 | 0.27 | 17.36 | 0.0252 |
| Curvature | 0.45 | 1 | 0.45 | 28.97 | 0.0126 |
| Residual | 0.047 | 3 | 0.016 | - | - |
| Lack of Fit | 0.000 | 1 | 0.000 | 0.000 | 1.0000 |

Table S4. ANOVA from the experimental design of Plackett Burmann showed significant factors of TPA medium for PHA biosynthesis by K. cowanii EP30.

| Source | Sum of Squares | df | Mean Square | F Value | p-value (Prob > F) |
| --- | --- | --- | --- | --- | --- |
| Model | 5.567 | 10 | 5.567 | 16.70 | 0.0203 |
| A-(NH₄)₂SO₄ | 1.333 | 1 | 1.333 | 4.00 | 0.1393 |
| B-KH₂PO₄ | 1.333 | 1 | 1.333 | 4.00 | 0.1393 |
| C-K₂HPO₄ | 1.333 | 1 | 1.333 | 4.00 | 0.1393 |
| E-CaCl₂·2H₂O | 1.333 | 1 | 1.333 | 4.00 | 0.1393 |
| F-FeSO₄·7H₂O | 5.333 | 1 | 5.333 | 16.00 | 0.0280 |
| G-NaH₂PO₄ | 1.333 | 1 | 1.333 | 4.00 | 0.1393 |
| H-ZnSO₄ | 5.333 | 1 | 5.333 | 16.00 | 0.0280 |
| J-TPA | 8.333 | 1 | 8.333 | 25.00 | 0.0154 |
| Curvature | 1.707 | 1 | 1.707 | 51.20 | 0.0056 |
| Residual | 1.000 | 3 | 3.333 | - | - |
| Lack of Fit | 3.333 | 1 | 3.333 | 1.00 | 0.4226 |

Table S5. ANOVA from the experimental design of Plackett Burmann showed significant factors of EG medium for CDW by K. cowanii EP30.

| Source | Sum of Squares | df | Mean Square | F Value | p-value (Prob > F) |
| --- | --- | --- | --- | --- | --- |
| Model | 0.40 | 10 | 0.040 | 23.93 | 0.0121 |
| A-(NH₄)₂SO₄ | 0.042 | 1 | 0.042 | 25.16 | 0.0153 |
| B-KH₂PO₄ | 0.24 | 1 | 0.24 | 145.96 | 0.0012 |
| C-K₂HPO₄ | 0.014 | 1 | 0.014 | 8.39 | 0.0627 |
| D-MgSO₄·7H₂O | 6.750 | 1 | 6.750 | 0.40 | 0.5701 |
| E-CaCl₂·2H₂O | 3.008 | 1 | 3.008 | 1.80 | 0.2720 |
| F-FeSO₄·7H₂O | 8.008 | 1 | 8.008 | 4.80 | 0.1162 |
| G-NaH₂PO₄ | 0.014 | 1 | 0.014 | 8.39 | 0.0627 |
| H-ZnSO₄ | 3.008 | 1 | 3.008 | 1.80 | 0.2720 |
| J-EG | 0.042 | 1 | 0.042 | 25.16 | 0.0153 |
| Curvature | 0.028 | 1 | 0.028 | 16.61 | 0.0267 |
| Residual | 5.008 | 3 | 1.668 | - | - |
| Lack of Fit | 8.333 | 1 | 8.333 | 0.0033 | 0.9592 |

Table S6. ANOVA from the experimental design of Plackett Burmann showed significant factors of EG medium for PHA biosynthesis by K. cowanii EP30.

| Source | Sum of Squares | df | Mean Square | F Value | p-value (Prob > F) |
| --- | --- | --- | --- | --- | --- |
| Model | 1.683 | 9 | 1.870 | 14.16 | 0.0107 |
| A-(NH₄)₂SO₄ | 5.208 | 1 | 5.208 | 3.94 | 0.1180 |
| B-KH₂PO₄ | 8.501 | 1 | 8.501 | 64.36 | 0.0013 |
| C-K₂HPO₄ | 1.021 | 1 | 1.021 | 7.73 | 0.0498 |
| D-MgSO₄·7H₂O | 8.008 | 1 | 8.008 | 6.06 | 0.0695 |
| F-FeSO₄·7H₂O | 9.075 | 1 | 9.075 | 6.87 | 0.0587 |
| G-NaH₂PO₄ | 4.083 | 1 | 4.083 | 0.31 | 0.6078 |
| J-EG | 3.101 | 1 | 3.101 | 23.48 | 0.0084 |
| Curvature | 1.838 | 1 | 1.838 | 13.91 | 0.0203 |
| Residual | 5.283 | 4 | 1.321 | - | - |
| Lack of Fit | 3.883 | 2 | 1.942 | 2.77 | 0.2650 |

Table S7. Response of Central Composite Design for the significant factor of TPA medium to determine their interaction

|  | Factor 1 | Factor 2 | Factor 3 | Response 1 | Response 2 |  |
| --- | --- | --- | --- | --- | --- | --- |
| Run | A: FeSO₄·7H₂O (g/L) | B: ZnSO₄ (g/L) | C: TPA (g/L) | CDW (g/L) | PHA (g/L) | PHA ( %) |
| 1 | 0.05 | 0.60 | 4.13 | 2.45 | 0.154 | 6.29 |
| 2 | 0.01 | 0.20 | 3.30 | 2.35 | 0.127 | 5.40 |
| 3 | 0.05 | 0.07 | 4.13 | 2.20 | 0.120 | 5.45 |
| 4 | 0.09 | 0.20 | 3.30 | 2.27 | 0.110 | 4.85 |
| 5 | 0.05 | 0.60 | 5.51 | 2.23 | 0.116 | 5.20 |
| 6 | 0.05 | 0.60 | 4.13 | 2.50 | 0.160 | 6.40 |
| 7 | 0.09 | 1.00 | 3.30 | 2.20 | 0.109 | 4.95 |
| 8 | 0.02 | 0.60 | 4.13 | 2.23 | 0.113 | 5.07 |
| 9 | 0.01 | 1.00 | 3.30 | 2.36 | 0.140 | 5.93 |
| 10 | 0.05 | 0.60 | 4.13 | 2.48 | 0.154 | 6.21 |
| 11 | 0.01 | 1.00 | 4.95 | 2.20 | 0.112 | 5.09 |
| 12 | 0.12 | 0.60 | 4.13 | 2.35 | 0.131 | 5.57 |
| 13 | 0.05 | 0.60 | 4.13 | 2.53 | 0.157 | 6.21 |
| 14 | 0.09 | 1.00 | 4.95 | 2.35 | 0.130 | 5.53 |
| 15 | 0.05 | 0.60 | 4.13 | 2.50 | 0.157 | 6.28 |
| 16 | 0.05 | 0.60 | 4.13 | 2.44 | 0.150 | 6.15 |
| 17 | 0.01 | 0.20 | 4.95 | 2.31 | 0.134 | 5.80 |
| 18 | 0.05 | 0.60 | 2.74 | 2.10 | 0.104 | 4.95 |
| 19 | 0.09 | 0.20 | 4.95 | 2.40 | 0.132 | 5.50 |
| 20 | 0.05 | 1.27 | 4.13 | 2.20 | 0.110 | 5.00 |

Table S8. Response of Central Composite Design for the significant factor of EG medium to determine their interaction

|  | Factor 1 | Factor 2 | Factor 3 | Response 1 | Response 2 |  |
| --- | --- | --- | --- | --- | --- | --- |
| Run | A: (NH4)2SO4 g/L | B: KH2PO4 g/L | C: EG g/L | CDW g/L | PHA g/L | PHA % |
| 1 | 1.32 | 4.85 | 2.18 | 2.3 | 0.076 | 3.30 |
| 2 | 2.00 | 6.00 | 2.50 | 2.5 | 0.12 | 4.80 |
| 3 | 3.00 | 4.85 | 1.64 | 2.35 | 0.10 | 4.26 |
| 4 | 3.00 | 2.92 | 2.18 | 2.35 | 0.083 | 3.53 |
| 5 | 2.00 | 3.70 | 1.86 | 2.37 | 0.087 | 3.67 |
| 6 | 4.00 | 3.70 | 1.86 | 2.29 | 0.10 | 4.37 |
| 7 | 3.00 | 4.85 | 2.18 | 2.37 | 0.092 | 3.88 |
| 8 | 3.00 | 4.85 | 2.18 | 2.35 | 0.087 | 3.70 |
| 9 | 2.00 | 6.00 | 1.86 | 2.4 | 0.10 | 4.17 |
| 10 | 3.00 | 4.85 | 2.18 | 2.42 | 0.089 | 3.68 |
| 11 | 3.00 | 4.85 | 2.18 | 2.39 | 0.09 | 3.77 |
| 12 | 3.00 | 6.78 | 2.18 | 2.54 | 0.10 | 3.94 |
| 13 | 4.68 | 4.85 | 2.18 | 2.21 | 0.10 | 4.52 |
| 14 | 4.00 | 6.00 | 2.50 | 2.41 | 0.10 | 4.15 |
| 15 | 3.00 | 4.85 | 2.18 | 2.37 | 0.086 | 3.63 |
| 16 | 3.00 | 4.85 | 2.72 | 2.38 | 0.082 | 3.45 |
| 17 | 4.00 | 6.00 | 1.86 | 2.31 | 0.099 | 4.29 |
| 18 | 3.00 | 4.85 | 2.18 | 2.42 | 0.085 | 3.51 |
| 19 | 4.00 | 3.70 | 2.50 | 2.28 | 0.074 | 3.25 |
| 20 | 2.00 | 3.70 | 2.50 | 2.38 | 0.086 | 3.61 |

Table S9. ANOVA from the experimental design of CCD showed significance and interaction of different factors in the medium for CDW response using TPA as a carbon source by K. cowanii EP30.

| Source | Sum of Squares | df | Mean Square | F Value | p-value (Prob > F) |
| --- | --- | --- | --- | --- | --- |
| Model | 0.25 | 9 | 0.027 | 5.34 | 0.0075 |
| A-FeSO₄.7H₂O | 0.003 | 1 | 0.003 | 0.58 | 0.4636 |
| B-ZnSO₄ | 0.003 | 1 | 0.003 | 0.69 | 0.4255 |
| C-TPA | 0.006 | 1 | 0.006 | 1.27 | 0.2867 |
| AB | 0.004 | 1 | 0.003 | 0.009 | 0.9233 |
| AC | 0.029 | 1 | 0.029 | 5.61 | 0.0394 |
| BC | 0.001 | 1 | 0.001 | 0.24 | 0.6324 |
| A² | 0.031 | 1 | 0.031 | 6.11 | 0.0329 |
| B² | 0.089 | 1 | 0.089 | 17.29 | 0.0020 |
| C² | 0.12 | 1 | 0.12 | 23.18 | 0.0007 |
| Residual | 0.051 | 10 | 0.005 | - | - |
| Lack of Fit | 0.046 | 5 | 0.009 | 7.95 | 0.0200 |

Table S10. Statistical analysis using ANOVA from experimental design of CCD between different nutritional factors of TPA medium for PHA yield from K. cowanii EP30.

| Source | Sum of Squares | df | Mean Square | F Value | p-value (Prob > F) |
| --- | --- | --- | --- | --- | --- |
| Model | 5.957 | 9 | 6.619 | 7.45 | 0.0021 |
| A-FeSO₄·7H₂O | 2.166 | 1 | 2.166 | 2.459 | 0.9614 |
| B-ZnSO₄ | 6.081 | 1 | 6.081 | 0.68 | 0.4274 |
| C-TPA | 1.303 | 1 | 1.303 | 1.47 | 0.2538 |
| AB | 4.500 | 1 | 4.500 | 0.051 | 0.8265 |
| AC | 5.120 | 1 | 5.120 | 5.76 | 0.0373 |
| BC | 1.620 | 1 | 1.620 | 1.82 | 0.2067 |
| A² | 1.291 | 1 | 1.291 | 14.53 | 0.0034 |
| B² | 2.055 | 1 | 2.055 | 23.12 | 0.0007 |
| C² | 2.708 | 1 | 2.708 | 30.47 | 0.0003 |
| Residual | 8.887 | 10 | 8.887 | - | - |
| Lack of Fit | 8.294 | 5 | 1.659 | 13.98 | 0.0058 |

Table S11. ANOVA from the experimental design of CCD showed significance and interaction of different factors in medium for CDW response using EG as a carbon source by K. cowanii EP30.

| Source | Sum of Squares | df | Mean Square | F Value | p-value Prob > F |
| --- | --- | --- | --- | --- | --- |
| Model | 0.096 | 9 | 0.011 | 13.29 | 0.0002 |
| A-(NH₄)₂SO₄ | 0.019 | 1 | 0.019 | 23.93 | 0.0006 |
| B-KH₂PO₄ | 0.028 | 1 | 0.028 | 35.12 | 0.0001 |
| C-EG | 4.593 | 1 | 4.593 | 5.74 | 0.0376 |
| AB | 0.000 | 1 | 0.000 | 0.000 | 1.0000 |
| AC | 5.000 | 1 | 5.000 | 0.062 | 0.8077 |
| BC | 5.000 | 1 | 5.000 | 6.25 | 0.0315 |
| A² | 0.027 | 1 | 0.027 | 34.09 | 0.0002 |
| B² | 8.072 | 1 | 8.072 | 10.09 | 0.0099 |
| C² | 3.072 | 1 | 3.072 | 0.38 | 0.5494 |
| Residual | 8.002 | 10 | 8.002 | - | - |
| Lack of Fit | 3.869 | 5 | 7.737 | 0.94 | 0.5281 |

Table S12. Statistical analysis using ANOVA from experimental design of CCD between different nutritional factors of EG medium for PHA yield from K. cowanii EP30.

| Source | Sum of Squares | df | Mean Square | F Value | p-value (Prob > F) |
| --- | --- | --- | --- | --- | --- |
| Model | 1.458 | 6 | 2.430 | 4.49 | 0.0111 |
| A-(NH₄)₂SO₄ | 3.036 | 1 | 3.036 | 0.56 | 0.4670 |
| B-KH₂PO₄ | 7.409 | 1 | 7.409 | 13.70 | 0.0027 |
| C-EG | 9.634 | 1 | 9.634 | 1.78 | 0.2049 |
| AB | 6.050 | 1 | 6.050 | 1.12 | 0.3095 |
| AC | 2.420 | 1 | 2.420 | 4.47 | 0.0543 |
| BC | 2.860 | 1 | 2.860 | 5.33 | 0.0381 |
| Residual | 7.031 | 13 | 5.408 | - | - |
| Lack of Fit | 6.683 | 8 | 8.353 | 11.99 | 0.0071 |