Supplementary Information:

Top-emitting 940-nm thin-film VCSELs 
transferred onto aluminum heatsinks

Sunghyun Moon1, Yeojun Yun1, Minhyung Lee1, Donghwan Kim2, Wonjin Choi2, and Jaejin Lee1,*

1Department of Electrical and Computer Engineering, Ajou University, Suwon, 16499, South Korea

2RayIR Corporation, LTD, 156 Gwanggyo-ro, Yeongtong-gu, Suwon, 16506, South Korea

*Corresponding author: jaejin@ajou.ac.kr

Reflectance spectrum of 940-nm thin-film VCSELs

The reflectance spectrum of 940-nm thin-film VCSELs with p-on-n structures, including 38-pair n-DBRs, 18-pair p-type DBRs, and 3-pair MQWs, is shown in Fig. S1. The bottom n-DBRs with 38 pairs exhibited maximal reflectivity, whereas the top p-DBRs with lower numbers than n-DBRs were designed to ensure the light emission of the thin-film VCSELs. The cavity mode (CM) dip in the reflectance spectrum of thin-film VCSELs was centered at 940.1 nm.

Supplementary Figure S1. Reflectance spectrum of 940-nm thin-film VCSELs with p-on-n structures. The epitaxial structures of thin-film VCSELs consist of top p-DBR and bottom n-DBR mirrors as well as an active gain region with InGaAs−AlGaAs MQWs.