A simple method to valorize silica sludges into sustainable coatings for indoor humidity buffering

Chi-Hong Kuok1, Wahid Dianbudiyanto2, Shou-Heng Liu1,2*

1Department of Environmental Engineering, National Cheng Kung University, Tainan 70101, Taiwan

2Department of Biology, Faculty of Science and Technology, Universitas Airlangga, Surabaya 60115, Indonesia

*Corresponding author. E-mail address: shliu@mail.ncku.edu.tw (S.-H. Liu)

Supplementary Material

Table S1 The main chemical components of waste silica sludges and commercial coatings

| Chemical compositions | Waste silica sludges |  | Commercial coatings |
| --- | --- | --- | --- |
| Elements (wt%)a | Si | 98.83 | 59.32 |
|  | S | 0.98 | 0.87 |
|  | Cl | 0.01 | 0.01 |
|  | Ca | 0.11 | 37.76 |
|  | Fe | 0.04 | 1.07 |
|  | Ti | 0.01 | 0.29 |
| Heavy metal (mg kg-1)b | Ni | 22 | 11 |
|  | Cu | 54 | 14 |
|  | Zn | 8 | 36 |
|  | As | 2 | 10 |
|  | Sr | 2 | - |
|  | Pb | 17 | 32 |

aidentified by XRF analysis

bmeasured by ICP-OES

Table S2 Textural properties of waste silica sludges

| BET surface area (m2 g-1) | 58.7 |
| --- | --- |
| t-Plot micropore area(m2 g-1) | 76.3 |
| Total pore volume (cm3 g-1) | 0.64 |
| t-Plot micropore volume (cm3 g-1) | 0.0416 |

Table S3 The benchmark of moisture adsorption for humidity control materials by Japanese Industrial Standards

| Level | Adsorbed moisture (g/m2) |  |  |
| --- | --- | --- | --- |
|  | 3 h | 6 h | 12 h |
| 3 | 26 | 50 | 71 |
| 2 | 25 | 35 | 50 |
| 1 | 15 | 20 | 29 |

Table S4 Heavy metals leaching of IHC-48 with blocks by TCLP tests

| Heavy metals | Leaching concentration (mg L-1) | Regulatory limit (mg L-1) |
| --- | --- | --- |
| Cu | ND | 5.0 |
| Cr | ND | 1.0 |
| Cd | ND | 5.0 |
| Ni | ND | 15.0 |
| Ba | ND | 100.0 |
| Co | ND | 5.0 |
| Pb | ND | 5.0 |
| ND: not detected (< 0.01 mg L-1) |  |  |

Table S5 Antibacterial efficacy of the IHC-48 samples

| E. coil | Blank (0 h) | Blank (24 h) | IHC-48 (24 h) |
| --- | --- | --- | --- |
| Bacteria concentrations CFU/ml | 9.9 ⅹ 104 | 6.0 ⅹ 106 | 99 |
| R factor | - | - | 4.8 |
| Antimicrobial efficacy | - | - | > 99.99% |