Ionic liquid crystals modifier to NiOnano@MWCNTs for effective electrocatalytic water splitting and hydrazine degradation

Hussien K. Srour1,2*, Nada F. Atta1, Mohamed W. Khalil1 and Ahmed Galal1*

1Department of Chemistry, Faculty of Science, Cairo University, 12613 Giza, Egypt

2Department of Applied Chemistry, Graduate School of Engineering, Kyushu University, 744 Motooka Nishi-ku Fukuoka 819-0395, Japan

* Corresponding authors (E-mails: galal@sci.cu.edu.eg;  srour.hussien.258@s.kyushu-u.ac.jp)

| ## ILCs/NiO-CNTs (As-prepared) |  |  |  |
| --- | --- | --- | --- |
| ## Element | ## Weight % | ## Atomic % | ## Error % |
| ## Ni K | ## 52.18 | ## 17.37 | ## 3.28 |
| ## O K | ## 8.09 | ## 9.28 | ## 13.16 |
| ## C K | ## 38.02 | ## 70.72 | ## 11.91 |
| ## N K | ## 1.71 | ## 2.63 | ## 71.65 |
| ## ILCs/NiO-CNTs (After exhaustive electrolysis) |  |  |  |
| ## Ni K | ## 49.45 | ## 15.91 | ## 3.31 |
| ## O K | ## 10.82 | ## 11.02 | ## 13.93 |
| ## C K | ## 38.11 | ## 70.82 | ## 11.04 |
| ## N K | ## 1.62 | ## 2.25 | ## 71.72 |

Table S1. Elemental composition of the ILCs/NiO-CNTs composite film before and after exposure to a constant applied potential of +0.85 V (vs. RHE) in 0.5 M Hyz/1.0 M KOH. Data from the EDS measurements of the surfaces displayed in Figures 1(D) and 1(E), respectively.

Figure S1. Peak current vs. square root of the scan rate relation for Ni/ILC/NiO-CNTs in 1.0 mM K4[Fe(CN)6] & 0.5 M KCl solution as electrolyte.

Figure S2. The standard phase diagrams of NiO nanoparticles (A), and MWCNTs  (B) [1,2].

From the Scherrer equation:

d=KλBcos θ

Where d is the grain size; K is constant related to the shape and index of crystals is = 0.89; λ is the wavelength of the X-ray (Cu Ka, is = 1.54056 Å); θ is the diffraction angle of the peak; B represents the full width at half-height of the peaks (in radian).  B is given by:

B2 = Bm2 − Bs2

Where Bm is the full width at half maximum (FWHM) of the sample and Bs is the half-width of a standard sample with a known crystal size. The particle size of NiO is 25.3 nm which was calculated from the spacing of the (111) plane.

Equation S1. Detailed calculation of particle size of NiO in ILCs/NiO-CNTs composite after exposure to 0.5 M Hyz/1.0 M KOH for one hour exhaustive electrolysis at +0.85 V vs. RHE. Data from XRD diffraction pattern of Figure 4.

Figure S3. Chronoamperograms over Ni/ILCs/NiO-CNTs electrode in presence of 0.50 M Hyz/1.0 M KOH for two hours. Eapp corresponds to the onset potential for Hyz-OER.

Figure S4. Correlated Arrhenius plot of log (anodic peak currents) vs. the reciprocal of temperature in 0.5 M Hyz /1.0 M KOH

| Type of Catalyst | T (K) | TOF (h-1 ) | Ea (kJ/mol) | Reference |
| --- | --- | --- | --- | --- |
| TiO2@Ni | 343 | 265.49 | 58.67 | [3] |
| Ni/CeO2 | 323 | 51.6 | 47.0 | [4] |
| PtNi/(MnOx)2-C3N4 | 323 | 2749 | 48.7 | [5] |
| NiPt/Al2O3 | 303 | 16.5 | 52.5 | [6] |
| NiPt/graphene | 323 | 846 | 23.9 | [7] |
| RhNi/Ce(OH)CO3 | 303 | 150 | 38.8 | [8] |
| PtNi/PDA-rGO | 323 | 2056 | 33.3 | [9] |
| Ni0.9Pt0.1/Ce2O3 | 298 | 28.1 | 42.3 | [10] |
| Ni-Cr (OH)3/C-TiO2 | 323 | 266 | 54.8 | [11] |
| Ni-La(OH)3/Ti-MOF | 343 | 870 | 36.8 | [12] |
| NiFeMo | 298 | 28.8 | 50.7 | [13] |
| RhNi@CeOx/rGO | 323 | 370 | 58.0 | [14] |
| RhNiB | 298 | 75 | - | [15] |
| NiPt/ZrO2 | 298 | 296 | 24.40 | [16] |
| PtNi/CNS | 323 | 3928 | 37.97 | [17] |
| PtNi/ Zr-MOF | 323 | 1716 | 33.7 | [18] |
| Ni–Pt @ MIL-101/rGO | 323 | 960 | 35.3 | [19,20] |
| Ni0.8Pt0.2/DT-Ti3C2Tx | 323 | 1220 | - | [21] |
| Ni/Fe/Pd | 313 | 25.3 | 32.1 | [22] |
| Ni/Fe/Ag | 313 | 38.4 | 42.3 | [22] |
| Ni/Fe/Cu | 313 | 40.2 | 44.6 | [22] |
| Pd/Ag/Ni | 313 | 30.2 | 75.9 | [22] |
| NiFePd | 323 | 21.5 | 40.0 | [23] |
| Ni0.6Pd0.4-MoOx | 323 | 405 | 32.6/49.7 | [24] |
| Ni@TNTs | 333 | 96.0 | - | [25] |
| Ni0.9Fe0.1- Cr2O3 | 343 | 893.5 | 83.6 | [26] |
| ILCs/NiO-CNTs | 298 | 1751 | 3.91 | This work |

$ Rate constant calculated when using 0.5 M hydrazine in 1.0 M KOH

Table S2. Comparison of the performance of the proposed catalyst to different Ni-containing catalysts

References

1.	Ravichandran, S., Sengodan, P. & Radhakrishnan, J. Evaluation of biosynthesized nickel oxide nanoparticles from Clerodendrum phlomidis: A promising photocatalyst for methylene blue and acid blue dyes degradation. Ceram. Int. 49, 12408–12414 (2023).

2.	Soleimani, H. et al. Impact of carbon nanotubes based nanofluid on oil recovery efficiency using core flooding. Results Phys. 9, 39–48 (2018).

3.	Liu, Y. et al. TiO2 nanoparticle-supported Ni catalyst for the dehydrogenation of hydrazine hydrate. Chemosphere 313, 137608 (2023).

4.	He, L. et al. Cerium-oxide-modified nickel as a non-noble metal catalyst for selective decomposition of hydrous hydrazine to hydrogen. ACS Catal. 5, 1623–1628 (2015).

5.	Zheng, J. et al. Mn-Modified Graphitic Carbon Nitride-Supported Bimetallic PtNi Nanoparticles for Hydrogen Generation from Hydrous Hydrazine. ChemistrySelect 7, (2022).

6.	He, L. et al. Surface modification of Ni/Al2O3 with Pt: Highly efficient catalysts for H2 generation via selective decomposition of hydrous hydrazine. J. Catal. 298, 1–9 (2013).

7.	Chen, J., Lu, Z. H., Huang, W., Kang, Z. & Chen, X. Galvanic replacement synthesis of NiPt/graphene as highly efficient catalysts for hydrogen release from hydrazine and hydrazine borane. J. Alloys Compd. 695, 3036–3043 (2017).

8.	Chen, J., Yao, Q., Zhu, J., Chen, X. & Lu, Z. H. Rh–Ni nanoparticles immobilized on Ce(OH)CO3 nanorods as highly efficient catalysts for hydrogen generation from alkaline solution of hydrazine. Int. J. Hydrogen Energy 41, 3946–3954 (2016).

9.	Song, F. Z., Zhu, Q. L. & Xu, Q. Monodispersed PtNi nanoparticles deposited on diamine-alkalized graphene for highly efficient dehydrogenation of hydrous hydrazine at room temperature. J. Mater. Chem. A 3, 23090–23094 (2015).

10.	Wang, H. L., Yan, J. M., Wang, Z. L., O, S. Il & Jiang, Q. Highly efficient hydrogen generation from hydrous hydrazine over amorphous Ni0.9Pt0.1/Ce2O3 nanocatalyst at room temperature. J. Mater. Chem. A 1, 14957–14962 (2013).

11.	Zhang, X. et al. Carbon-doped mesoporous TiO2-immobilized Ni nanoparticles: Oxygen defect engineering enhances hydrogen production. Appl. Catal. B Environ. 339, 123153 (2023).

12.	Long, J., Yao, Q., Zhang, X., Wu, H. & Lu, Z. H. Defects engineering of metal-organic framework immobilized Ni-La(OH)3 nanoparticles for enhanced hydrogen production. Appl. Catal. B Environ. 320, 121989 (2023).

13.	Wang, H. L., Yan, J. M., Li, S. J., Zhang, X. W. & Jiang, Q. Noble-metal-free NiFeMo nanocatalyst for hydrogen generation from the decomposition of hydrous hydrazine. J. Mater. Chem. A 3, 121–124 (2015).

14.	Zhang, Z., Lu, Z. H., Tan, H., Chen, X. & Yao, Q. CeOx-modified RhNi nanoparticles grown on rGO as highly efficient catalysts for complete hydrogen generation from hydrazine borane and hydrazine. J. Mater. Chem. A 3, 23520–23529 (2015).

15.	Wang, J., Li, W., Wen, Y., Gu, L. & Zhang, Y. Rh-Ni-B nanoparticles as highly efficient catalysts for hydrogen generation from hydrous hydrazine. Adv. Energy Mater. 5, (2015).

16.	Hussain, S. N. et al. NiPt nanoparticle immobilization on zirconia (ZrO2) for the production of hydrogen through selected decomposition of alkaline hydrazine solution. Mater. Sci. Eng. B 302, 117267 (2024).

17.	Xu, F., Wang, Y., Wang, C., Huang, W. & Liu, X. Dehydrogenation of hydrous hydrazine over carbon nanosphere- supported PtNi nanoparticles for on-demand H2 release. Fuel 332, 126116 (2023).

18.	Hu, X. et al. Fine-tuning catalytic performance of ultrafine bimetallic nickel-platinum on metal-organic framework derived nanoporous carbon/metal oxide toward hydrous hydrazine decomposition. Int. J. Hydrogen Energy 48, 16001–16006 (2023).

19.	Zou, H. et al. Immobilization of Ni–Pt nanoparticles on MIL-101/rGO composite for hydrogen evolution from hydrous hydrazine and hydrazine borane. J. Alloys Compd. 835, 155426 (2020).

20.	Berčič, G. & Blaž Likozar. Analysis and recompilation of kinetic data about the hydrogen production by the catalytic decomposition of hydrous hydrazine. Int. J. Hydrogen Energy 47, 29348–29357 (2022).

21.	Guo, F., Zou, H., , Qilu Yao, B. H. & Lu, Z.-H. Monodispersed bimetallic nanoparticles anchored on TiO2-decorated titanium carbide MXene for efficient hydrogen production from hydrazine in aqueous solution. Renew. Energy 155, 1293–1301 (2020).

22.	Al-Thubaiti, K. S. & Zaheer Khan. Trimetallic nanocatalysts to enhanced hydrogen production from hydrous hydrazine: The role of metal centers. Int. J. Hydrogen Energy 45, 13960–13974 (2020).

23.	Bhattacharjee, D. & Dasgupta, S. Trimetallic NiFePd nanoalloy catalysed hydrogen generation from alkaline hydrous hydrazine and sodium borohydride at room temperature. J. Mater. Chem. A 3, 24371–24378 (2015).

24.	Yao, Q., Yang, K., Nie, W., Li, Y. & Zhang-Hui Lu. Highly efficient hydrogen generation from hydrazine borane via a MoOx-promoted NiPd nanocatalyst. Renew. Energy 147, 2024–2031 (2020).

25.	Wang, H. et al. Ni nanoparticles encapsulated in the channel of titanate nanotubes: Efficient noble-metal-free catalysts for selective hydrogen generation from hydrous hydrazine. Chem. Eng. J. 332, 637–646 (2018).

26.	Chen, J. et al. Cr2O3-modified NiFe nanoparticles as a noble-metal-free catalyst for complete dehydrogenation of hydrazine in aqueous solution. Appl. Surf. Sci. 501, 144247 (2020).