Cerium Oxide-Textiles dyes- Table:

- Various dyes structural, Molecular weight and UV-Vis maximum absorbance range

- Effect of Annealing On The Structural Properties Of Cerium Oxide NPs

- Elemental analysis of Cerium Oxide Nps

- Surface Area and Pore Volume of CeO2 samples calcined at different Temperature

- Kinetic constants for the degradation of reactive dyes

Table-1 Various dyes structural, Molecular weight and UV-Vis maximum absorbance range

| Dye | Structure Formula , Molecular weight and UV-Vis maximum absorbance |
| --- | --- |
| Reactive Green 19 (RG 19) | 1419.93 / 640 nm Chemical formula: C40H23Cl2N15Na6O19S6 |
| Reactive Orange 84 (RO-84) | 1850.25/495nm Chemical formula: C58H30Cl2N14Na8O26S8 |
| Reactive Violet 1(RV-1) | 926.51 / 555nm Chemical formula: C25H13Cl2N7Na4O14S4 |

Table: 2 Effect of Annealing On The Structural Properties Of Cerium Oxide NPs

| Temperature (0C) | Crystalline size (D) nm |  | strain (ε) 10-3 | Dislocation density (δ ) 1015 | % of crystallinity |
| --- | --- | --- | --- | --- | --- |
|  | XRD | SEM |  |  |  |
| 300 | 7 | 8 | 9.13 | 11.6 | 45 |
| 400 | 12 | 14 | 8.05 | 5.10 | 64 |
| 500 | 17 | 19 | 7.20 | 2.77 | 86 |

Table:3 Elemental analysis of Cerium Oxide Nps

| Temperature (0C) | Ce | O |
| --- | --- | --- |
|  | Atomic (%) |  |
| 300 | 49.2 | 50.8 |
| 400 | 49.9 | 50.1 |
| 500 | 50.8 | 49.2 |

Table: 4 Surface Area and Pore Volume of CeO2 samples calcined at different Temperature

| Calc Temp (°C) | SBET( m2/g) | Mean pore size (nm) | Mean pore volume(cm3/g |
| --- | --- | --- | --- |
| 300 | 125 | 9 | 0.036 |
| 400 | 95 | 9.8 | 0.028 |
| 500 | 75 | 10.4 | 0.019 |

Table: 5 Kinetic constants for the degradation of reactive dyes

| Dyes | Fixed pH-9 |  | Kapp x 10-3 | t1/2 Half life |
| --- | --- | --- | --- | --- |
|  | Dye Loading-20mg/L | Amount of catalyst-1 g/L |  |  |
|  | Temperature | Degradation |  |  |
| RG19 | 300 | 75 |  |  |
|  | 400 | 85 |  |  |
|  | 500 | 93 | 15.3 | 45.30 |
| RO84 | 300 | 73 |  |  |
|  | 400 | 87 |  |  |
|  | 500 | 90 | 10.4 | 66.64 |
| RV1 | 300 | 86 |  |  |
|  | 400 | 88 |  |  |
|  | 500 | 98 | 8.6 | 80.59 |

Kinetic constant for the degradation of Textile dyes:

| Dyes | First order | Second Order |
| --- | --- | --- |
|  | R2 | R2 |
| RG19 | 0.9814 | 0.988 |
| RO84 | 0.9789 | 0.9848 |
| RV1 | 0.9981 | 0.9984 |