Supplementary Information

The preparation and electrochemical performance analysis of different porous silicon composites

Xuchun Wang1*, Qianrui Liu2, Jiaohong Shu1, Dongdong Ouyang1,3, Xuemei Zhang1, Junming Chen1, Huaguang Zhou1, Yuyang Zhang1, Jinming Kong2*

1College of Chemistry and Material Engineering, Anhui Science and Technology University, Bengbu Anhui 233030, PR China; wangxc@ahstu.edu.cn.

2School of Environmental and Biological Engineering, Nanjing University of Science and Technology, Nanjing Jiangsu 210094, PR China.

3School of Materials Science and Engineering, Anhui Polytechnic University, Wuhu Anhui 241000, PR China.

2 Experimental

Materials and reagents

White carbon black, KOH, HCl, Li2CO3 and ethanol were purchased from Sinopharm Chemical Reagent Co., Ltd. (Shanghai, China). LiAlH4 was got from Eon Chemical Technology Co., Ltd. (Shanghai, China). Activated carbon powder was obtained from Macklin Inc. (Shanghai, China). AgNO3 was bought from Zhuzhou Institute of Chemical Industry (Hunan, China). Ferrocene and hydrofluoric acid (HF) were purchased from Yongda Chemical Reagent Co., Ltd. (Tianjin, China). Teflon was got from Zhenjiang Tongde Plastic Products Co., Ltd. (Jiangsu, China), and acetylene black was obtained from Yiboru i Chemical Co. Ltd. (Tianjin, China). All of those reagents were analytical grade.

Apparatus

X-ray diffraction (XRD) was performed on XRD-6100 (Shimadzu, Japan). Scanning electron microscopy (SEM) was got from Zeiss Evo 18 Research (Jena, Germany). Electrochemical techniques were conducted on a traditional three-electrode workstation (CHI800D) consisting of Hg/HgO as reference electrode, carbon electrode and nickel foam (1cm*1cm) welded with nickel strip as battery pole piece.

The preparation of porous silicon

First, 0.6175 g white carbon black and 0.4352 g LiAlH4 were ground evenly, and activated carbon powder was added to the mixed powder. Carbon powder was added to this sample to remove the oxygen in the muffle furnace. Subsequently, the above mixed powder was preheated at 150℃ for 1 h and calcined at 600℃ for 5 h in muffle furnace (Heating rate: 10 ℃/min). Then, the mixed powder was cooled to room temperature. Excessive HF was added to the mixed powder, and the solution was stirred and stood for 12 h to remove the unreacted SiO2. Soon afterwards, the above solution was centrifuged at 1500 r for 3 min, and the resulting product soaked in HCl for 12 h to remove impurities following by centrifuging at 1500 r for 3 min. Then, the resulting product was washed with ethanol for 2-3 times to obtain the pure filter cake. The pure filter cake was kept in oven at 95 ℃ for 24 h to get porous silicon.

The preparation of AgNPs

1.5373 g ferrocene was used to reduce 5 mM AgNO3 aqueous solution for 2.5 h. After the reaction, the solution was centrifuged. The resulting product was cleaned with alcohol for 3 times, and then kept in oven at 85 ℃ for 2 h to obtain AgNPs.

The preparation of porous silicon composites

The preprepared porous silicon (0.2530 g, 0.2501 g, 0.1617 g) were respectively mixed with 0.2530 g AgNPs, 0.2529 g Li2CO3 and 0.1532 g AgNPs/0.1683 g Li2CO3 to obtain three different porous silicon composites.