Supplementary Information

Multimodal smart sensing via wavelength-selective hydrochromism in zero-dimensional metal halides

Joo Hyeong Han, Jeong Min Seo, Tuhin Samanta, Sung Woo Jang, Yong Min Park, San Ha Choi, Ji Hyeon Cha, and Won Bin Im*

Division of Materials Science and Engineering, Hanyang University, 222 Wangsimni-ro, Seongdong-gu, Seoul, 04763, Republic of Korea

*To whom correspondence should be addressed.

E-mail: imwonbin@hanyang.ac.kr

Supplementary Table 1. Rietveld refinement parameters of combined X-ray diffraction profiles of Cs3GdCl6. The numbers in parentheses are the estimated standard deviations of the last signiﬁcant ﬁgure.

| parameters | value |
| --- | --- |
| symmetry | monoclinic |
| space group | C2/c |
| a (Å) | 27.025(8) |
| b (Å) | 8.172(2) |
| c (Å) | 13.235(9) |
| α (°) | 90.000 |
| β (°) | 100.094(2) |
| γ (°) | 90.000 |
| V (Å3) | 2877.568(2) |
| Rwp (%) | 7.63 |
| χ2 | 1.826 |

Supplementary Fig. 1. Normalized PL intensity of Cs3Gd1-xLnxCl6 as a function of a Er3+, b Yb3+-Er3+, and c Tb3+ concentration.

Supplementary Fig. 2. PL spectra under 980 nm and 1550 nm excitation of Cs3Gd0.78Yb0.2Er0.02Cl6.

Supplementary Fig. 3. PL and PLE spectra of Cs3Gd0.75Tb0.25Cl6.

Supplementary Fig. 4. Schematic illustration of hydrochromic upconversion mechanism under 1550 nm excitation for Yb/Er co-doped and Er-doped systems.

Supplementary Fig. 5. Laser power-dependent PL spectra under 980 nm and 1550 nm excitation of a-d Cs3Gd0.8Er0.2Cl6 and Cs3Gd0.78Yb0.2Er0.02Cl6. Pump power dependence of green and red upconversion intensity: e-h Cs3Gd0.8Er0.2Cl6 and Cs3Gd0.78Yb0.2Er0.02Cl6under 980 nm and 1550 nm excitation.

Supplementary Fig. 6. Temperature-dependent upconversion luminescence contour maps of Cs3Gd0.8Er0.2Cl6 and Cs3Gd0.78Yb0.2Er0.02Cl6 under 980 nm and 1550 nm excitations in the temperature range of 20–200℃.

Supplementary Fig. 7. Optical thermometry performance of Cs3Gd0.78Yb0.2Er0.02Cl6 under 1550 nm excitation. a Comparison of absorbance slopes, b temperature-dependent PL spectra showing thermally coupled level behavior, c relative PL intensity variations of 525 nm and 550 nm emissions, and d fluorescence intensity ratio (FIR) fitting and relative sensitivity (Sr) curve.

Supplementary Fig. 8. X-ray detection characteristics of Cs3Gd0.75Tb0.25Cl6. a Spectral matching between radioluminescence (RL) emission and the spectral sensitivity of a commercial CMOS sensor. b Linear relationship between RL intensity and X-ray dose rate.